Supporting Information

# Detecting PEGs in real-world cosmetic products using ToF-SIMS

Yanjie Shena,b, Jiyoung Sonc, and Xiao-Ying Yub*

a College of Biology and Oceanography, Weifang University, 5147 Dongfeng East Street, Weifang, Shandong 261061, China

b Materials Science and Technology Division, Oak Ridge National Laboratory, Oak Ridge, TN, 37830, United States

c Energy and Environment Directorate, Pacific Northwest National Laboratory, Richland, WA 99354, United States

* Correspondence: Dr. Xiao-Ying Yu, Email: yuxiaoying@ornl.gov

Table of Contents

Supplementary Figures	S-4

Fig. S1a. Normalized static SIMS spectra showing reproducibility of the PEG 300 sample in the positive mode of m/z+ 0–200.	S-4

Fig. S1b. Normalized static SIMS spectra showing reproducibility of the PEG 300 sample in the positive mode of m/z+ 200–500.	S-5

Fig. S1c. Normalized static SIMS spectra showing reproducibility of the PEG 300 sample in the positive mode of m/z+ 500–800.	S-6

Fig. S2a. Static SIMS spectra showing reproducibility of the PEG 300 sample in the positive mode of m/z+ 0–200.	S-7

Fig. S2b. Static SIMS spectra showing reproducibility of the PEG 300 sample in the positive mode of m/z+ 200–500.	S-8

Fig. S2c. Static SIMS spectra showing reproducibility of the PEG 300 sample in the positive mode of m/z+ 500–800.	S-9

Fig. S3a. Normalized static SIMS spectra showing reproducibility of the PEG 300 sample in the negative mode of m/z− 0–200.	S-10

Fig. S3b. Normalized static SIMS spectra showing reproducibility of the PEG 300 sample in the negative mode of m/z− 200–500.	S-11

Fig. S3c. Normalized static SIMS spectra showing reproducibility of the PEG 300 sample in the negative mode of m/z− 500–800.	S-12

Fig. S4a. Static SIMS spectra showing reproducibility of the PEG 300 sample in the negative mode of m/z− 0–200.	S-13

Fig. S4b. Static SIMS spectra showing reproducibility of the PEG 300 sample in the negative mode of m/z− 200–500.	S-14

Fig. S4c. Static SIMS spectra showing reproducibility of the PEG 300 sample in the negative mode of m/z− 500–800.	S-15

Fig. S5. Normalized SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the positive mode of m/z+ 0–200.	S-16

Fig. S6a. Normalized SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the negative mode of m/z− 0–200.	S-17

Fig. S6b. Normalized SIMS spectral comparison of HEG, PEGs, Clinique and Purity in the negative mode of m/z− 200–500.	S-18

Fig. S6c. Normalized SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the negative mode of m/z− 500–800.	S-19

Fig. S7. Static SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the positive mode of m/z+ 200–500 (a) and 500–800 (b).	S-21

Fig. S8. Static SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the positive mode of m/z+ 0–200.	S-22

Fig. S9a. Static SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the negative mode of m/z− 0–200.	S-23

Fig. S9b. Static SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the negative mode of m/z− 200–500.	S-24

Fig. S9c. Static SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the negative mode of m/z− 500–800.	S-25

Fig. S10. SIMS spectral PCA results of HEG, PEGs, Clinique, and Purity in the negative mode: Scores plots of PC1 vs. PC2 (a), PC2 vs. PC4 (b) and loadings plots of PC1 (c), PC2 (d), and PC4 (e) in m/z− 50–800.  Peaks are labelled in their center masses.	S-26

Fig. S11. SIMS 2D image comparisons of key peaks (371.227, 415.252, 657.367, and 701.392) in the positive mode: (a) HEG, (b) PEG 200, (c) PEG 300, (d) PEG 400, (e) PEG 4000, (f) Purity, and (g) Clinique.	S-28

Fig. S12. Normalized SIMS 2D image comparisons of key peaks (53.001, 107.075, 129.059, and 217.106) in the positive mode: (a) HEG, (b) PEG 200, (c) PEG 300, (d) PEG 400, (e) PEG 4000, (f) Purity, and (g) Clinique.	S-29

Fig. S13. Normalized SIMS 2D image comparisons of key peaks (371.227, 415.252, 657.367, and 701.392) in the positive mode: (a) HEG, (b) PEG 200, (c) PEG 300, (d) PEG 400, (e) PEG 4000, (f) Purity, and (g) Clinique.	S-30

Fig. S14. Normalized SIMS 2D image comparisons of key peaks in the negative mode: (a) HEG, (b) PEG 200, (c) PEG 300, (d) PEG 400, (e) PEG 4000, (f) Purity, and (g) Clinique.	S-31

Fig. S15. SIMS 2D image comparisons of key peaks in the positive mode: (a) HEG, (b) PEG 200, (c) PEG 300, (d) PEG 400, (e) PEG 4000, (f) Purity, and (g) Clinique.	S-32

Supplementary Tables	S-33

Table S1. The HEG, PEGs, and real-word domestic products sample matrix.	S-33

Table S2. Key possible peak identification in the negative mode.	S-34

Table S3. Summary of peak area and peak height of PEG 300 representative peaks in positive ion mode.	S-35

Table S4. Ratios of peak area and peak height of PEG 300 representative peaks in positive ion mode.	S-36

Table S5. Summary of peak area and peak height of PEG 300 representative peaks in negative ion mode.	S-37

Table S6. Ratios of peak area and peak height of PEG 300 representative peaks in negative ion mode.	S-38

Table S7. Signal to noise ration of PEG 300 representative peaks in positive ion mode.	S-39

Table S8. Signal to noise ration of PEG 300 representative peaks in negative ion mode.	S-40

Reference	S-41

# Supplementary Figures

### Fig. S1a. Normalized static SIMS spectra showing reproducibility of the PEG 300 sample in the positive mode of m/z+ 0–200.

Normalized intensity (Norm. Int.) is calculated by dividing specific peak intensities to the total ion intensities of each sample, respectively. P1, P2, P3, P4, P5 and P6 represent the first, second, third, fourth, fifth and sixth positive ion mode data acquired consecutively in the PEG 300 sample.

### Fig. S1b. Normalized static SIMS spectra showing reproducibility of the PEG 300 sample in the positive mode of m/z+ 200–500.

Normalized intensity (Norm. Int.) is calculated by dividing specific peak intensities to the total ion intensities of each sample, respectively. P1, P2, P3, P4, P5 and P6 represent the first, second, third, fourth, fifth and sixth positive ion mode data acquired consecutively in the PEG 300 sample.

### Fig. S1c. Normalized static SIMS spectra showing reproducibility of the PEG 300 sample in the positive mode of m/z+ 500–800.

Normalized intensity (Norm. Int.) is calculated by dividing specific peak intensities to the total ion intensities of each sample, respectively. P1, P2, P3, P4, P5 and P6 represent the first, second, third, fourth, fifth and sixth positive ion mode data acquired consecutively in the PEG 300 sample.

Overall, the positive SIMS spectral comparisons of the same sample (e.g., PEG 300) in the positive ion mode show good reproducibility, thus giving assurance of data quality. The same applies to other samples we studied in this work.

### Fig. S2a. Static SIMS spectra showing reproducibility of the PEG 300 sample in the positive mode of m/z+ 0–200.

P1, P2, P3, P4, P5 and P6 represent the first, second, third, fourth, fifth and sixth positive ion mode data acquired consecutively in the PEG 300 sample.

### Fig. S2b. Static SIMS spectra showing reproducibility of the PEG 300 sample in the positive mode of m/z+ 200–500.

P1, P2, P3, P4, P5 and P6 represent the first, second, third, fourth, fifth and sixth positive ion mode data acquired consecutively in the PEG 300 sample.

### Fig. S2c. Static SIMS spectra showing reproducibility of the PEG 300 sample in the positive mode of m/z+ 500–800.

P1, P2, P3, P4, P5 and P6 represent the first, second, third, fourth, fifth and sixth positive ion mode data acquired consecutively in the PEG 300 sample.

Overall, the absolute SIMS spectral comparisons of the same sample (e.g., PEG 300) in the positive ion mode are consistent with the normalized ones and show good reproducibility, thus giving assurance of data quality. The same applies to other samples we studied in this work.

### Fig. S3a. Normalized static SIMS spectra showing reproducibility of the PEG 300 sample in the negative mode of m/z− 0–200.

Normalized intensity (Norm. Int.) is calculated by dividing specific peak intensities to the total ion intensities of each sample, respectively. N1, N2, N3, N4, N5 and N6 represent the first, second, third, fourth, fifth and sixth negative ion mode data acquired consecutively in the PEG 300 sample.

### Fig. S3b. Normalized static SIMS spectra showing reproducibility of the PEG 300 sample in the negative mode of m/z− 200–500.

Normalized intensity (Norm. Int.) is calculated by dividing specific peak intensities to the total ion intensities of each sample, respectively. N1, N2, N3, N4, N5 and N6 represent the first, second, third, fourth, fifth and sixth negative ion mode data acquired consecutively in the PEG 300 sample.

### Fig. S3c. Normalized static SIMS spectra showing reproducibility of the PEG 300 sample in the negative mode of m/z− 500–800.

Normalized intensity (Norm. Int.) is calculated by dividing specific peak intensities to the total ion intensities of each sample, respectively. N1, N2, N3, N4, N5 and N6 represent the first, second, third, fourth, fifth and sixth negative ion mode data acquired consecutively in the PEG 300 sample.

Overall, the negative SIMS spectral comparisons of the same sample (e.g., PEG 300) in the negative ion mode show good reproducibility, thus giving assurance of data quality. The same applies to other samples we studied in this work.

### Fig. S4a. Static SIMS spectra showing reproducibility of the PEG 300 sample in the negative mode of m/z− 0–200.

N1, N2, N3, N4, N5 and N6 represent the first, second, third, fourth, fifth and sixth negative ion mode data acquired consecutively in the PEG 300 sample.

### Fig. S4b. Static SIMS spectra showing reproducibility of the PEG 300 sample in the negative mode of m/z− 200–500.

N1, N2, N3, N4, N5 and N6 represent the first, second, third, fourth, fifth and sixth negative ion mode data acquired consecutively in the PEG 300 sample.

### Fig. S4c. Static SIMS spectra showing reproducibility of the PEG 300 sample in the negative mode of m/z− 500–800.

N1, N2, N3, N4, N5 and N6 represent the first, second, third, fourth, fifth and sixth negative ion mode data acquired consecutively in the PEG 300 sample.

Overall, the absolute SIMS spectral comparisons of the same sample (e.g., PEG 300) in the negative ion mode are consistent with the normalized ones, and show good reproducibility, thus giving assurance of data quality. The same applies to other samples we studied in this work.

### Fig. S5. Normalized SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the positive mode of m/z+ 0–200.

Normalized intensity (Norm. Int.) is calculated by dividing specific peak intensities to the total ion intensities of each sample, respectively.  The red, blue, and green color represent different series of PEG peaks, namely red stands for HO(CH2CH2O)nH2+, bule stands for HO(CH2CH2O)nHNa+, and green corresponds to fragment peaks.  More details of discussion can be found in main text.

### Fig. S6a. Normalized SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the negative mode of m/z− 0–200.

Normalized intensity (Norm. Int.) is calculated by dividing specific peak intensities to the total ion intensities of each sample, respectively.  More details of discussion can be found in main text.

### Fig. S6b. Normalized SIMS spectral comparison of HEG, PEGs, Clinique and Purity in the negative mode of m/z− 200–500.

Normalized intensity (Norm. Int.) is calculated by dividing specific peak intensities to the total ion intensities of each sample, respectively.  More details of discussion can be found in main text.

### Fig. S6c. Normalized SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the negative mode of m/z− 500–800.

Normalized intensity (Norm. Int.) is calculated by dividing specific peak intensities to the total ion intensities of each sample, respectively.  More details of discussion can be found in main text.  Figures S6a-6c show similar observations to those in the positive ion mode can be found in the negative ion mode.  First, a series of PEG characteristic peak are observed with reasonable peak intensities (Table S2), such as m/z− 61.032 C2H5O2−, 105.054 C4H9O3−, 149.082 C6H13O4−, 193.108 C8H17O5−, 237.134 C10H21O6−, 281.159 C12H25O7−, 325.185 C14H29O8−, 369.216 C16H33O9−, 413.240 C18H37O10−, 457.267 C20H41O11−, 501.290 C22H45O12−, 545.290 C24H49O13−, 589.366 C26H53O14−, 633.371 C28H57O15−, and 677.397 C30H61O16−.  These peaks exhibit a mass change that can be expressed by the general formula, i.e., HO(CH2CH2O)n−, where n ranges from 1 to 15.  These peaks are formed when the PEG molecules HO(CH2CH2O)nH lose a H atom.  This observation confirms that ToF-SIMS can capture the characteristic peak patterns in PEG samples.  A previous study also reported ToF-SIMS could capture PEG characteristic peaks in the cross-section of ink-printed paper.  However, they did not give the formula of the peaks (https://www.eag.com/app-note/imaging-cross-sections-by-tof-sims/).  Second, ToF-SIMS can identify differences among PEGs.  For example, the identified characteristic peak m/z− 325.185 C14H29O8− is observed with highest intensities in HEG and PEG 200 samples, respectively.  However, other characteristic peaks, such as m/z− 61.032 C2H5O2−, 105.054 C4H9O3−, 369.216 C16H33O9−, 413.240 C18H37O10−, 457.267 C20H41O11−, 501.290 C22H45O12−, 545.290 C24H49O13−, 589.366 C26H53O14−, and 633.371 C28H57O15− are observed with relative high intensities in PEG 300 and 400 samples.  Third, ToF-SIMS can detect PEGs in real-word cosmetic products.  For instance, characteristic peaks of PEG, such as m/z− 61.032 C2H5O2−, 193.108 C8H17O5−, 281.159 C12H25O7−, and 325.185 C14H29O8− are observed not only in PEG samples but also in Purity and Clinique cosmetic product samples.  Additionally, the peak m/z− 193.108 C8H17O5− is observed with relative high intensity in both Purity and Clinique samples.  Interestingly, the peak m/z− 281.159 C12H25O7− is observed with highest intensity in Clinique sample.

### Fig. S7. Static SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the positive mode of m/z+ 200–500 (a) and 500–800 (b).

The red, blue, and green color represent different series of PEG peaks. Namely, red stands for HO(CH2CH2O)nH2+, bule stands for HO(CH2CH2O)nHNa+, and green corresponds to fragment peaks.  More details of discussion can be found in main text.

### Fig. S8. Static SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the positive mode of m/z+ 0–200.

The red, blue, and green color represent different series of PEG peaks. Namely, red stands for HO(CH2CH2O)nH2+, bule stands for HO(CH2CH2O)nHNa+, and green corresponds to fragment peaks.  More details of discussion can be found in main text.

### Fig. S9a. Static SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the negative mode of m/z− 0–200.

The absolute counts of these peaks are reasonable and consistent with normalized ones.

### Fig. S9b. Static SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the negative mode of m/z− 200–500.

The absolute counts of these peaks are reasonable and consistent with normalized ones.

### Fig. S9c. Static SIMS spectral comparison of HEG, PEGs, Clinique, and Purity in the negative mode of m/z− 500–800.

The absolute counts of these peaks are reasonable and consistent with normalized ones.

### Fig. S10. SIMS spectral PCA results of HEG, PEGs, Clinique, and Purity in the negative mode: Scores plots of PC1 vs. PC2 (a), PC2 vs. PC4 (b) and loadings plots of PC1 (c), PC2 (d), and PC4 (e) in m/z− 50–800.  Peaks are labelled in their center masses.

Figure S10 displays scores plots of PC1 vs. PC2, PC2 vs. PC4, and corresponding principal component (PC) loadings plots in the negative mode.  PC1, PC2, and PC4 can explain more than 77% of all data.  Specifically, PC1 explains 40.7% of data; and it primarily separates PEG 300, and PEG 400 from HEG, PEG 200, PEG 4000, Purity, and Clinique (Fig. S10a).  PC2 explains 30.8% of data; and it separates HEG, PEG 200 and PEG 4000 from PEG 300, PEG 400, Purity, and Clinique (Fig. S10a).  PC4 explains 6.0% of data and separates HEG, PEG 200, PEG 300, and Purity from PEG 400, PEG 4000, and Clinique (Fig. S10b).

In PC1 positive mode loadings, PEG 300 and PEG 400 are the main contributors, indicating PEG 300 and PEG 400 share significant similarities in terms of their components.  This observation is consistent with the spectral result that the most characteristic peaks are observed with relative high intensities in these two samples.  The characteristic peaks, such as m/z− 61.031 C2H5O2−, 105.054 C4H9O3−, 193.108 C8H17O5−, 325.185 C14H29O8−, 369.216 C16H33O9−, 413.240 C18H37O10−, 457.267 C20H41O11−, 501.290 C22H45O12−, 545.290 C24H49O13−, 589.366 C26H53O14−, 633.371 C28H57O15−, and 677.397 C30H61O16− make great contributions to the variance (Fig. S10c).  PC1 negative separates HEG, PEG 200, PEG 4000, Purity, and Clinique from the PEG 300 and PEG 400 (Fig. S10a), suggesting that the compositions of these sample are largely different from PEG 300 and PEG 400.  Several unidentified peaks, such as m/z− 79.970, 97.029, 151.015, 183.011, 265.079, and 279.104, display high loadings in PC1 negative mode loadings, showing that these peaks contribute more in HEG, PEG 200, PEG 4000, Purity, and Clinique.

In PC2 negative mode loadings, Purity and Clinique share common peaks with PEG 300 and PEG 400; and some of these peaks are identified as m/z− 413.240 C18H37O10−, 457.267 C20H41O11−, 501.290 C22H45O12−, 545.290 C24H49O13−, and 589.366 C26H53O14− (Fig. S10d).  In PC2 positive mode loadings, HEG, PEG 200, and PEG 4000 share some similarities in their compositions.  The identified peak m/z− 325.185 C14H29O8− and unidentified peaks, such as m/z− 63.963, 79.970, 136.919, 183.011, 197.022, 311.174, 339.186, 645.316, 647.309, 659.324, and 673.338 are the main contributors.

In PC4 positive mode loadings, Purity shares some common peaks with HEG, PEG 200, and PEG 300.  These peaks, including m/z−369.216 C16H33O9−, 413.240 C18H37O10−, and 457.267 C20H41O11−, are the main contributors of PC4 positive (Fig. S10e).  In addition, several unidentified peaks, such as m/z− 62.016, 77.050, 136.919, 147.071, 265.079, 297.147, 396.149, 410.151, and 499.374 make contributions.  In PC4 negative mode loadings, Clinique share similarities with PEG 400 and PEG 4000, and the main contribute peaks are m/z− 325.185 C14H29O8−, 659.324 and 673.338.

### Fig. S11. SIMS 2D image comparisons of key peaks (371.227, 415.252, 657.370, and 701.392) in the positive mode: (a) HEG, (b) PEG 200, (c) PEG 300, (d) PEG 400, (e) PEG 4000, (f) Purity, and (g) Clinique.

The absolute counts of these peaks are reasonable and consistent with normalized ones.  The counts of peaks m/z+ 657.370 and 701.392 in PEG 300 are approximately 10; however, the SNRs of them are larger than 160 (Table S7), suggesting they are real signals not noise.  The same applies to other samples studied in this work. Black color in 2D images means no signals are detected.

### Fig. S12. Normalized SIMS 2D image comparisons of key peaks (53.001, 107.075, 129.059, and 217.106) in the positive mode: (a) HEG, (b) PEG 200, (c) PEG 300, (d) PEG 400, (e) PEG 4000, (f) Purity, and (g) Clinique.

The detailed discussion is illustrated in main text. Normalized intensity (Norm. Int.) is calculated by dividing specific peak intensities to the total ion intensities of each sample, respectively.

### Fig. S13. Normalized SIMS 2D image comparisons of key peaks (371.227, 415.252, 657.370, and 701.392) in the positive mode: (a) HEG, (b) PEG 200, (c) PEG 300, (d) PEG 400, (e) PEG 4000, (f) Purity, and (g) Clinique.

The detailed discussion is illustrated in main text. Normalized intensity (Norm. Int.) is calculated by dividing specific peak intensities to the total ion intensities of each sample, respectively.

### Fig. S14. Normalized SIMS 2D image comparisons of key peaks in the negative mode: (a) HEG, (b) PEG 200, (c) PEG 300, (d) PEG 400, (e) PEG 4000, (f) Purity, and (g) Clinique.

Normalized intensity (Norm. Int.) is calculated by dividing specific peak intensities to the total ion intensities of each sample, respectively.  Figure S14 illustrates the 2D comparisons of selected key peaks observed in representative HEG, PEGs, and real-world cosmetic products in the negative ion mode.  The color scale ranging from red to dark signifies higher and lower relative ion intensities, respectively.  The 2D image comparison in negative ion mode shows similar results to those observed in positive ion mode.  First, HEG shares some common peaks with HEGs, albeit with varying intensities, suggesting that ToF-SIMS detects the similarities and differences among samples.  For example, peaks m/z− 61.032 C2H5O2−, 105.054 C4H9O3−, 193.108 C8H17O5−, 281.159 C12H25O7−, and 325.185 C14H29O8− are observed in HEG, PEG 200, PEG 300, PEG 400, and PEG 4000.  Among these peaks, m/z− 325.185 C14H29O8− is more abundant in HEG, and the rest peaks are more abundant in PEGs.  What’s more, peaks m/z− 457.267 C20H41O11− and 501.290 C22H45O12− are detected with rich abundance only in PEG 300 and PEG 400.  Second, ToF-SIMS detects PEGs in real-word cosmetic products.  For instance, peaks m/z− 193.108 C8H17O5− and 281.159 C12H25O7− are observed with rich abundance in Purity and Clinique.

### Fig. S15. SIMS 2D image comparisons of key peaks in the positive mode: (a) HEG, (b) PEG 200, (c) PEG 300, (d) PEG 400, (e) PEG 4000, (f) Purity, and (g) Clinique.

The absolute counts of these peaks are reasonable and consistent with normalized ones.  The counts of peaks m/z+ 193.108 C8H17O5− and 281.159 C12H25O7− in PEG 300 are around 10, however, the SNRs of them are larger than 240 (Table S8), suggesting that they are real signals not noise.  The same applies to other samples studied in this work. Black color in 2D images means no signals were detected in the surface.

# Supplementary Tables

### Table S1. The HEG, PEGs, and real-word domestic products sample matrix.

| Sample No. | Sample name | Description |
| --- | --- | --- |
| 1 | HEG | Clear, colorless liquid |
| 2 | PEG 200 | Clear, colorless liquid |
| 3 | PEG 300 | Clear, colorless liquid |
| 4 | PEG 400 | Clear, colorless liquid |
| 5 | PEG 4000 | Milky-colored solid |
| 6 | Clinique | Yellow liquid |
| 7 | Purity | Light yellow liquid |
| 8 | Si control | Sample control |

The sample preparation was conducted in the fume hood to reduce possible air contamination. The preparation of the silicon wafer control follows existing procedures reported in our earlier publications 1, 2.

### Table S2. Key possible peak identification in the negative mode.

| m/z−theo. | m/z−obs. | ΔM, ppm | Formula | Description | Ref. |
| --- | --- | --- | --- | --- | --- |
| 61.028 | 61.031 | 49.158 | C2H5O2− | HO(CH2CH2O)− | This study |
| 105.055 | 105.054 | 9.519 | C4H9O3− | HO(CH2CH2O)2− | This study |
| 149.081 | 149.082 | 6.708 | C6H13O4− | HO(CH2CH2O)3− | This study |
| 193.107 | 193.108 | 5.178 | C8H17O5− | HO(CH2CH2O)4− | This study |
| 237.133 | 237.134 | 4.217 | C10H21O6− | HO(CH2CH2O)5− | This study |
| 281.159 | 281.159 | 0.000 | C12H25O7− | HO(CH2CH2O)6− | This study |
| 325.186 | 325.185 | 3.075 | C14H29O8− | HO(CH2CH2O)7− | This study |
| 369.212 | 369.216 | 2.708 | C16H33O9− | HO(CH2CH2O)8− | This study |
| 413.238 | 413.240 | 4.840 | C18H37O10− | HO(CH2CH2O)9− | This study |
| 457.264 | 457.267 | 6.561 | C20H41O11− | HO(CH2CH2O)10− | This study |
| 501.291 | 501.290 | 1.995 | C22H45O12− | HO(CH2CH2O)11− | This study |
| 545.317 | 545.290 | 49.512 | C24H49O13− | HO(CH2CH2O)12− | This study |
| 589.343 | 589.366 | 39.027 | C26H53O14− | HO(CH2CH2O)13− | This study |
| 633.369 | 633.371 | 3.158 | C28H57O15− | HO(CH2CH2O)14− | This study |
| 677.395 | 677.397 | 2.952 | C30H61O16− | HO(CH2CH2O)15− | This study |

Footnote:

m/z−theo.: theoretical mass to charge ratio in the negative ion mode.

m/z−obs.: observed mass to charge ratio in the negative ion mode.

ΔM:= Abs (106 × (m/z−obs.− m/z−theo.)/ m/z−theo.) (expressed in ppm) 3, 4.

### Table S3. Summary of peak area and peak height of PEG 300 representative peaks in positive ion mode.

| m/z+obs.a | Peak Areab | Area S.D.c | Area RSD%c | Peak heightd | Peak height S.D.e | Peak height RSD%e |
| --- | --- | --- | --- | --- | --- | --- |
| 31.019 | 4.23E+03 | 6.08E+01 | 1.44% | 4.32E+05 | 2.09E+04 | 4.84% |
| 45.035 | 2.16E+04 | 2.10E+01 | 0.10% | 2.72E+06 | 1.23E+05 | 4.52% |
| 53.001 | 8.63E+02 | 1.25E+01 | 1.45% | 5.84E+04 | 7.08E+03 | 12.13% |
| 63.045 | 3.13E+01 | 1.40E+00 | 4.49% | 2.10E+03 | 6.95E+01 | 3.32% |
| 81.074 | 3.99E+01 | 2.58E+00 | 6.47% | 1.82E+03 | 6.12E+01 | 3.36% |
| 89.064 | 1.70E+04 | 3.18E+02 | 1.87% | 5.91E+05 | 4.67E+04 | 7.91% |
| 107.075 | 6.32E+01 | 1.87E+00 | 2.95% | 2.38E+03 | 1.34E+02 | 5.63% |
| 129.059 | 7.57E+01 | 4.19E+00 | 5.54% | 1.68E+03 | 1.36E+01 | 0.81% |
| 133.094 | 5.28E+03 | 1.49E+02 | 2.82% | 1.23E+05 | 2.62E+03 | 2.13% |
| 151.098 | 8.88E+01 | 4.97E+00 | 5.60% | 2.42E+03 | 1.10E+02 | 4.55% |
| 173.081 | 6.50E+01 | 1.99E+00 | 3.06% | 1.05E+03 | 4.22E+01 | 4.03% |
| 175.103 | 1.64E+03 | 1.35E+02 | 8.23% | 3.91E+04 | 1.03E+03 | 2.63% |
| 195.123 | 1.31E+02 | 6.61E+00 | 5.04% | 3.60E+03 | 6.17E+01 | 1.72% |
| 217.106 | 9.61E+01 | 8.61E-01 | 0.90% | 1.80E+03 | 7.25E+01 | 4.03% |
| 221.150 | 8.03E+02 | 3.49E+01 | 4.34% | 1.49E+04 | 6.81E+02 | 4.58% |
| 239.148 | 2.69E+02 | 7.18E+00 | 2.67% | 4.39E+03 | 3.69E+02 | 8.40% |
| 261.128 | 1.45E+02 | 5.45E+00 | 3.76% | 2.70E+03 | 2.00E+02 | 7.40% |
| 283.176 | 4.47E+02 | 1.11E+01 | 2.49% | 6.52E+03 | 3.37E+02 | 5.17% |
| 305.151 | 2.00E+02 | 8.48E+00 | 4.24% | 3.91E+03 | 8.14E+01 | 2.08% |
| 327.201 | 2.00E+03 | 4.66E+01 | 2.33% | 3.91E+04 | 1.49E+03 | 3.80% |
| 349.181 | 3.56E+03 | 9.39E+01 | 2.63% | 6.70E+04 | 5.84E+02 | 0.87% |
| 371.227 | 9.93E+03 | 3.96E+02 | 3.99% | 1.81E+05 | 1.28E+04 | 7.10% |
| 393.210 | 1.82E+04 | 1.10E+03 | 6.04% | 3.36E+05 | 8.51E+03 | 2.53% |
| 415.252 | 9.19E+03 | 3.88E+02 | 4.22% | 1.48E+05 | 9.11E+03 | 6.14% |
| 437.238 | 1.53E+04 | 3.17E+02 | 2.08% | 2.41E+05 | 8.90E+03 | 3.70% |
| 459.280 | 6.38E+03 | 1.75E+02 | 2.74% | 8.83E+04 | 4.72E+03 | 5.34% |
| 481.263 | 8.74E+03 | 2.04E+02 | 2.34% | 1.19E+05 | 1.51E+03 | 1.27% |
| 503.307 | 3.26E+03 | 1.31E+02 | 4.02% | 3.95E+04 | 1.83E+03 | 4.64% |
| 525.293 | 4.15E+03 | 8.28E+01 | 2.00% | 4.57E+04 | 6.46E+02 | 1.41% |
| 547.300 | 1.28E+03 | 6.01E+01 | 4.70% | 1.31E+04 | 6.50E+02 | 4.97% |
| 569.281 | 1.71E+03 | 5.10E+01 | 2.99% | 1.67E+04 | 4.07E+02 | 2.44% |
| 591.354 | 4.90E+02 | 2.43E+01 | 4.96% | 6.42E+03 | 2.50E+02 | 3.89% |
| 613.352 | 7.95E+02 | 2.12E+01 | 2.67% | 6.41E+03 | 1.82E+02 | 2.84% |
| 635.399 | 2.69E+02 | 7.95E+00 | 2.95% | 2.05E+03 | 6.76E+01 | 3.30% |
| 657.367 | 3.18E+02 | 6.37E+00 | 2.00% | 2.43E+03 | 5.51E+01 | 2.27% |
| 679.417 | 1.22E+02 | 4.94E+00 | 4.04% | 8.56E+02 | 5.91E+01 | 6.90% |
| 701.392 | 1.72E+02 | 5.51E+00 | 3.21% | 1.16E+03 | 4.71E+01 | 4.05% |

Footnote:

a: m/z+obs.: observed mass to charge ratio in the positive ion mode.

b: average peak area of three replicate samples.

c: standard deviation (S.D.) and relative standard deviation (RSD%) of peak area.  Relative standard deviation (RSD%)=S.D./Average100%.

d: average peak height of four replicate samples.

e: standard deviation (S.D.) and relative standard deviation (RSD%) of peak height.

### Table S4. Ratios of peak area and peak height of PEG 300 representative peaks in positive ion mode.

| m/z+obs. | Peak Area ratioa | Area ratio S.D.b | Area ratio RSD%b | Peak height ratiod | Height ratio S.D.e | Peak height ratio RSD%f |
| --- | --- | --- | --- | --- | --- | --- |
| 31.019 | 0.0366 | 0.0007 | 1.91% | 0.1657 | 0.0037 | 2.23% |
| 45.033 | 0.1556 | 0.0019 | 1.22% | 0.5065 | 0.0146 | 2.88% |
| 53.001 | 0.0075 | 0.0002 | 2.67% | 0.0224 | 0.0021 | 9.38% |
| 63.045 | 0.0003 | 0.0000 | 0.00% | 0.0008 | 0.0000 | 0.00% |
| 81.074 | 0.0003 | 0.0000 | 0.00% | 0.0007 | 0.0000 | 0.00% |
| 89.064 | 0.1468 | 0.0041 | 2.79% | 0.2264 | 0.0118 | 5.21% |
| 107.075 | 0.0005 | 0.0000 | 0.00% | 0.0009 | 0.0001 | 11.11% |
| 129.059 | 0.0007 | 0.0000 | 0.00% | 0.0006 | 0.0000 | 0.00% |
| 133.094 | 0.0457 | 0.0014 | 3.06% | 0.0472 | 0.0015 | 3.18% |
| 151.098 | 0.0008 | 0.0000 | 0.00% | 0.0009 | 0.0000 | 0.00% |
| 173.081 | 0.0006 | 0.0000 | 0.00% | 0.0004 | 0.0000 | 0.00% |
| 175.096 | 0.0118 | 0.0009 | 7.63% | 0.0073 | 0.0003 | 4.11% |
| 195.123 | 0.0011 | 0.0001 | 9.09% | 0.0014 | 0.0000 | 0.00% |
| 217.106 | 0.0008 | 0.0000 | 0.00% | 0.0007 | 0.0000 | 0.00% |
| 221.150 | 0.0069 | 0.0003 | 4.35% | 0.0057 | 0.0003 | 5.26% |
| 239.148 | 0.0023 | 0.0000 | 0.00% | 0.0017 | 0.0001 | 5.88% |
| 261.128 | 0.0013 | 0.0000 | 0.00% | 0.0010 | 0.0001 | 10.00% |
| 283.176 | 0.0039 | 0.0001 | 2.56% | 0.0025 | 0.0001 | 4.00% |
| 305.151 | 0.0017 | 0.0001 | 5.88% | 0.0015 | 0.0000 | 0.00% |
| 327.201 | 0.0173 | 0.0004 | 2.31% | 0.0150 | 0.0009 | 6.00% |
| 349.181 | 0.0308 | 0.0004 | 1.30% | 0.0257 | 0.0006 | 2.33% |
| 371.227 | 0.0859 | 0.0025 | 2.91% | 0.0692 | 0.0040 | 5.78% |
| 393.210 | 0.1572 | 0.0075 | 4.77% | 0.1289 | 0.0061 | 4.73% |
| 415.252 | 0.0795 | 0.0030 | 3.77% | 0.0570 | 0.0046 | 8.07% |
| 437.238 | 0.1321 | 0.0026 | 1.97% | 0.0924 | 0.0053 | 5.74% |
| 459.280 | 0.0552 | 0.0022 | 3.99% | 0.0339 | 0.0010 | 2.95% |
| 481.263 | 0.0756 | 0.0017 | 2.25% | 0.0458 | 0.0015 | 3.28% |
| 503.307 | 0.0282 | 0.0014 | 4.96% | 0.0152 | 0.0004 | 2.63% |
| 525.293 | 0.0359 | 0.0007 | 1.95% | 0.0175 | 0.0006 | 3.43% |
| 547.300 | 0.0110 | 0.0006 | 5.45% | 0.0050 | 0.0001 | 2.00% |
| 569.281 | 0.0148 | 0.0004 | 2.70% | 0.0064 | 0.0003 | 4.69% |
| 591.354 | 0.0042 | 0.0002 | 4.76% | 0.0025 | 0.0001 | 4.00% |
| 613.352 | 0.0069 | 0.0001 | 1.45% | 0.0025 | 0.0001 | 4.00% |
| 635.399 | 0.0023 | 0.0001 | 4.35% | 0.0008 | 0.0000 | 0.00% |
| 657.367 | 0.0028 | 0.0000 | 0.00% | 0.0009 | 0.0000 | 0.00% |
| 679.417 | 0.0011 | 0.0000 | 0.00% | 0.0003 | 0.0000 | 0.00% |
| 701.392 | 0.0015 | 0.0000 | 0.00% | 0.0004 | 0.0000 | 0.00% |

Footnote:

a: average peak area ratio between the counts of specific peaks and total counts of all key products/fragments

b: standard deviation (S.D.) of peak area ratio.

c: Relative standard deviation (RSD%)=S.D./Average100%, RSD of the peak area ratio.

d: average peak height ratio of three replicate samples.

e: standard deviation (S.D.) of the peak height ratio.

f: RSD of peak height ratio.

### Table S5. Summary of peak area and peak height of PEG 300 representative peaks in negative ion mode.

| m/z−obs.a | Peak Areab | Area S.D.c | Area RSD%c | Peak Heightd | Peak height S.D.e | Peak height RSD%e |
| --- | --- | --- | --- | --- | --- | --- |
| 61.031 | 1.03E+04 | 1.45E+02 | 1.41% | 4.03E+05 | 9.25E+03 | 2.30% |
| 105.054 | 4.25E+03 | 4.51E+01 | 1.06% | 1.24E+05 | 4.15E+03 | 3.35% |
| 149.082 | 4.34E+02 | 8.71E+00 | 2.01% | 9.06E+03 | 3.00E+02 | 3.31% |
| 193.108 | 4.83E+02 | 1.40E+01 | 2.90% | 8.77E+03 | 4.16E+02 | 4.74% |
| 237.134 | 7.22E+02 | 5.95E+00 | 0.82% | 1.22E+04 | 4.65E+02 | 3.81% |
| 281.159 | 1.02E+03 | 3.10E+01 | 3.04% | 1.42E+04 | 6.89E+02 | 4.85% |
| 325.185 | 8.87E+03 | 5.49E+02 | 6.19% | 1.38E+05 | 7.81E+03 | 5.66% |
| 369.216 | 1.19E+04 | 6.15E+02 | 5.17% | 2.15E+05 | 1.17E+04 | 5.44% |
| 413.240 | 9.55E+03 | 5.24E+02 | 5.49% | 1.38E+05 | 1.11E+04 | 8.04% |
| 457.267 | 4.93E+03 | 1.16E+01 | 0.24% | 6.97E+04 | 4.50E+03 | 6.46% |
| 501.290 | 2.36E+03 | 1.42E+02 | 6.02% | 2.60E+04 | 1.28E+02 | 0.49% |
| 545.290 | 1.00E+03 | 5.30E+01 | 5.30% | 9.34E+03 | 8.11E+02 | 8.68% |
| 589.366 | 4.04E+02 | 1.71E+01 | 4.23% | 4.09E+03 | 2.54E+02 | 6.21% |
| 633.371 | 1.72E+02 | 3.52E+00 | 2.05% | 1.73E+03 | 9.98E+01 | 5.77% |
| 677.397 | 1.02E+02 | 8.39E+00 | 8.23% | 8.92E+02 | 6.74E+01 | 7.56% |

Footnote:

a: m/z−obs..: observed mass to charge ratio in the negative ion mode.

b: average peak area of three replicate samples.

c: standard deviation (S.D.) and relative standard deviation (RSD%) of peak area.  Relative standard deviation (RSD%)=S.D./Average100%.

d: average peak height of four replicate samples.

e: standard deviation (S.D.) and relative standard deviation (RSD%) of peak height.

### Table S6. Ratios of peak area and peak height of PEG 300 representative peaks in negative ion mode.

| m/z−obs. | Peak Area ratioa | Area ratio S.D.b | Area ratio RSD%c | Peak height ratiod | Height ratio S.D.e | Peak height ratio RSD%f |
| --- | --- | --- | --- | --- | --- | --- |
| 61.031 | 0.1817 | 0.0031 | 1.71% | 0.3435 | 0.0060 | 1.75% |
| 105.054 | 0.0752 | 0.0014 | 1.86% | 0.1057 | 0.0033 | 3.12% |
| 149.082 | 0.0077 | 0.0001 | 1.30% | 0.0077 | 0.0001 | 1.30% |
| 193.108 | 0.0086 | 0.0004 | 4.65% | 0.0075 | 0.0002 | 2.67% |
| 237.134 | 0.0128 | 0.0004 | 3.13% | 0.0104 | 0.0002 | 1.92% |
| 281.159 | 0.0180 | 0.0002 | 1.11% | 0.0120 | 0.0003 | 2.50% |
| 325.185 | 0.1571 | 0.0092 | 5.86% | 0.1174 | 0.0059 | 5.03% |
| 369.216 | 0.2111 | 0.0057 | 2.70% | 0.1834 | 0.0056 | 3.05% |
| 413.240 | 0.1690 | 0.0056 | 3.31% | 0.1172 | 0.0097 | 8.28% |
| 457.267 | 0.0874 | 0.0024 | 2.75% | 0.0593 | 0.0024 | 4.05% |
| 501.290 | 0.0418 | 0.0014 | 3.35% | 0.0221 | 0.0005 | 2.26% |
| 545.290 | 0.0178 | 0.0006 | 3.37% | 0.0079 | 0.0005 | 6.33% |
| 589.366 | 0.0071 | 0.0002 | 2.82% | 0.0035 | 0.0002 | 5.71% |
| 633.371 | 0.0031 | 0.0001 | 3.23% | 0.0015 | 0.0000 | 0.00% |
| 677.397 | 0.0018 | 0.0001 | 5.56% | 0.0008 | 0.0000 | 0.00% |

Footnote:

a: average peak area ratio between the counts of specific peaks and total counts of all key products/fragments.

b: standard deviation (S.D.) of peak area ratio.

c: Relative standard deviation (RSD%)=S.D./Average100%, RSD of the peak area ratio.

d: average peak height ratio of three replicate samples.

e: standard deviation (S.D.) of the peak height ratio.

f: RSD of peak height ratio.

### Table S7. Signal to noise ration of PEG 300 representative peaks in positive ion mode.

| m/z+obs. | Formula | SNRa |
| --- | --- | --- |
| 31.019 | CH3O+ | 61181.57 |
| 45.035 | C2H5O+ | 24762.88 |
| 53.001 | C3HO+ | 2360.79 |
| 63.045 | C2H7O2+ | 47.79 |
| 81.074 | C6H9+ | 45.31 |
| 89.064 | C4H9O2+ | 18901.72 |
| 107.075 | C4H11O3+ | 65.58 |
| 129.059 | C6H9O3+ | 36.56 |
| 133.094 | C6H13O3+ | 2637.15 |
| 151.098 | C6H15O4+ | 101.62 |
| 173.081 | C8H13O4+ | 39.91 |
| 175.103 | C8H15O4+ | 1789.73 |
| 195.123 | C8H19O5+ | 149.86 |
| 217.106 | C10H17O5+ | 43.68 |
| 221.150 | C14H21O2+ | 385.41 |
| 239.148 | C10H23O6+ | 97.20 |
| 261.128 | C12H21O6+ | 46.96 |
| 283.176 | C12H27O7+ | 121.60 |
| 305.151 | C14H25O7+ | 60.84 |
| 327.201 | C14H31O8+ | 815.46 |
| 349.181 | C16H29O8+ | 1442.41 |
| 371.227 | C16H35O9+ | 3266.17 |
| 393.210 | C18H33O9+ | 5961.19 |
| 415.252 | C18H39O10+ | 4046.90 |
| 437.238 | C20H37O10+ | 5004.03 |
| 459.280 | C20H43O11+ | 2501.32 |
| 481.263 | C22H41O11+ | 3337.48 |
| 503.307 | C22H47O12+ | 1912.00 |
| 525.293 | C24H45O12+ | 1614.50 |
| 547.300 | C24H51O13+ | 1057.20 |
| 569.281 | C26H49O13+ | 743.69 |
| 591.354 | C26H55O14+ | 551.89 |
| 613.352 | C28H53O14+ | 455.30 |
| 635.399 | C28H59O15+ | 319.60 |
| 657.367 | C30H57O15+ | 848.00 |
| 679.417 | C30H63O16+ | 165.25 |
| 701.392 | C32H61O16+ | 168.40 |

Footnote:

a SNR: signal to noise ratio.

### Table S8. Signal to noise ration of PEG 300 representative peaks in negative ion mode.

| m/z−obs. | Formula | SNRa |
| --- | --- | --- |
| 61.031 | C2H5O2− | 17996.30 |
| 105.054 | C4H9O3− | 9166.14 |
| 149.082 | C6H13O4− | 666.71 |
| 193.108 | C8H17O5− | 246.32 |
| 237.134 | C10H21O6− | 376.00 |
| 281.159 | C12H25O7− | 401.32 |
| 325.185 | C14H29O8− | 2207.52 |
| 369.216 | C16H33O9− | 2987.04 |
| 413.240 | C18H37O10− | 2306.15 |
| 457.267 | C20H41O11− | 1454.48 |
| 501.290 | C22H45O12− | 772.69 |
| 545.290 | C24H49O13− | 407.00 |
| 589.366 | C26H53O14− | 218.72 |
| 633.371 | C28H57O15− | 87.10 |
| 677.397 | C30H61O16− | 45.95 |

Footnote:

a SNR: signal to noise ratio.

# Reference

1.	Y. Fu, Y. Zhang, F. Zhang, J. Chen, Z. Zhu and X.-Y. Yu, Atmos. Environ., 2018, 191, 36-45.

2.	X. Sui, Y. Zhou, F. Zhang, Y. Zhang, J. Chen, Z. Zhu and X. Y. Yu, Surf. Interface Anal., 2018, 50, 927-938.

3.	I. S. Gilmore and M. P. Seah, Appl. Surf. Sci., 2000, 161, 465-480.

4.	X.-Y. Yu, C. Yang, J. X. Gao, J.; , X. Sui, L. Zhong, Y. Zhang and J. Son, Front. Chem., 2023, 11, 1253685.