Comparative Study of Thermal Stability and Thermal Degradation Kinetics of Poly(Vinyl Ethers) with Different Side Groups

Nikolaos V. Plachouras, Kosmas Michos–Stavridis, Stavros Zouganelis and Marinos Pitsikalis*

Industrial Chemistry Laboratory, Department of Chemistry, National and Kapodistrian University of Athens, Panepistimiopolis Zografou, Athens 15771, Greece.

Figure S1. 1H–NMR spectrum of the monomer PEVE in CDCl3.

PPEVE 2K compared to PPEVE 8K at 3 ℃/min heating rate:

PPEVE 2K compared to PPEVE 8K at 5 ℃/min heating rate:

PPEVE 2K compared to PPEVE 8K at 7 ℃/min heating rate:

PPEVE 2K compared to PPEVE 8K at 10 ℃/min heating rate:

PPEVE 2K compared to PPEVE 8K at 15 ℃/min heating rate:

PPEVE 2K compared to PPEVE 8K at 20 ℃/min heating rate:

Figure S2. Comparative TGA and DTG plots for samples PPEVE 2K and PPEVE 8K at various heating rates

PPEVE 2K compared to PAEVE 8K at 3 ℃/min heating rate:

PPEVE 2K compared to PAEVE 8K at 5 ℃/min heating rate:

PPEVE 2K compared to PAEVE 8K at 7 ℃/min heating rate:

PPEVE 2K compared to PAEVE 8K at 10 ℃/min heating rate:

PPEVE 2K compared to PAEVE 8K at 15 ℃/min heating rate:

PPEVE 2K compared to PAEVE 8K at 20 ℃/min heating rate:

Figure S3. Comparative TGA and DTG plots for samples PPEVE 2K and PAEVE 2K at various heating rates

Table S1. Models for the analysis of the thermal decomposition

| No. | Model | g(a) | f(a) | Rate-determining mechanism |
| --- | --- | --- | --- | --- |
| 1. Chemical process or mechanism non-involving equations |  |  |  |  |
| 1 | F 1/3 | 1−(1−a)2/3 | (3/2)(1−a)1/3 | Chemical reaction |
| 2 | F ¾ | 1−(1−a)1/4 | 4(1−a)3/4 | Chemical reaction |
| 3 | F 3/2 | (1−a)−1/2−1 | 2(1−a)3/2 | Chemical reaction |
| 4 | F 2 | (1−a)−1−1 | (1−a)2 | Chemical reaction |
| 5 | F 3 | (1−a)−2−1 | (1/2)(1−a)3 | Chemical reaction |
| 6 | F 4 | (1−a)−3−1 | (1/3)(1−a)4 | Chemical reaction |
| 7 | G 1 | 1−(1−a)2 | 1/[2(1−a)] | Chemical reaction |
| 8 | G 2 | 1−(1−a)3 | 1/[3(1−a)2] | Chemical reaction |
| 9 | G 3 | 1−(1−a)4 | 1/[4(1−a)3] | Chemical reaction |
| 2. Acceleratory rate equations |  |  |  |  |
| 10 | P 3/2 | a3/2 | (2/3)a−1/2 | Nucleation (power law) |
| 11 | P ½ | a1/2 | 2a1/2 | Nucleation (power law) |
| 12 | P 1/3 | a1/3 | 3a2/3 | Nucleation (power law) |
| 13 | P ¼ | a1/4 | 4a3/4 | Nucleation (power law) |
| 14 | P 2 | a2 | (1/2)a−1 | Nucleation (parabolic law) |
| 15 | E 1 | lna | a | Nucleation (exponential law) |
| 16 | E 2 | lna2 | a/2 | Nucleation (exponential law) |
| 3. Sigmoidal rate equations or random nucleation and subsequent growth |  |  |  |  |
| 17 | A 1, F 1 | −ln(1−a) | 1−a | Random nucleation/first order (Mampel) |
| 18 | A 2/3 | [−ln(1−a)]3/2 | (2/3)(1−a)[−ln(1−a)]−1/2 | Random nucleation (Avrami-Erofeev) |
| 19 | A 3/2 | [−ln(1−a)]2/3 | (3/2(1−a)[−ln(1−a)]1/3 | Random nucleation (Avrami-Erofeev) |
| 20 | A ¾ | [−ln(1−a)]4/3 | (3/4)(1−a)[−ln(1−a)]−1/3 | Random nucleation (Avrami-Erofeev) |
| 21 | A 5/2 | [−ln(1−a)]2/5 | (5/2)(1−a)[−ln(1−a)]3/5 | Random nucleation (Avrami-Erofeev) |
| 22 | A 2 | [−ln(1−a)]1/2 | 2(1−a)[−ln(1−a)]1/2 | Random nucleation (Avrami-Erofeev) |
| 23 | A 3 | [−ln(1−a)]1/3 | 3(1−a)[−ln(1−a)]2/3 | Random nucleation (Avrami-Erofeev) |
| 24 | A 4 | [−ln(1−a)]1/4 | 4(1−a)[−ln(1−a)]3/4 | Random nucleation (Avrami-Erofeev) |
| 25 | A ½ | [−ln(1−a)]2 | 1/2(1−a)[−ln(1−a)]−1 | Random nucleation (Avrami-Erofeev) |
| 26 | A 1/3 | [−ln(1−a)]3 | 1/3(1−a)[−ln(1−a)]−2 | Random nucleation (Avrami-Erofeev) |
| 27 | A ¼ | [−ln(1−a)]4 | 1/4(1−a)[−ln(1−a)]−3 | Random nucleation (Avrami-Erofeev) |
| 28 | B 1 | ln[a/(1−a)] | a/(1−a) | Branching nuclei (Prout–Tompkins) |
| 4. Deceleratory rate equations (phase boundary reaction) |  |  |  |  |
| 29 | R 1, F 0, P 1 | a | 1 | Contracting disk |
| 30 | R 2, F 1/2 | 1−(1−a)1/2 | 2(1−a)1/2 | Contracting cylinder |
| 31 | R 3, F 2/3 | 1−(1−a)1/3 | 3(1−a)2/3 | Contracting sphere |
| 5. Deceleratory rate equations (equations based on the diffusion mechanism) |  |  |  |  |
| 32 | D 1 | a2 | 1/(2a) | One-dimensional diffusion |
| 33 | D 2 | a+(1−a)ln(1−a) | [−ln(1−a)]−1 | Three-dimensional diffusion |
| 34 | D 3 | [1−(1−a)1/3]2 | (3/2)(1−a)2/3[1−(1−a)1/3]−1 | Three-dimensional diffusion (Jander) |
| 35 | D 4 | 1−(2/3)a−(1−a)2/3 | (3/2)[(1−a)−1/3−1]−1 | Three-dimensional diffusion (Ginstling–Brounshtein) |
| 36 | D 5 | [(1−a)−1/3−1]2 | (3/2)(1−a)4/3[(1−a)−1/3−1]−1 | Three-dimensional diffusion (Crank) |
| 37 | D 6 | [(1+a)1/3−1]2 | (3/2)(1+a)2/3[(1+a)1/3−1]−1 | Three-dimensional diffusion |
| 38 | D 7 | 1+(2/3)a−(1+a)2/3 | 3/2[(1+a)−1/3−1]−1 | Three-dimensional diffusion |
| 39 | D 8 | [(1+a)−1/3−1]2 | 3/2(1+a)4/3[(1+a)−1/3−1]−1 | Three-dimensional diffusion |
| 6. Other kinetic equations with unjustified mechanism |  |  |  |  |
| 40 | G 7 | [1−(1−a)1/2]1/2 | 4{(1−a)[1−(1−a)1/2]}1/2 |  |
| 41 | G 8 | [1−(1−a)1/3]1/2 | 6(1−a)2/3[1−(1−a)1/3]1/2 |  |

Table S2. TGA data at different heating rates

| 3 °C/min |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1st Peak |  |  | 2nd Peak |  |  | 3rd Peak |  |  | 4th Peak |  |  |
| Sample | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) |
| PPEVE 2K | 224.27 | 336.32 | 324.20 | 338.03 | 475.20 | 359.37 | - | - | - | 493.15 | 691.07 | 583.76 |
| PPEVE 8K | - | - | - | - | - | - | 217.78 | 478.07 | 398.09 | 492.21 | 673.89 | 577.94 |
| PAEVE 2K | 143.98 | 263.31 | 236.64 | 269.08 | 338.83 | 282.28 | 383.99 | 460.19 | 426.20 | 483.78 | 624.09 | 537.19 |

| 5 °C/min |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1st Peak |  |  | 2nd Peak |  |  | 3rd Peak |  |  | 4th Peak |  |  |
| Sample | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) |
| PPEVE 2K | 214.87 | 346.95 | 337.25 | 349.87 | 488.46 | 369.91 | - | - | - | 524.32 | 697.60 | 617.36 |
| PPEVE 8K | - | - | - | - | - | - | 227.55 | 493.27 | 407.52 | 533.37 | 706.09 | 603.70 |
| PAEVE 2K | 137.45 | 274.72 | 245.00 | 283.21 | 353.18 | 293.72 | 397.23 | 468.68 | 435.83 | 502.44 | 651.31 | 549.26 |

| 7 °C/min |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1st Peak |  |  | 2nd Peak |  |  | 3rd Peak |  |  | 4th Peak |  |  |
| Sample | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) |
| PPEVE 2K | 231.94 | 354.10 | 340.80 | 356.71 | 500.12 | 370.78 | - | - | - | 522.47 | 745.28 | 620.43 |
| PPEVE 8K | - | - | - | - | - | - | 227.57 | 50140 | 414.03 | 534.61 | 706.41 | 598.07 |
| PAEVE 2K | 158.35 | 284.02 | 249.78 | 291.25 | 353.51 | 297.72 | 401.00 | 486.87 | 438.77 | 509.10 | 677.10 | 559.24 |

| 10 °C/min |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1st Peak |  |  | 2nd Peak |  |  | 3rd Peak |  |  | 4th Peak |  |  |
| Sample | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) |
| PPEVE 2K | 136.76 | 364.14 | 351.55 | 365.80 | 505.16 | 376.39 | - | - | - | 539.29 | 761.06 | 663.23 |
| PPEVE 8K | - | - | - | - | - | - | 235.37 | 529.34 | 425.49 | 553.95 | 731.62 | 621.84 |
| PAEVE 2K | 152.83 | 380.89 | 259.69 | - | - | - | 391.98 | 506.32 | 448.44 | - | - | - |

| 15 °C/min |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1st Peak |  |  | 2nd Peak |  |  | 3rd Peak |  |  | 4th Peak |  |  |
| Sample | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) |
| PPEVE 2K | 122.95 | 375.91 | 363.65 | 376.66 | 522.71 | 392.80 | 542.99 | 616.10 | 592.69 | 618.98 | 800.00 | 675.93 |
| PPEVE 8K | - | - | - | - | - | - | 244.23 | 544.35 | 435.07 | 588.54 | 745.24 | 659.76 |
| PAEVE 2K | 176.47 | 365.55 | 282.12 | - | - | - | 413.60 | 511.60 | 464.94 | - | - | - |

| 20 °C/min |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1st Peak |  |  | 2nd Peak |  |  | 3rd Peak |  |  | 4th Peak |  |  |
| Sample | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) | Start (°C) | End (°C) | Peak (°C) |
| PPEVE 2K | 241.03 | 378.56 | 370.57 | 382.90 | 526.80 | 393.08 | - | - | - | 567.06 | 776.58 | 667.90 |
| PPEVE 8K | - | - | - | - | - | - | 250.50 | 531.94 | 443.79 | 559.16 | 720.96 | 631.63 |
| PAEVE 2K | 183.68 | 372.13 | 291.06 | - | - | - | 421.02 | 423.36 | 465.44 | 553.94 | 764.33 | 608.54 |