Removal of U(VI) from aqueous solution by Al0/Ni0 bimetallic material

Mengyue Ma1; Weixuan Sang1; Yishuo Zhang 1*; Xiaoyan Li 1*

(State Key Laboratory of Nuclear Resources and Environment,

East China University of Technology, Nanchang, Jiangxi 330013, China)

Fig. S1 N2 adsorption–desorption isotherms of Al0/Ni0-BM

Fig. S1 showed the nitrogen adsorption-desorption curve of AlNi-NPs. The adsorption-desorption isotherm of AlNi-NPs material conformed to the IUPAC classification of Ⅳ curve and generated H3 hysteresis loop, which indicated that there were slit-type gaps between particles. According to nitrogen adsorption-desorption data, the relevant parameters were calculated by BET equation and BJH algorithm. The specific surface area of the composite AlNi-NPs was 47.498 m2/g, the pore volume was 0.303 cm3/g, average pore size was 25.523 nm, and the single-layer molecular adsorption capacity was 10.913 cm3.

Fig. S2 SEM and EDS (a) (b) fresh Al0/Ni0-BM; (c) (d) reacted Al0/Ni0-BM.

Table S1 EDS parameters of Al0/Ni0-BM before and after reaction with U(Ⅵ)

| Element | Before the reaction |  | After the reaction with U(Ⅵ) |  |
| --- | --- | --- | --- | --- |
|  | Wt (%) | Atomic (%) | Wt (%) | Atomic (%) |
| C | 6.13 | 14.33 | 5.06 | 12.05 |
| O | 21.42 | 42.86 | 33.87 | 60.53 |
| Ni | 57.41 | 27.45 | 38.41 | 18.71 |
| Al | 15.04 | 15.36 | 6.37 | 6.75 |
| U | 0 | 0 | 16.29 | 1.96 |

Table S2 Parameters for pseudo-first-order and pseudo-second-order kinetics

| T/K | Pseudo-first-order kinetic |  |  |  | pseudo-second-order kinetic |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Qe (mgg-1) | k1 (min-1) | R2 |  | Qe (mgg-1) | k2 (min-1) | R2 |
| 288 | 60.72 | 0.0293 | 0.8481 |  | 109.89 | 0.00034 | 0.9920 |
| 293 | 62.08 | 0.0348 | 0.8542 |  | 113.38 | 0.00049 | 0.9920 |
| 298 | 64.61 | 0.0424 | 0.8693 |  | 115.74 | 0.00067 | 0.9947 |
| 303 | 64.81 | 0.0525 | 0.8802 |  | 120.63 | 0.00098 | 0.9964 |

Table S3 Reduction kinetic parameters

| T/K | Kobs | R2 |
| --- | --- | --- |
| 288 | 0.04579 | 0.95083 |
| 293 | 0.05292 | 0.95301 |
| 298 | 0.07289 | 0.95991 |
| 303 | 0.10255 | 0.97713 |

Table S4 Isotherms parameters for Langmuir and Freundlich models

| T/K | Langmuir |  |  |  | Freundlich |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Qm (mgg-1) | KL (Lmg-1) | R2 |  | KF (Lg-1) | 1/n | R2 |
| 293 | 153.85 | 0.1643 | 0.9484 |  | 79.38 | 0.1249 | 0.7489 |
| 298 | 167.50 | 0.1839 | 0.9600 |  | 87.80 | 0.1227 | 0.7811 |
| 303 | 186.21 | 0.1827 | 0.9410 |  | 98.71 | 0.1154 | 0.7365 |
| 308 | 211.42 | 0.1791 | 0.9245 |  | 111.40 | 0.1100 | 0.7145 |