Photodegradation, DFT and electrochemical studies of carbon nanohorns modified BiSbO4/BiSbS3 heterostructure for an endocrine disrupting agent pentachlorophenol

Maria Batool, Muhammad Nadeem Zafar*

Department of Chemistry, University of Gujrat, Gujrat 50700, Pakistan

*Corresponding author emails:  nadeem.zafar@uog.edu.pk, znadeempk@gmail.com; ORCID ID: 0000-0002-2109-7601 (MN Zafar)

Supporting information

S1. Crystal structure determination of BiSbO4 by using Vesta software

Figure S1. Structural representation of BiSbO4 nanocomposite (a) atomic positions of BiSbO4 without Bismuth (b) bonding of Sb and (type 1) oxygen (c) bonding of Sb and (type 5) oxygen (d) atomic positions of elements in BiSbO4 composite with Bismuth (e) bonding of Bismuth and (type 1) oxygen (f) bonding of bismuth and (type 5) oxygen (g) lateral view of bonding of (type 1) and (type 5) oxygen atoms (h) front view of bonding (type 1) and (type 5) oxygen atoms

S2. Crystal structure determination of BiSbS3 by using Vesta software

Figure S2. Structural representation of BiSbS3 (a) positions of atoms in BiSbS3 composite (b) bonding of (type 1) sulphur with Bismuth (c) bonding of (type 3) sulphur with bismuth (d) bonding of (type 2) sulphur with bismuth (e) bonding of Bismuth and antimony (f) bonding of (type 1) sulphur with antimony (g) bonding of (type 2) sulphur with antimony (h) bonding of (type 3) sulphur with antimony

Figure S3. (a) Effect of BiSbO4, BiSbS3 and BiSbO4/BiSbS3/CNHs dosage and (b) effect of PCP concentration on degradation of PCP onto BiSbO4, BiSbS3 and heterostructure BiSbO4/BiSbS3/CNHs

Figure S4. (a) Time study of (a) BiSbS4 (b) BiSbO3 and (c) heterostructure BiSb O4/BiSbS3/CNHs at optimum conditions for degradation of PCP

Figure S5. Tauc Plot–Optical band gap energy estimation of BiSbO4 and BiSbS3

Figure S6. (a) Effect of other pollutants and (b) effect of scavengers on efficiency of heterostructure BiSbO4/BiSbS3/CNHs for degradation of PCP

Figure 7. Time vs. potential plots of (a) heterostructure BiSbO4/BiSbS3/CNHs, (b) BiSbO4 and (c) BiSbS3

Figure S8. Current density versus scan rate for BiSbO4, BiSbS3 and heterostructure BiSbO4/BiSbS3/CNHs