Supplementary Material

Activated carbon supported Ni-Co and Ni-Cu bimetallic catalysts for lignin depolymerization into short-chain phenolic substances with isopropanol as the H-donating solvent: Activity enhancement and products distribution studies

Fig. S1 N2 adsorption-desorption isotherms of (a) Co/C, (b) Ni/C, (c) Ni-Co/C and (d) Ni-Cu/C catalysts.

Fig. S2 SEM and EDX elemental mapping images of Ni/C. Mag.: 5 kX and 30 kX.

Fig. S3 SEM and EDX elemental mapping images of Co/C. Mag.: 10 kX and 30 kX.

Fig. S4 SEM and EDX elemental mapping images of Cu/C. Mag.: 3 kX and 30 kX.

Fig. S5 The results of the catalysis experiments. (Reaction condition: lignin = 0.5 g, catalysts = 0.3 g, isopropanol = 16 mL, n-decane = 0.5 mL, 4 MPa N2, 250 ℃, 4 h and 700 rpm).

Table S1

Summary of GC-MS analysis of the product distributions from lignin hydrogenolysis.

| Retention Time (Min) | Area (counts) | Compound | Chemical Structure | Molecular Weight (g/mol) |
| --- | --- | --- | --- | --- |
| 9.74 | 278512 | Phenol |  | 94.11 |
| 12.78 | 17688845 | Phenol, 2-methoxy |  | 164.20 |
| 14.51 | 410551 | Benzene, 1,2-dimethoxy |  | 178.23 |
| 15.16 | 932608 | Phenol, 4-ethyl |  | 152.19 |
| 15.56 | 91066 | Phenol, 3-(1-methylethyl) |  | 283.40 |
| 15.81 | 8893457 | Creosol |  | 138.16 |
| 17.16 | 359472 | 3,4-Dimethoxytoluene |  | 152.19 |
| 17.75 | 328228 | Phenol, 2-propyl |  | 346.50 |
| 18.24 | 21890722 | Phenol, 4-ethyl-2-methoxy |  | 166.22 |
| 19.12 | 167691 | 2-Methoxy-4-vinylphenol |  | 150.17 |
| 19.47 | 727304 | Benzene, 4-ethyl-1,2-dimethoxy |  | 166.22 |
| 20.34 | 709333 | Eugenol |  | 164.20 |
| 20.61 | 23554360 | Phenol, 2-methoxy-4-propyl- |  | 264.36 |
| 24.25 | 1008126 | Phenol, 2,5-bis(1,1-dimethylethyl |  | 240.77 |
| 24.69 | 1116098 | Phenol, 3-(dimethylamino) |  | 151.21 |
| 25.10 | 1214620 | Phenol, 4-(ethoxymethyl)-2-methoxy |  | 182.22 |
| 26.64 | 385246 | Benzoic acid, 3-(methylthio) |  | 210.29 |
| 39.27 | 969005 | Benzeneacetic acid, 4-hydroxy |  | 182.17 |
| 42.83 | 198635 | Benzene, 1,4-dimethoxy-2-methyl |  | 220.19 |
| 44.21 | 984385 | Benzaldehyde, 2,4-dihydroxy |  | 152.15 |

Reaction conditions: Lignin = 0.5g, catalyst = 0.3g, isopropanol = 16mL, 250 ℃, 4 h, 4 MPa. using GC-MS,  where acetophenone was used as the internal standard chemical. The components listed were those with a GC-MS yield of more than 0.1 %.

Fig. S6 FT-IR spectra of the nonvolatile products with the Ni-based bimetallic catalysts.

Fig. S7 FT-IR spectra of raw lignin.