Supplementary Information for

An sp-sp2-hybridized molecular carbon allotrope: C16 flake

Wenze Gao, Wei Zheng, Luye Sun, Faming Kang, Zheng Zhou, Wei Xu*

*Corresponding author: xuwei@tongji.edu.cn

The supplementary information includes:

Supplementary Figures 1-4

Supplementary Fig. 1. Characterizations of the C16Cl10 precursor. (a) Chemical structure, (b) STM, and (c) AFM images of C16Cl10. (d-f) Top, left, and front views of DFT-calculated structure of C16Cl10 molecule on the NaCl surface. AFM image was recorded with a CO-functionalized tip, with respect to an STM set point of I = 3 pA, V = 0.3 V above the NaCl surface. Scale bars: 0.5 nm.

Supplementary Fig. 2. Other observed intermediates generated after the manipulation of C16Cl10. (a-c) C16Cl4. (d-f) C16Cl3. (g-i) C16Cl2. Molecular structures are shown in line 1. AFM images (line 2) were recorded with a CO-functionalized tip, with respect to an STM set point of I = 3 pA, V = 0.3 V above the NaCl surface. Line 3 shows corresponding Laplace-filtered AFM images. The scale bar in (b) applies to all images.

Supplementary Fig. 3. Bond length and Mayer bond order analysis of C16 flake. Calculations were conducted at the ωB97XD/def2-TZVP level.

Supplementary Fig. 4. AV1245 analysis for C16 flake calculated over the path indicated by highlight colour (ωB97XD/def2-TZVP). The AV1245 is a robust method for quantifying electron delocalization along a specific path. A higher positive value of AV1245 indicates greater delocalization along the path.