Table 4 The percent content of minerals in the enamel during all three stages of treatment with the different remineralizing agents.

|  | Initial (%) |  |  |  |  |  | Demineralized enamel (%) |  |  |  |  | Remineralized enamel (%) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | C | O | F | P | Ca |  | C | O | F | P | Ca |  | C | O | F | P | Ca |
| Natural tooth | 10.31.2 | 21.76.8 | 1.51.1 | 23.52.1 | 42.96.1 |  | 10.51 | 14.84.9 | 1.80.7 | 25.31.4 | 47.513.9 |  | - | - | - | - | - |
| Distilled water | 18.846 | 13.423.9 | 2.480.6 | 24.263.3 | 417.4 |  | 18.676.6 | 21.193.6 | 2.380.2 | 20.433.2 | 37.327.2 |  | 15.601.4ABC | 23.992.3CB | 2.150.6B | 20.910.4ABC | 37.351.4AB |
| Fluoride varnish | 12.830.4 | 16.280.7 | 1.130.7b | 25.784.6b | 43.970.6 |  | 12.182.4 | 21.61.6 | 1.981.5ab | 23.341.4ab | 40.94.2 |  | 18.390.7C | 14.531.2A | 6.50.4Aa | 18.780.4ACa | 41.782.2B |
| Fluoride varnish | 12.830.4 | 16.280.7 | 1.130.7 | 25.784.6b | 43.970.6b |  | 12.182.4 | 21.61.6 | 1.981.5 | 23.341.4ab | 40.94.2ab |  | 60.815.8Aa | 12.391.7A | 1.970.5B | 8.911.7ACa | 15.904.8Aa |
| CPP-ACP | 15.323.52 | 22.630.7 | 2.781.1 | 22.771.1 | 36.493.7 |  | 23.1111.6 | 18.852.5 | 1.650.9 | 194.8 | 34.43.9 |  | 15.661.1BC | 17.961.2ABC | 1.770.4B | 22.450.3B | 42.161.4B |
| CPP-ACPF | 14.932.3 | 21.632.2 | 2.980.1 | 22.931.4 | 37.522.0 |  | 22.8211.7 | 19.660.7 | 2.060.1 | 20.543.7 | 34.947.3 |  | 12.790.3B | 24.311.2B | 2.290.2B | 22.250.3B | 38.380.9B |

The underlined figures are for fluoride varnish treated enamel portions that did not have the varnish residue removed.

Upper case characters represent statistically significant difference (P < 0.05) within a column.

Lower case characters represent statistically significant difference (P < 0.05) between values for a single element across the three stages.