Table 1. List of some general characteristics of MR and MB dyes.

| Azo dye | Methyl Red | Methyl Blue |
| --- | --- | --- |
| Molecular weight | 269.30 g/mol | 799.80 g/mol |
| Solubility in water | Soluble | Soluble |
| C.I | 12003 | 8600 |
| Λmax | 503 nm | 508 nm |
| pKa | 4.4 | 5.6 |
| Molecular structure |  |  |
| Molecular formula | C15H15N3O2 | C37H27N3Na2O9S3 |
| IUPAC name | (2-(N, N-dimethyl-4-aminophenyl) azobenzene carboxylic acid) | ([[4-[Bis[4-[(sulphonyl)amino] phenyl] methylene]-2,5-cyclohexadiene-1-ylidene] amino]-benzenesulfonic acid disodium salt) |

Table 2.

Catalytic degradation of methyl red and methyl blue dyes by different reported catalysts compared with the current study (Co@TiO2, Ni@TiO2, and Ni-Co@TiO2 photocatalyst).

| No. | Catalyst | Concentration (g/L) | Percent degradation | Ref. |
| --- | --- | --- | --- | --- |
| 1 | YMnO3/CeO2 | 0.053 | 84 % in 60 min | [34] |
| 2 | Ag+-doped TiO2 | 0.110 | >85 % in 40 min | [35] |
| 3 | Mg/TiO2 | 0.449 | >83 % in 70 min | [36] |
| 4 | Au+-doped SiO2 NPs | 0.370 | 91 % in 100 min | [37] |
| 5 | Ag+-doped SiO2 NPs | 0.500 | 89 % in 70 min | [38] |
| 6 | SiO2 Nps | 0.020 | 81 % in 1 hr. | [39] |
| 7 | ZnO NPs | 2.5 | 92 % in 100 min | [40] |
| 4 | CuO NPs | 0.01 | 85 % in 80 min | [41] |
| 8 | Fe3O4 NPs | 0.075 | 50 % in 60 min | [42] |
| 9 | TiO2/foam | 0.05 | 86 % in 30 min | [7] |
| 10 | TiO2/g-C3N4 | 0.2 | 98 % in 100 min. | [26] |
| 11 | Co60Fe18Ti18Nb4 alloys | 0.2 | 98 % in 1 hr. | [12] |
| 12 | Ni@TiO2 | 0.04 | 60 % in 18 min. | Current work |
| 13 | Ni-Co@TiO2 | 0.04 | 89 % in 18 min | Current work |
| 14 | Co@TiO2 | 0.04 | 72 % in 18 min | Current work |