Supplementary Material for

Multi-state chiral switching through adiabaticity control in encircling exceptional points

Aodong Li1,5, Jian Wang1, Andrea Alù2,3 and Lin Chen1,4,*

1 Wuhan National Laboratory for Optoelectronics and School of Optical and Electronic Information, Huazhong University of Science and Technology, Wuhan 430074, China

2 Photonics Initiative, Advanced Science Research Center, City University of New York, New York, NY 10031, USA

3 Physics Program, Graduate Center, City University of New York, New York, NY 10016, USA

4 Shenzhen Huazhong University of Science and Technology Research Institute, Shenzhen 518063, China

5 School of Science and Engineering, The Chinese University of Hong Kong, Shenzhen, 518172, China

Email: chen.lin@mail.hust.edu.cn

* Corresponding author.

Supplementary Note 1: Eigenstates of an N-order Hamiltonian with a double-symmetric matrix form

The double-symmetric form indicates the  Hamiltonian  is symmetric with respect to its main diagonal and skew diagonal elements, simultaneously, i.e.,  and , where

(A1)

If  is an even number,  can be expressed as

(A2)

where  and  are  matrix. Provided that the eigenvalue and eigenstate are  and  for , and are  and  for , i.e.,  and , we can obtain

(A3)

(A4)

where  and  are also the eigenvalues of . The eigenstates of  are  and , which are symmetric and anti-symmetric eigenstates, respectively. Because  cannot be expressed as the linear combination of all  and vice versa, the eigenstates of  can be divided into , where  and  denote the set of  and , respectively. Since  is double-symmetric over the time, the transformation relation of the eigenstates during the evolution can be expressed as

(A5)

indicating that  and  are the invariant subspace of . Therefore, if two eigenstates belong to  and , respectively, they cannot excite each other during the evolution, regardless of the eigenstate loss.

Supplementary Note 2: Evolution paths with injected states  and

Supplementary Fig. S1 Evolution paths with injected states  and . a, b CW (a) and ACW (b) loops on the RSs formed by the real part of the eigenvalues. The colour of the surface indicates the imaginary part of eigenvalues. The yellow and green lines denote the evolution paths, when  and  are injected, respectively. The eigenvalue spectrum is spited into two separate RS1 and RS2, as shown in the right panel of the graph.

Supplementary Note 3: Dynamics of encircling loops

Supplementary Fig. S2 Dynamics of encircling loops. a-d Coefficients ,  versus the evolution time  for CW (a, c) and ACW (b, d) loops, when the initial states are  (a, b) and (c, d). (e-h) Coefficients ,  versus the evolution time  for CW (e, g) and ACW (f, h) loops, when the initial states are  (e, f) and  (g, h). Here, , , , and  are the amplitudes of eigenstates that evolve from , , , . In the strict adiabatic evolution, also called quasi-static evolution, , ,  and  evolve to , ,  and , when the system finishes the EP-encircling loop, respectively. For example, when the initial state is  for CW loop (a),  is the dominant after the evolution with the final state being of . When the initial state is  for ACW loop (b),  is the dominant after evolution with the final state being of .

Supplementary Note 4: Relationship between structural parameters and Hamiltonian parameters

Supplementary Fig. S3 Relationship between the structural parameters and Hamiltonian parameters. a, b  (a) and  (b) versus  and . c  versus  and . d The encircling trajectory around EPs, corresponding to the four-coupled waveguides as shown in Fig. 2a of the main text.
Supplementary Note 5: Geometrical parameters of the four coupled silicon waveguides

Supplementary Fig. S4 Geometrical parameters of the four-coupled silicon waveguides. a The top view of the four-coupled silicon waveguides. b-d ,  (b),  (c) and  (d) versus .

The specific parameters of the multimode asymmetric switching device with four- coupled waveguides are as shown in Fig. S4. The lengths of AB, BC and CD sections are ,  and , respectively. Figures S4b-d respectively show the variations of waveguide widths  and , gap separation , and the width of the chromium  along the propagation distance . In the BC section, the chromium strips are tapered with a length of 2 μm on both ends. This is done to reduce the light reflection and scattering at the interface between the chromium-coated waveguides with chromium layers and the waveguides without chromium layers. The geometrical parameters of the branch that connects bus waveguide and four-coupled waveguides are shown in Fig. S5.

Supplementary Fig. S5 The branch connecting the bus waveguide and four-coupled waveguides.

Supplementary Note 6: Fabrication process

Supplementary Fig. S6 Fabrication process of four-coupled silicon waveguides.

Figure S6 shows the fabrication process of four-coupled silicon waveguides with a combination of three-step electron-beam lithography (EBL), inductively coupled plasma (ICP) etching, electron-beam evaporation (EBE), and plasma-enhanced chemical vapor deposition (PECVD).

Firstly, an SOI wafer was successively cleaned in ultrasound bath in acetone, isopropyl alcohol and DI water, and then was dried under nitrogen flow. The alignment marks, 20-nm-thick Aurum with 5-nm-thick Chromium as an adhere layer, were fabricated by the first-step EBL, EBE and lift-off process. Photoresist was spin-coated onto the wafer surface and was patterned by EBL, which was followed by development and fixation. The Chromium and Aurum layers were successively deposited by EBE, and the final alignment marks were formed by lift-off process. Secondly, the silicon waveguides and gratings were fabricated by using a second-step EBL and ICP etching. The photoresist was patterned by use of the above-mentioned EBL process, followed by ICP etching to define waveguides and gratings. Thirdly, the Chromium strips on the two sideward waveguides were fabricated by the third-step EBL, EBE and lift-off process. After the photoresist film was spin-coated, the pattern of Chromium was formed by EBL with careful alignment. Subsequently, a 20-nm-thick Chromium layer was deposited using EBE, followed by lift-off process to achieve the required Chromium pattern. Finally, a 1-μm-thick SiO2 layer is deposited by PECVD, to cover the entire sample for the optical field symmetry and structural protection.

Supplementary Note 7: Measurement setup

Figure S7a presents the experimental setup for measuring the transmittance of fabricated multimode asymmetric switching device. The near infrared light source is provided by an amplified spontaneous emission (ASE) broadband light source. The polarization of the light source is adjusted by polarization beam splitter (PBS) and polarization controller (PC) before light is coupled into the grating coupler (GC) through the fiber. The emergent light from the SOI chip is coupled back into the fiber through the GC, and reaches 50/50 coupler, which is connected to the optical power meter and spectrometer. The optical power meter is used to adjust the angle between the fiber and the GC so as to maximize the coupling efficiency between them. The spectrometer is used to extract the transmittance for all the output modes. Figure S7b presents the SEM image of the on-chip experimental configuration. TE1 to TE3 modes are separated from the straight bus waveguide and are converted to TE0 mode using three (de)multiplexers, respectively.

Supplementary Fig. S7 Measurement setup. a Measurement configuration of the fabricated multimode asymmetric switching device. b SEM image of the on-chip devices consisting of four-mode asymmetric switching device, TE1 to TE3 mode (de)multiplexers and GCs.

Supplementary Note 8: Asymmetric switching device splitting eight modes into four groups

The eigenstate grouping method for encircling EPs can be extended to higher-order non-Hermitian systems with more eigenstates. Here, we take an eight-state system as an example. The eigenstates are divided into four groups, and each group contains two eigenstates. The eigenstates within each group undergo asymmetric switching independently, and are not interacted with the eigenstates in other groups. This allows for selective control and manipulation of specific states in the system.

Let us assume an eight-order Hamiltonian with a double-symmetric matrix form as , where ,  and  are all  matrices. According to the derivation in Note 1, the eigenstates can be divided into two distinct groups based on their symmetry and anti-symmetry, corresponding to even and odd modes in the waveguides, respectively. The eigenstates of these two groups, denoted as  and , can be obtained by mirroring and anti-mirroring the eigenstates  of matrices  and  of , respectively, i.e.,  and . To further increase the number of groups,  or  can be chosen as double-symmetric matrices. For example, , with . Assuming that the eigenstate is  for , and  for , the eigenstates of  can be divided into two groups, i.e.,  and . For the planer coupled silicon waveguides system where only adjacent coupling between waveguides is considered,  cannot be a double-symmetric matric, if  is not equal to zero. It is to say that,  cannot be grouped into two groups. The eigenstates of are finally divided into 3 groups.

If ,  and  can be divided into two groups, respectively, as all the eigenstates are divided into four groups as , with

(A6)

where  and  are two dimensional vectors and each group contains two states. In the eight-coupled waveguides system,  is achievable by setting sufficient gap separation () between the fourth and fifth waveguides (Fig. S8a). The eight-coupled silicon waveguides are made of three sections, and support eight eigenmodes TE0 to TE7. In section 2, the eight-coupled waveguides are divided into two four-coupled waveguides, each of which is the same as the four-coupled waveguides used for asymmetric switching of four eigenmodes in Fig. 2 of the main text. In sections 1 and 3, the eight eigenmodes cannot be divided into four groups, in which neither  nor  is double-symmetric. The device lengths in sections 1 and 3 are sufficiently long to improve adiabaticity and minimize the mutual crosstalk between different eigenmodes.

Supplementary Fig. S8 Eight-mode asymmetric switching. a The whole device is symmetrical with respect to the red dashed line. The sections 1 and 3 are 120 μm in length. The two four-coupled waveguides in section 2 are both symmetrical with respect to the green dashed line. b  versus  in section 1. Section 3 is mirrored with respect to section 1.

The transmission of eight-mode asymmetric switching device with four pairs of eigenmodes are obtained by FDTD simulations as shown in Fig. S9. One can see that, the expected eigenmode is dominant in the output, significantly larger than all the other modes. For the left- (right-) port input, the output is TE4 (TE0) mode for group  (Fig. S9a), TE6 (TE2) mode for group  (Fig. S9b) , TE5 (TE1) mode for group  (Fig. S9c) , and TE7 (TE3) mode for group  (Fig. S9d). It can be observed that there is slight mode crosstalk between groups  and  (groups  and ). This does not come from the second section, for which eight eigenmodes are divided into four groups without mutual crosstalk between different groups. The mode crosstalk between different groups actually originates from the first and third sections, which are not purposely designed for double-symmetrical  and .

Supplementary Fig. S9 Simulated transmittance spectra. a-d Simulated transmittance spectra of eight-mode asymmetric switching device for four pairs of eigenmodes: TE0 and TE4 modes (a); TE2 and TE6 modes (b); TE1 and TE5 modes (c); TE3 and TE7 modes (d).