Supporting Information

A novel Cu9S8 antibacterial based on magnetic chestnut shell biochar for the removal of sulfonamides in water environment: Differential adsorption and mechanism study

* Rui-peng Lia,1, Zheng-rong Hua,1, Xing Wanga, Jun Chena, Qing-qing Liu a, Ying Zhaoa, Zhong-bao Zhaob, Xu-lin Lua, Zhi-wei Zhanga

a Chemical Engineering College, Hebei Normal University of Science and Technology, Qinhuangdao, 066600, China.

b Hebei University of Environmental Engineering, Hebei Key Laboratory of Agroecological Safety., Qinhuangdao, 066100, China.

1 These authors contributed equally to this work.

Text S1

1.35 g FeCl3·6H2O and 2.46 g CH3COONa were dispersed in 40 mL ethylene glycol solution and stirred ultrasonically until completely dissolved. Then 2 g polyethylene glycol was weighed and further ultrasonic stirring is carried out. After the above solute was completely dissolved, 2.7 g BC was added and ultrasonic stirring continues until complete mixing was achieved. Subsequently, the obtained mixture was transferred to a 50 mL reactor with the hydrothermal temperature of 200 ℃ and the heating time of 8 h. After the reaction was completed, it was rinsed multiple times with deionized water and then rinsed once with anhydrous ethanol. The filtered sample was placed in a fume hood and dried naturally.

Text S2

The crystalline phase of Cu9S8, BC and Cu9S8/Fe3O4@BC were detected by the X-ray powder diffraction (XRD) pattern with the scanning speed of 8 °/min (Cu–Kα, operating conditions: 40 kV, 200 mA, range: 10–80 °). X-ray photoelectron spectroscopy (XPS) analyses were carried out using the Quantera SXM X-ray photoelectron spectrometer (Thermo Scientific Escalab 250Xi) equipped. The N2 adsorption-desorption of Cu9S8 and Cu9S8/Fe3O4@BC were determined at 77.3 K with the surface area and porosity analyzer (Micromeritics, Tristar II 3020). The pore size distributions (PSDs) were derived with Barrett-Joyner-Halenda (BJH) method considering the large pore size from the N2 desorption data. Elemental analyses for the Cu, S, Fe, O and C contents of the samples were conducted using the elemental analyzer (Octane Elect Super C5) with the thermal conductivity detector. Scanning electron microscopy (SEM) was performed using the SEM instrument from Hitachi (Regulus8100). Transmission electron microscopy (TEM, Tecnai G2 F20 S-Twin, USA) was used to examine the morphology of the materials. The magnetization of Cu9S8/Fe3O4@BC was tested by using the Vibrating Sample Magnetometer (VSM, Lake Shore 8600, USA). The zeta potential of Cu9S8 was measured by the zeta potentiometer (Malvern Zetasizer Nano ZS90).

Text S3

Prior to the inactivation experiments, all glassware and nutrient agar and saline solution (0.85%) were sterilized at 121 ℃ for 30 min to ensure sterility. In a typical disinfection experiment, S. aureus and E. coil were separately packed in 50ml conical bottles (initial concentration: 2.9×107 colony-forming units CFU/mL) and 2 mg of antibacterial materials were added to it. During the disinfection process, at certain time intervals, the bacterial suspension (50 μL) was retrieved and evenly spread on agar plates, thus incubated at 37 ℃ for 24 h to evaluate the bacterial viability. For comparison, three parallel photocatalytic inactivation experiments were operated and the antibacterial data represented the average of these triplicates.

Fig. S1 Effects of (a) different Cu9S8 dosage on adsorption of SMZ, (b) different initial concentrations of SMZ on adsorption, (c) different pH values on the adsorption rate of Cu9S8 for SMZ in quartz tubes and NaCl (d), MgCl2 (e) and CaCl2 (f) on Cu9S8 adsorption of SMZ (dosage 0.02 g, concentration 10 mg/L).

Fig. S2 Isotherms models describing the ST sorption: (a) Langmuir, (b) Freundlich and (c) Temkin models; isotherms models describing the SD sorption: (d) Langmuir, (e) Freundlich and (f) Temkin models.

Fig. S3 Pore size distribution of (a) Cu9S8 and (b) Cu9S8/Fe3O4@BC.

Fig. S4 The state of SMZ at different pH values.

Fig.S5 Antibacterial properties of (a) BC, (c) Fe3O4, (f) Cu2+ for S. aureus and (b) BC, (d) Fe3O4 ,(e) Cu2+ for E. coil.

Table S1 Adsorption isotherm fitting parameters for the SMZ adsorption by Cu9S8

| T(K) |  |  | 303 | 313 | 323 |
| --- | --- | --- | --- | --- | --- |
| SMZ | Langmuir Model | qm/( mg·g-1 ) | 37.7644 | 43.6110 | 76.5111 |
|  |  | KL | 0.1358 | 0.3906 | 0.3771 |
|  |  | RL | 0.4241 | 0.2038 | 0.2096 |
|  |  | R2 | 0.9876 | 0.9848 | 0.9893 |
|  | Feundlich Model | KF | 6.9168 | 15.2648 | 29.2658 |
|  |  | 1/n | 0.4473 | 0.2979 | 0.2842 |
|  |  | R2 | 0.9457 | 0.9847 | 0.9723 |
|  | Temkin Model | KT | 1.4652 | 4.0129 | 4.9915 |
|  |  | a | 7.9406 | 8.5679 | 14.7312 |
|  |  | R2 | 0.9863 | 0.9658 | 0.9174 |
| SD | Langmuir Model | qm/( mg·g-1 ) | 13.2188 | 35.7398 | 35.7782 |
|  |  | KL | 0.1764 | 0.6456 | 1.0390 |
|  |  | RL | 0.3617 | 0.1341 | 0.0878 |
|  |  | R2 | 0.9085 | 0.97853 | 0.97628 |
|  | Feundlich Model | KF | 1.8691 | 13.1588 | 14.3611 |
|  |  | 1/n | 0.4939 | 0.3409 | 0.3554 |
|  |  | R2 | 0.9216 | 0.9834 | 0.9073 |
|  | Temkin Model | KT | 0.5747 | 2.6834 | 3.2331 |
|  |  | a | 4.5535 | 9.1020 | 9.2644 |
|  |  | R2 | 0.9615 | 0.9884 | 0.9923 |
| ST | Langmuir Model | qm/( mg·g-1 ) | 13.1458 | 30.2024 | 32.6477 |
|  |  | KL | 0.1946 | 0.4858 | 0.4059 |
|  |  | RL | 0.5139 | 0.2059 | 0.2464 |
|  |  | R2 | 0.9378 | 0.9892 | 0.9859 |
|  | Feundlich Model | KF | 1.7286 | 12.3940 | 14.0801 |
|  |  | 1/n | 0.6051 | 0.2425 | 0.2307 |
|  |  | R2 | 0.9599 | 0.9516 | 0.8774 |
|  | Temkin Model | KT | 0.6221 | 6.8212 | 9.0420 |
|  |  | a | 4.3671 | 5.5703 | 5.4309 |
|  |  | R2 | 0.9185 | 0.8968 | 0.9789 |

Table S2 Adsorption thermodynamics parameters for the SMZ adsorption by Cu9S8

| T (K) |  | 303 | 313 | 323 |
| --- | --- | --- | --- | --- |
| SMZ | ∆G (KJ·mol-1) | -3347.39 | -3832.44 | -5464.43 |
|  | ∆H (KJ·mol-1) | +28916.97 |  |  |
|  | ∆S (J·(mol·K)-1) | +105.85 |  |  |
| SD | ∆G (KJ·mol-1) | -702.98 | -3314.47 | -3423.25 |
|  | ∆H (KJ·mol-1) | +40092.03 |  |  |
|  | ∆S (J·(mol·K)-1) | +136.01 |  |  |
| ST | ∆G (KJ·mol-1) | -689.03 | -2876.40 | -3177.36 |
|  | ∆H (KJ·mol-1) | +36694.83 |  |  |
|  | ∆S (J·(mol·K)-1) | +124.42 |  |  |

Table S3 Adsorption kinetic fitting parameters for the SMZ adsorption by Cu9S8

|  |  | SMZ | SD | ST |
| --- | --- | --- | --- | --- |
| pseudo-first-order | qe/( mg·g-1 ) | 23.1614 | 14.4154 | 16.1491 |
|  | qec/( mg·g-1 ) | 24.0502 | 16.4276 | 15.3846 |
|  | k | 0.3159 | 0.1762 | 0.1183 |
|  | R2 | 0.9853 | 0.9839 | 0.9792 |
| pseudo-second-order | qe/( mg·g-1 ) | 24.3368 | 15.6031 | 17.0999 |
|  | qec/( mg·g-1 ) | 24.0502 | 16.4276 | 15.3846 |
|  | k | 0.0586 | 0.0212 | 0.0075 |
|  | R2 | 0.9996 | 0.9985 | 0.9930 |

Table S4 Desorption kinetic fitting parameters for the SMZ adsorption by Cu9S8

|  |  | SMZ | SD | ST |
| --- | --- | --- | --- | --- |
| pseudo-first-order | qe/( mg·g-1 ) | 15.3909 | 12.2784 | 10.5611 |
|  | qec/( mg·g-1 ) | 16.6080 | 13.4327 | 11.7452 |
|  | k | 0.2285 | 0.2176 | 0.1010 |
|  | R2 | 0.9598 | 0.9368 | 0.8784 |
| pseudo-second-order | qe/( mg·g-1 ) | 16.8265 | 13.6874 | 12.1699 |
|  | qec/( mg·g-1 ) | 16.6080 | 13.4327 | 11.7452 |
|  | k | 0.0215 | 0.0216 | 0.0115 |
|  | R2 | 0.9974 | 0.9957 | 0.9859 |

Table S5 Study on antibacterial effects of different materials in references

| Material | Dosage (mg) | Time (min) | Bacterial type | Inactivation rate (%) | References |
| --- | --- | --- | --- | --- | --- |
| CuBi2O4/Bi2MoO6 | 40 | 360 | E. coli | ＞99 | [Shi et al. 2020] |
| CdIn2S4/W18O49 | 20 | 120 | E. coli | ＞99 | [Yang et al. 2020] |
| MgTi2O5/g-C3N4 | 25 | 180 | E. coli | ＞99 | [Jiang et al. 2019] |
| Bi4O5I2/AgI | 20 | 30 | E. coli | ＞99 | [Yang er al. 2019] |
| Agar/CuS NP | 50 | 420 | E. coli | ＞99 | [Roy et al. 2019] |
| Ti3C2Tx@CuS | 0.5 | 30 | E. coli | ＞99 ＞99 | [Li et al. 2021] |
|  |  |  | S.aureus |  |  |
| Cu9S8 | 2 | 20 | S.aureus E. coli | ＞99 | Current |
| Cu9S8/Fe3O4@BC |  | 30 |  |  |  |

Corresponding authors: Dr. Zhang. Email: zhangzhiweia@163.com