List of Tables

Table captions

| Table No | Title |
| --- | --- |
| Table 1 | A summary of deployed solution compositions for the fabrication of alternate organic acid based PVA composite films. |

Table 1

A summary of deployed solution compositions for the fabrication of alternate organic acid based PVA composite films.

| S. no. | Formulation | PVA (w/w%) | St (w/w%) | Gl (wt%) | CA (wt%) | TA (wt%) | MA (wt%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | CA based EXP-%E | 5 | 10 | 15 | 15 | 0 | 0 |
| 2 | CA based EXP+%E | 7.5 | 7.5 | 27.5 | 27.5 | 0 | 0 |
| 3 | CA based RSM-%E | 5.5 | 8.1 | 22.7 | 22.8 | 0 | 0 |
| 4 | CA based RSM+%E | 7.5 | 7 | 18.38 | 28.6 | 0 | 0 |
| 5 | TA based EXP-%E | 5 | 10 | 15 | 0 | 15 | 0 |
| 6 | TA based EXP+%E | 7.5 | 7.5 | 27.5 | 0 | 27.5 | 0 |
| 7 | TA based RSM-%E | 5.5 | 8.1 | 22.7 | 0 | 22.8 | 0 |
| 8 | TA based RSM+%E | 7.5 | 7 | 18.38 | 0 | 28.6 | 0 |
| 9 | MA based EXP-%E | 5 | 10 | 15 | 0 | 0 | 15 |
| 10 | MA based EXP+%E | 7.5 | 7.5 | 27.5 | 0 | 0 | 27.5 |
| 11 | MA based RSM-%E | 5.5 | 8.1 | 22.7 | 0 | 0 | 22.8 |
| 12 | MA based RSM+%E | 7.5 | 7 | 18.38 | 0 | 0 | 28.6 |