Supporting information for

Conveyor CVD to high-quality and productivity of large-area graphene and its potentiality

Dong Yun Lee1, Jungtae Nam1, Gil Yong Lee1, Imbok Lee1, A-Rang Jang2, *, and Keun Soo Kim1, *

1 Department of Physics and Graphene Research Institute, Sejong University, Seoul, 05006, Republic of Korea

2 Division of Electrical, Electronic and Control Engineering, Kongju National University, Cheonan-si, Chungcheongnam-do, 31080, Republic of Korea

* indicates the corresponding author

* Corresponding author: Keun Soo Kim1, A-Rang Jang2

Tel.: +82-02-3408-39881, +82-041-521-91872

E-mail address: kskim2676@sejong.ac.kr1, arjang@kongju.ac.kr2

Figure S1. Comparison of photograph images for thermally deposited copper film(300 nm) on SiO2/Si substrate and conventional/rapid synthesis of graphene on it and their Raman spectra.

Figure S2. Raman peak ratio of pristine graphene synthesized at 900 ℃ by growth time. Compared to 60 sec data, 30, 45 and 90 sec data have larger D peak and smaller 2D peak, and bigger error bars indicate that the properties of each graphene are non-uniform.

Figure S3. Correlation between Dirac Voltage and mobility of the graphene by growth temperature and doping.

Figure S4. Annealing time dependence Raman spectra of pristine graphene at 1000 ℃.