### Micro-crystalline Evolution and Enhanced Mechanical Properties of Continuous BN Fibers

Xueli Qia,b, Weichen Dingb, Haonan Xub, Yujiao Wangb, Zhiqiang Chengb, Meng Zhangc,*, Zhihao Wangd,*, Jianyao Yaoa,*

a College of Aerospace Engineering, Chongqing University, Chongqing 400044, PR China

b Shandong Industrial Ceramic Research & Degisn insitute Co.Ltd., Zibo 255000, PR China

c College of Materials Science and Engineering, Qingdao University of Science and Technology, Qingdao, Shandong province, 266042, China.

d School of Material Science and Engineering, Qilu University of Technology (Shandong Academy of Sciences), Jinan 250353, PR China

E-mail addresses: mengzhang@qust.edu.cn (M. Zhang), wangzhihao0805@126.com (Z. Wang), yaojianyao@cqu.edu.cn (J. Yao)

Figure S1 Low magnification SEM images of BNO samples (a) BNO-250, (b) BNO-300, (c) BNO-350, (d) BNO-400, (e) BNO-500, (f) BNO-600, (g) BNO-800, (h) BNO-1000;

Table S1 Reaction thermodynamic data of BNO samples at different calcination temperatures

| T K | ∆H kcal | ∆G kcal | K | Log(K) |
| --- | --- | --- | --- | --- |
| 523.000 | 33.194 | 13.590 | 2.092E-006 | -5.679 |
| 573.000 | 33.119 | 11.719 | 3.387E-005 | -4.470 |
| 623.000 | 33.018 | 9.856 | 3.485E-004 | -3.458 |
| 673.000 | 32.890 | 8.002 | 2.519E-003 | -2.599 |
| 773.000 | 26.404 | 4.742 | 4.562E-002 | -1.341 |
| 873.000 | 25.549 | 1.994 | 3.169E-001 | -0.499 |
| 1073.000 | 24.081 | -3.239 | 4.569E+000 | 0.660 |
| 1273.000 | 22.791 | -8.217 | 2.575E+001 | 1.411 |

Table S2 Crystal structure parameters of the samples obtained at 1000℃

| 2θ(002) (o) | d(002) (nm) | Lc(002) (nm) | La(10) (nm) | η (%) |
| --- | --- | --- | --- | --- |
| 25.32 | 0.352 | 0.935 | 1.932 | 57.66 |

Figure S2 Macro picture of the prepared continuous BN fiber

Figure S3 Schematic diagram of the working principle of SAXS characterization

Table S3 Average sizes parameters of B2O3 precursor fiber, BNO-1000 sample, and BN fibers obtained at various temperatures

| Sample | Average length c (nm) | Average length a (nm) | Ratio c/a | Q0/Q90 |
| --- | --- | --- | --- | --- |
| B2O3 | 65.85 | 59.47 | 1.11 | 0.64 |
| BNO-1000 | 72.33 | 53.18 | 1.36 | 0.59 |
| BN | 101.35 | 28.63 | 3.54 | 0.43 |

Table S4 Mechanical properties of BN fibers obtained at various temperatures

| Sample | F (cN) | ε (%) | D (μm) | R (MPa) | E (GPa) |
| --- | --- | --- | --- | --- | --- |
| 1000℃ | 1.29 | 0.015 | 6.48 | 391.91 | 33.59 |
| 1850℃ | 2.8 | 0.022 | 6.326 | 890.9 | 40.8 |