Supplementary information

Aqueous benzene, toluene, ethylbenzene and xylene (BTEX) removal using core-shell structure activated carbon ball as a permeable reactive barrier material

Eunji Myung1, Hyunsoo Kim2, Nagchoul Choi3 and Kanghee Cho3

1 Institutes of Green Bio Science and Technology, Seoul National University, Gangwon-do 25354, Republic of Korea

2 Department of Energy and Resource Engineering, Chosun University, Gwangju 61452, Republic of Korea

3 Research Institute of Agriculture and Life Sciences, Seoul National University, Seoul 08826, Republic of Korea

* Corresponding authors: Kanghee Cho

E-mail; kanghee1226@snu.ac.kr

- Data analysis

The following equations were adopted for the determination of the coefficient (R2), chi-square coefficient (χ2), and the sum of the squared error (SSE) to estimate the adsorption data and verify their fitness to the model:

R2=i=1m(yc-ye)i2i=1m(yc-ye)i2+i=1m(yc-ye)i2 (1)

χ2=i=1m(ye-yc)2yci (2)

SAE=i=1nyc-yei (3)

where yc is the removal capacity calculated from the model, ye is the removal capacity measured in the experiment, and ye is the average measured removal capacity.

- Column data analysis

The data obtained from the fixed-bed column adsorption system were plotted in breakthrough curves in the form of Ct/C0 versus time. In this study, a Ct/C0 value of 0.1 was point as break point. The following parameters were calculated using the equations below to evaluate the performance of the fixed bed column; absorption capacity in saturated state (qe), and removal efficiency in saturated state (Re)

| qe=QMt=0t=ts(C0-Ct)dt |  | (4) |
| --- | --- | --- |
| Re=qeMC0Qts | (5) |

where qe(mg/g) is the accumulative adsorption amount till time t (min), M (g) is the adsorbent mass, breakthrough state (ts) and Q (mL/min) is the flow rate of the influent solution.

Fig. S1 Kinetics for the adsorption of BTEX by AC30.

Table S1. Kinetic model parameters obtained from model fitting to experimental data.

| Material | Pseudo first-order model |  |  | Pseudo second-order model |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | qe | k1 | R2 | qe | k2 | R2 |
|  | (mg/g) | (1/h) |  | (mg/g) | (g/mg/h) |  |
| Benzene | 4.90 | 1.44 | 0.95 | 4.88 | 0.73 | 0.94 |
| Toluene | 3.37 | 1.82 | 0.93 | 3.63 | 0.57 | 0.81 |
| Ethylbenzene | 1.16 | 1.54 | 0.97 | 1.28 | 2.45 | 0.92 |
| Xylene | 0.46 | 1.30 | 0.82 | 0.54 | 3.45 | 0.84 |

Fig. S2 Comparison of (a-b) equilibrium (Langmuir and Freundlich) and (c-d) kinetics (PFO and PSO) for the adsorption of benzene and toluene by AC10 and AC30.

Table S2. Fixed-bed column experimental conditions.

| Column diameter (cm) | Bed depth (cm) | Pore volume (ml) |
| --- | --- | --- |
| 2.5 | 10 | 20.62 |
| Mass of adsorbent (g) | Flow rate (mL/min) | Initial concentration (mg/L) |
| 43.09 | 0.5, 1.0, 5.0 | 200 |

Fig. S3 Digital images of AC30 after 20 cycles of adsorption/desorption of benzene using microwave.