Supplementary material

Characterization of polystyrene-degrading bacteria isolated from plastic processing plants

Table S1

List and number of bacterial strains, isolated from plastic raw material or plastic final products from three processing plants.

| Microorganism | No. (%) of strains |
| --- | --- |
| Gram positive bacteria | 93 (96.87) |
| Staphylococcus spp. | 38 (39.58) |
| S. epidermidis | 15 (15.62) |
| S. warneri | 3 (3.12) |
| S. aureus | 6 (6.25) |
| S. condimenti | 1 (1.04) |
| S.saprophyticus | 1 (1.04) |
| S. haemolyticus | 2 (2.08) |
| S. cohnii | 1 (1.04) |
| S. capitis | 2 (2.08) |
| S. hominis | 7 (7.29) |
| Micrococcus spp. | 11 (11.45) |
| M. luteus | 11 (11.45) |
| Bacillus spp. | 44 (45.83) |
| B. megaterium | 1 (1.04) |
| B. cereus | 12 (12.5) |
| B. licheniformis | 14 (14.58) |
| B. clausii | 1 (1.04) |
| B. subtilis | 4 (4.07) |
| B. pumilus | 6 (6.25) |
| B. safensis | 1 (1.04) |
| Brevibacillus parabrevis | 4 (4.17) |
| Lysinibacillus boronitolerans | 1 (1.04) |
| Gram-negative bacteria | 3 (3.1) |
| Moraxella nonliquefaciens | 1 (1.04) |
| Burkholderia fungorum | 2 (2.08) |
| Total | 96 (100 %) |

Fig. S1 The concentration of bacterial strains after 60 days incubation at 37 °C in MSM and NB in the presence of PS.

Strain No. 1: Burkholderia fungorum; 2: Bacillus subtilis; 3: Bacillus licheniformis; 4: Micrococcus luteus; 5: Micrococcus luteus; 6: Bacillus cereus; 7: Moraxella nonliquefaciens; 8: Bacillus licheniformis; 9: Bacillus cereus; 10: Micrococcus luteus

Fig. S2 SEM images of the biofilms formed on PS coupons after 60 days incubation in MSM at 37 °C, taken at the magnification of 5,000 ×.

C. negative control without bacteria; 1: Burkholderia fungorum; 4: Micrococcus luteus; 6: Bacillus cereus.

Fig. S3 ATR-FTIR spectra of pristine PS pellets (before UV) and PS pellets after 30 minutes exposure to UV light (after UV).

Fig. S4 ATR-FTIR vibrational band ratios: A - 750 cm-1/696 cm-1, B - 1027 cm-1/696 cm-1, C - 1455 cm-1/696 cm-1, D - 1494 cm-1/696 cm-1, E - 2850 cm-1/696 cm-1, F - 2924 cm-1/696 cm-1, and G - 3026 cm-1/696 cm-1. * Signifies the statistically significant differences between the sample and the control (p < 0,05).PS strain No. 1: Burkholderia fungorum; 2: Bacillus subtilis; 3: Bacillus licheniformis; 4: Micrococcus luteus; 5: Micrococcus luteus; 6: Bacillus cereus; 7: Moraxella nonliquefaciens; 8: Bacillus licheniformis; 9: Bacillus cereus; 10: Micrococcus luteus.