Table 1 Main absorption bands (cm-1) of FT-IR spectral data.

Description; Silica; POMA-ES; POMA-EB; POMA-NSSSA-ES1; POMA-NSSSA-ES2. O-H and/or N-H stretching vibration; 3428; 3188,3392; 3328,3367; 3500-4000; 3500-4000. O-H bending vibration (H2O); 1636; -; -; 3384; 3387. O-H bending vibration of silanol group and/or Symmetric stretching vibration of Si-O-Si bond; 813; -; -; 744; 714. Asymmetric stretching vibration of Si-O-Si bond; 1108; -; -; 1110; 1107. Rocking deformation vibration of Si-O-Si bond; 466; -; -; 478; 471. Aliphatic C-H vibration stretching; -; 2930; 2834,2935; 2977; 2928-2832. Raman active -C1/4C- ring stretching; -; -; -; 1533; 1545. Stretching vibration of C1/4C and C1/4N of quinoid ring; -; 1561; 1588; 1553; 1566. Stretching vibration of C1/4C of benzenoid ring; -; 1492; 1507; 1489; 1490. C-H bending mode of the OCH3 group; -; 1453; 1463; 1455; 1460. Aromatic C-N stretching vibration; -; 1294,1340; 1260,1331; 1289,1338; 1291,1332. Alkyl/Aryl/Ether linkage C-O-C stretching; -; 1256; 1260; masked; masked. In-plane C-H vibration of quinoid ring stretching vibration (silanol); -; 950; 951; masked; masked. The Benzenoid ring 1,2,4-trisubstituted; -; 824; 833; 799; 802. Out-of-plane C-H vibration; -; 590; 608; 669; 666. C-H bending vibration and/or –N+-H stretching vibration; -; 530; 538; 540; 548. S-O vibration; -; -; -; 628; 639. HSO4- vibrations; -; -; -; 824; -. Alkyl/Aryl/Ether linkage C-O-C stretching; -; 1012; 1027; 1110; 1017. Vibration mode of -NH.+ 1/4 and/or C-H and/or ring amine bending vibration; -; 1175; 1167; 1156; 1168. Secondary aromatic amine C-N stretching vibration and/or –C-N1/4 stretching vibration and/or C-H of the 1,2,4-trisubstituted benzene ring; -; 1205; 1204; 1193; 1196.

Table 2 Main absorption bands (nm) of UV-vis spectral data, and conductivity(s/cm) of polymers.

Sample; π→π*; n→π*; π→polaron; polaron→π*; Solvent; Color; Acid/mon; Anion; Conductivity(X); Ref. PANI-ES; 330; 640; -; -; NMP; Blue; 1; Cl-; 44×10-1; 40. PANI-EB; 330; 640; -; -; NMP; Blue; 1; -; 6×10-11; 40. POMA -ES; 305; 628; -; -; NMP; Blue; 1; Cl-; 4×10-3; -. POMA -EB; 310; 627; -; -; NMP; Blue; 1; -; <10-5; -. POMA -ES; 320; -; 410; 845; MeOH; Green; 1; Cl-; 4×10-3; -. POMA -EB; 330; 670; -; -; MeOH; Green; 1; -; <10-5; -. POMA -ES; -; -; 410; 871; MCR; Green; 1; Cl-; 4×10-3; -. POMA -EB; 350; 685; 425; 910; MCR; Green; 1; -; <10-5; -. POMA-SA; 315; 615; -; -; NMP; Blue; 0.5; HSO4-; 3.4×10-2; -. POMA-SA; 324; -; 413; 885; MCR; Green; 0.5; HSO4-; 3.4×10-2; -. POMA-SA; 310; 615; 425; 850; DMSO; Green; 0.5; HSO4-; 3.4×10-2; -. POMA–SSSA-ES1; 340; 635; -; -; NMP; Blue; 0.5; HSO4-; 5.19×10-3; -. POMA–SSSA-ES2; 340; 635; -; -; NMP; Blue; 0.5; SO42-; 1.05×10-3; -. POMA–SSSA-ES1; 340; -; 410; 840; MCR; Green; 0.5; HSO4-; 5.19×10-3; -. POMA–SSSA-ES2; 319; -; 421; 895; MCR; Green; 0.5; SO42-; 1.05×10-3; -. POMA–SSSA-ES1; 310; 615; 425; 850; DMSO; Green; 0.5; HSO4-; 5.19×10-3; -. POMA–SSSA-ES2; 310; 620; 440; 845; DMSO; Green; 0.5; SO42-; 1.05×10-3; -. POMA–NSSSA-ES1; 320; 625; -; -; NMP; Blue; 0.5; HSO4-; 2.4×10-4; -. POMA–NSSSA-ES2; 335; 615; -; -; NMP; Blue; 0.5; SO42-; 1.5×10-5; -. POMA–NSSSA-ES1; 325; 615; -; 852; DMSO; Blue; 0.5; HSO4-; 2.4×10-4; -. POMA–NSSSA-ES2; 325; 612; -; -; DMSO; Blue; 0.5; SO42-; 1.5×10-5; -. POMA–NSSSA-ES1; 330; -; 435; 850; DMSO; Green; 1.5; HSO4-; 2.4×10-4; -. POMA–NSSSA-ES2; 325; 635; 420; 875; DMSO; Green; 1.5; SO42-; 1.5×10-5; -. POMA–NSSSA-ES1; 335; -; 415; 850; DMSO; Green; 2.0; HSO4-; 2.4×10-4; -. POMA–NSSSA-ES2; 325; 625; 430; 870; DMSO; Green; 2.0; SO42-; 1.5×10-5; -.

Table 3

The results of the elemental analysis (CHNS)

| Element | Samples elemental composition (%) |  |  |
| --- | --- | --- | --- |
|  | POMA-SA | POMA-NSSSA-ES1 | POMA-NSSSA-ES2 |
| C | 40.73 | 23.17 | 30.17 |
| N | 6.73 | 8.54 | 5.20 |
| S | 9.49 | 6.89 | 2.92 |
| H | 5.12 | 2.23 | 2.65 |
| O | 37.93 | - | - |
| Si+O | - | 63.99 | 59.07 |
| Ʃ | 100 | 100 | 100 |
| N/S | 1.62 | 1.24 | 4.07 |
| C/S | 11.46 | 8.97 | 27.58 |
| C/N | 7.06 | 7.24 | 6.77 |
| H/C | 1.50 | 1.14 | 1.04 |
| O/S | 8.01 | - | - |
| S/N×100 | 61.64 | 80.66 | 24.57 |
| Formula | [(C7H7NO)4]+2[(HSO4)2]-2 | [(C7H7NO)4]+2[(HSO4)2]-2 | [(C7H7NO)4]+2[SO4]-2 |