Supporting Information

Synthesis, Reaction Kinetics and Properties of Aromatic Hyperbranched Polyesters of different Generations (G1 to G4) prepared via One-shot Solution Polycondensation

Ramadasu Gunasekhar1,‡, Balaraman Indumathy1,‡, Prasad Gajula2,

Jin Woo Bae2,**, Arun Anand Prabu1,*

1Department of Chemistry, School of Advanced Sciences, Vellore Institute of Technology, Vellore 632014, Tamil Nadu, India

2Multifunctional Organic Polymer Laboratory, Future Convergence Engineering, School of Energy, Materials and Chemical Engineering, Korea University of Technology and Education, 1600, Chungjeol-ro, Cheonan 31253, Republic of Korea

*Correspondence E-mail: anandprabu@vit.ac.in (A.A.P); **Co-Correspondence E-mail: jwbae@koreatech.ac.in (J.W.B)

‡R.G. and B.I. have contributed equally to this work.

Table S1. Integrations of 1H-NMR spectra of Ar.HBPs (G1-G4)

| H atom (Proton Position) | Chemical Shift (ppm) |  |  |  |
| --- | --- | --- | --- | --- |
|  | Ar.HBP-G1 | Ar.HBP-G2 | Ar.HBP-G3 | Ar.HBP-G4 |
| a. (-CH3) | 1.9 | 2.1 | 2.3 | 2.8 |
| b. (-CH2-) for (CH2-O-C=O) | 3.4 | 3.4 | 3.4 | 3.4 |
| c. (-CH2-) for (CH2-OH) | 4.0 | 4.0 | 4.1 | 4.1 |
| d. Ar.(-CH2-) | 6.6 | 6.6 | 6.7 | 6.7 |
| e. Ar.(-CH2-) | 6.8 | 6.8 | 6.9 | 6.9 |
| f. Ar.(-OH) | 9.2 | 9.2 | 9.2 | 9.2 |

Figure S1. (a-c). 1H-NMR spectra of Ar.HBPs (G1–G4) and (d-f). 13C-NMR spectra of Ar.HBPs (G1–G4).

Polymerization reaction kinetics of Ar.HBPs:

Table S2: FTIR transmittance data of acid and ester carbonyl peaks as a function of reaction time and ester-to-acid peak ratio for Ar.HBP-G1.

| Reaction Time (h) | Transmittance % |  | 1706/1648 (cm-1) ratio |
| --- | --- | --- | --- |
|  | Acid C=O, 1648 cm-1 | Ester C=O, 1706 cm-1 |  |
| 3 | 93.15 | 72.56 | 0.7789 |
| 5 | 91.39 | 71.05 | 0.7774 |
| 9 | 88.88 | 71.05 | 0.7993 |
| 13 | 79.09 | 81 | 1.0241 |
| 15 | 69.72 | 85.36 | 1.2243 |
| 19 | 46.89 | 93.4 | 2.0133 |
| 21 | 40.45 | 95.16 | 2.3525 |
| 23 | 40.69 | 95.91 | 2.3570 |

Table S3: FTIR transmittance data of acid and ester carbonyl peaks as a function of reaction time and ester-to-acid peak ratio for Ar.HBP-G2.

| Reaction Time (h) | Transmittance % |  | 1707/1648 (cm-1) ratio |
| --- | --- | --- | --- |
|  | Acid C=O, 1648 cm-1 | Ester C=O, 1707 cm-1 |  |
| 3 | 93.75 | 71.56 | 0.7774 |
| 5 | 91.49 | 71.89 | 0.7789 |
| 9 | 87.88 | 72.25 | 0.7897 |
| 13 | 79.59 | 81.34 | 1.0344 |
| 15 | 68.12 | 86.16 | 1.2286 |
| 19 | 45.59 | 93.56 | 2.0145 |
| 21 | 40.11 | 95.34 | 2.3509 |
| 23 | 39.34 | 96.11 | 2.3680 |
| 25 | 37.69 | 102.4 | 3.1345 |
| 29 | 37.55 | 102.76 | 3.1409 |

Table S4: FTIR transmittance data of acid and ester carbonyl peaks as a function of reaction time and ester-to-acid peak ratio for Ar.HBP-G3.

| Reaction Time (h) | Transmittance % |  | 1709/1648 (cm-1) ratio |
| --- | --- | --- | --- |
|  | Acid C=O, 1648 cm-1 | Ester C=O, 1709 cm-1 |  |
| 3 | 93.66 | 71.36 | 0.7755 |
| 5 | 91.19 | 71.59 | 0.7799 |
| 9 | 86.28 | 72.52 | 0.7879 |
| 13 | 78.76 | 82.45 | 1.0324 |
| 15 | 68.12 | 86.96 | 1.2268 |
| 19 | 44.65 | 93.26 | 2.0154 |
| 21 | 40.17 | 95.44 | 2.3418 |
| 23 | 39.43 | 96.91 | 2.3862 |
| 25 | 37.97 | 102.54 | 3.1463 |
| 29 | 35.55 | 104.2 | 3.8944 |
| 31 | 35.27 | 104.76 | 3.8777 |

Table S5: FTIR transmittance data of acid and ester carbonyl peaks as a function of reaction time and ester-to-acid peak ratio for Ar.HBP-G4.

| Reaction Time (h) | Transmittance % |  | 1711/1648 (cm-1) ratio |
| --- | --- | --- | --- |
|  | Acid C=O, 1648 cm-1 | Ester C=O, 1711 cm-1 |  |
| 3 | 92.99 | 71.22 | 0.7699 |
| 5 | 91.29 | 71.76 | 0.7723 |
| 9 | 85.82 | 72.45 | 0.7845 |
| 13 | 79.87 | 83.21 | 1.0442 |
| 15 | 68.31 | 87.32 | 1.2245 |
| 19 | 45.22 | 92.98 | 2.0324 |
| 21 | 40.66 | 95.67 | 2.3397 |
| 23 | 39.76 | 97.12 | 2.3797 |
| 25 | 37.13 | 101.99 | 3.1411 |
| 29 | 35.74 | 104.67 | 3.8886 |
| 31 | 34.27 | 108.46 | 4.2587 |
| 33 | 34.11 | 108.76 | 4.2954 |