SUPPORTING INFORMATION

Figure S1

Figture S1. Schematic illustration of the simplified Jablonski energy level diagram.

Figure S2

Figure S2. AAS of SiPc-ddCPP in DMF.

Figure S3

Figure S3. Cytotoxicity of MC3T3 cells treated with SiPc-ddCPP at different concentrations and irradiated by different light powers (808 nm laser at 3.0 W/cm2 for PTT, LED light λ = 660 nm 0.2 mW/cm2 for PDT) for 5 min.

Synthesis of SiPc-NH2 1,2

Silicon phthalocyanine dichloride (SiPcCl2) (0.33 mmol), 2-(2-aminoethoxy)ethanol (6.35 mmol), K2CO3 (3.62 mmol), and pyridine (3 mL) were dissolved in 40 mL of toluene. The reaction mixture was heated and refluxed at 130°C for 12 h under nitrogen atmosphere. After evaporation the volatiles, the residue was dissolved in chloroform (100 mL) and filtered. The filtrate was washed three times with deionized water and then concentrated under reduced pressure. The crud product was recrystallized from

chloroform/n-hexane to give SiPc-NH2 as a green solid (52.3%).

- Ouyang A., Zhao D., Wang X., Zhang W., Jiang T., Li A., et al. (2022). Covalent RGD–graphene–phthalocyanine nanocomposite for fluorescence imaging-guided dual active/passive tumor-targeted combinatorial phototherapy. Journal of Materials Chemistry B. 10 (2), 306-320. doi:10.1039/d1tb02254g

- Pan J., Yang Y., Fang W., Liu W., Le K., Xu D., et al. (2018). Fluorescent Phthalocyanine–Graphene Conjugate with Enhanced NIR Absorbance for Imaging and Multi-Modality Therapy. ACS Applied Nano Materials. 1 (6), 2785-2795. doi:10.1021/acsanm.8b00449