Supplementary Information

Sanghyeok Im1, Peyman Asghari-Rad1, Kelly Elizabeth Varnell1, Alex T. Vai2, Jianyi Cui2, Rachael Howland2, David Bradwell2, Hojong Kim1*

1Materials Science and Engineering, The Pennsylvania State University, 419 Steidle Building, University Park, PA 16802, United States

2Ambri Incorporated, Marlborough, MA 01752, United States

Figure S1. A 3-electrode cell configuration consisting of a Ca-Sb alloy (xCa = 0.40) as the counter electrode (CE) and a Ca-Bi alloy (xCa = 0.40) as the reference electrode (RE) to measure electrochemical performance of working electrode (WE) materials in a eutectic CaCl2-LiCl electrolyte at 520 °C.

Figure S2. Sequential coulometric titration of an Sb electrode subjected to -20 mA for 0.5 h, after which OCP was monitored for 2 h to determine the equilibrium potential (Eeq) as a function of discharge capacity, as reported in Figure 1d.

Figure S3. XRD patterns of Ca-Sb alloys (xCa = 0.54–0.65) used for emf measurements in Figure 1e, confirming the equilibrium phases present.

Table S1. Description of each electrode fabricated for 3-electrode cell testing and its role, composition, dimensions, and related figures in the main text (Figure S1).

| Electrode Composition |  |  | Electrode Holder |  | Corresponding Figure(s) |
| --- | --- | --- | --- | --- | --- |
| Type | Material | Mass | Material | Dimension |  |
| RE | Ca-Bi alloy (xCa = 0.4) | 2.0 g | BN | 8 mm ID, 12 mm OD, 25 mm Height (two capillary holes) | Figure 1,2,4 |
| CE | Ca-Sb alloy (xCa = 0.4) | 15.0 g | BN | 21 mm ID, 25 mm OD, 12 mm Height |  |
| WE | Monolithic Sb | 1.0 g | BN | 8 mm ID, 12 mm OD, 12 mm Height | Figure 1a–b |
|  | Particulate Sb | 0.36 g | SS | 8 mm ID, 12 mm OD, 12 mm Height (SS mesh cover) | Figure 1d |
|  | Ca-Sb alloys (xCa=0.54–65) | 2.0 g | BN | 8 mm ID, 12 mm OD, 25 mm Height (with capillary holes) | Figure 1e |
|  | Particulate Sb | 0.68 g | SS | 8 mm ID, 12 mm OD, 12 mm Height (SS mesh cover) | Figure 2a |
|  | Particulate Sb | 0.41 g | SS | 8 mm/12 mm, 12 mm (SS mesh cover) | Figure 2b |
|  | Ca-Li (Deposited in-situ) | - | Fe foam | 10 mm D, 15 mm Height (95% porosity) | Figure 4d |

Table S2. Cell component and the dimensions of electrode holder for the Ca||Sb(s) battery and its components.

| Component |  |  | Cell #1 (Figure 3) | Cell #2 (Figure 5) |
| --- | --- | --- | --- | --- |
| Cathode |  | Mass | 0.70 g Sb | 7.0 g Sb |
|  |  | Current collector | 300-series SS mesh (mesh size: 40×40) | 300-series SS mesh (mesh size: 80×700) |
| Anode |  | Mass | 0.70 g Ca | 3.3 g Ca |
|  |  | Current collector | Fe foam (porosity 95%) (1.0 cm D, 1.5 cm H) | 300-series SS mesh stack (6 layers of 2.7 cm H × 7.3 cm W, 35×35 mesh) |
| Electrolyte | Mass | 120 g | 602 g |
|  | Interelectrode distance | 0.5 cm | 1.3 cm |
| Crucible | Material | 300-series SS | 300-series SS |
|  | Dimensions | 6.8 cm D | 9.5 cm L × 9.5 cm W × 6.0 cm H |

Table S3. Estimation of electrode cost based on the performance of the Ca | CaCl2-LiCl | Sb(s) battery presented in Figure 3.

|  | Ca | Sb | Total |
| --- | --- | --- | --- |
| mass, m / g | 0.7 | 0.7 | 1.4 |
| Commodity bulk price, P / $/kg | 4.0 | 9.7 |  |
| Average discharge capacity, Q / mAh | 500 |  |  |
| Average discharge energy, ED / kWh | 0.62E-03 |  |  |
| Electrode cost, C / $/kWh | 15.5 |  |  |
| Energy density / Wh/kg | 620 |  |  |

Table S4. Specific capacity per mass of cathode used and calculated electrode cost for the Ca||Sb(s) cell (Figure 3), compared to previously reported liquid metal batteries.

| Electrode couple | Operating temperature (°C) | Specific capacity (mAh g-1) | Electrode cost ($/kWh) | Reference |
| --- | --- | --- | --- | --- |
| Ca¦¦Sb(s) | 520 | 715 | 15.5 | This work |
| Ca¦¦Sb(l) | 700 | 136 | 90 | doi 10.1149/2.0801412jes |
| Ca-Mg¦¦Bi(l) | 550 | 90 | 144 | doi: 10.1038/ncomms10999 |
| Li¦¦Sb-Pb(l) | 450 | 121 | 68 | doi:10.1038/nature13700 |
|  | 500 | 171 | 65 |  |
| Li¦¦Bi(l) | 550 | 293 | 169 | doi.org/10.1016/j.jpowsour.2014.10.173 |
| Li¦¦Sb-Sn(l) | 500 | 259 | 73 | doi.org/10.1021/acsami.6b02576 |
| Li¦¦Te-Sn(l) | 500 | 368 | 143 | doi.org/10.1016/j.ensm.2018.04.017 |
| Mg¦¦Sb(l) | 700 | 147 | 276 | doi.org/10.1021/ja209759s |