Supplementary Information for

“Discovery of universal phonon thermal Hall effect in crystals”

Xiaobo Jin1*, Xu Zhang1*✉, Wenbo Wan1, Hanru Wang1, Yihan Jiao1 and Shiyan Li1,2,3✉

1State Key Laboratory of Surface Physics, Department of Physics, Fudan University, Shanghai 200433, China

2Shanghai Research Center for Quantum Sciences, Shanghai 201315, China

3Collaborative Innovation Center of Advanced Microstructures, Nanjing 210093, China

Corresponding author. Email: shiyan_li@fudan.edu.cn (S.Y.L.); xuzhang_fd@fudan.edu.cn (X.Z.)

Supplementary Note 1: Thermal Hall measurements on glass and Cu3TeO6

To validate the thermal Hall results from our experiment setup, we first carried out measurements on an amorphous non-magnetic sample—a piece of glass, in which there is negligible thermal Hall signal1. A standard microscope slide was cut and polished to the similar dimensions as other samples. Figure S1a shows the thermal conductivity of the glass sample. Indeed, the thermal Hall signal in glass is negligible, as shown in Fig. S1b, which is consistent with previous report1. This excludes an artificial finite xy from our experiment setup.

For comparison, we measured the antiferromagnetic insulator Cu3TeO6, in which large xy has been reported2. As expected, we observed a large thermal Hall signal in Cu3TeO6 with a thermal Hall angle of 0.25% at 9 T (Fig. S1b), which is comparable with that in SiO2. Further, we did detailed measurements on the Cu3TeO6 sample. In Fig. S1c, xx(T) shows a phonon peak at around 20 K and a kink at TN, suggesting the high quality of our sample. In a field of 12 T, large xy(T) is observed, following the trend of xx(T). All these behaviors are consistent with previous report, depicted as blue circles2. Note that the relatively smaller value of xy in our sample is due to the smaller xx and magnetic field. The reproducibility of these data validates our experiment setup.

Figure S1 | The thermal Hall signals in glass and Cu3TeO6. a, κxx of glass as a function of temperature in zero field. b, The thermal Hall angles of glass and Cu3TeO6 as a function of magnetic field. The average temperature Tavg = (T1 + T2)/2 was hold at 12 K for both samples. c, κxx of Cu3TeO6 as a function of temperature in zero field. The inset gives the zoom-in κxx(T) around TN. d, xy of Cu3TeO6 measured at H = 12 T as a function of temperature. For comparison, the data from ref. 2 were also plotted in c and d as blue empty circles.

Supplementary Note 2: Thermal Hall measurements on VI3 and CrI3

If κxy(T) always follows κxx(T) in our samples, we still worry about whether it is an artificial result. Therefore, we chose to measure ferromagnetic insulators VI3 and CrI3, since the κxy(T) of VI3 has special temperature dependence and different sign from that of CrI3 (refs. 3 and 4).  Figure S2a and b show κxx(T) and κxy(T) of VI3, respectively. xx(T) manifests a kink at Tc = 50 K. A large positive xy, as reported in ref. 3, arises around Tc, then shows a broad peak at low temperature. For CrI3, as shown in Fig. S2c and d, it has a negative xy and it peaks at the same temperature as xx(T). Compared with the data extracted from refs. 3 and 4, all the features we observed in VI3 and CrI3 are consistent with previous reports3,4, thus further validate the reliability of our thermal Hall measurements.

Starting from a universal phonon THE in crystals, the conclusion of this work, one can see that the magnetic environment below Tc = 61 K in CrI3 only slightly affects the phonon xy(T). However, for VI3, the distinct shape and positive sign of xy(T) suggest that the magnetic environment below Tc = 50 K has huge effect on the phonon THE. We discuss it in the main text together with other ferromagnetic insulators.

Figure S2 | The thermal Hall effect in VI3 and CrI3. a, κxx of VI3 as a function of temperature in zero field. b, κxy of VI3 measured at H = 0.5 T in the spin polarized state, plotted as κxy vs T. For comparison, the data from ref. 3 were also plotted in a and b as empty circles. c, κxx of CrI3 as a function of temperature in zero field. d, κxy of CrI3 measured at H = 1 T in the spin polarized state, plotted as κxy vs T. For comparison, the data from ref. 4 were also plotted in c and d as blue empty circles.

Supplementary Note 3: Crystal structure of SiO2

SiO2 (quartz) has a chiral crystal structure, in which SiO4 tetrahedra form a chiral helix along [001]. The resulting chiral space group is either P3221 (left quartz) or P3121 (right quartz). Figure S3 gives the crystal structure of right quartz.

Figure S3 | Crystal structure of SiO2.

Supplementary Note 4: Check the effect of copper block heat sink

In our thermal transport experiments, a copper block is used as the heat sink. In ref. 5, the authors observed a non-zero Hall signal in non-magnetic Y2Ti2O7 (the data was extracted and plotted in Fig. S4a) and attributed this signal to temperature gradients on the heat sink (brass block). Although it is unlikely to generate a finite transverse temperature gradient that could affect the sample due to the large size of the copper block, we conducted comparative experiment to check it. The measurement on SiO2 sample was conducted again with a different configuration. The measurement in the main text involved the direct adhesion of the sample to the copper block (Fig. 1a), while the comparative experiment took another configuration where the sample was connected to the copper block via silver wire (Configuration B in Fig. S4b). The results of both measurements are consistent (Fig. S4c and d), confirming that using copper block as the heat sink does not result in any detectable contamination on thermal Hall data. Based on our finding, the non-zero thermal Hall signal observed in ref. 5 should arise from Y2Ti2O7 itself, in which the thermal Hall angle is approximately 0.25  10-3 at 15 K and 9 T, on the same order of magnitude as that of SrTiO3. In ref. 5, the thermal Hall angle of magnetic Tb2Ti2O7 is approximately 8  10-3 at 15 K and 9 T, which is comparable to the value of 5.5  10-3 for Si at 30 K and 9 T. The finite thermal Hall signal of non-magnetic Y2Ti2O7 observed in ref. 5 further confirms the universal phonon THE in crystals discovered in our current work.

Figure S4 | Check the effect of copper block heat sink. a, The thermal Hall angle of Y2Ti2O7 as a function of magnetic field. The data are from ref. 5. b, A measurement configuration in which the sample is connected to the copper block via silver wire. This is named Configuration B to distinguish it from the configuration in main text (Configuration A). c, d, Comparison of two thermal transport measurements with Configuration A and B on the same SiO2 sample. The results of both measurements are consistent, confirming that using copper block as the heat sink does not result in any detectable contamination on thermal Hall data.

Supplementary Note 5:  Thermal Hall measurements on KTaO3

Previous work suggests that KTaO3 (KTO) has a tiny κxy (ref. 6), which is at odds with the universal phonon THE observed in this study. Therefore, we also conducted thermal Hall measurements on KTO single crystal. As shown in Fig. S5a, the temperature dependence of κxx for our sample is consistent with that reported in ref. 7, and slightly different from that in ref. 6 at low temperature. Clearly, a finite κxy is observed, with the peak value about one-third of STO (Fig. S5). This finding further confirms the existence of universal phonon THE in crystals. The difference between our data and the previous work on KTO needs further study.

Figure S5 | The thermal Hall effect in KTaO3 and SrTiO3. a, κxx of KTaO3 and SrTiO3 measured in this work as a function of temperature in zero field. b, κxy of KTaO3 and SrTiO3 measured at H = 9 T as a function of temperature. The κxx and κxy of KTaO3 from ref. 6 are also plotted for comparison.

Supplementary Note 6: yy of SiO2 single crystals

The thermal Hall conductivity is defined as κxy = κyy(ΔTy/ΔTx)(L/w), where κyy is the longitudinal thermal conductivity along the y axis. For crystals with high symmetry (SrTiO3, KTaO3, MgO, MgAl2O4, Si and Ge), x is along the [100] axis, and [100], [010] and [001] directions are equivalent. Therefore, we take κyy = κxx when calculating κxy. For the samples of SiO2, x is along the [001] axis and y is along the [1_10] axis. Due to the chiral crystal structure, κyy and κxx in SiO2 should be unequal. We cut and polished another SiO2 sample with the longest edges along [1_10] axis (y) to the same dimensions as the sample in main text. κyy was measured in this sample with J || [1_10]. As shown in Fig. S6, κyy exhibits a slightly larger value than κxx.

Figure S6 | xx and yy of SiO2 single crystals.

Supplementary Note 7: Scaling law in MgAl2O4 and black phosphorous

In Fig. S7, we plot the conventional κxy (κxz and κzx) as a function of κxx for MgAl2O4 and black phosphorous (BP). The data of BP were extracted from ref. 8. The thermal transport data of MgAl2O4 and BP also obey the scaling law |xy| ~ xx2, as the other non-magnetic insulators and semiconductors studied in this work.

Figure S7 | |xy| vs xx for MgAl2O4 and black phosphorous.

Supplementary Note 8: Scaling law between planar κxy and κxx in SiO2

In Fig. S8, we plot the conventional κxy and two planar κxy as a function of κxx for SiO2 sample. One can clearly see that the planar κxy also obeys the scaling law |xy| ~ xx2, as the conventional κxy does.

Figure S8 | |xy| vs xx in different configurations for SiO2.

Supplementary Note 9: Absence of scaling law between xy and xx in magnetic materials

In Fig. S9, we plot |xy| vs. xx for various magnetic insulators in which THE has been observed9-12. Unlike most non-magnetic insulators and semiconductors measured in this work, these materials manifest a deviation from the scaling law |xy| ~ xx2, indicating the effect of magnetic environment on the phonon THE.

Figure S9 | |xy| vs xx for various magnetic insulators. |xy| plotted as a function of xx for La2CuO4 (ref. 9), Sr2CuO2Cl2 (ref. 9), Nd2CuO4 (ref. 9), Sr2Ir0.5Rh0.5O4 (ref. 10), -RuCl3 (ref. 11) and Na2Co2TeO6 (ref. 12). The blue lines represent the scaling relation of |xy| ~ xx2.

Supplementary references

- Kim, H.-L. et al. Modular thermal Hall effect measurement setup for fast-turnaround screening of materials over wide temperature range using capacitive thermometry. Rev. Sci. Instrum. 90, 103904 (2019).

- Chen, L., Boulanger, M.-E., Wang, Z.-C., Tafti, F. & Taillefer, L. Large phonon thermal Hall conductivity in the antiferromagnetic insulator Cu3TeO6. Proc. Natl. Acad. Sci. U.S.A. 119, e2208016119 (2022).

- Zhang, H. et al. Anomalous thermal Hall effect in an insulating van der Waals magnet. Phys. Rev. Lett. 127, 247202 (2021).

- Xu, C. et al. Thermal Hall effect in the van der Waals ferromagnet CrI3. Phys. Rev. B 109, 094415 (2024).

- Hirschberger, M., et al. Large thermal Hall conductivity of neutral spin excitations in a frustrated quantum magnet. Science 348, 106-109 (2015)

- Li, X., Fauqué, B., Zhu, Z. & Behnia, K. Phonon thermal Hall effect in strontium titanate. Phys. Rev. Lett. 124, 105901 (2020).

- Tachibana, M., Kolodiazhnyi, T., Takayama-Muromachi, E. Thermal conductivity of perovskite ferroelectrics. Appl. Phys. Lett. 93, 092902 (2008).

- Li, X. et al. The phonon thermal Hall angle in black phosphorus. Nat. Commun. 14, 1027 (2023).

- Boulanger, M.-E. et al. Thermal Hall conductivity in the cuprate Mott insulators Nd2CuO4 and Sr2CuO2Cl2. Nat. Commun. 11, 5325 (2020).

- Ataei, A. et al. Phonon chirality from impurity scattering in the antiferromagnetic phase of Sr2IrO4. Nat. Phys. (2024).

- Lefrançois, É. et al. Evidence of a phonon Hall effect in the Kitaev spin liquid candidate α-RuCl3. Phys. Rev. X 12, 021025 (2022).

- Yang, H. et al. Significant thermal Hall effect in the 3d cobalt Kitaev system Na2Co2TeO6. Phys. Rev. B 106, L081116 (2022).