Characterization of Tobacco Stalk Ash

Ananya Buragohain †,⸙, Victoria Vartic,⸙, Rebecca Lalmuanpuii†,‡, Khawlhring Lalrammawia†, Kahramon Mamatkuhlov, Grigory Arzymanyan,*, Nikita Yushin, Pavel Nekhoroshkov, Inga Zinicovscaia, Rajendra Bose Muthukumaran†,*

Fig.  S1(a)					Fig.  S1(b)

Fig.  S1(c)					Fig.  S1(d)

Fig.  S1(e)

Fig. S1: XPS features of various elements present in tobacco stalk ash: (a) Si 2p; (b) S 2p; (c) P 2p; (d) Mg 1s; (e) Cl 2p

Fig. S2(a)						 Fig. S2(b)

Fig. S2: EDS analysis of tobacco stalk ash

Table S2(a): Mineral components of tobacco stalk ash.

| Element | Weight% | Atomic % |
| --- | --- | --- |
| Carbon(C) | 16.44 | 25.31 |
| Oxygen(O) | 50.36 | 58.18 |
| Sodium(Na) | 0.34 | 0.28 |
| Magnesium(Mg) | 4.67 | 3.55 |
| Aluminum(Al) | 0.28 | 0.19 |
| Silicon(Si) | 1.04 | 0.68 |
| Phosphorous(P) | 1.22 | 0.73 |
| Potassium(K) | 2.60 | 1.23 |
| Calcium(Ca) | 20.94 | 9.66 |

Table S2(b): Mineral components of tobacco stalk ash.

| Element | Weight% | Atomic % |
| --- | --- | --- |
| Oxygen(O) | 55.59 | 75.93 |
| Sodium(Na) | 0.69 | 0.66 |
| Magnesium(Mg) | 1.05 | 0.95 |
| Sulfur(S) | 1.26 | 0. 86 |
| Chlorine(Cl) | 4.08 | 2.51 |
| Potassium(K) | 5.54 | 3.10 |
| Calcium(Ca) | 28.71 | 15.65 |