Layered gel emulsion-templated Janus porous composites for emulsified oil separation

Shixiang Zuo,a,b Chunyu Wang,c,* Nawaa Ali Husaykan Alshammari,d Salah Mohamad El-Bahy,e Rong Xu,a Saijie Li,c Lei Wang,c Chao Yao,a,b Zeinhom Mohamad El-Bahy,f Haoguan Gui,a,b,*

a Advanced Catalysis and Green Manufacturing Collaborative Innovation Center, School of Petrochemical Engineering, Changzhou University, Changzhou 213164, China

b R&D Center of Xuyi Attapulgite Applied Technology, Changzhou University, Xuyi 211700, China

c State Key Laboratory of NBC Protection for Civilian, Beijing 102205, China

d Department of Chemistry, Faculty of Science, Northern Border University, Arar 73222, Saudi Arabia

e Department of Chemistry, Turabah University College, Taif University, P.O. Box 11099, Taif 21944, Saudi Arabia

f Department of Chemistry, Faculty of Science, Al-Azhar University, Nasr City 11884, Cairo, Egypt

Corresponding authors:

wcy18@tsinghua.org.cn (C.W.)

guihaoguan@cczu.edu.cn (H.G.)

Supporting Information Includes:

Additional Data:

- Fig. S1. Morphology for GO-based HIPEs.

- Fig. S2. Rheological properties for GO-based HIPEs.

- Fig. S3. Morphology for PCL-based HIPEs.

- Fig. S4. Rheological properties for PCL-based HIPEs.

- Fig. S5. Cyclic compressive stress-strain curves of polyHIPEs

- Table S1. Formation of GO-based polyHIPEs.

- Table S2. Formation of PCL-based polyHIPEs.

Figures

Fig. S1. Optical images for GO-based HIPEs: a) GO-2, b) GO-5 and c) GO-10

Fig. S2. Rheological properties of GO-based HIPEs: a) storage (G’) and loss (G’’) moduli, and b) complex viscosity (η*)

Fig. S3. Optical images for PCL-based HIPEs: a) PCL-2, b) PCL-5 and c) PCL-10

Fig. S4. Rheological properties for PCL-based HIPEs: a) storage (G’) and loss (G’’) moduli, and b) complex viscosity (η*)

Fig. S5. Cyclic compressive stress-strain curves of polyHIPEs: a) GO-2 and b) PCL-2

Tables

Table S1. Recipes of the GO-based polyHIPEs

|  | GO-4 | GO-8 | GO-12 |
| --- | --- | --- | --- |
| External continuous phase (wt%) |  |  |  |
| DMSO | 20.40 | 18.30 | 16.20 |
| GO | 1.00 | 2.00 | 3.00 |
| PolyMDI | 1.00 | 2.00 | 3.00 |
| F-127 | 2.50 | 2.50 | 2.50 |
| Total | 24.90 | 24.80 | 24.70 |
| Internal dispersed phase (wt%) |  |  |  |
| Paraffin oil | 75.00 | 75.00 | 75.00 |
| Catalyst (added after HIPEs formation, wt%) |  |  |  |
| DBTDL | 0.10 | 0.20 | 0.30 |

Table S2. Recipes of the PCL-based polyHIPEs

|  | PCL-5 | PCL-10 | PCL-20 |
| --- | --- | --- | --- |
| External continuous phase (wt%) |  |  |  |
| DMSO | 19.87 | 17.25 | 12.00 |
| PCL-Triol | 1.25 | 2.50 | 5.00 |
| PolyMDI | 1.25 | 2.50 | 5.00 |
| F-127 | 2.50 | 2.50 | 2.50 |
| Total | 24.87 | 24.75 | 24.50 |
| Internal dispersed phase (wt%) |  |  |  |
| Paraffin oil | 75.00 | 75.00 | 75.00 |
| Catalyst (added after HIPEs formation, wt%) |  |  |  |
| DBTDL | 0.13 | 0.25 | 0.50 |