Supplementary Material

Adsorption behavior and quantum chemical analysis of surface functionalized polystyrene nano-plastics on gatifloxacin.

Table S1. Parameters of ESP

| Model | Positive surface area (Å2) | Negative surface area (Å2) | MPI (kcal/mol) | PSA (Å2) |
| --- | --- | --- | --- | --- |
| GAT | 241.53204 | 128.40917 | 13.88327 | 203.98 |
| PS | 170.52487 | 108.12740 | 6.98274 | 60.20 |
| PS-COOH | 186.15511 | 123.57650 | 8.89366 | 101.20 |
| PS-NH2 | 158.17261 | 136.19955 | 8.36184 | 87.67 |

Table S2. Van der Waals penetration distances between nano-plastics and Gats and interacting functional groups.

| Nano-plastic type | Van der Waals penetration distance(Å) | Interacting functional groups |
| --- | --- | --- |
| PS-COOH | 1.06 | GAT carboxyl group =O, quinoline =O and PS-COOH carboxyl group H |
| PS-COOH | 0.94 | GAT carboxyl group H and PS-COOH carboxyl group =O |
| PS-NH2 | 0.80 | GAT carboxyl group =O, quinoline =O and PS-NH2 amino group H |
| PS-NH2 | 1.20 | GAT carboxyl group H and N on the amino group of PS-NH2 |

Fig.S1 Quantification of surface electrostatic potential. (a)GAT, (b)PS, (c)PS-COOH, (d)PS-NH2

Fig.S2 (a) PS and GAT van der Waals penetration positions. (b) IRI analysis of PS and GAT.

Fig.S3 PS-COOH(a), PS-NH2(b) and GAT van der Waals penetration positions. A nanoplastic polymer was simulated with a compound composed of 2 monomers, and the force between GAT and the nanoplastic polymer was calculated at M062X/6-31G(D).

Text S1 Adsorption kinetics

The 50 mL 10 mg ·L-1 GAT solutions were made up from 5 mL GAT stock solution in a 100 mL conical bottles. Adjusted the pH of the solution to 6.0. The 50 mL 10 mg ·L-1 PSNPs were added to the above solutions respectively. The conical bottles were then placed in a constant temperature oscillator with a temperature of 298K and a rotational speed of 150 r·min-1. Six groups of parallel experiments were set up, and 10 mL samples were taken at 1, 2, 3, 5, 7, 10, 22, 24 and 36 h, respectively. Then, the samples were quickly filtered with 0.22 μm cellulose acetate membrane, and then the concentration of GAT in the samples was measured. The adsorption capacity was obtained by measuring the concentration of GAT, and the kinetic data were analyzed using models (1) (2) (3).

Pseudo-first-order kinetic:

Pseudo-second-order kinetic:

Intra-particle diffusion model:

In the formula, Qt is the adsorption amount of nano-plastic at t time (mg·g-1); Qe is the adsorption amount of nano-plastic at adsorption equilibrium (mg·g-1); k1 and k2 are the pseudo-first-order and pseudo-second-order kinetic constants, respectively (min-1); t is the adsorption time (min); ki is the intra-particle diffusion rate constant (mg·mg-0.5·min-0.5); c is the constant related to thickness and boundary layer.

Text S2 Adsorption isotherm

The concentration gradient of GAT to 2, 4, 6, 8, 10, 12 mg·L-1 was set, with the solution pH 6. The GAT solution with the above concentration gradient was added to 50 mL 10 mg·L-1 PSNPs at 283, 298, 313 K, respectively, in a 100mL conical bottle and then placed in an oscillator and oscillate in dark. The speed of the oscillator was set to 150r/min. After 24 hours, samples were taken and tested for GAT concentration in the samples. Models (4) and (5) were used to analyze the adsorption isotherm.

Langmuir isotherm model:

Freundlich isotherm model:

In the formula, Qe is the adsorption amount of nano-plastic at adsorption equilibrium (mg·g-1); Qmax is the maximum adsorption amount of GAT (mg·g-1); Ce is the concentration of GAT in solution at adsorption equilibrium (mg·L-1); KL is the adsorption constant, (L·mg-1); Kf is a constant related to the capacity and adsorption strength of the adsorbent, ((mg/mg)·(mg/L)-1/n); n is related to the affinity of the adsorption process.

Text S3 Adsorption thermodynamics

The experimental conditions of thermodynamic analysis are the same as those of adsorption isotherm experiment. The thermodynamic parameters were calculated at 283, 298 and 313K. The thermodynamic parameters are calculated as follows:

In the formula, kd is the adsorption distribution coefficient, R is the general gas constant (8.314 J·(mol·K)-1), and T is the temperature (K).

References

Wang K, Han T, Chen X, et al. Insights into behavior and mechanism of tetracycline adsorption on virgin and soil-exposed microplastics[J]. Journal of Hazardous Materials, 2022, 440: 129770.

Meng S ,Yongkui Y ,Menglu H , et al. Adsorption behaviors and mechanisms of antibiotic norfloxacin on degradable and nondegradable microplastics.[J]. The Science of the total environment,2021,807(P3).