Characterisation of materials properties and defects in structure fabricated via additive friction stir deposition

Author identifiers removed for double anonymised peer review (per submission instructions)

Supplementary information 1

Supplementary Table 1. A summary of the XCT scanning parameters

| Part identifier | Voxel size (µm3) | Voltage (kV) | Current (µA) | Integration time (ms) | Number of projections | Number of images averaged/projection |
| --- | --- | --- | --- | --- | --- | --- |
| B1 | 24.986 | 100 | 90 | 1000 | 1000 | 3 |
| B2 | 30.06 | 100 | 90 | 1000 | 1000 | 3 |
| T1+B3 | 30.87 | 100 | 90 | 1000 | 1000 | 3 |
| T2+B4 | 30.06 | 100 | 90 | 1000 | 1000 | 3 |
| T3+B5 | 30.06 | 100 | 90 | 1000 | 1000 | 3 |
| T4+b6 | 30.06 | 100 | 90 | 1000 | 1000 | 3 |

Supplementary information 2

Supplementary Figure S1. Virtual machining analysis for section B5+T3 and B6+T4 (sections stitched) along the length. Scale bar corresponds to 5 mm.