Removal, mechanistic and kinetic studies of Cr(VI), Cd(II) and Pb(II) cations using Fe₃O₄ functionalized Schiff base chelating ligands

George S. Nyamato1*, Ian T. Kabogo1, Siphosethu Maqinana2, Rene Bachmann³, Markus Schmitz³, Joanne Ogunah1, Wolfgang Kleist³, Stephen O. Ojwach2,

1Department of Physical Sciences, University of Embu, P.O Box 6-60100, Embu, Kenya

2School of Chemistry and Physics, University of KwaZulu-Natal, Pietermaritzburg Campus, Private Bag X01, Scottsville, 3209, South Africa

3Fachbereich Chemie, RPTU Kaiserslautern-Landau, Erwin-Schrödinger-Str. 54, 67663, Kaiserslautern, Germany

SUPPLEMENTARY MATERIALS

TABLE OF CONTENTS

1. Synthesis and characterization of chelating Schiff base ligands and their immobilization onto Fe₃O₄ MNPs	1

1.1 Preparation of Fe₃O₄ MNPs	1

1.2 Synthesis of functionalized Schiff base ligands	2

1.2.1 (E)-2-(3,3-dimethoxy-2-oxa-7,10-diaza-3-silaundec-10-en-11-yl)phenol (L1)	2

1.2.2 (E)-N-(2-((pyridine-2ylmethylene)amino)ethyl)-3-(Trimethoxysilyl)propan-1-amine (L2)	2

1.2.3 (E)-N-(2-((thiophen-2-ylmethylene)amino)ethyl)-3-(Trimethoxysilyl)propan-1-amine (L3)	3

2. Statistical parameters and removal efficiencies for the respective metal cations	9

1. Synthesis and characterization of chelating Schiff base ligands and their immobilization onto Fe₃O₄ MNPs

## 1.1 Preparation of Fe₃O₄ MNPs

The MNPs were prepared using co-precipitation method. About 1.50 g of ferrous chloride (Fe²⁺) was dissolved in 100 mL deionized water at a temperature of 85℃ under nitrogen atmosphere. After dissolving, 3.00 g of ferric chloride (Fe³⁺) was added to the mixture and a red-brown color was observed. Overall, the molar ratio attained of Fe³⁺ to Fe²⁺ was 2:1. After one hour, about 15 mL of 25% ammonium hydroxide (NH₄OH) was rapidly added into the mixture and stirred vigorously, immediately forming a black precipitate which indicated the nucleation of Fe₃O₄. The mixture was then left to stir for about 1 h after which it was filtered, and the residue washed three times with deionized water and ethanol. The residue was then dried under vacuum for 8 h at 65℃.

## 1.2 Synthesis of functionalized Schiff base ligands

### 1.2.1 (E)-2-(3,3-dimethoxy-2-oxa-7,10-diaza-3-silaundec-10-en-11-yl)phenol (L1)

To a methanol solution of salicylaldehyde (0.50 mL, 4.70 mmol), AEAPTMS (1 mL, 4.60 mmol) was added dropwise. The reaction mixture was refluxed for 24 h at 65℃ after which methanol was removed by evaporation in vacuum to yield L1 as a yellow oily liquid. Yield: 1.46 g (97%). ¹H NMR (400 MHz, CDCl₃): δH 0.60 (s, 2H, Si-CH₂); 1.56 (s, 3H, CH₂, C-NH), 2.61 (s, 4H, (CH₂)2), 2.89 (s, 2H, CH₂), 3.55-3.42 (m, 9H, ³JHH=6.32 Hz, O-CH3), 6.84 (s, 1H, Ph), 6.92 (d, 1H, ³JHH=3.16 Hz, Ph), 7.21 (d, 1H, ³JHH=2.68Hz, Ph), 7.28 (d, 1H, ³JHH=3.44Hz, Ph), 8.35 (s, 1H, C=NH). ¹³C NMR (100 MHz, CDCl₃,): δ 10.16, 23.29, 50.26, 52.43, 59.58, 116.95, 118.60, 131.29, 132.24, 161.11, 165.99. FT-IR (cm⁻¹): υ(N-H)=3392, υ(O-H)=3290, υ(C=N)=1625, υ(Si-O)=744.

Compounds L2 and L3 were prepared following the same procedure as described for compound L1, using the appropriate reagents.

### 1.2.2 (E)-N-(2-((pyridine-2ylmethylene)amino)ethyl)-3-(Trimethoxysilyl)propan-1-amine (L2)

Compound 2-pyridine-carboxaldehyde (0.50 mL, 5.30 mmol) was reacted with AEAPTMS (1 mL, 4.60 mmol) and isolated as a dark orange oily liquid. Yield 1.43 g (95%). ¹H NMR (400 MHz, CDCl₃): δH 0.36 (m, 2H, ³JHH=4.12 Hz, CH₂), 1.29 (s, 3H, CH₂, NH), 2.08 (t, 2H, ³JHH=3.46Hz), 2.29 (q, 2H, ³JHH=5.72 Hz, CH₂), 2.94 (t, 2H, ³JHH=2.68Hz, CH₂), 3.16 (s, 9H, O-CH₃), 7.06 (s, 1H, Py), 7.26 (s, 1H, Py), 7.51 (t, 2H, ³JHH=7.43 Hz, Py), 8.39 (s, 1H, NH). ¹³C NMR (100 MHz, CDCl₃,): δ 10.02, 22.04, 49.58, 52.56, 55.66, 122.72, 123.29, 136.63, 149.32, 153.92, 159.01.  FT-IR (cm⁻¹): υ(N-H)=3300, υ(C=N)= 1650, υ(Si-O)=764.

### 1.2.3 (E)-N-(2-((thiophen-2-ylmethylene)amino)ethyl)-3-(Trimethoxysilyl)propan-1-amine (L3)

Compound 2-thiophene-carboxaldehyde (0.50 mL, 5.30 mmol) was reacted with AEAPTMS (1 mL, 4.60 mmol) and a dark brown oily liquid was obtained. Yield 0.99 g (66%). ¹H NMR (400 MHz, CDCl₃): δH 0.58 (s, 2H, CH₂), 1.55 (s, 3H, CH₂, NH), 2.61 (s, 2H, CH₂), 2.88 (s, 2H, CH₂), 3.24 (s, 2H, CH₂), 3.42 (m, 9H, ³JHH=3.24 Hz, O-CH₃), 6.93 (s, 1H, Th), 7.04 (s, 1H, Th), 7.36 (s, 1H, Th), 8.38 (s, 1H, NH). ¹³C NMR (100 MHz, CDCl₃,): δ 9.51, 23.01, 50.30, 52.37, 55.69, 127.39, 128.95, 130.64, 142.19, 155.55. FT-IR (cm⁻¹): υ(N-H)=3312, υ(C=N)= 1631, υ(O-Si)=744.

Fig. S1: ¹H-NMR for L1 showing the imine proton at 8.34 ppm

Fig. S2: ¹H-NMR for L2 showing the imine proton at 8.39 ppm

Fig. S3: ¹H-NMR for L3 showing the imine proton 8.38 ppm

Fig. S4: ¹³C-NMR for L1 showing the C=N carbon at 161 ppm

Fig. S5: ¹³C-NMR for L2 showing the C=N carbon at 153 ppm

Fig. S6: ¹³C-NMR for L3 showing the C=N carbon at 155 ppm

Fig. S7: FT-IR spectra of the Schiff base chelating ligands, L1-L3, showing vibrational frequencies  for  O-Si signals between 1087-1104 cm⁻¹ after which there was the appearance of Fe-O signals between 540-560 cm⁻¹ upon immobilization of the ligands on MNPs

Fig. S8: N2 adsorption-desorption isotherms for L1@Fe3O4-L3@Fe3O4, a-c respectively

Fig. S9: Pore-size distribution (according to BJH) for L1@Fe3O4-L3@Fe3O4, a-c respectively

Fig. S10: TGA plots showing the decomposition patterns for L1@Fe₃O₄-L3@Fe₃O₄

Fig. S11: DSC plots showing the decomposition patterns for L1@Fe₃O₄-L3@Fe₃O₄

Fig. S12: Stacked FTIR spectra of fresh and used L1@Fe3O4 adsorbent showing the υ(C=N) at 1666 and 1624 cm⁻¹, respectively, and disappearance of O-H and N-H peaks at 3290 and 3394 cm⁻¹, respectively, in the used adsorbent due to deprotonation upon complexation

Fig. S13: Stacked FT-IR spectra of fresh and used L2@Fe3O4 adsorbent showing the υ(C=N) at 1634 and 1643 cm⁻¹, respectively, and disappearance of N-H peak at 3384 cm⁻¹ in the used adsorbent due to deprotonation upon complexation

Fig. S14: Stacked FTIR spectra of the fresh and used L3@Fe3O4 adsorbent showing υ(C=N) at 1625 and 1632 cm⁻¹, respectively, and disappearance of N-H peak at 3382 cm⁻¹ in the used adsorbent due to deprotonation upon complexation

# 2. Statistical parameters and removal efficiencies for the respective metal cations

Table S1: Adsorption parameters for the removal of Cr(VI) cations on L1@Fe3O4

| Entry | Co (mg/L) | Ce (mg/L) | qe | 1/Ce | 1/qe | Log Ce | Log qe | ln Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 20 | 6.4 | 20.4 | 0.156 | 0.049 | 1.856 | 1.31 | 1.856 |
| 2 | 30 | 13 | 25.5 | 0.077 | 0.039 | 2.565 | 1.407 | 2.565 |
| 3 | 40 | 21.25 | 28.13 | 0.047 | 0.036 | 3.056 | 1.449 | 3.056 |
| 4 | 50 | 31.1 | 28.35 | 0.032 | 0.035 | 3.437 | 1.452 | 3.437 |
| 5 | 60 | 39.79 | 30.32 | 0.025 | 0.033 | 3.684 | 1.482 | 3.684 |

Table S2: Adsorption parameters for the removal of Cd(II) cations on L1@Fe3O4

| Entry | Co (mg/L) | Ce (mg/L) | qe | 1/Ce | 1/qe | Log Ce | Log qe | ln Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 20 | 10.76 | 13.86 | 0.093 | 0.072 | 1.032 | 1.142 | 2.376 |
| 2 | 30 | 17.36 | 18.96 | 0.058 | 0.053 | 1.24 | 1.278 | 2.854 |
| 3 | 40 | 24.34 | 23.49 | 0.041 | 0.043 | 1.386 | 1.371 | 3.192 |
| 4 | 50 | 33.15 | 25.28 | 0.0302 | 0.04 | 1.52 | 1.403 | 3.501 |
| 5 | 60 | 42.35 | 26.48 | 0.024 | 0.038 | 1.627 | 1.423 | 3.746 |

Table S3: Adsorption parameters for the removal of Pb(II) cations on L1@Fe3O4

| Entry | Co (mg/L) | Ce (mg/L) | qe | 1/Ce | 1/qe | Log Ce | Log qe | ln Ce |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 100 | 1.53 | 147.705 | 0.654 | 0.007 | 0.185 | 2.17 | 0.425 |
| 2 | 200 | 7.49 | 288.765 | 0.134 | 0.003 | 0.874 | 2.461 | 2.014 |
| 3 | 300 | 27.5 | 408.825 | 0.036 | 0.002 | 1.439 | 2.612 | 3.312 |
| 4 | 400 | 108.9 | 436.665 | 0.009 | 0.002 | 2.037 | 2.64 | 4.690 |
| 5 | 500 | 175.9 | 486.06 | 0.006 | 0.002 | 2.245 | 2.687 | 5.170 |

Table S4: % Removal efficiencies by variation of pH

| Entry | pH | Metal cation / % Extraction efficiency |  |  |
| --- | --- | --- | --- | --- |
|  |  | Cr(VI) | Pb(II) | Cd(II) |
| 1 | 1 | 38 | 19 | 25 |
| 2 | 3 | 68 | 47 | 46 |
| 3 | 5 | 55 | 83 | 45 |
| 4 | 7 | 45 | 98 | 41 |
| 5 | 9 | 42 | 99 | 36 |

Reaction conditions: contact time 24 hrs, adsorbent dose 10 mg, initial metal concentration 20 ppm (Cr(VI), Cd(II)), 100 ppm (Pb(II)) using L1@Fe3O4.

Table S5: % Removal efficiencies by variation of initial metal concentration

| Entry | Initial metal concentration (ppm) | Metal cation / % Removal efficiency |  |  |
| --- | --- | --- | --- | --- |
|  |  | Cr(VI) | Cd(II) | Pb(II) |
| 1 | 20 | 68 | 46 | NR |
| 2 | 30 | 57 | 42 |  |
| 3 | 40 | 47 | 39 |  |
| 4 | 50 | 38 | 34 |  |
| 5 | 60 | 34 | 29 |  |
| 6 | 100 | NR |  | 98 |
| 7 | 200 |  |  | 96 |
| 8 | 300 |  |  | 91 |
| 9 | 400 |  |  | 79 |
| 10 | 500 |  |  | 65 |

Reaction conditions: contact time 24 hrs, adsorbent dose 10 mg, pH 3 (Cr(VI), Cd(II)) , pH 9 ( Pb(II)) using L1@Fe3O4. NR- Not reported.

Table S6: % Removal efficiencies by contact time variation

| Entry | Contact time (hrs) | Metal cation / % Removal efficiency |  |  |
| --- | --- | --- | --- | --- |
|  |  | Cr(VI) | Pb(II) | Cd(II) |
| 1 | 1 | 27 | 86 | 16 |
| 2 | 6 | 53 | 92 | 36 |
| 3 | 12 | 64 | 96 | 42 |
| 4 | 18 | 68 | 98 | 46 |
| 5 | 24 | 68 | 98 | 46 |

Reaction conditions: initial metal concentration 20 ppm (Cr(VI), Cd(II)), 100 ppm (Pb(II)), adsorbent dose 10 mg, pH 3 (Cr(VI), Cd(II)) , pH 9 ( Pb(II)) using L1@Fe3O4.

Table S7: Kinetic models and other statistical parameters of adsorption using L1@Fe3O4

|  | Kinetic model | Parameters | Metal ions solution |  |  |
| --- | --- | --- | --- | --- | --- |
| Entry |  |  | Cr(VI) (20ppm) | Cd(II) (20ppm) | Pb(II) (100ppm) |
| 1 | Pseudo-first-order equation | K1 (min− 1) | 0.0118 | 0.0231 | 0.0951 |
|  |  | qe exp (mg/g) | 23.565 | 20.685 | 147.705 |
|  |  | qe cal (mg/g) | 19.539 | 13.396 | 144.233 |
|  |  | R2 | 0.9321 | 0.9870 | 0.9969 |
|  | Pseudo-second-order equation | K2 (g mg− 1 min− 1) | 0.0377 | 0.0351 | 0.0349 |
|  |  | qe, exp (mg/g) | 23.565 | 20.685 | 147.705 |
| 2 |  | qe, cal (mg/g) | 21.222 | 14.533 | 148.148 |
|  |  | h (mg g− 1 min− 1) | 18.853 | 10.560 | 763.358 |
|  |  | R2 | 0.9950 | 0.9940 | 0.9997 |
| 3 | Elovich equation | α (mg/g min) | 28.333 | 12.886 | 1.25E10 |
|  |  | β (g/mg) | 0.240 | 0.317 | 0.1666 |
|  |  | R2 | 0.9946 | 0.9937 | 0.9995 |
| 4 | Intraparticle diffusion | Kdiff (mg/g min1/2) | 4.149 | 2.880 | 63.752 |
|  |  | C | 2.875 | 1.571 | 25.285 |
|  |  | R2 | 0.9126 | 0.9282 | 0.8294 |

Table S8: RL values for the adsorption of metal cations based on Langmuir isotherm using L1@Fe3O4

| Entry | Metal cation/RL value |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Initial conc. (mg L−1) | Cr(VI) | Cd(II) | Initial conc. (mg L−1) | Pb(II) |
| 1 | 20 | 0.162 | 0.516 | 100 | 0.031 |
| 2 | 30 | 0.114 | 0.415 | 200 | 0.016 |
| 3 | 40 | 0.088 | 0.347 | 300 | 0.010 |
| 4 | 50 | 0.072 | 0.299 | 400 | 0.008 |
| 5 | 60 | 0.061 | 0.262 | 500 | 0.006 |

Table S9: Isotherm models and other statistical parameters of adsorption using L1@Fe3O4

| Entry | Isotherm Model |  | Cr(VI) ion |  | Cd(II) ion |  | Pb(II) ion |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Parameter | R2 | Parameter | R2 | Parameter | R2 |
| 1 | Langmuir | Linear | qm=32.840 KL=0.2581 | 0.9903 | qm=41.771 KL=0.0469 | 0.9881 | qm=450.450 KL=0.3153 | 0.9911 |
|  |  | Non-linear | qm=32.762 KL=0.2619 | 0.9824 | qm=36.619 KL=0.0561 | 0.9775 | qm=472.245 KL=0.2426 | 0.9785 |
| 2 | Freundlich | Linear | KF=14.420 n=4.860 | 0.940 | KF=4.672 n=2.0820 | 0.9482 | KF=156.070 n=4.233 | 0.9042 |
|  |  | Non-linear | Kfr =14.869 nfr =5.106 | 0.9371 | Kfr =5.372 nfr =2.285 | 0.9389 | Kfr =184.109 nfr =5.181 | 0.9038 |
| 3 | Redlich-Peterson | Linear | αR=0.069 β=0.794 | 0.9957 | αR=0.214 β=0.520 | 0.9775 | αR=0.0064 β=0.764 | 0.9899 |
|  |  | Non-linear | KR=8.583 αR=0.087 β=3.021 | 0.9823 | KR=2.166 αR=0.040 β=1.398 | 0.9775 | KR=114.6 αR=0.0018 β=1.384 | 0.9785 |
| 4 | Temkin | Linear | A=9.407 B=5.142 | 0.9559 | A=0.426 B=9.478 | 0.9722 | A=7.745 B=68.404 | 0.9594 |
|  |  | Non-linear | A=9.407 B=5.141 | 0.9552 | A=0.425 B=9.478 | 0.9720 | A=7.744 B=68.403 | 0.9593 |