Supplementary Information for

Pillar-Pore-Structured Nanophotonic Coating with Superior Solar and Thermal Modulation Abilities

Jin Li,1 Chunhui Zhang,1 Yifei Liu,1 Yunxiang Chen,1 Miaoran Xu,1 Jing Tong,1 Shasha Yi,1 Liying Zhang,1 Zongtao Zhang1, * and Yanfeng Gao1, 2,*

1 School of Materials Science and Engineering, Zhengzhou University, Kexue Ave 100, Zhengzhou 450001, China

2 School of Materials Science and Engineering, Shanghai University, Shangda Rd 99, Shanghai 200444, China

* To whom all correspondence should be addressed. (Z. Zhang) ztzhang@zzu.edu.cn and (Y. Gao) yfgao@shu.edu.cn

Figure S1. (a)TEM image of VO2(M) NCs. (b)HRTEM image of an isolated VO2(M) NC. (c)Scanning electron microscope (SEM) image of the synthesized VO2 nanoparticles. (d)The X-ray diffraction (XRD) patterns of the synthesized VO2 nanoparticles.

Figure S2. (a) SEM image of a cross section of the as-prepared Cr2O3-based STMC. (b) EDS elemental mappings of Cr, O, V and C in a. Scale bars, 25 µm.

Figure S3. (a) SEM image of a cross section of the as-prepared Fe2O3-based STMC. (b) EDS elemental mappings of Fe, O, V and C in a. Scale bars, 25 µm.

Figure S4. (a) IR reflectance spectra of VO2 composite coating with different

WxV1-xO2 (x=0.6%) additions at high temperature (100°C) and low temperature (30°C). (b) Temperature-dependent infrared spectra of VO2 composite coating made with WxV1-xO2 (x=0.6%). (c) IR reflectance spectra of VO2 composite coating after given numbers of heating/cooling cycles. (d) Sky-window emissivity of VO2 composite coating after given number of heating/cooling cycles

Figure S5. (a) Photograph and infrared images of the outdoor experimental. (b) The relationship of the surface apparent temperature and the emissivity of the VO2 composite coating during heating process. (c) The reflectance spectra of the VO2 composite coating deposited. (d) Experimental results of temperature of different surfaces. (e) Experimental results of temperature−time curves of interior of the small house. The insulation foam box containing comparative samples was placed 0.2 m above the ground.

Figure S6. (a) SEM of iron oxide (upper), zinc oxide (middle), chromium oxide (lower) pigments. Scale bars, 1 µm. (b) FTIR transmittance spectra of the selected inorganic pigment particles.

Figure S7. Infrared reflectance spectroscopy experiments of STMC with different colors.

Figure S8. Infrared reflectance spectroscopy experiments of STMC with different colors and W doping content of 0.6%.

Figure S9. (a) Schematic of the experiment examining the surface temperatures of samples on a hot stage. Optical photographs (b) and thermal images (c~d) of the commercial white paint (left) and ZnO based STMC (right) on the same hot stage.

Figure S10. Predicted energy saving for cooling, heating and fans for the modeled building with installation of STMC on walls in 15 cities by EnergyPlus.

Table S1: Thermal emissivity for samples with a varied VO2 concentration measured at 30 °C and 100°C, respectively.

| VO2 concentration | 4% | 6% | 8% | 10% | 12% |
| --- | --- | --- | --- | --- | --- |
| εh | 0.6 | 0.73 | 0.77 | 0.74 | 0.81 |
| εl | 0.27 | 0.24 | 0.24 | 0.19 | 0.3 |
| Δε | 0.33 | 0.49 | 0.53 | 0.55 | 0.51 |

Table S2 Thermal emissivity for samples with a varied VO2 concentration with 0.6% W doping measured at 30 °C and 60°C, respectively.

| VO2 concentration | 2% | 4% | 6% | 8% | 10% |
| --- | --- | --- | --- | --- | --- |
| εh | 0.33 | 0.57 | 0.73 | 0.72 | 0.71 |
| εl | 0.21 | 0.33 | 0.37 | 0.34 | 0.35 |
| Δε | 0.12 | 0.24 | 0.36 | 0.38 | 0.36 |