# Supplementary Data

Synthesis, Characterization and antibacterial study of Ag-loaded TiO2 Electrospun nanofibers: Mechanistic insights of nanofibers interacting with bacteria

Bisma Khanama, Shahzad Anwarb *, Muhammad Zakriab, Taj Muhammad Khanb, A. Rahmanb, Ahmad Adnana, Nida Ali Shanc, Rafaqat Ali Khanb, Muhammad Raffib *

a Department of Chemistry, Government College University (GCU), Lahore, Pakistan

b National Institute of Lasers and Optronics College, Pakistan Institute of Engineering and Applied Sciences, Islamabad 45650, Pakistan

c Center for Omic Sciences, Islamia College University Peshawar KP Pakistan 25120

*Corresponding Authors

Shahzad Anwar

(Shahzadanwar112@yahoo.com)

Muhammad Raffi

(doctormat@gmail.com)

Fig. S1. Photograph of indigenously developed electrospinning setup used in synthesis process

Figure. S2. Brightfield images of bacterial interaction with nanofibers with two different focus point

Table S1. Summary of mean diameter, Ag loading and antibacterial activity (log10 CFU and ZOI) of nanofibers

| Samples | Mean dia. (after calcination) | Composition of Ag in TiO2 matrix (Wt. %) EDX Analysis | Antibacterial efficacy CFU ZOI (mm) |  |
| --- | --- | --- | --- | --- |
| A | 83.06 nm | 0 | 4.35 | 3.17 ± 0.40 |
| B | 70.33 nm | 1.5 | 3.87 | 14.31 ± 0.23 |
| C | 31.87 nm | 3.7 | 3.69 | 15.60 ± 0.34 |
| D | 28.90 nm | 5.1 | 3.60 | 16.09 ± 0.23 |
| E | 25.80 nm | 7.2 | 3.00 | - 0.19 |