Table 1 Chemical compositions of the constituent materials used

| Constituents | Oxides and percentages |
| --- | --- |
|  | Al2O3 CaO Fe2O3 K2O SiO2 MgO Na2O SO3 MnO3 TiO2 |
| Cement 3.91 66.55 3.62 0.39 19.21 1.17 0.40 3.23 - - Periwinkle shell ash 6.42 52.10 4.64 0.25 0.14 0.82 0.26 0.26 0.14 - Quarry dust 15.52 14.30 6.53 4.35 45.4 3.54 - 0.55 - 2.65 |  |

(Kufre Etim et al., 2021; Sathiparan and De Zoysa, 2018; Umoh and Ujene, 2015)

Table 2 Physical properties of the constituents

| Properties | Constituents |
| --- | --- |
|  | OPC Periwinkle shell ash Quarry dust River sand Granite |
| Specific gravity 3.13 2.00 3.21 2.60 2.60 Bulk density (kg/m3) 830 727 2147 1397 2711 Particle size (mm) 5.00 4.50 7.50 6.80 20.00 Fineness modulus (%) 2.5 2.62 2.82 2.50 6.78 Colour greenish-grey white-ash grey pale green grey/white/black |  |

Table 3 Concrete mix designations and constituent percentages

Concrete mix designations Constituent percentages

A (Control) 0% PSA and QD; 100% Cement, Sand and Granite B 5% PSA and QD; 95% Cement, Sand and Granite C 10% PSA and QD; 90% Cement, Sand and Granite D 15% PSA and QD; 85% Cement, Sand and Granite E 20% PSA and Q; 80% Cement, Sand and Granite F 100% PSA, Sand and Granite; 0% QD and Cement G 100% Cement, QD and Granite; 0% PSA and Sand H 100% PSA, QD and Granite; 0% Cement and Sand

Table 4 Amounts of concrete constituents used

| Mix designation | Cement PSA Sand QD | Granite Water | Water/cement ratio |
| --- | --- | --- | --- |
|  | in (kg/m3) |  |  |
| A 6.8970 nil 13.8185 nil 27.6276 4.1382 0.6 B 6.5520 0.3450 13.1276 0.6909 27.6276 4.1382 0.6 C 6.2073 0.6897 12.4367 1.3819 27.6276 4.1382 0.6 D 5.8620 1.0350 11.7455 2.0730 27.6276 4.1382 0.6 E 5.5180 1.3790 11.0548 2.7637 27.6276 4.1382 0.6 F nil 6.8970 13.8185 nil 27.6276 4.1382 0.6 G 6.8970 nil nil 13.8185 27.6276 4.1382 0.6 H nil 6.8970 nil 13.8185 27.6276 4.1382 0.6 |  |  |  |

Table 5 Minerals and associated band groups in PSA

Minerals Wave Number (cm-1) Band Group

Carbon-based 1394 CH and CH2 bendings Vaterite 872 C – O vibrations Vaterite 711 C – O vibrations Bassanite 656 S – O stretching Anhydrite 611 S – O stretching Alite (tricalcium silicate) 533 Si – O stretching

(Fernández-Carrasco et al., 2012; Tararushkin et al., 2020)

Table 6 Minerals and associated band groups in quarry dust

Minerals Wave Number (cm-1) Band Group

Kaolinite 3391 O – H deformation Magnesium and Chlorite 1640 O – H deformation Carbonate 1457 C – H bend Quartz 980 Si – O stretching in plane Quartz and Feldspar 726.8 Si – O asymmetrical bending Quartz and Feldspar 574 Si – O asymmetrical bending

(Coates 2000; Jozanikohan and Abarghooei, 2022)

Table 7 Effect of PSA and QD partial and full replacements on the workability of the concrete

| Concrete Designation | % Partial replacements | Slump (mm) |
| --- | --- | --- |
|  | PSA QD |  |
| A 0 0 66.1 B 5 5 67.0 C 10 10 67.0 D 15 15 68.0 E 20 20 68.2 F 100 0 41.1 G 0 100 79.6 H 100 100 55.9 |  |  |