Supplemental Information

Chemical looping synthesis of amines from N2 via iron nitride as a mediator

Haoyue Li,ab Tie Wang,ab Shifu Wang,d Xuning Li,d Yanqiang Huang,d Ning Yan*abc

* Corresponding author

a Joint School of National University of Singapore and Tianjin University, International Campus of Tianjin University, Binhai New City, Fuzhou 350207, China

b Department of Chemical and Biomolecular Engineering, National University of Singapore, Singapore 117585, Singapore

c Centre for Hydrogen Innovations, National University of Singapore, Singapore 117585, Singapore

d State Key Laboratory of Catalysis, Dalian Institute of Chemical Physics, Chinese Academy of Sciences, Dalian 116023, China

Table of contents

Figure S1. SEM images of (a) fresh FexN and (f) 32 h spent FexN. EDS color mapping images of (b-e) fresh FexN and (g-j) 32 h spent FexN.	4

Figure S2. TEM images and EDS color mapping images of (a-f) fresh FexN and (g-k) 32 h spent FexN.	5

Figure S3. XPS survey spectra of fresh Fe2.5N, 2 h spent Fe2.5N, and 32 h spent Fe2.5N.	6

Figure S4. XPS high-resolution spectra of the (a) Fe 2p and (b) O 1s regions of the fresh Fe2.5N, 2 h spent Fe2.5N, and 32 h spent Fe2.5N.	7

Figure S5. Ar-TPD-MS spectra of fresh Fe2.5N, pure Ar gas was used for Ar-TPD. The outlet gas was connected to the MS for the real-time observation. N2 MS signal: m/z=14.	8

Figure S6. Conversion of isopropanol and the yields of main products using Fe2.5N at 250 ℃ and 10 bar total pressure with 30 mL/min Ar and 30 mL/min H2 flow. IPO bubbling chamber temperature is 25 ℃ (equivalent flow rate: 1.438*10-5 mol/min).	9

Figure S7. Accumulated chemicals amount and conversion of N in Fe2.5N at different temperatures with 5 bar H2 partial pressure.	10

Figure S8. Conversion of isopropanol or acetone to isopropylamine at different temperatures. Accumulated chemicals amount represents the obtained chemicals amount within the first 300 min. Conversion of N in Fe2.5N = (nNfresh-nNspent)/nNfresh. Total flow rate is 60 mL/min, and the total pressure is 10 bar. IPO bubbling chamber temperature is 25 ℃ (equivalent flow rate: 1.438*10-5 mol/min).	11

Figure S9. DRIFTS spectra of adsorbed NH3 at various temperatures over fresh Fe2.5N. Ammonia was injected at 50 ℃, and spectrums were collected under Ar purging flow when increasing temperature to 200 ℃.	12

Figure S10. DRIFTS spectra of isopropanol, isopropylamine and acetone adsorption on fully spent Fe2.5N at Ar atmosphere at 25 ℃.	13

Figure S11. SEM image and EDX mapping images (a-c), TEM image and EDX mapping images (d-f) of N2-nitridated FexN.	14

Table S1. Summary of some existing amination reaction systems.	15

Table S2. C, N, O, and Fe element content of fresh FexN, spent FexN, N2-nitridated FexN, spent N2-nitridated FexN obtained by TEM-EDS mapping and SEM-EDS mapping.	16

Table S3. BET surface area of iron nitrides.	17

Table S4. Fe 2p, N 1s, and O 1s binding energies (eV) and relative peak area obtained by XPS of fresh Fe2.5N, 2 h spent Fe2.5N, and 32 h spent Fe2.5N.	18

Table S5. C, H, N element content obtained by elemental analysis of different particles. The reaction was conducted at 250 ℃.	19

Table S6. Values of the Mössbauer hyperfine parameters, derived from the least-square fitting of the Mössbauer spectra of the fresh Fe2.5N and spent Fe2.5N of 2 h, 5 h, and 32 h.	20

Table S7. IR band assignments for isopropanol absorbed over Fe2.5N.	21

Table S8. N content of N2-nitridated FexN and spent N2-nitridated FexN determined by acid treatment.	22

REFERENCES	23

Figure S1. SEM images of (a) fresh FexN and (f) 32 h spent FexN. EDS color mapping images of (b-e) fresh FexN and (g-j) 32 h spent FexN.

Figure S2. TEM images and EDS color mapping images of (a-f) fresh FexN and (g-k) 32 h spent FexN.

Figure S3. XPS survey spectra of fresh Fe2.5N, 2 h spent Fe2.5N, and 32 h spent Fe2.5N.

Figure S4. XPS high-resolution spectra of the (a) Fe 2p and (b) O 1s regions of the fresh Fe2.5N, 2 h spent Fe2.5N, and 32 h spent Fe2.5N.

Figure S5. Ar-TPD-MS spectra of fresh Fe2.5N, pure Ar gas was used for Ar-TPD. The outlet gas was connected to the MS for the real-time observation. N2 MS signal: m/z=14.

Figure S6. Conversion of isopropanol and the yields of main products using Fe2.5N at 250 ℃ and 10 bar total pressure with 30 mL/min Ar and 30 mL/min H2 flow. IPO bubbling chamber temperature is 25 ℃ (equivalent flow rate: 1.438*10-5 mol/min).

Figure S7. Accumulated chemicals amount and conversion of N in Fe2.5N at different temperatures with 5 bar H2 partial pressure.

Figure S8. Conversion of isopropanol or acetone to isopropylamine at different temperatures. Accumulated chemicals amount represents the obtained chemicals amount within the first 300 min. Conversion of N in Fe2.5N = (nNfresh-nNspent)/nNfresh. Total flow rate is 60 mL/min, and the total pressure is 10 bar. IPO bubbling chamber temperature is 25 ℃ (equivalent flow rate: 1.438*10-5 mol/min).

Figure S9. DRIFTS spectra of adsorbed NH3 at various temperatures over fresh Fe2.5N. Ammonia was injected at 50 ℃, and spectrums were collected under Ar purging flow when increasing temperature to 200 ℃.

Figure S10. DRIFTS spectra of isopropanol, isopropylamine and acetone adsorption on fully spent Fe2.5N at Ar atmosphere at 25 ℃.

Figure S11. SEM image and EDX mapping images (a-c), TEM image and EDX mapping images (d-f) of N2-nitridated FexN.

Table S1. Summary of some existing amination reaction systems.

| Ref | Catalyst | Reaction | T (℃) | Yield (%) | NH3 : substrate | N utilization efficiency (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | Ru/ZrO2 | Glycolaldehyde to ethanolamine | 85 | 94 | 14.7 | 6.4 |
| 2 | Ru/Nb2O5 | Furfural to furfurylamine | 90 | 99 | 16 | 6.2 |
| 3 | Ru/CNT | Lactic acid to alanine | 220 | 62 | 73.5 | 0.8 |
| 4 | Ru/C | Isomannide to monoamine or diamine | 170 | 45 | 11.8 | 3.8 |
| 5 | Ru NPs | 1-Octanol to 1-Octylamine | 180 | 80 | 17 | 4.7 |
| 6 | Ru1Ni7/MgO | Lactic acid to alanine | 220 | 6.2 | 26.5 | 0.2 |
| 7 | Pt/graphite | Butyraldehyde to butylamine | 50 | 83 | 16.5 | 5.0 |
| 8 | Pt/ZrO2 | Trilaurin to dodecylamine | 220 | 59 | 150 | 0.4 |
| 9 | Rh/α- Al2O3 | Butyraldehyde to butylamine | 80 | 66.2 | 11.3 | 5.9 |
| 10 | Rh/Al2O3 | Furfural to furfurylamine | 80 | 91.5 | 33.3 | 2.7 |
| 11 | Pd/C | Dodecanol to dodecylamine | 200 | 96.5 | 64.6 | 1.5 |
| 12 | Au/TiO2 + Cu/SiO2 | Benzyl alcohol to benzylamine | 225 | 95 | 40 | 2.4 |
| 13 | Ag-Co/Al2O3 | 1-Octanol to 1-Octylamine | 200 | 78 | 21 | 3.7 |
| 14 | Co-DABCO-TPA@C | Acetophenone to phenethylamine | 120 | 87 | 121.1 | 0.7 |
| 15 | Ni/Al2O3 | Furfural to furfurylamine | 100 | 92 | 21 | 4.3 |
| 16 | Ni@C/Al2O3 | 5-Hydroxymethylfurfural to 5-Hydroxymethylfurfurylamine | 30 | 96 | 14 | 6.9 |

Table S2. C, N, O, and Fe element content of fresh FexN, spent FexN, N2-nitridated FexN, spent N2-nitridated FexN obtained by TEM-EDS mapping and SEM-EDS mapping.

|  | Particles | C (wt.%) | N (wt.%) | O (wt.%) | Fe (wt.%) |
| --- | --- | --- | --- | --- | --- |
| TEM-mapping | Fresh FexN | 2.99 | 5.94 | 1.19 | 89.88 |
|  | 32 h Spent FexN | 5.98 | -0.23 | 1.72 | 92.53 |
|  | N2-nitridated FexN | 7.30 | 0.11 | 2.02 | 90.58 |
|  | Spent N2-nitridated FexN | 5.36 | -0.31 | 0.96 | 93.99 |
| SEM-mapping | Fresh FexN | 23.44 | 8.21 | 4.34 | 64.01 |
|  | 32 h Spent FexN | 7.31 | 0.09 | 3.72 | 88.89 |
|  | N2-nitridated FexN | 4.43 | 0.53 | 1.76 | 93.27 |
|  | Spent N2-nitridated FexN | 5.57 | -0.12 | 1.33 | 93.22 |

Table S3. BET surface area of iron nitrides.

| Catalyst | BET specific surface area (m2 g-1) |
| --- | --- |
| Fresh FexN | 14 |
| 32 h Spent FexN | 12 |
| 5 h Spent FexN | 11 |

Table S4. Fe 2p, N 1s, and O 1s binding energies (eV) and relative peak area obtained by XPS of fresh Fe2.5N, 2 h spent Fe2.5N, and 32 h spent Fe2.5N.

|  | Fe |  |  | N |  |  | O |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Particles | B.E. (eV) | State | Rel. area (%) | B.E. (eV) | State | Rel. area (%) | B.E. (eV) | State | Rel. area (%) |
| Fresh Fe2.5N | 706.8, 719.8 | FexN/Fe0 | 12.5, 7.5 | 396.7 | Fe-N | 35.6 | 529.7 | Fe-O | 20.7 |
|  | 709.0, 711.3, 723.0, 728.2 | Fe-O/Fe-O-N | 30.5, 13.8, 17.7, 6.9 | 397.6 | Fe-O-N | 27.6 | 530.7 | Fe-O-N | 10.2 |
|  | 716.3, 734.2 | Fe sat. | 3.8, 7.5 | 399.1 | NH3 ad | 36.9 | 532.2 | H2O ad | 69.1 |
| 2 h Spent Fe2.5N | 707.1, 720.0 | FexN/Fe0 | 5.2, 7.0 | 396.7 | Fe-N | 55.8 | 529.8 | Fe-O | 36.2 |
|  | 710.7, 714.1, 724.2, 727.1 | Fe-O/Fe-O-N | 39.2, 10.2, 17.7, 9.7 | 397.8 | Fe-O-N | 23.5 | 531.2 | Fe-O-N | 41.7 |
|  | 717.8, 733.2 | Fe sat. | 3.6, 7.4 | 399.1 | NH3 ad | 20.77 | 532.4 | H2O ad | 22.1 |
| 32 h Spent Fe2.5N | 706.3, 720.4 | FexN/Fe0 | 4.0, 4.6 | --- | --- | --- | 529.6 | Fe-O | 41.4 |
|  | 710.4, 714.8, 723.6, 726.4 | Fe-O/Fe-O-N | 49.0, 6.7, 17.2, 7.9 | --- | --- | --- | 531.0 | Fe-O-N | 39.1 |
|  | 718.5, 732.8 | Fe sat. | 4.9, 5.8 | --- | --- | --- | 532.4 | H2O ad | 19.5 |

Table S5. C, H, N element content obtained by elemental analysis of different particles. The reaction was conducted at 250 ℃.

| Particles | Reaction time (hrs.) | PH2 (bar) | N (wt.%) | H (wt.%) | C (wt.%) |
| --- | --- | --- | --- | --- | --- |
| Fresh Fe2.5N | --- | --- | 9.07 | 0.00 | 0.36 |
| Spent Fe2.5N | 2 | 5 | 1.57 | 0.00 | 0.55 |
| Spent Fe2.5N | 5 | 5 | 0.24 | 0.00 | 0.32 |
| Spent Fe2.5N | 32 | 5 | 0.09 | 0.09 | 0.39 |
| Spent Fe2.5N | 5 | 3 | 0.25 | 0.00 | 0.33 |
| Spent Fe2.5N | 5 | 1 | 0.31 | 0.00 | 0.37 |
| N2-nitridated FexN | --- | --- | 0.10 | 0.00 | 0.00 |
| Spent N2-nitridated FexN | 6 | 10 | 0.00 | 0.00 | 0.00 |

Table S6. Values of the Mössbauer hyperfine parameters, derived from the least-square fitting of the Mössbauer spectra of the fresh Fe2.5N and spent Fe2.5N of 2 h, 5 h, and 32 h.

| sample | δa (mm/s) | Δb (mm/s) | Hc (T) | Line width | Aread (%) | Assignmente |
| --- | --- | --- | --- | --- | --- | --- |
| Fresh Fe2.5N | 0.24 | 0.13 | 20.78 | 0.78 | 26.11 | γ-Fe4N |
|  | 0.40 | 0.27 | -- | 0.62 | 73.89 | ε-Fe2.1N |
| 2 h Spent Fe2.5N | 0.024 | -- | 32.95 | 0.30 | 100 | α-Fe |
| 5 h Spent Fe2.5N | 0.0018 | -- | 33.01 | 0.30 | 100 | α-Fe |
| 32 h Spent Fe2.5N | 0.0028 | -- | 33.03 | 0.33 | 100 | α-Fe |

aδ is the isomer shift.

bΔ is the quadrupole splitting.

cH is the hyperfine magnetic field.

dArea is the relative spectral area of individual spectral components identified during fitting.

eThe spectra were recorded at 298 K.

Table S7. IR band assignments for isopropanol absorbed over Fe2.5N.

| Wavenumber (cm-1) | Assignment | Ref |
| --- | --- | --- |
| 3656 | O-H stretching | 17 |
| 3566, 3553, 3545, 3528, 3524 | Fe-NHx stretching | 18 |
| 2655 | N-H stretching | 19 |
| 1738 | C=O stretching | 20,21 |
| 1651, 1642 | C=N stretching | 22,23 |
| 1246 | C-N stretching | 23,24 |
| 1625, 1593, 1579~1508, 966, 931 | N-H bending | 22,23,25 |

Table S8. N content of N2-nitridated FexN and spent N2-nitridated FexN determined by acid treatment.

| Sample | Sample amount (g) | NH4+ conc. in diluted H2SO4 (mg/L) [a] | N amount (μmol) in 0.5 g sample |
| --- | --- | --- | --- |
| N2-nitridated FexN | 0.50 | 2.46 | 143.58 |
| Spent N2-nitridated FexN | 0.50 | n.d. | n.d. |

[a] H2SO4 adsorption solution was 10 times diluted for IC test, and the volume is 10.5 mL.

REFERENCES

1.	Liang, G. et al. Production of primary amines by reductive amination of biomass-derived aldehydes/ketones. Angew. Chem. Int. Ed. 56, 3050-3054 (2017).

2.	Komanoya, T., Kinemura, T., Kita, Y., Kamata, K. & Hara, M. Electronic effect of Ruthenium nanoparticles on efficient reductive amination of carbonyl compounds. J. Am. Chem. Soc. 139, 11493-11499 (2017).

3.	Deng, W. et al. Catalytic amino acid production from biomass-derived intermediates. Proc. Natl. Acad. Sci. 115, 5093-5098 (2018).

4.	Niemeier, J., Engel, R. V. & Rose, M. Is water a suitable solvent for the catalytic amination of alcohols? Green Chem. 19, 2839-2845 (2017).

5.	Liang, G., Zhou, Y., Zhao, J., Khodakov, A. Y. & Ordomsky, V. V. Structure-sensitive and insensitive reactions in alcohol amination over nonsupported Ru nanoparticles. ACS Catal. 8, 11226-11234 (2018).

6.	Wang, Y. et al. Catalytic production of alanine from waste glycerol. Angew. Chem. Int. Ed. 59, 2289-2293 (2020).

7.	Bódis, J., Lefferts, L., Müller, T. E., Pestman, R. & Lercher, J. A. Activity and selectivity control in reductive amination of butyraldehyde over noble metal catalysts. Catal. Lett. 104, 23-28 (2005).

8.	Jamil, M. A. R. et al. Selective transformations of triglycerides into fatty amines, amides, and nitriles by using heterogeneous catalysis. ChemSusChem 12, 3115-3125 (2019).

9.	Luo, D. et al. Intrinsic mechanism of active metal dependent primary amine selectivity in the reductive amination of carbonyl compounds. J. Catal. 395, 293-301 (2021).

10.	Chatterjee, M., Ishizaka, T. & Kawanami, H. Reductive amination of furfural to furfurylamine using aqueous ammonia solution and molecular hydrogen: an environmentally friendly approach. Green Chem. 18, 487-496 (2016).

11.	Ruiz, D. et al. Direct amination of dodecanol with NH3 over heterogeneous catalysts. Catalyst screening and kinetic modelling. Chem. Eng. J. 307, 739-749 (2017).

12.	Li, M., Pischetola, C., Cárdenas-Lizana, F. & Keane, M. A. Production of benzylamine by tandem dehydrogenation/amination/reduction over Cu and Au catalysts. Appl. Catal., A 590, (2020).

13.	Ibáñez, J., Kusema, B. T., Paul, S. & Pera-Titus, M. Ru and Ag promoted Co/Al2O3 catalysts for the gas-phase amination of aliphatic alcohols with ammonia. Catal. Sci. Technol. 8, 5858-5874 (2018).

14.	Jagadeesh, R. V. et al. MOF-derived cobalt nanoparticles catalyze a general synthesis of amines. Science 358, 326-332 (2017).

15.	Dong, C. et al. Facile and efficient synthesis of primary amines via reductive amination over a Ni/Al2O3 Catalyst. ACS Sustainable Chem. Eng. 9, 7318-7327 (2021).

16.	Hu, Q. et al. Ambient-temperature reductive amination of 5-Hydroxymethylfurfural over Al2O3-supported carbon-doped Nickel catalyst. ChemSusChem 15, e202200192 (2022).

17.	Xu, W., Raftery, D. & Francisco, J. S. Effect of irradiation sources and oxygen concentration on the photocatalytic oxidation of 2-propanol and acetone studied by in situ FTIR. J. Phys. Chem. B 107, 4537-4544 (2003).

18.	Zhao, B. et al. Unveiling the activity origin of iron nitride as catalytic material for efficient hydrogenation of CO2 to C2+ hydrocarbons. Angew Chem Int Ed Engl 60, 4496-4500 (2021).

19.	Brzezinski, B. & Zundel, G. An intramolecular charge relay system via easily polarizable hydrogen bonds in the N-(4-methyl-2-pyridyl)amide of 6-methylpicolinic acid N-oxide. J.Phys.Chem. 83, 1787-1789 (1979).

20.	Araña, J. et al. FTIR study of photocatalytic degradation of 2-propanol in gas phase with different TiO2 catalysts. Appl. Catal. B. 89, 204-213 (2009).

21.	Gu, Q. et al. Photocatalytic reforming of C3-polyols for H2 production: Part II. FTIR study on the adsorption and photocatalytic reforming reaction of 2-propanol on Pt/TiO2. Appl. Catal. B. 106, 689-696 (2011).

22.	Sotowa, K.-I., Amamoto, T., Sobana, A., Kusakabe, K. & Imato, T. Effect of treatment temperature on the amination of chlorinated diamond. Diam. Relat. Mater. 13, 145-150 (2004).

23.	Maiyalagan, T. & Viswanathan, B. Template synthesis and characterization of well-aligned nitrogen containing carbon nanotubes. Mater. Chem. Phys. 93, 291-295 (2005).

24.	Wilfong, W. C., Srikanth, C. S. & Chuang, S. S. In situ ATR and DRIFTS studies of the nature of adsorbed CO2 on tetraethylenepentamine films. ACS Appl. Mater. Interfaces 6, 13617-13626 (2014).

25.	Yang, X. et al. DRIFTS Study of Ammonia Activation over CaO and Sulfated CaO for NO Reduction by NH3. Environ. Sci. Technol. 45, 1147-1151 (2011).