Supplementary Information

Printing of Fine, Continuous, and Soft Fibers in Complex 3D Trajectories via Embedded Solvent Exchange

Wonsik Eom, Mohammad Tanver Hossain, Vidush Parasramka, Jeongmin Kim, Ryan W. Y. Siu, Kate A. Sanders, Dakota Piorkowski, Andrew Lowe, Hyun Gi Koh, Michael F. L. De Volder, Douglas S. Fudge, Randy H. Ewoldt, and Sameh H. Tawfick*

Supplementary Note 1: Concentration Dependency of SEBS polymer in Toluene

The viscosity of the solvent (toluene) and polymer solution up to 3.98wt.% were measured using a microfluidic viscometer m-VROC (RheoSense, Inc.). This microfluidic viscometer requires microliter sample volumes and has access to a wide range of shear rates around two orders of magnitude. The measuring chip is made from borosilicate glass containing a rectangular slit flow channel with a uniform cross-section with width w = 2 mm and height h = 50 μm. The fluid is pushed by a syringe pump at a constant volume flow rate Q, which is related to the apparent shear rate by1 The actual shear rate  is related to  by1

where for Newtonian fluids. The wall shear stress τ is calculated from the pressure drop per unit length using four pressure sensors mounted at the boundary wall in the channel as

where L is the length over which the pressure drop ΔP is measured. Finally, the viscosity is calculated from As the concentration increased, measuring the viscosity with the microfluidic viscometer became problematic due to practical issues (i.e., chip cleaning, loading the sample). The viscosity at higher concentrations of polymer solution (from 5wt.% to 30wt.%) were measured using a rotational rheometer (DHR-3, TA instruments) with 40 mm diameter cone and plate with 0.04 rad cone angle. The viscosity of toluene (Sigma Aldrich, USA, at 25oC) was ηs=550±0.6 µPa.s obtained from m-VROC. To describe the concentration-dependent viscosity, we used the Huggins equation, which is based on the Einstein equation for increase of viscosity with concentration and adds a higher-order term,

where is the intrinsic viscosity and is the Huggins coefficient that quantifies interaction between solute objects. Figure S1a shows the concentration-dependent viscosity of the polymer solution where hollow and filled symbols represent data obtained from the microfluidic viscometer and the rotational rheometer, respectively. We see a good fit for viscosity obtained from the microfluidic viscometer with concentrations using the Huggins equation as shown in Figure S1a. The intrinsic viscosity of the polymer solution is defined in the limit of , while all the measurements are done at finite concentrations. We used an extrapolation method to calculate the intrinsic viscosity by rearranging the Huggins equation as

Where is the reduced viscosity. The reduced viscosity vs concentration is fitted to a linear function and the intrinsic viscosity is evaluated as the intercept at zero concentration as shown in Figure S1b. The critical overlap concentration c* can be obtained from intrinsic viscosity from c*∼1.46η where the numerical factor depends on an assumption of the polymer chain distribution, here assuming non-draining Gaussian coils.2–5 The critical overlap concentration of the polymer solution was found to be c* = 2.89wt.% based on the Huggins equation fit. To check consistency in the measured value of c*, we also used the Kramer equation which relates the inherent viscosity to the intrinsic viscosity as  where  is the inherent viscosity. The critical overlap concentration using the Kramer equation was found to be c* = 2.76wt.% as shown in Figure S1c which is consistent with the value obtained from the Huggins equation. The hydrodynamic radius of the polymer coil can be obtained from intrinsic viscosity using the relation6

where M is the molecular weight of the polymer (M = 0.087 g/mol) and NA is Avogadro’s constant. The hydrodynamic radius of the polymer coil is around Rh = 9 nm which suggests that the polymer length scales are much smaller than the printed fiber diameter using solvent exchange.

Figure S1. (a) Concentration-dependent viscosity of SEBS polymer solution. Viscosity of concentrations up to 3.98wt.% were measured using m-VROC shown by hollow symbols. Viscosity of higher concentrations (> 5wt.%) were measured using DHR-3 rotational rheometer with cone-plate geometry. (b) Intrinsic viscosity inference based on Huggins equation. (c) Intrinsic viscosity inference based on Kramer’s equation.

Supplementary Note 2: Rheological characterization of solid SEBS polymer film

Here we describe the rheological properties of stable SEBS polymer film after solidification via solvent exchange. During the solvent exchange process, SEBS polymer solutions undergo a transition from a viscoelastic liquid to viscoelastic solid. Briefly, we poured SEBS polymer solution into a Petri dish and stored it in air for 4 hours. Then, the petri dish was immersed in an ethanol bath for 12 hours. After the solidified SEBS polymer was dried to evaporate the ethanol in the air for 12 hours, we obtained the solid SEBS film. The thickness of the SEBS film was controlled by changing the initial volume of SEBS solution in the Petri dish. Stable SEBS polymer films of different thickness were prepared and measured on a rotational rheometer. All tests were carried out on an 8 mm diameter parallel plate on a DHR-3 rheometer at 25oC. A linear viscoelastic frequency sweep, and a nonlinear oscillatory amplitude sweep, were carried out at 0.1% strain amplitude and 20 rad/s, respectively. As seen in the frequency sweep data in Figure S2a, we obtained good agreement between the storage modulus and loss modulus at different film thickness prepared from three different batches. The SEBS film shows a linear storage modulus of ~ 0.9 MPa after solidification and linear viscoelastic behavior up to 0.3% strain as shown in the amplitude sweep in Figure S2b. The film behaves as a viscoelastic solid as seen from the frequency sweep down to 0.1 rad/s and (lack of) stress relaxation beyond 100 s (taken at 0.1% strain) (Figure S2).

Figure S2. Rheological charecterization of solid SEBS polymer flim with 8mm parallel plate geometry with DHR-3 rheometer. (a) Frequency sweep at 0.1% strain amplitude. (b) Amplitude sweep at 20 rad/s (c) Stress relaxation at 0.1% strain. All test at 25oC.

Supplementary Note 3: Solidification rate of SEBS polymer solution

We devised an experimental setup to measure the rate of solidification using the rheometer. In this setup, a polymer solution is placed between the rheometer plates and exposed to ethanol from the lateral direction as shown in Figure S3. To achieve consistent ethanol exposure circumferentially on a short timescale, ethanol was dispensed into the upper trough of the top geometry (usually intended for solvent when used with a solvent trap) and made to overflow. This produced a liquid sheet flowing radially outward around the entire geometry as a fountain. The dispensing of ethanol is stopped once it accumulates sufficiently as a pool around the polymer solution.

When ethanol encounters the polymer solution, solvent exchange occurs, leading to the solidification of the polymer. In the rheometer, the solidification process involves the solvent leaving the polymer which forms an outer core within the rheometer geometry, as confirmed visually through a transparent glass bottom plate (Figure S4). We applied a continuous small amplitude oscillatory strain amplitude to the sample before and after ethanol exposure to measure the apparent viscoelastic moduli function of time. We emphasize “apparent” moduli because the rheometer geometries are probing a spatial gradient of material properties in the radial direction, leading to apparent moduli values that integrate across the entire sample. Despite this, through careful analysis, we were able to infer the thickness of the solidified polymer after solvent exchange, as discussed in this section.

Figure S3. Schematic of the ethanol exposure setup. The storage and loss modulus are measured before the ethanol exposure and continued throughout. After ethanol exposure, solvent exchange takes place, and a solidified shell is formed.

3.1. Visualization of solvent exchange after ethanol exposure:

To visualize the solvent exchange after ethanol exposure, we incorporated a custom-made bottom glass setup utilizing the DHR-3 rheometer, and direct visual observations were made through the bottom plate as ethanol was introduced. The configuration is illustrated in Figure S4a. The progression of the diffusion process is depicted in Figure S4b, illustrating varying concentrations of polymer loadings. Notably, a blurred image is evident for the 5wt.% polymer concentration, indicating ongoing diffusion over a broad radial distance. In contrast, the 25wt.% polymer concentration exhibits a restricted region of solidification. We observed consistent behavior for 8mm (Figure S4b) and 40mm parallel plate (inset of Figure S5b). This confirms that the solidification via solvent exchange is concentrated at the outer radius of the rheometer plates and independent of the plate diameter.

Figure S4. (a) Optical view of the SEBS polymer solution with solvent trap using a custom glass made bottom plate. (d) Evaluation of SEBS polymer solution upon ethanol exposure in 8 mm parallel plate.

3.2. Solvent evaporation of SEBS polymer solution:

We measured the solvent evaporation rate of the SEBS/toluene solution after exposure to air. We employed a solvent trap to evaluate polymer solution properties while minimizing toluene evaporation in a 40mm diameter parallel plate geometry (10 rad/s frequency, 0.1% strain amplitude, 1mm gap, 25oC). As depicted in Figure S5a, the storage and loss moduli of distinct polymer solutions remained constant in time with use of a solvent trap. Upon removal of the solvent trap, exposure to air triggered toluene evaporation, resulting in an increase in polymer concentration in the solution, concentrated at the outer radius. The increase in apparent storage and loss moduli, observed after solvent trap removal, was attributed to this toluene evaporation from the polymer solution as illustrated in Figure S5a. As the polymer concentration increases in the solution, it resembles solidification due to solvent evaporation in the electrospinning process,7 where complete solidification occurs upon the departure of all solvent from the solution. After 600 s, the storage and loss modulus reached a steady state, suggesting a lower rate of solvent evaporation or complete solidification at this time. However, the storage modulus of 25wt.% polymer solution reaches only a value of ~104 Pa after 600 s which is two orders of magnitude lower than the modulus reported in Figure S2a for the solid SEBS film. This may be an indication of diffusion-limited transport and a slowing of the solidification process, like encapsulation, spherification, and reverse spherification methods,8 where the solidifying layer reduces diffusive transport thereby slowing the kinetics of solidification. In this case of our confined material between rheometer plates, a complete solidification may not be possible within the time of our experimental setup, as a concentration gradient of the polymer can exist inside the rheometer geometry and can limit the evaporation of the solvent (evidence of which is seen after the removal of the geometry). Nevertheless, we can compare the relative timescale required to reach the apparent steady-state value among different polymer concentrations. A more rapid solidification was anticipated for higher polymer concentrations, since their initial condition is closer to solidification, e.g. as evidenced by the rapid increase of viscosity with concentration in Figure S1a. This trend is indeed observed, e.g. based on the crossover of G' and G'' manifesting at 44 s, 145 s, and 469 s for polymer solutions with concentrations of 25 wt.%, 15 wt.%, and 5 wt.%, respectively, following the removal of the solvent trap. Considering a linear increase in the modulus up to the crossover point, the crossover timescale can be correlated with the polymer solution transitioning from a viscoelastic liquid to a viscoelastic solid and is very important for 3D printing. The development of a solidified layer during filament printing helps to resist capillary forces that would otherwise break the filament into droplets. In the rheometer, solidification primarily occurs in the outer shell of the parallel plate, resembling 3D printing, and leads to a cessation of solvent diffusion as the outer shell solidifies. Conversely, lower polymer concentrations exhibit continued diffusion even after 10 min, implying that these concentrations might not facilitate fiber formation, as capillary forces could disrupt the filament during a slow solidification process.

Figure S5.  (a) solvent evaporation experiment of SEBS polymer solution when exposed to ambient air at 25oC.  (b) Ethanol exposure experiment with 40 mm parallel plate. Inset shows the diffusion process from a view from below through a custom-made glass bottom plate.

3.3. Solvent exchange after ethanol exposure of SEBS polymer solution:

In the actual printing process, the outer ambient medium is an ethanol-based gel rather than air, and this variation accelerates the polymer solidification rate. To study this, we designed an experiment involving the rapid introduction of ethanol to the exposed polymer solution interface. In this novel setup, we introduced ethanol from above with a curtain flow down the rheometer geometry. To evenly distribute the flow, the upper geometry solvent-trap trough (of a 40 mm diameter parallel plate with 1mm gap, 25oC), was gradually filled until deliberate and continuous overflow, creating a curtain flow that descended the geometry and coated the exposed surface of the polymer solution. Even after reaching full capacity, ethanol continued to be supplied, gradually descending, and enveloping the outer region in contact with the polymer solution. Throughout this process, we consistently monitored the storage and loss modulus (10 rad/s frequency, 0.1% strain amplitude), witnessing a distinct transition. The modulus experienced a swift and pronounced increase before stabilizing at a steady value as shown in Figure S5b. In the case of a 25wt.% polymer solution, it attains a steady state, forming a stable outer core without further noticeable mutation. Conversely, for a 15wt.% polymer solution, diffusion persists throughout the observation time, since the concentration is apparently not sufficiently high to impede toluene diffusion, as indicated by the decrease in modulus after reaching its peak value. In the case of a 5wt.% polymer solution, the storage modulus experiences a gradual increase, implying that the material was evolving slowly, e.g. it may not establish a stable structure capable of withstanding capillary breakup during the printing process.

3.4. Thickness of SEBS polymer after solidification:

In this section, we described the assumptions and equations used to calculate the solidification rate and thickness development after exposing the solution to ethanol, based on rheometer measurements. Seeking a more comprehensive understanding of the diffusion process, we narrowed the gap to 100μm to approximate 1D diffusion with an 8mm diameter parallel plate (20 rad/s, 1% strain amplitude, 25oC). Although the precise concentration profile is unknown, our direct visual observations suggest that during the solvent exchange process, there is a highly concentrated polymer outer core region and a lower concentration polymer inner core region. In the rheometer, this spatial gradient leads to 'apparent' moduli values based on the total measured torque. With reasonable assumptions, we can relate the overall apparent moduli to the thickness of the developing outsider solid layer, based on an assumed ratio of the modulus of the outer and inner regions. The total torque is dominated by the outer region, which assists in this inference.

The apparent storage modulus Gapp' is related to the apparent stress σ'0,R,app measured on the transducer, with the strain at the outer radius γ0,R as

where γ0,R is known independent of the rheology and is proportional to the radius for a parallel plate geometry (assuming laminar shear deformation). The apparent stress is calculated from the total torque measured by the rheometer.  For parallel plates, this relation is

where R is the radius of the plate and  is the total apparent torque measured by the instrument which is calculated from

where σ(r) is the radial stress distribution. Equation 8 suggests that the stresses near r=R are the most important contributor to torque. However, now we have two different regions, and the outer core has a higher modulus than the inner core (Figure S6a). For parallel plate geometry, the total torque can be written as a sum of the contributions of two different regions as

where Ri and R are the radius of the inner and outer core, respectively (Figure S6a). If we are in the linear viscoelastic region, the stress is linear with strain and therefore linear with r, and can be written as

where is the stress at r = R and is the stress at r = Ri. Substituting this in eqn. (9) and integrating, we have

,

which can be reduced to

where is the radius ratio. Now, is the apparent stress signal (eqn. 7) obtained from the rheometer which gives . From linear viscoelasticity, the stress is proportional to the modulus G and strain  by , and strain at any r is related to . Thus, eqn. (12) can be written as

.

Or,

where andare the modulus of the inner and outer core, respectively. The outer shell radius as shown in Fig S5a can be obtained from

.

From equation (12), the total torque is dominated by the outer region and from equation (13) the apparent modulus is dominated by the outer core storage modulus even for large . For example, if the inner core storage modulus is negligible, the apparent modulus dominates () the overall measurement when the outer thickness is only 16% of the total radius and decreases with the increasing value of the inner core modulus as shown in Figure S6b.

After exposure to ethanol, a solid layer forms in the outer core of the polymer solution, which exhibits a higher modulus than the inner core. Using the analysis described above to calculate the thickness and rheological properties of both the polymer solution and SEBS in solid form, we can employ eqn. (14) and (15) to observe how  evolves over time. However, the outer core may not be completely solidified (as observed in Figure S4). To account for this, we model a linear increase in the storage modulus from Ri to Ro and from eqn. (9) we obtain

.

At the test frequency of 20 rad/s, the storage modulus of 5, 15 and 25wt.% SEBS are 0.8, 1.67 and 98 Pa, respectively and solid SEBS film has a storage modulus of ~0.9 MPa. Using storage modulus evaluation after ethanol exposure (Figure 3e), we used eqn. to infer the thickness evolution δ(t), which is plotted as a function of time in Figure 3f. The outer shell thickness increases rapidly at short times and eventually reaches a quasi-steady state. Compared to the assumed linear spatial gradient in eqn. , a discontinuous transition between the liquid and solid regions will result in a lower inferred thickness δ at quasi-steady state. For example, if the gradient is discontinuous, then using eqn.  gives an inferred thickness δ = 5.4 μm for 25wt.% SEBS, compared to 11.4 μm with the linear gradient assumption using eqn. (15). Better approximation can be made by considering a linear transition of concentration (rather than modulus) as solvent exchange occurs, however, the viscosity will diverge rapidly (ηsp~c7) as seen in the concentration dependent viscosity measurement in Figure 3a suggesting that the transition is rapid and outer shell will dominate the apparent modulus.

These measurements of δ(t) evolution suggest that during printing there is the possibility of an inner liquid core at short timescales when the printed filament diameter exceeds 11 μm due to the self-limiting nature of solvent exchange. Waiting for a long enough time may eventually lead to a solid filament with no inner liquid core with a smaller diameter.

Figure S6. Inference of solid thickness evolution δ(t) from rotational rheometry. (a) Schematic of the solid outer region δ that develops in the rheometer geometry. (b) Ratio of apparent modulus to outer region modulus as a function of radial fill fraction for different relative contributions of the inner region modulus.

Supplementary Note 4: Yield stress of the gel

The bath medium exhibits a yield stress, and this is supported by the protorheology9 evidence shown in Figure 3g, with the stable pile height confirming that our gel behaves as a yield stress fluid, with yield stress increasing with microgel particle concentration. Taking protorheology one step further, these photos can be quantitatively analyzed to infer the yield stress, using the slump test analysis from Eqn. (52) within Hossain & Ewoldt (2024). At the final stage of the slump, if height h >> radius R of the slump, the overall shape of the sample is minimally affected by the corresponding flow in the yielded region, we have

where σy is the yield stress of the fluid, s is the slump from an initial height h, and ρ is the density. Eqn. (16) can be used for a stable height of the slump with s =0 yields

.

However, for some of cases the height of the slump is smaller than the radius of the slump for a yield stress fluid, so that shear deformation dominates, and the final state can be modeled as a thin sheet spread radially over a surface. We can consider the limiting case of a very thin puddle (left two images of the yield stress fluid in Figure 3g), where one can approximate the volume as where r and h are the radius and height of the slump, respectively. In this case, the yield stress of the material can be approximated using the relation from eqn. (53) within Hossain & Ewoldt (2024),

.

From Figure 3g., the heights of the yield stress gels are 0.2 cm, 0.3 cm, 0.8 cm, 1 cm, and 1.4 cm respectively from left to right. For the two fluids on the left (puddles), we used equation (18) with radius of 1.2 mm of the puddle. For the other images, we used equation (17). Results from protorheology inference are shown in Table S1. The flow sweep curves of different concentrations of Carbopol solution are shown in Figure 3h. We conducted printing within a range of yield stress baths, with dynamic yield stress values ranging from 1.3 Pa to 48.4 Pa.

Protorheology was a very useful method for rapid assessment when formulating different concentrations of ethanol in the bath gel. Our protorheology estimates are compared to the dynamic yield stress from steady simple shear flow in a rotational rheometer are summarized in Table S1. Our protorheology estimates yield values higher than those obtained from the rheometer data, indicating that the difference may be attributed to a comparison with the dynamic yield stress. Yet, this was sufficient quick assessment of bath gel formulations with different ethanol concentrations, where we used protorheology estimation to achieve a desired yield stress.

The bath gel transitions from a viscoelastic solid to viscoelastic liquid at large strain amplitude as shown in the frequency sweep (1% strain) and amplitude sweep (10 rad/s) plots (Figure S7). The frequency sweep and large amplitude oscillatory shear data of the bath with 48 Pa yield stress are shown in Figure S7a and S7b. The bath gel exhibits negligible thixotropic behavior as shown in Figure S7c.

Table S1: Comparison of protorheology estimation eqn. (17) and (18) applied to Figure 3g of dynamic yield stress with rotational rheometer data

|  | Concentration of Carbopol (wt.%) | Dynamic yield stress, (Pa) | Protorheology, (Pa) |
| --- | --- | --- | --- |
| 70% ethanol | 1 | 48 | 73 |
|  | 0.75 | 28 | 55 |
|  | 0.5 | 19 | 42 |
|  | 0.25 | 7 | 12 |
|  | 0.1 | 1 | 5 |

Figure S7. (a) Frequency sweep of σy=48 Pa yield stress bath at 1% strain amplitude with 20 mm diameter parallel plate obtained from ARES-G2 rotational rheometer. (b) Amplitude sweep at 10 rad/s frequency. (c) Thixotropic recovery test of  σy=7 Pa obtained from DHR-3 rotational rheometer with step-down-rate test. Experiments were conducted at 25oC.

Supplementary Note 5: Capillary breakup timescale

In this section, we rationalize how our process can achieve such small diameters by comparing the timescales of capillary breakup versus solidification, and how these depend on the feature size, rheological properties of ink and bath, and the kinetics of solidification of an outer shell.

For the small diameters of our printed filaments, the capillary stress (>46,000 Pa) is much larger than the yield stress of the bath gel. Capillarity will therefore cause filament breakup at a rate set by the largest viscous effect resisting the deformation. This may come from the ink or the bath. We assume that the nominal polymer ink viscosity is most likely to set this breakup time. The polymer ink is only weakly shear thinning with a shear viscosity >45 Pa.s, which is larger than the dramatically shear-thinning bath gel which has a high shear rate viscosity η∞ = 0.3 Pa.s at these large stresses well above the yield stress. The polymer ink extensional viscosity may also be relevant at these large stresses, where the breakup time can be estimated10 from the linear viscoelastic relaxation time τ = 6.4 ms, and assuming an upper-convected Maxwell type model (such as Oldroyd-B or FENE-P), an exponential decay of the diameter is predicted to be , providing a characteristic breakup time of 3τ = 19.2 ms.  We will see that this might only apply for diameters less than 2 μm.

A characteristic capillary velocity can be obtained for a viscous fluid thread as where is the zero-shear viscosity, when viscosity (rather than inertia) sets the time scale, i.e. for Ohnesorge number . We can obtain a characteristic timescale of the breakup depending on the capillary velocity resisted by the shear viscosity from (also known as the visco-capillary breakup timescale). More specifically, the breakup time can be related to the extensional viscosity using the relation

,

where constant X depends on the details of the curvature developed in the filament and ηE is the extensional viscosity which is 3ηs for a Newtonian fluid. The parameter X = 1 for a uniform cylindrical thread (the maximum possible driving stress), whereas X = 0.7127 has been found for Newtonian viscous fluid filaments (there is a smaller driving capillary stress due to axial curvature along the filament, according to the similarity solution of Papageorgiou for visco-capillary breakup1). The Newtonian assumption gives a lower bound estimate of the breakup timescale as

.

The shear rate linked to the breakup can be determined using . Using an interfacial tension of 35 mN/m between toluene and water, a polymer viscosity of 45 Pa.s, and a thread diameter of 2 μm (Oh > 3 × 104), we obtain a lower bound estimate of the capillary breakup timescale as 18.1 ms for a Newtonian viscous thread.11 This analysis is like capillary breakup extensional rheology analysis where the fluid is in a Newtonian medium.

For the filament to not break due to capillary, the time to solidify a sufficiently thick solid SEBS outer core, which we call tδ, must be shorter than the lower bound estimate of the capillary breakup timescale, tcap. It has been shown that if a soft solid with diameter d and shear modulus G is placed in a liquid medium with interfacial tension Γ, the Rayleigh-Plateau instability causes deformation of the filament. This capillarity-driven instability can deform the solid when the diameter is smaller than the length scale Γ/G, known as the elasto-capillary length scale (LEC).12 In our case, we are dealing with elasto-capillary instability of thin-walled tubes which is a much more complicated scenario, as it consists of two liquid interfaces, inner and outer liquids that are non-Newtonian, and two different length scales d and δ (Figure S8). To build foundational insight, we characterized the solidification timescale as the time to solidify a solid outer core to a sufficient thickness δcrit = LEC, based on the solidification rate as

.

From Figure 3f, we obtained solidification rates of 2.33 μm/s and 0.07 μm/s for 25wt.% and 15wt.% SEBS solutions, respectively, by fitting the linear region at short timescales. For 25wt.% SEBS solution, the ratio of the interfacial tension to the storage modulus of the solid SEBS polymer ~ΓG, yields 0.04μm. Thus, 25wt.% SEBS can develop an outer shell of this length scale δ in 16.7 ms.  In Figure 3i, we compare the capillary breakup timescale (increases with increasing diameter) with the solidification timescale (constant line for a particular concentration). The printing window is indicated by diameters that satisfy the criteria tcap>>tδ where the solid shell can resist the capillary breakup. As shown in Figure 3i, for the 15wt.% SEBS solution, the printing window does not exist for diameters 100 μm or less, suggesting the outer shell will not form fast enough to resist capillary breakup. However, in Figure 3i the 25wt.% SEBS solution has an available printing window down to diameters of around 2 μm where tcap ≈ tδ .. This validates why we were able to print 1.5μm filament with the 25wt.% SEBS solution.

Figure S8. (a) Schematic showing the capillary instability criteria for a soft solid. (b) Schematic showing the complexity of our system. We hypothesize that similar instability should show up when thickness is less than a critical thickness which is related to the elasto-capillary length scale.

Supplementary Note 6: Empirical ternary phase diagrams for ethanol, water, and toluene and SEBS, toluene, and mixture of ethanol-water

As our 3DPX conducted in the ethanol containing hydrogel, we studied the phase transition of SEBS, toluene, and mixture of ethanol-water, instead of ethanol.

Figure S9. (a) Ternary phase diagrams for ethanol, water, and toluene. (b) Ternary phase diagram for SEBS (polymer), toluene (solvent), and the mixture of ethanol-water (non-solvent).

Supplementary Note 7: In situ observation of extrusion behavior of ink polymer in gel using an optical microscope

The extrusion behavior of ink polymer in the support gel was investigated by taking a video using an optical microscope. We set up the nozzle and linear stage under the optical microscope and observe the appearance and deformation of printed filaments at the micro-scale.

Figure S10. (a) Illustration showing the setup for observing the extrusion behavior in the ethanol-based gel. (b) Optical microscopic image of embedded 3D printing depending on printing speed of 0.3 and 0.5 mm/s. (c) Illustration showing the definition of Δp, defined as the area between the designed and printed trajectories divided by the edge length squared.

Supplementary Note 8: Diameter of printed filaments

The diameter of printed filaments of SEBS, SIS, TPU, PS, and PVC was measured by scanning electron microscope. To take the images of filament, the samples were taken out from the support gel and washed with water. After drying the sample in a vacuum oven, we obtained the filament sample.

Figure S11. SEM image showing the diameter of the printed filament made of (a) SEBS, (b) SIS, (c) TPU, (d) PS, and (e) PVC.

Supplementary Note 9: Hair sweeping test

To demonstrate the softness of our hair array, we sweep the SEBS hair array with a metal wire having a diameter of 50 µm. During the sweeping, while the metal wire does not visibly bend, the SEBS hairs were gently bent by the wire and restored to their original position. This shows the softness and flexibility of SEBS hair.

Figure S12. (a) Illustration of the hair sweeping test setup; (b) captured hair sweeping images over time.

Supplementary Note 10: Comparison with reported minimum feature diameter

We compared the minimum feature diameter of our filament with the records from previous references.

Table S2. Comparison to previously reported minimum feature diameter with Embedded 3D printing, as shown in Figure 4c.

|  | Materials | Gel | Feature diameter (µm) | References |
| --- | --- | --- | --- | --- |
| R1 | Alginate | Pluronic F 127-CaCl2 | 50 | M. Rocca et al., SLAS Technology, 23, 154-163 (2018) |
| R2 | GelMA | Carbopol | 200 | L. Ning et al., ACS Appl. Mater. Interfaces, 12, 44563 (2020) |
| R3 | GelMA | Pluronic F-127 - hydrophobically modified hydroxypropyl methyl cellulose | 44 | Q. Li et al., ACS Appl. Mater. Interfaces, 14, 41695 (2022) |
| R4 | PVA and other polymers | Carbopol microgels | 100 | T. Bhattacharjee et al., Sci. Adv., 1, e1500655 (2015) |
| R5 | PVA | Pemulen TR-2NF microgel | 20 | C. S. O’Bryan et al., Bioprinting, 11, e00037 (2018) |
| R6 | Fugitive Pluronic F127 | Pluronic F-127-DA | 18 | W. Wu et al., Adv. Mater., 23, H178 (2011) |
| R7 | Collagen | Gelatin microgels | 20 | A. Lee et al., Science, 365, 482 (2019) |
| R8 | Pepsinized collagen-based hydrogel collagen | Calcium-alginate nanoparticles and xanthan gum | 10 | A. Shapira et al., Biomed. Mater., 15, 045018 (2020) |
| R9 | Silicone elastomer | SEP and SEBS block copolymer micro-organogel | 80 | C. S. O’Bryan et al., Sci. Adv., 3, e1602800 (2017) |
| R10 | Silicone elastomer (PDMS based, Gelest ExSil-100) | Water-in-oil emulsion | 8 | S. Duraivel et al., Science, 379, 1248 (2023) |
| This work | SIS in Toluene | Ethanol-based hydrogel | 2.0 |  |
|  | SEBS in Toluene | Ethanol-based hydrogel | 1.5 |  |
|  | TPU in DMF | Ethanol-based hydrogel | 3.8 |  |
|  | PS in THF | Ethanol-based hydrogel | 1.6 |  |
|  | PVC in THF | Ethanol-based hydrogel | 1.8 |  |

Supplementary Note 11: Setup of high-precision 3D printer

The custom-built high-precision 3D printer has two major subassemblies: the motion system and the dispensing system (shown in Figure S12). Precision motion stages from Physik Instrumente (PI, Germany) were used to build a custom 3-axis motion system. The system has translational freedom of motion in X, Y, and Z. To print micro-scale features, it is important to have high precision stages with small step sizes and high encoder resolution. The system was also built to be extremely rigid using Nexus breadboards and 1.5” optical posts. The mounting plates and adapters were custom designed. The entire printer is mounted on a granite slab (Standridge Granite Corp.) which is stabilized using a table stable vibration isolator system (AVI-350S/LP, HERZAN). The active vibration isolator helps remove any external vibration that would cause a print to fail.

Figure S13. 3D model of the designed printer setup

The X and Y axis stages are V-508 direct drive linear motion stages with a travel range of 80 mm. The Z-axis stage is a V-308 voice coil direct drive with a travel range of 7 mm. The printer has a build volume of 44,800 mm.13 The larger travel range in X and Y axes can allow the repeating printing process of a hair array to scale manufacturing. Table S3 shows the specifications of each motion stage. All the stages are driven using the G-901 ACS motion controller (shown in Figure S14) from PI. The motion controller uses the ACS SPiiPlus software to tune and program the stages. The programming software directly read g-codes that are generated using MATLAB.

Table S3. Motion stage specifications

| Axis | Travel range (mm) | Max Velocity (mm/sec) | Minimum step size (nm) | Sensor resolution (nm) |
| --- | --- | --- | --- | --- |
| x, y | 80 | 600 | 1 | 0.2 |
| z | 7 | 200 | 10 | 1 |

Figure S14. G-901 ACS motion controller

For the dispensing system, the Ultimus V pneumatic dispenser and the HP3cc dispensing tool from Nordson are used (shown in Figure S15). The dispenser has a pressure range of 0-100 psi. The pneumatic piston pushes on the ink to precisely extrude at the required extrusion rate. The dispenser is also actuated by the G-901 controller. The motion controller sends an analog output to an Arduino Uno R3 microcontroller which controls a relay switch. The relay switch is used to actuate the dispenser. This allows for precise extrusion as required by the motion program.

Figure S15. Nordson Ultimus V and HP3cc dispensing system

Pre-pulled glass micropipettes from WPI are used as extrusion nozzles. The nozzles have an inner diameter ranging from 0.1 – 30 μm. Through testing, the smallest inner diameter nozzle which could be used with our printer was 5 μm. This is a physical limitation of our pneumatic dispensing system and polymer ink.

Supplementary Note 12: Determination of ternary phase diagram

Simple titration was used to obtain the ternary phase diagram of polymer/solvent/non-solvent systems. Titration is a relatively quick and commonly used technique for the determination of the cloud point curve.2 First, 5, 15, 25 wt.% SEBS solution was prepared by dissolving in toluene. Then, 6 g of SEBS solution is placed in a glass vial at ambient temperature. After that, a small amount of ethanol or water/ethanol mixture was added dropwise to the mechanically stirred polymer solution by using a 0.1 ml syringe until turbidity was visually observed. The cloud point was allocated when the turbidity of the solution remained for 30 min. It should be mentioned that when the solution is opaque, it separates into two phases, and liquid-liquid demixing is induced. The composition of the components can be calculated by the total amount of SEBS, toluene, and non-solvent present. The drifting down of 5, 15, and 25 wt.% SEBS solution curves in Figure 2a results from the experimental method. We prepared several vials containing the same amount of SEBS/toluene solution. Then we added different amounts of ethanol in each vial. As the amount of ethanol increased, the amount of SEBS was the same, but the ratio gradually decreased.

Supplementary Note 13: Experimental Section

Materials: Styrene-ethylene-butylene-styrene (SEBS; styrene 30 wt.%; G1650, Molecular weight = 9.8 × 104 g/mol; Density = 0.89 g/cm3) copolymer and Styrene Ethylene Propylene Styrene (SEPS; styrene 28 wt.%; G1702, Molecular weight = 1.7 × 105 g/mol; Density = 0.88 – 0.95 g/cm3) copolymer was provided by Kraton™ (USA). Thermoplastic polyurethane (TPU; Elastollan® 1185A, Molecular weight = 108.5 kDa; Density = 1.12 g/cm3) was purchased by BASF (Germany). Polystyrene-block-polyisoprene-block-polystyrene (SIS; styrene 22wt.%; Density = 0.93 g/cm3, catalog #432415) copolymer, polystyrene (PS; molecular weight 3.5 × 103 g/mol; Density = 1.06 g/cm3), polyvinyl chloride (PVC; high molecular weight; Density = 1.40 g/cm3), Toluene (ACS grade; Density = 0.86 g/cm3), Dimethylformamide (DMF; ACS reagent; Density = 0.94 g/cm3), and tetrahydrofuran (THF; GC grade; Density = 0.89 g/cm3) were purchased from Sigma-Aldrich (USA). NC7000 multi-walled carbon nanotubes (MWNTs) with an average diameter of 9.5 nm and length of 1.5 μm were supplied from Nanocyl. Triethanolamine (≥99.0% (GC)) was purchased from Sigma-Aldrich (USA). Carbopol® Ultrez 10 was purchased from Lubrizol Corp. (USA). Ethanol (Anhydrous; USP grade) was purchased from Decon Labs (USA). Distilled water (ASTM Type II) purchased from Aqua Solutions (USA). All chemicals were used as received without further purification.

Characterization: To observe the extrusion behavior of polymer ink through the glass nozzle in a support gel, a customized setup was installed under the optical microscope (Zeiss). The customized setup consisted of a linear stage, 3 axis stage, and a dispenser (Ultimus V; Nordson). The images of printed filaments in Figure 4 were taken by using a confocal microscope (VK-X1000; Keyence). The rheological properties of polymer inks and gels were analyzed by using rotational rheometers (DHR-3 and ARES-G2; TA Instruments). The images of printed filament samples were obtained by using a scanning electron microscope (SEM; Axia ChemiSEM) at a voltage of 20 kV and a pressure of 50 Pa without platinum sputtering.

Analysis of the toluene concentration of supernatant in the phase-separated solution: The toluene concentration of supernatant in the mixed solution was analyzed by using high-performance liquid chromatography (HPLC). A supernatant of the phase-separated solution which is a mixture of SEBS, toluene, and ethanol was diluted 1000 times in acetonitrile. Toluene was measured using a Shimadzu HPLC-20 series (Shimadzu, Japan) equipped with a photodiode array detector (SPD-M20A, Shimadzu, Japan). The supernatant was injected into HPLC and separated using a Chromolith® Performance DIOL (100 × 4.6 mm, suitable for USP L20) at 23 ℃. A dual mobile phase condition with 80% of mobile phase A: acetonitrile, B: 5mM Ammonium acetate buffer (pH=6.8), was adopted at a flow rate of 0.5 mL/min for 10 minutes. For the standard curve, toluene was diluted to 0.05 g/L, 0.1 g/L, 0.5 g/L, 1g/L, 4 g/L, and 8 g/L in acetonitrile media. All the chemicals were purchased from Millipore Sigma. The toluene concentration in SEBS is presented in the unit of g/mL instead of wt.% due to the unknown density of the sediment.

References

1.	Macosko, C. W. Rheology: Principles, Measurements, and Applications. (VCH, 1994).

2.	Graessley, W. W. Polymer chain dimensions and the dependence of viscoelastic properties on concentration, molecular weight and solvent power. Polymer (Guildf) 21, 258–262 (1980).

3.	Harrison, G. M., Remmelgas, J. & Leal, L. G. The dynamics of ultradilute polymer solutions in transient flow: Comparison of dumbbell-based theory and experiment. J Rheol (N Y N Y) 42, 1039–1058 (1998).

4.	Vadillo, D. C., Mathues, W. & Clasen, C. Microsecond relaxation processes in shear and extensional flows of weakly elastic polymer solutions. Rheol Acta 51, 755–769 (2012).

5.	Rodrigues, T., Galindo-Rosales, F. J. & Campo-Deaño, L. Critical overlap concentration and intrinsic viscosity data of xanthan gum aqueous solutions in dimethyl sulfoxide. Data Brief 33, 106431 (2020).

6.	Armstrong, J. K., Wenby, R. B., Meiselman, H. J. & Fisher, T. C. The Hydrodynamic Radii of Macromolecules and Their Effect on Red Blood Cell Aggregation. Biophys J 87, 4259–4270 (2004).

7.	Xue, J., Wu, T., Dai, Y. & Xia, Y. Electrospinning and electrospun nanofibers: Methods, materials, and applications. Chem Rev 119, 5298–5415 (2019).

8.	Tsai, F.-H., Chiang, P.-Y., Kitamura, Y., Kokawa, M. & Islam, M. Z. Producing liquid-core hydrogel beads by reverse spherification: Effect of secondary gelation on physical properties and release characteristics. Food Hydrocoll 62, 140–148 (2017).

9.	Hossain, M. T. & Ewoldt, R. H. Protorheologya). J Rheol (N Y N Y) 68, 113–144 (2024).

10.	Anna, S. L. & McKinley, G. H. Elasto-capillary thinning and breakup of model elastic liquids. J Rheol (N Y N Y) 45, 115–138 (2001).

11.	Toor, A., Helms, B. A. & Russell, T. P. Effect of nanoparticle surfactants on the breakup of free-falling water jets during continuous processing of reconfigurable structured liquid droplets. Nano Lett 17, 3119–3125 (2017).

12.	Mora, S., Phou, T., Fromental, J.-M., Pismen, L. M. & Pomeau, Y. Capillarity Driven Instability of a Soft Solid. Phys Rev Lett 105, 214301 (2010).

13.	Boom, R. M., Van den Boomgaard, T. & Smolders, C. A. Equilibrium thermodynamics of a quaternary membrane-forming system with two polymers. 1. Calculations. Macromolecules 27, 2034–2040 (1994).