Supporting Information

Improving photophysical properties and hydrophily of conjugated polymers simultaneously by side-chain modification for near-infrared cell imaging

Min Zhou, Fenglei Wang, Yongdong Jin, Shanyong Chen * and Chuanqin Xia *

College of Chemistry, Sichuan University, Chengdu 610064, P.R. China.

* Corresponding Authors

* E-mail address: Chuanqin Xia：xiachqin@163.com

Shanyong Chen: chensy@scu.edu.cn

Instrumentation

Fourier transform infrared (FT-IR) spectra were recorded on a Nicolet 670 FT-IR spectrophotometer (Thermo Nicolet, USA). Scanning electron microscopy (SEM) was performed using an S-4800 field-emission scanning electron microscopy at 5-18 kV accelerating voltage (FE-SEM, Hitachi, Japan). Transmission electron microscope (TEM) was performed using JEM-F200. The 1H NMR (400 MHz) and was recorded on a Bruker AV III 400 MHz spectrometer with DMSO‑d6 as the solvent and tetramethylsilane (TMS) as an internal reference. The sizes of the Nano-conjugated polymers were measured by a DLS instrument (Malvern Instruments Ltd, Southborough, MA). UV-vis absorption spectra were collected using a JASCO V650. The MCF-7 cell was incubated at CO2 thermostatic training box (WIGGENSWCI-180, China). The CCK-8 cell viability experiment was performed on an ultra-clean bench (SW-CJ-2FD, China). Near-infrared cell imaging is taken by laser confocal microscopy (Olympus, FV1000).

Calculation

All calculations were performed on Gaussian 09 package. Optimized geometric structures were calculated at B3LYP/6-311G (d, p) level based on one repeating-unit. The HOMO–LUMO distribution were calculated on multifunctional wavefunction software Multiwfn 3.61.

Calculation of the photothermal conversion efficiency

The photothermal conversion efficiencies were calculated as the methods reported in the literature2. Typically, 1.0 mL of pTOB aqueous solution (150 µg mL-1) was irradiated with an 808 nm laser continually, until the temperature elevation reached a steady state, and then naturally cooling down to the ambient temperature. The temperature was measured every 60 s with an IR thermal imaging camera (E6-XT, FLIR). The water was used as a control. The photothermal conversion efficiency (PCE) was calculated according to the following Equation (1):

PCE=hATmax-Tsurr-QdisI(1-10-A808)      (1)

where h is the heat transfer coefficient, A is the superficial area of the container, Tmax and Tsurr are the maximum temperature reached and ambient temperature, respectively, Qdis represents heat dissipated from the laser mediated by the solvent and container. The value of hA was derived from Equation (2):

hA=mDcDτ       (2)

where mD and cD are the mass and heat capacity of water (cD = 4.2 J g-1 C-1), and τ is the time constant for heat transfer of the system determined by Equation (3):

τ=-tlnθ         (3)

where the t is time and θ is the dimensionless driving force of the temperature fall period. The value of θ was derived from Equation (4):

θ=-Tsurr-TTsurr-Tmax   (4)

Qdis is the heat dissipation from the light absorbed by the solvent and was calculated according to Equation (5):

Qdis=mDmc(Tmax,water-Tsurr)τwater   (5)

Where τwater and Tmax,water  were determined to be 307.9 and 31.4 °C,  respectively.

Scheme 1. Synthetic route of pTB, pTRB, pTOB.

Figure S1 1H NMR of TTBA

Figure S2 Solid- state 13C-NMR spectra of pTRB, pTB and pTOB.

Figure S3 picture of pTRB, pTB and pTOB scattered in water.

Figure S4 UV−vis DR spectra of pTRB, pTB and pTOB, inset: Tauc plot and the

corresponding band gap.

References

1.T. Lu and F. Chen, Journal of Computational Chemistry, 2011, 33, 580-592.

2.M. Su, Q. Han, X. Yan, Y. Liu, P. Luo, W. Zhai, Q. Zhang, L. Li and C. Li, ACS Nano, 2021, 15, 5032-5042.