Synthesis of supramolecular complex based on β-cyclodextrin and melamine

To synthesise β-CD/ME supramolecular complex, 1702.5 mg of β-CD (99%, Yuwi Jinchi Cosmetics Co Ltd. China.) was dissolved in 100 ml of distilled water. Also, 189 mg of ME was dissolved in 100 ml of distilled water. Both solutions were mixed separately for 30 min, then stirred (72 °C, 900 r/min) for 3 hours. The resulting supramolecular product was then precipitated at 0 °C for 24 hours. The resulting product was filtered and dried at 87 °C (5 hours). For purification, the product was dissolved in distilled water and the resulting solution was recrystallised by cooling in a refrigerator at a temperature of 0 oC. The above recrystallisation process was repeated 3 times. As a result, 1380.8 mg (73%) of targetted product was formed. The resulting solid state product was named β-CD/ME supramolecular complex. The reaction schema for the synthesis of a supramolecular complex based on β-cyclodextrin and melamine is written as follows (Schema 1):

Schema 1S. Reaction procedure of β-CD/ME supramolecular complex.

Figure 1S. Raman spectroscopy of β-CD.

Figure 2S. Raman spectroscopy of ME.

Figure 3S. Raman spectroscopy of β-CD/ME.

Figure 4S. IQ of β-CD.

Figure 5S. IQ of ME.

Figure 6S. IQ of β-CD/ME.

Figure 7S. 1H NMR of β-CD.

Figure 8S. 1H NMR of β-CD/ME.

Table 1S. TG results of β-SD.

| № | Temperature, oC | Mass loss, % | Rate in mass loss, mg/min | DTA, uV |
| --- | --- | --- | --- | --- |
| 1 | 37 | - | - | -5.238 |
| 2 | 80 | 1.0843 | 0.0741 | -8.654 |
| 3 | 90 | 1.3253 | 0.2376 | -7.81 |
| 4 | 100 | 2.8112 | 1.5867 | -12.032 |
| 5 | 110 | 4.8193 | 1.0684 | -17.062 |
| 6 | 120 | 7.3092 | 1.3196 | -20.652 |
| 7 | 130 | 10.2811 | 1.6062 | -19.42 |
| 8 | 140 | 11.4458 | 0.6473 | -12.882 |
| 9 | 150 | 12.0482 | 0.4100 | -2.714 |
| 10 | 160 | 12.0482 | 0.0000 | 2.728 |
| 11 | 170 | 12.1687 | 0.0681 | 4.418 |
| 12 | 180 | 12.4498 | 0.1731 | 4.724 |
| 13 | 190 | 12.4498 | 0.0000 | 4.692 |
| 14 | 200 | 12.4498 | 0.0000 | 4.686 |
| 15 | 210 | 12.4498 | 0.0000 | 4.582 |
| 16 | 220 | 12.4498 | 0.0000 | 4.37 |
| 17 | 230 | 12.4498 | 0.0000 | 4.692 |
| 18 | 240 | 12.4498 | 0.0000 | 4.864 |
| 19 | 250 | 12.4498 | 0.0000 | 4.934 |
| 20 | 260 | 12.4498 | 0.0000 | 4.98 |
| 21 | 270 | 12.4498 | 0.0000 | 4.967999 |
| 22 | 280 | 12.4498 | 0.0000 | 5.16 |
| 23 | 290 | 12.4498 | 0.0000 | 5.3 |
| 24 | 300 | 12.8514 | 0.2187 | 5.176 |
| 25 | 310 | 12.8514 | 0.0000 | 4.604 |
| 26 | 320 | 13.7349 | 0.4667 | 3.474 |
| 27 | 330 | 14.5783 | 0.4650 | 6.9 |
| 28 | 340 | 22.7309 | 4.6893 | 13.298 |
| 29 | 350 | 34.2972 | 6.3955 | 14.748 |
| 30 | 360 | 48.1526 | 7.7011 | 17.096 |
| 31 | 370 | 62.0482 | 7.6258 | 18.504 |
| 32 | 380 | 72.4900 | 5.4313 | 20.206 |
| 33 | 390 | 79.0763 | 3.4655 | 21.434 |
| 34 | 400 | 81.9277 | 1.4945 | 24.194 |
| 35 | 410 | 82.9317 | 0.5289 | 24.65 |
| 36 | 420 | 83.9357 | 0.5147 | 22.838 |
| 37 | 430 | 85.1406 | 0.6044 | 21.34 |
| 38 | 440 | 85.5422 | 0.2112 | 20.5 |
| 39 | 450 | 85.9438 | 0.2016 | 19.562 |
| 40 | 460 | 86.3454 | 0.1993 | 18.676 |
| 41 | 470 | 87.1486 | 0.4002 | 18.164 |
| 42 | 480 | 87.7912 | 0.3344 | 17.834 |
| 43 | 490 | 88.3534 | 0.2895 | 17.53 |
| 44 | 500 | 88.7550 | 0.2105 | 17.234 |

Table 1S (continue). TG results of ME.

| № | Temperature, oC | Mass loss, % | Rate in mass loss, mg/min | DTA, uV |
| --- | --- | --- | --- | --- |
| 1 | 35.4 | - | - | 0.82 |
| 2 | 80 | 0.0000 | 0.0000 | 7.916 |
| 3 | 90 | 0.0000 | 0.0000 | 7.99 |
| 4 | 100 | 0.0000 | 0.0000 | 8.008 |
| 5 | 110 | 0.0000 | 0.0000 | 7.902 |
| 6 | 120 | 0.4717 | 0.2306 | 7.682 |
| 7 | 130 | 0.4717 | 0.0000 | 7.076 |
| 8 | 140 | 0.4717 | 0.0000 | 6.568 |
| 9 | 150 | 0.4717 | 0.0000 | 5.952 |
| 10 | 160 | 0.8491 | 0.1896 | 5.43 |
| 11 | 170 | 0.9434 | 0.0470 | 4.878 |
| 12 | 180 | 0.9434 | 0.0000 | 4.318 |
| 13 | 190 | 0.9434 | 0.0000 | 3.774 |
| 14 | 200 | 1.0849 | 0.0682 | 3.184 |
| 15 | 210 | 1.4151 | 0.1588 | 2.548 |
| 16 | 220 | 1.4151 | 0.0000 | 1.942 |
| 17 | 230 | 1.8868 | 0.2118 | 1.452 |
| 18 | 240 | 2.0283 | 0.0704 | 0.83 |
| 19 | 250 | 2.3585 | 0.1542 | 0.176 |
| 20 | 260 | 2.8302 | 0.2198 | -0.432 |
| 21 | 270 | 2.8302 | 0.0000 | -1.182 |
| 22 | 280 | 3.6321 | 0.3688 | -2.064 |
| 23 | 290 | 4.2453 | 0.2772 | -4.818 |
| 24 | 300 | 5.7547 | 0.6685 | -6.342 |
| 25 | 310 | 7.2642 | 0.6762 | -8.2079 |
| 26 | 320 | 10.1887 | 1.2952 | -10.558 |
| 27 | 330 | 14.1038 | 1.6722 | -14.822 |
| 28 | 340 | 19.2453 | 2.2527 | -18.114 |
| 29 | 350 | 26.6981 | 3.1388 | -22.314 |
| 30 | 360 | 36.3679 | 4.0392 | -24.75 |
| 31 | 370 | 48.6792 | 4.8096 | -26.02 |
| 32 | 380 | 62.3113 | 4.8963 | -27.02 |
| 33 | 390 | 84.4340 | 8.2774 | -25.838 |
| 34 | 400 | 90.7075 | 3.9075 | -17.836 |
| 35 | 410 | 92.9245 | 1.1783 | -12.422 |
| 36 | 420 | 93.3962 | 0.2349 | -13.792 |
| 37 | 430 | 93.8679 | 0.2121 | -15.408 |
| 38 | 440 | 94.3396 | 0.2049 | -16.84 |
| 39 | 450 | 94.8113 | 0.1986 | -17.834 |
| 40 | 460 | 94.8113 | 0.0000 | -18.638 |
| 41 | 470 | 95.2830 | 0.2028 | -19.54 |
| 42 | 480 | 95.3774 | 0.0398 | -20.39 |
| 43 | 490 | 95.7547 | 0.1618 | -21.152 |
| 44 | 500 | 96.2264 | 0.2044 | -21.724 |

Table 1S (continue). TG results of mechanical mixture (β-CD +ME).

| № | Temperature, oC | Mass loss, % | Rate in mass loss, mg/min | DTA, uV |
| --- | --- | --- | --- | --- |
| 1 | 35,4 | - | - | -0.296 |
| 2 | 80 | 0.0433 | 0.0031 | -5.354 |
| 3 | 90 | 1.3853 | 0.6709 | -8.368 |
| 4 | 100 | 3.1602 | 0.8410 | -12.57 |
| 5 | 110 | 5.2381 | 1.0886 | -16.63 |
| 6 | 120 | 8.0952 | 1.3284 | -19.866 |
| 7 | 130 | 9.9567 | 0.9892 | -16.702 |
| 8 | 140 | 10.7792 | 0.4690 | -9.31 |
| 9 | 150 | 11.2554 | 0.2685 | -2.786 |
| 10 | 160 | 11.2554 | 0.0000 | -0.268 |
| 11 | 170 | 11.2554 | 0.0000 | 0.08 |
| 12 | 180 | 11.2554 | 0.0000 | -0.16 |
| 13 | 190 | 11.6883 | 0.2317 | -0.56 |
| 14 | 200 | 11.6883 | 0.0000 | -0.914 |
| 15 | 210 | 12.1212 | 0.2297 | -1.294 |
| 16 | 220 | 12.1212 | 0.0000 | -1.8 |
| 17 | 230 | 12.5541 | 0.2218 | -2.182 |
| 18 | 240 | 12.5541 | 0.0000 | -2.058 |
| 19 | 250 | 12.5541 | 0.0000 | -2.168 |
| 20 | 260 | 12.9437 | 0.1997 | -2.626 |
| 21 | 270 | 12.9870 | 0.0217 | -3.17 |
| 22 | 280 | 13.5498 | 0.2857 | -3.662 |
| 23 | 290 | 14.2857 | 0.3685 | -3.994 |
| 24 | 300 | 15.6710 | 0.6830 | -3.332 |
| 25 | 310 | 17.7056 | 1.0365 | -0.326 |
| 26 | 320 | 19.4805 | 0.9437 | 5.401999 |
| 27 | 330 | 23.3766 | 2.0827 | 8.74 |
| 28 | 340 | 40.1732 | 8.6255 | 14.258 |
| 29 | 350 | 62.3377 | 11.8122 | 24.602 |
| 30 | 360 | 68.5281 | 3.8220 | 48.196 |
| 31 | 370 | 71.4286 | 1.6176 | 50.518 |
| 32 | 380 | 72.9004 | 0.7057 | 43.622 |
| 33 | 390 | 74.0260 | 0.5066 | 36.332 |
| 34 | 400 | 75.2814 | 0.5682 | 30.152 |
| 35 | 410 | 76.1905 | 0.4112 | 24.886 |
| 36 | 420 | 77.0563 | 0.3893 | 20.328 |
| 37 | 430 | 78.3550 | 0.5944 | 16.734 |
| 38 | 440 | 78.7879 | 0.1997 | 13.746 |
| 39 | 450 | 79.6537 | 0.3977 | 11.412 |
| 40 | 460 | 80.5195 | 0.4025 | 9.746 |
| 41 | 470 | 81.6450 | 0.5327 | 8.598 |
| 42 | 480 | 82.7273 | 0.5021 | 7.736 |
| 43 | 490 | 83.9827 | 0.5895 | 7.086 |
| 44 | 500 | 85.2814 | 0.6098 | 6.686 |

Table 1S (continue). TG results of β-CD/ME complex.

| № | Temperature, oC | Mass loss, % | Rate in mass loss, mg/min | DTA, uV |
| --- | --- | --- | --- | --- |
| 1 | 26,1 | - | - | 2.52 |
| 2 | 80 | 2.9839 | 0.0977 | 3.342 |
| 3 | 90 | 5.4839 | 0.6624 | 2.798 |
| 4 | 100 | 7.6613 | 0.5769 | 1.69 |
| 5 | 110 | 10.7258 | 0.8352 | 0.61 |
| 6 | 120 | 14.5161 | 1.0359 | 0.694 |
| 7 | 130 | 16.9355 | 0.6032 | 1.996 |
| 8 | 140 | 17.7419 | 0.2791 | 3.788 |
| 9 | 150 | 18.5484 | 0.2433 | 4.716 |
| 10 | 160 | 18.7097 | 0.0461 | 5.0520 |
| 11 | 170 | 19.3548 | 0.1977 | 5.362 |
| 12 | 180 | 20.1613 | 0.2370 | 5.448 |
| 13 | 190 | 20.5645 | 0.1172 | 5.47 |
| 14 | 200 | 20.9677 | 0.1129 | 5.522 |
| 15 | 210 | 20.9677 | 0.0000 | 5.464 |
| 16 | 220 | 20.9677 | 0.0000 | 5.484 |
| 17 | 230 | 22.0161 | 0.2888 | 5.38 |
| 18 | 240 | 22.8226 | 0.2221 | 5.322 |
| 19 | 250 | 23.3871 | 0.1563 | 5.5 |
| 20 | 260 | 23.3871 | 0.0000 | 5.618 |
| 21 | 270 | 23.3871 | 0.0000 | 5.628 |
| 22 | 280 | 23.3871 | 0.0000 | 5.596 |
| 23 | 290 | 23.9516 | 0.1519 | 5.686 |
| 24 | 300 | 25.0000 | 0.2854 | 6.002 |
| 25 | 310 | 25.8065 | 0.2256 | 6.4019 |
| 26 | 320 | 26.9355 | 0.3160 | 6.846 |
| 27 | 330 | 28.2258 | 0.3436 | 6.6519 |
| 28 | 340 | 34.3548 | 1.6751 | 10.136 |
| 29 | 350 | 43.4677 | 2.4708 | 11.552 |
| 30 | 360 | 62.5000 | 5.5309 | 12.628 |
| 31 | 370 | 75.4839 | 3.4923 | 13.706 |
| 32 | 380 | 84.1935 | 2.3166 | 16.298 |
| 33 | 390 | 88.7097 | 1.2243 | 19.194 |
| 34 | 400 | 90.3226 | 0.4180 | 19.408 |
| 35 | 410 | 91.9355 | 0.4081 | 17.618 |
| 36 | 420 | 92.7419 | 0.2045 | 15.94 |
| 37 | 430 | 93.5484 | 0.2079 | 14.83 |
| 38 | 440 | 94.3548 | 0.2043 | 13.888 |
| 39 | 450 | 94.3548 | 0.0000 | 13.304 |
| 40 | 460 | 95.1613 | 0.2004 | 12.87 |
| 41 | 470 | 95.1613 | 0.0000 | 12.4 |
| 42 | 480 | 96.7742 | 0.4014 | 11.922 |
| 43 | 490 | 97.0968 | 0.0812 | 11.53 |
| 44 | 500 | 97.2581 | 0.1852 | 10.686 |

Table 2S. Results of gravimetric determination of the effectiveness of β-CD/ME inhibitor at different temperatures and concentrations in 0.5 M HCl medium.

| Cing, mg/L/mM | Тemperatura, К | CRGrav., mg/sm2·soat | ηGrav., % | θGrav. |
| --- | --- | --- | --- | --- |
| Fon | 303 | 1.67 | - | - |
| 25/0.02 |  | 0.269 | 83.89 | 0.8389 |
| 50/0.04 |  | 0.211 | 87.37 | 0.8737 |
| 75/0.06 |  | 0.124 | 92.57 | 0.9257 |
| 100/0.08 |  | 0.052 | 96.89 | 0.9689 |
| Fon | 313 | 1.84 | - | - |
| 25/0.02 |  | 0.332 | 81.96 | 0.8196 |
| 50/0.04 |  | 0.268 | 85.43 | 0.8543 |
| 75/0.06 |  | 0.224 | 87.83 | 0.8783 |
| 100/0.08 |  | 0.15 | 91.85 | 0.9185 |
| Fon | 323 | 2.01 | - | - |
| 25/0.02 |  | 0.412 | 79.50 | 0.7950 |
| 50/0.04 |  | 0.351 | 82.54 | 0.8254 |
| 75/0.06 |  | 0.302 | 84.98 | 0.8498 |
| 100/0.08 |  | 0.252 | 87.46 | 0.8746 |
| Fon | 333 | 2.18 | - | - |
| 25/0.02 |  | 0.521 | 76.10 | 0.7610 |
| 50/0.04 |  | 0.473 | 78.30 | 0.7830 |
| 75/0.06 |  | 0.421 | 80.69 | 0.8069 |
| 100/0.08 |  | 0.378 | 82.66 | 0.8266 |

Figure 9S. (a) Arrhenius and (b) trans-station plots of the corrosive and inhibited systems

(β-CD/ME).

Table 3S. Thermodynamic activation function values for systems that are both uninhibited and inhibited (β-CD/ME).

| Functions | Blank | 25 mg/L/ 0.02 mM | 50 mg/L/ 0.04 mM | 75 mg/L/ 0.06 mM | 100 mg/L/ 0.08 mM |
| --- | --- | --- | --- | --- | --- |
| Ea, kJ/mol | 7.45 | 18.42 | 22.53 | 33.39 | 54.59 |
| ∆Ha, kJ/mol | 4.81 | 15.78 | 19.89 | 30.75 | 51.94 |
| ∆Sa kJ/mol T | -382.09 | -361.16 | -349.71 | -317.57 | -254.04 |
| Ea-∆Ha | 2.64 | 2.64 | 2.64 | 2.64 | 2.65 |

Figure 10S. (a) Arrhenius and (b) trans-station plots of the corrosive and inhibited systems

(β-CD/ME).

Table 4S. Values in thermodynamic functions of activation for uninhibited and inhibited systems (β-CD/ME).

| Temperature, K | Kads, M-1 | ∆Gadso, kJ/mol | ∆Hadso, kJ/mol | ∆Sadso, J/mol K |
| --- | --- | --- | --- | --- |
| 303 | 183.48 | -23.25 | -12.86 | -119.5 |
| 313 | 234.74 | -24.66 |  |  |
| 323 | 273.97 | -25.86 |  |  |
| 333 | 291.54 | -26.84 |  |  |

Figure 11S. Raman spectra of Fe surface after immersion in 0.5 M HCl.

Figure 12S. Raman spectra of Fe surface after immersion in 0.5 M HCl with the addition of β-CD/ME.

Figure 13S. The Mulliken Atomic Charges (MAC) distribution for oxygen (O) and nitrogen (N) atoms in the supramolecular (host-guest) complex of β-cyclodextrin and melamine inhibitor.

Table 5S: Calculated theoretical parameters of the β-cyclodextrin and melamine supramolecular(Host-guest) Complex inhibitor.

| Theoretical parameters | Complex inhibitor |
| --- | --- |
| EHOMO (eV) ELUMO (eV) ΔE (eV) I (eV) A (eV) χ (eV) η (eV) σ (eV-1) ∆N ∆Eback-donation | -5.717 0.240 5.951 5.717 -0.240 2.738 2.978 0.335 0.715 -0.744 |

Figure 14S. Adsorption energy distribution curves of the β- cyclodextrin and melamine supramolecular(Host-guest) Complex inhibitor, obtained via MC.