Supporting Information

Observing Dendrite Growth in Solid-State Sodium Batteries Using Fluorescence Tomography Technology

Shuaishuai Yang1, Na Li4, Enyue Zhao4, Chengzhi Wang1, 2*, Jingxin He1, Xiong Xiao1, Debao Fang1, 2, Qing Ni1, Xile Han3, Xiaobin Xue3, Lai Chen1 2*, Ning Li1, 2, Jingbo Li1, Tuan Guo3, Yuefeng Su1, 2, Haibo Jin1, 2*

1School of Materials Science and Engineering, Beijing Key Laboratory of Construction Tailorable Advanced Functional Materials and Green Applications, Beijing Key Laboratory of Environmental Science and Engineering, Beijing Institute of Technology, Beijing 100081, China. 2Chongqing Innovation Center, Beijing Institute of Technology, Chongqing 401120, China. 3Guangdong Key Laboratory of Optical Fiber Sensing and Communications, Institute of Photonics Technology, Jinan University, Guangzhou, Guangdong 511443, China. 4Songshan Lake Materials Laboratory, Dongguan 523808, China.

*Correspondence: wang_cz@bit.edu.cn (C.Z Wang), chenlai144@sina.com (L. Chen), hbjin@bit.edu.cn (H.B. Jin)

Fig. S1. Photoluminescence mechanism of Eu3+ ions under UV light excitation.

Fig. S2. Photoluminescence spectra of the NZSP-xEO solid electrolytes with the blank NZSP as comparison.

Fig. S3. Equivalent circuit containing the bulk resistance (Rb) and the grain boundary resistance (Rgb) for conductivity analysis of the solid electrolytes.

Fig. S4. Cross-sectional SEM images and relative densities of the NZSP-xEO solid electrolytes with the blank NZSP as comparison. (a) NZSP, (b) NZSP-2%EO, (c) NZSP-5%EO, (d) NZSP-7%EO, (e) NZSP-10%EO, (f) NZSP-15%EO. The relative densities were determined by an Archimedes drainage method.

Fig. S5. Time-resolution Nquist plots of the symmetric Na//Na cells using the various NZSP-x%EO solid electrolytes for 14 days. (a) NZSP, (b) NZSP-2%EO, (c) NZSP-5%EO, (d) NZSP-7%EO, (e) NZSP-10%EO, (f) NZSP-15%EO.

Fig. S6. In-depth ToFSIMs profile of the NZSP-5%EO after short circuit and the derived 3D models of Na, Eu, Si, Zr species and their overlay.

Fig. S7. (a) XRD patterns and (b) SEM image of the commercial Na3V2(PO4)3 cathode materials.

Fig. S8. Fluorescence emission maps of the NZSP-5%EO solid electrolytes after different charge/discharge cycles. (a) 1st, (b) 300th, (c) 600th, (d) 1100th.

| Composition | Space group | a (Å) | b (Å) | c (Å) | beta（deg） | Volume (Å) |
| --- | --- | --- | --- | --- | --- | --- |
| NZSP | C2/c | 15.625774 | 9.038793 | 9.212119 | 123.7010 | 1082.441 |
| NZSP-5%EO | C2/c | 15.627126 | 9.037405 | 9.215243 | 123.6705 | 1083.124 |

Table S1. The comparative crystalline parameters of NZSP and NZSP-5%EO from Rietveld refinement results.