Polydopamine Surface Engineering of Iron Single-Atom Nanozyme: a Novel Strategy for Doxorubicin Immobilization, Tumor Microenvironment Remodeling and Synergistic Multimodel Therapy

Jing Liu a, Minjuan Wang b, Haoyu Chen a, Xing Yang a, Mingjie Wei b*, Xingfeng Wang a, Shigang Shan c, Xiaohua Zhu a, Youyu Zhang a, Meiling Liu a*, Shouzhuo Yao a

[a] J. Liu, H. Chen, X. Yang, Dr. X. Zhu, Prof. Y. Zhang, Prof. M. Liu, Prof. S. Yao

Key Laboratory of Chemical Biology & Traditional Chinese Medicine Research (Ministry of Education, China), College of Chemistry and Chemical Engineering, Hunan Normal University

Changsha 410081, P. R. China

E-mail: liumeilingww@126.com, liuml@hunnu.edu.cn

[b] M. Wang, Dr. M. Wei, Dr. X. Wang

School of Pharmacy, Xianning Medical College, Hubei University of Science and Technology

Xianning 437100, P. R. China

E-mail: weimj5@mail3.sysu.edu.cn

[c] Dr. S. Shan

School of Public Health, Xianning Medical College, Hubei University of Science and Technology

Xianning, 437100, P. R. China.

Supporting information for this article is given via a link at the end of the document.

* Corresponding author: Email: liumeilingww@126.com, liuml@hunnu.edu.cn

Jing Liu and Minjuan Wang contribute equally to this work.

Contents

Figure S1. TEM imaging of Fe SAN.	5

Figure S2. SEM image of Fe SAN.	6

Figure S3. HRTEM image of Fe SAN.	7

Figure S4. SAED image of Fe SAN.	8

Figure S5. TEM image of Fe SAN-PDA.	9

Figure S6. SEM image of Fe SAN-PDA.	10

Figure S7. Fe 2p XPS spectrum of Fe SAN.	11

Figure S8. C1s XPS spectrum of Fe SAN-PDA.	12

Figure S9. O1s XPS spectrum of Fe SAN-PDA.	13

Figure S10. EXAFS fitting curves of Fe SAN at k space.	14

Figure S11. The UV absorbance of ox-TMB at 652 nm at different pH values (5.5, 6.5, 7.4) with different time.	15

Figure S12. The degradation of MB with different time.	16

Figure S13. (a) Reaction principle of coumarin with hydroxyl radical (·OH). (b) Fluorescence spectrum evolution for detection of ·OH radicals catalyzed by H2O2 (1), coumarin (2), coumarin+Fe SAN-PDA (3), coumarin+ H2O2 (4), coumarin+Fe SAN-PDA+ H2O2 (5) using coumarin as the trapping agent. pH= 5.5, Fe SAN-PDA (200 µg mL-1), H2O2 (10 mM), coumarin (5 mM), Ex = 332 nm.	17

Figure S14. OXD-like activity of (a-b) Steady-state kinetic assay of the Fe SAN-PDA by using TMB as the substrate, pH = 4.0.	18

Figure S15. The UV absorbance of ox-TMB with various pH (5.5, 6.5, 7.4)	19

Figure S16. Normalized intensity of RDPP at different time in the presence of H2O2 (10 mM), Fe SAN/Fe SAN-PDA (20 μg·mL-1), RDPP (30 μg·mL-1), PBS (6.5).	20

Figure S17. Fluorescence reduction of RDPP catalyzed by CAT-like activity of Fe SAN-PDA for 15 min in PBS at different pH.	21

Figure S18. The photograph of bubble at different groups, control (1), Fe SAN (2) and Fe SAN-PDA (3).	22

Figure S19. CAT-like activity of Fe SAN-PDA (a) Steady-state kinetic assay in different H2O2 concentrations (b) Corresponding double reciprocal plots.	23

Figure S20. UV-vis absorption spectra of Ti(SO4)2 solutions after incubation with Fe SAN-PDA, (a) Ti(SO4)2+H2O2, (b) Ti(SO4)2+H2O2+ Fe SAN-PDA.	24

Figure S21. The UV spectra of NADPH in different conditions: 0.1 mM NADPH, 1U GR, 50 μg/mL Fe SAN-PDA, 1 mM H2O2, 0.5 mM GSH, pH 7.4 PBS.	25

Figure S22. Cells viability of LO2 after incubation with various concentrations of (i) DOX, (ii) Fe SAN-PDA@HA, (iii) Fe SAN-PDA@DOX@HA and (iv) Fe SAN-PDA@DOX@HA+ 808 nm.	26

Figure S23. Corresponding FL intensity of DOX with different incubation time.	27

Figure S24. Flow cytometry analysis of apoptotic HepG2 cells after various treatments using Annexin V-APC/7-AAD staining.	28

Figure S25. Fe element content of different organs for Fe SAN-PDA@HA by ICP-OES.	29

Table S1. Atomic ratios of different elements of Fe SAN and Fe SAN-PDA.	30

Table S2. EXAFS fitting parameters at the Fe K-edge for various samples（Ѕ02=0.85）	31

Table S3. Comparison of steady-state kinetic parameter for Fe SAN-PDA	32

References	34

Figure S1. TEM imaging of Fe SAN.

Figure S2. SEM image of Fe SAN.

Figure S3. HRTEM image of Fe SAN.

Figure S4. SAED image of Fe SAN.

Figure S5. TEM image of Fe SAN-PDA.

Figure S6. SEM image of Fe SAN-PDA.

Figure S7. Fe 2p XPS spectrum of Fe SAN.

Figure S8. C1s XPS spectrum of Fe SAN-PDA.

Figure S9. O1s XPS spectrum of Fe SAN-PDA.

Figure S10. EXAFS fitting curves of Fe SAN at k space.

Figure S11. The UV absorbance of ox-TMB at 652 nm at different pH values (5.5, 6.5, 7.4) with different time.

Figure S12. The degradation of MB with different time.

Figure S13. (a) Reaction principle of coumarin with hydroxyl radical (·OH). (b) Fluorescence spectrum evolution for detection of ·OH radicals catalyzed by H2O2 (1), coumarin (2), coumarin+Fe SAN-PDA (3), coumarin+ H2O2 (4), coumarin+Fe SAN-PDA+ H2O2 (5) using coumarin as the trapping agent. pH= 5.5, Fe SAN-PDA (200 µg mL-1), H2O2 (10 mM), coumarin (5 mM), Ex = 332 nm.

Figure S14. OXD-like activity of (a-b) Steady-state kinetic assay of the Fe SAN-PDA by using TMB as the substrate, pH = 4.0.

Figure S15. The UV absorbance of ox-TMB with various pH (5.5, 6.5, 7.4)

Figure S16. Normalized intensity of RDPP at different time in the presence of H2O2 (10 mM), Fe SAN/Fe SAN-PDA (20 μg·mL-1), RDPP (30 μg·mL-1), PBS (6.5).

Figure S17. Fluorescence reduction of RDPP catalyzed by CAT-like activity of Fe SAN-PDA for 15 min in PBS at different pH.

Figure S18. The photograph of bubble at different groups, control (1), Fe SAN (2) and Fe SAN-PDA (3).

Figure S19. CAT-like activity of Fe SAN-PDA (a) Steady-state kinetic assay in different H2O2 concentrations (b) Corresponding double reciprocal plots.

Figure S20. UV-vis absorption spectra of Ti(SO4)2 solutions after incubation with Fe SAN-PDA, (a) Ti(SO4)2+H2O2, (b) Ti(SO4)2+H2O2+ Fe SAN-PDA.

Figure S21. The UV spectra of NADPH in different conditions: 0.1 mM NADPH, 1U GR, 50 μg/mL Fe SAN-PDA, 1 mM H2O2, 0.5 mM GSH, pH 7.4 PBS.

Figure S22. Cells viability of LO2 after incubation with various concentrations of (i) DOX, (ii) Fe SAN-PDA@HA, (iii) Fe SAN-PDA@DOX@HA and (iv) Fe SAN-PDA@DOX@HA+ 808 nm.

Figure S23. Corresponding FL intensity of DOX with different incubation time.

Figure S24. Flow cytometry analysis of apoptotic HepG2 cells after various treatments using Annexin V-APC/7-AAD staining.

Figure S25. Fe element content of different organs for Fe SAN-PDA@HA by ICP-OES.

Table S1. Atomic ratios of different elements of Fe SAN and Fe SAN-PDA.

| Sample | Fe Atomic (%) | C Atomic (%) | N Atomic (%) | O Atomic (%) |
| --- | --- | --- | --- | --- |
| Fe SAN | 0.25 | 76.45 | 11.59 | 11.67 |
| Fe SAN-PDA | 0.19 | 67.54 | 8.69 | 23.58 |

Table S2. EXAFS fitting parameters at the Fe K-edge for various samples（Ѕ02=0.85）

|  | shell |  | CNa | Rb(Å) |  |  | σ2c(Å2) | ΔE0d(eV) | R factor |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Fe-foil | Fe-Fe1 | 8 |  |  | 2.47±0.01 | 0.0048 |  | 6.0±1.6 | 0.0036 |
|  | Fe- Fe2 | 6 |  |  | 2.85±0.01 | 0.0062 |  |  |  |
| Fe SAN | Fe-C/N | 4.04±0.1 |  |  | 1.99±0.05 | 0.0098 |  | -1.2±1.0 | 0.0038 |

Table S3. Comparison of steady-state kinetic parameter for Fe SAN-PDA

| POD-like |  |  |  |
| --- | --- | --- | --- |
| Catalyst | Km (mM) TMB/H2O2 | Vmax (10-7 M s-1) TMB/H2O2 | Reference |
| Mo-CDs | 0.245 /0.176 | 0.320 /0.476 | 1 |
| MIL-53 (Fe) | 1.08/0.04 | 3.12/1.39 | 2 |
| Mo-Co3O4 nanotubes | 0.0558 /22.48 | 0.954/0.523 | 3 |
| Fe-PCN-222 | 0.78/1.49 | 3.06/4.46 | 4 |
| CZIF/Au | 0.21/22.27 | 0.508/1.37 | 5 |
| Fe SAN-PDA | 0.9/0.62 | 4.01/0.97 | This work |
| OXD-like |  |  |  |
| Catalyst | Km (mM) TMB | Vmax (10-7 M s-1) TMB | Reference |
| Co3O4/CoFe2O4 HNCs | 0.028 | 8.30 | 6 |
| Fe-N-C nanozyme | 0.21 | 14.0 | 7 |
| Mn3O4 | 0.02715 | 1.267 | 8 |
| Fe-N/C | 0.134 | 1.96 | 9 |
| Fe-PCN-222 | 0.78 | 3.06 | 4 |
| Fe SAN-PDA | 0.215 | 4.88 | This work |
| CAT-like |  |  |  |
| Catalyst | Km (mM) H2O2 | Vmax (10-6 M s-1) H2O2 | Reference |
| Fe-SANzyme | 18.80 | 9.317 | 10 |
| Co-N3PS SAzyme | 6.10 | 52.0 | 11 |
| CuO NPs-POM | 0.12 | 0.0187 | 12 |
| Fe SAN-PDA | 0.0113 | 5.85 | This work |

References

1.	Lu, W. et al. Smartphone-assisted colorimetric sensing platform based on molybdenum-doped carbon dots nanozyme for visual monitoring of ampicillin. Chem. Eng. J. 468, 143165 (2023).

2.	Zheng, H.-Q. et al. MOF-808: a metal-organic framework with intrinsic peroxidase-like catalytic activity at neutral pH for colorimetric biosensing. Inorg. Chem. 57, 9096-9104 (2018).

3.	Gao, M. et al. Enhanced peroxidase-like activity of Mo6+-doped Co3O4 nanotubes for ultrasensitive and colorimetric L-cysteine detection. ACS Applied Nano Materials. 1, 4703-4715 (2018).

4.	Shu, Y. et al. Metalloporphyrin-based metal-organic framework nanorods for peroxidase-like catalysis. ACS Applied Nano Materials. 5, 17909-17918 (2022).

5.	Li, Y. et al. Skillfully manipulating electron transitions of Au nanoparticles for the modulation of nanozyme functions. New. J. Chem 47, 11222-11231 (2023).

6.	Jiang, S. et al. Co3O4/CoFe2O4 hollow nanocube multifunctional nanozyme with oxygen vacancies for deep-learning-assisted smartphone biosensing and organic pollutant degradation. ACS Appl. Mater. Interfaces. 15, 11787–11801 (2023).

7.	Pan, M. et al. Construction of metal organic framework-derived Fe-N-C oxidase nanozyme for rapid and sensitive detection of alkaline phosphatase. Nanomaterials. 13, 2496 (2023).

8.	Xi, J., Zhu, C., Wang, Y., Zhang, Q. & Fan, L. Mn3O4 microspheres as an oxidase mimic for rapid detection of glutathione. Rsc Advances. 9, 16509-16514 (2019).

9.	Ge, J. et al. A colorimetric smartphone-based platform for pesticides detection using Fe-N/C single-atom nanozyme as oxidase mimetics. J. Hazard. Mater. 436, 129199 (2022).

10.	Zhang, R. et al. Edge-site engineering of defective Fe-N4 nanozymes with boosted catalase-like performance for retinal vasculopathies. Adv. Mater. 34, 2205324 (2022).

11.	Chen, Y. et al. Atomic-level regulation of cobalt single-atom nanozymes: engineering high-efficiency catalase mimics. Angew. Chem. Int. Ed. 135, e202301879 (2023).

12.	Xu, Y. et al. Polyoxometalate nanostructures decorated with CuO nanoparticles for sensing ascorbic acid and Fe2+ ions. ACS Applied. Nano. Materials. 4, 8302-8313 (2021).