Supporting information

Janus Hollow Microstructures via an Interfacial Phase Hydrogen bond Network

Materials: All chemical agents and solvents for polymerization were purchased from Aladdin Co. Styrene (St), butyl acrylate (BA), methyl methacrylate (MMA) and methyl acrylate (MA) were purified by basic aluminum oxide to remove inhibitors. The aqueous acryloyloxyethyl trimethyl ammonium chloride (DAC) solution was freeze-drized to obtain solid DAC. The styrene used for fluorescence experiments was analytical standard from Aladdin Co. 2,2'-Azobis (2-methylpropionitrile) (AIBN) was recrystallized before used. The molecular weight of Polyvinylprrolidone (K30) is ca. 40000 g/mol. Other materials were used without further purification.

The characterizations of poly(styrene-co-acrylamide) hollow microspheres: The prepared poly(styrene-co-acrylamide) hollow microspheres (1a) exhibited an obvious suck hollow structure with 20- 60 μm particle size (FigureS1 a). The SEM-EDS mapping data showed that the molar ratios of O element and N element on the outside surface of the hollow microspheres are 7.62% and 4.95% respectively. However, O and N elements were not detected on the inside surface. Only polyacrylamide inside the hollow microspheres contained O and N elements, resulting in hydrophilicity on the outside surface and complete hydrophobicity on the inside surface (FigureS1 b). FTIR and XPS were also shown in FigureS1 c-g , proving the presence of C=O group and -NH2 group in the hollow microspheres (Characteristic band at 1659 cm-1 and 3430 cm-1 respectively assigned to C=O group and -NH2 in FTIR. The three additional peaks at 288.80 eV, 286.40 eV and 284.80 eV corresponded to C-N group. C=O group and C-H groups respectively in C 1s scan. The two additional peaks at 402.70 eV and 399.65 eV corresponded to C-N group and -NH2 group in N 1s scan. The additional peak at 532.40 eV corresponded to C=O group in O 1s scan). In addition to, the molar content of polyacrylamide was 2.05% in the hollow microspheres through element analysis measurement. These characteristics indicated the successful synthesis of the Janus poly (St-co-AM) hollow microspheres. Obviously, the polymerization method was facile and one-pot to obtain amphiphilic hollow microspheres. Note: the preparation process of other hollow microparticles in the paper were similar to the above. The recipes of all prepared hollow microstructures were listed in the Table S1.

g

f

e

d

c

a

b

Figure S1. (a) SEM of the poly (St-co-Am) hollow microspheres; (b) SEM-EDS mapping of the poly (St-co-Am) hollow microspheres inside and outside surface; (c) FTIR of the poly (St-co-AM) hollow microspheres; (d) XPS survey of the poly (St-co-AM) hollow microspheres; (e-g) C 1s scan, N 1s scan and O 1s scan of the poly (St-co-AM) hollow microspheres, respectively.

Scheme S1. The reaction monomers used in the preparation microparticles.

Table S1. Recipes of prepared hollow microparticles.

| Entry | Hydrophobic monomer (mmol) | Crosslinking Agent1 (mmol) | Higher alkane* (ml) | Initiator* (mmol) | Hydrophilic monomer (mmol) | Crosslinking agent2 (mmol) | K30 (g) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1a | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 28.80 AM | 0 | 0.10 |
| 1b* | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 28.80 AM | 0 | 0.10 |
| 1c | 28.80 St | 0 | 0 | 0.29 | 0 | 0 | 0 |
| 1d* | 28.80 St | 0 | 0 | 0.29 | 0 | 0 | 0 |
| 1e* | 28.80 St | 0 | 0 | 0.29 | 0 | 0 | 0 |
| 2a | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 28.80 AM | 0 | 1.50 |
| 2b | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 28.80 AM | 0 | 1.00 |
| 2c | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 28.80 AM | 0 | 0.50 |
| 2d | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 28.80 AM | 0 | 0.10 |
| 2e | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 28.80 AM | 0 | 0 |
| 3a | 28.80 St | 0.29DVB | 6.67 | 0.29 | 0 | 0 | 0.10 |
| 3b | 28.80 BA | 0.29 EGDMA | 6.67 | 0.29 | 0 | 0 | 0.10 |
| 3c | 28.80 MMA | 0.29 EGDMA | 6.67 | 0.29 | 0 | 0 | 0.10 |
| 3d | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 28.80 MA | 0 | 0.10 |
| 3e | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 28.80 AA | 0 | 0.10 |
| 3f | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 28.80 MAH | 0 | 0.10 |
| 3g | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 28.80 DAC | 0 | 0.10 |
| 3h | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 28.80 AMPS | 0 | 0.10 |
| 3i | 28.80 BA | 0.29 EGDMA | 6.67 | 0.29 | 28.80 AM | 0 | 0.10 |
| 3j | 28.80 BA | 0.29 EGDMA | 6.67 | 0.29 | 28.80 AA | 0 | 0.10 |
| 3k | 28.80 BA | 0.29 EGDMA | 6.67 | 0.29 | 28.80 DAC | 0 | 0.10 |
| 3l | 28.80 BA | 0.29 EGDMA | 6.67 | 0.29 | 28.80 AMPS | 0 | 0.10 |
| 3m | 28.80 BA | 0.29 EGDMA | 6.67 | 0.29 | 28.80 MAH | 0 | 0.10 |
| 4a | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 14.40 AM | 0 | 0.10 |
| 4b | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 28.80 AM | 0 | 0.10 |
| 4c | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 43.20 AM | 0 | 0.10 |
| 4d | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 86.40 AM | 0 | 0.10 |
| 4e | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 115.20 AM | 0 | 0.10 |
| 4f | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 115.20 AM | 0.52 MBA | 0.10 |
| 4g | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 115.20 AM | 2.60 MBA | 0.10 |
| 4h | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 115.20 AM | 5.20 MBA | 0.10 |
| 4i | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 115.20 AM | 7.80 MBA | 0.10 |
| 5a | 28.80 St | 0.29 DVB | 6.67 | 0.29 | 28.80 AM | 0 | 0.10 |
| 5b | 21.89 St | 0.29 DVB | 7.50 | 0.29 | 21.89 AM | 0 | 0.10 |
| 5c | 17.51 St | 0.29 DVB | 8.00 | 0.29 | 17.51 AM | 0 | 0.10 |
| 5d | 14.59 St | 0.29 DVB | 8.33 | 0.29 | 14.59 AM | 0 | 0.10 |
| 5e | 12.51 St | 0.28 DVB | 8.57 | 0.29 | 12.51 AM | 0 | 0.10 |

Note. 1b*, 1d*; H2O as continuous phase. 1e*; DES containing H2O of 5% mass content as continuous phase. Initiator*: AIBN as initiator for all polymerization. High alkane*: n-hexadecane as high alkane for all polymerization.

e

d

c

b

a

f

Figure S2. (a) Particle size distribution of the prepared poly (St-co-AM) hollow microspheres with 1.5, 1.0, 0.5, 0.1 and 0 g K30 dosage, respectively; (b) Median particle diameter (d (0.5)) particle size of the prepared poly (St-co-AM) hollow microspheres with 1.5 g, 1.0 g, 0.5 g, 0.1 g and 0 g K30 dosage, respectively (c-e) SEM of prepared poly St, poly BA and poly MMA products, respectively; (f) FTIR of the poly (BA-co-AM) hollow microparticle.

b

a

Figure S3. (a) Optical microscopy of the St/DESs emulsion; (b) Optical microscopy of the C16H34/DESs emulsion.

c                               d                                   e                                  f

k

j

i

h

g

Figure S3. (c) SEM of the prepared Poly (St-co-AM) product with H2O as solvent; (d) SEM of the prepared Poly St product in the DES system; (e) SEM of the prepared Poly St product in the H2O system; (f) SEM of the prepared Poly St product in the 5% H2O system. (g) UV absorbance of St with different concentration in ethanol; (h) UV standard curve of St. (i) UV absorbance curve of 10ppm dye probe in the five DESs; (j) Empirical parameters (ET (30), ET N) of the five DESs polarity; (k) Dynamic interfacial tension of DESs-styrene interface in the five DESs.

a

c

b

Figure S4.  (a) CFM of aggregate AIE luminogen at DES phase, St phase and DES-St interface, respectively; (b) UVRR of St; (c) The emission maximum wavelength of 10 ppm St in various solvents.

Table S2: hardness (η), softness (S) and electrophilicity of DES + n St model (consisting of one molecule of DESs and n molecule of St) and n St model (consisting n molecule of St).

|  | DESs | DESs+1St | DESs+2St | DESs+3St | DESs+4St | DESs+5St | DESs+6St |
| --- | --- | --- | --- | --- | --- | --- | --- |
| [I=-EHOMO]/ eV | 7.22800 | 7.35752 | 7.06597 | 7.09545 | 7.04001 | 6.99436 | 6.90908 |
| [A=-ELUMO]/ eV | -2.30000 | -0.15883 | -0.35625 | -0.02561 | 0.10240 | 0.02704 | 0.17966 |
| [η=(I-A)/2]/ eV | 4.764 | 3.75815 | 3.71111 | 3.56053 | 3.46881 | 3.48366 | 3.36471 |
| [S=1/2η]/ eV-1 | 0.10495 | 0.13304 | 0.13473 | 0.14043 | 0.14414 | 0.14353 | 0.14860 |
| [μ=-(I+A)/2]/ eV | -2.4640 | -3.59935 | -3.35486 | -3.53492 | -3.57121 | -3.5107 | -3.54437 |
| [ω=μ2/η]/ eV | 1.27411 | 3.44723 | 3.03281 | 3.50949 | 3.67633 | 3.53795 | 3.73762 |
|  | St | 2St | 3St | 4St | 5St | 6St |  |
| [I=-EHOMO]/ eV | 7.41987 | 7.213731 | 7.064487 | 7.106849 | 6.996495 | 6.836311 |  |
| [A=-ELUMO]/ eV | -0.14843 | -0.149509 | -0.185271 | -0.064807 | 0.044491 | 0.079332 |  |
| [η=(I-A)/2]/ eV | 3.78415 | 3.68162 | 3.62488 | 3.58583 | 3.47600 | 3.37849 |  |
| [S=1/2η]/ eV-1 | 0.13213 | 0.13581 | 0.13794 | 0.13944 | 0.14384 | 0.14800 |  |
| [μ=-(I+A)/2]/ eV | -3.63572 | -3.53207 | -3.43961 | -3.52102 | -3.52050 | -3.45782 |  |
| [ω=μ2/η]/ eV | 3.49311 | 3.38867 | 3.26381 | 3.45739 | 3.53555 | 3.53902 |  |

a

b

Figure S5. (a) The excitation and emission maximum wavelength of the fluorescent agent;(b) In-suit time SEM observation at different polymerization time periods.