S1. In-vitro evaluation of SAS-margosa nanocomposite, SAS and Margosa leaf extract against FFSC complex at different concentrations
	Serial no.
	Seed coating material
	%radial growth inhibition

	
	
	25% (a.i.)
	50% (a.i.)
	75% (a.i.)

	Fusarium fujikuroi

	1
	nSAS-Margosa composite
	57.34±0.24
	68.12±0.45
	89.20±0.28

	2
	SAS 
	26.23±0.64
	38.16±0.18
	41.24±0.31

	3
	Margosa leaf extract
	31.24±0.5
	39.86±0.58
	43.12±0.13

	4
	Control
	0
	0
	0

	Fusarium verticillioides

	5
	nSAS-Margosa composite
	56.17±0.84
	64.59±1.25
	90.13±0.65

	6
	SAS
	28.45±0.65
	39.76±0.98
	43.58±0.59

	7
	Margosa leaf extract
	33.45±0.47
	37.14±0.47
	42.79±0.47

	8
	Control
	0
	0
	0

	Fusarium proliferatum

	9
	nSAS- Margosa composite
	59.73±0.35
	66.14±1.4
	87.45±0.32

	10
	SAS
	32.44±0.69
	36.47±0.84
	40.28±0.14

	11
	[bookmark: _GoBack]Margosa leaf extract
	31.79±0.71
	36.25±0.91
	39. 89±0.65

	12
	Control
	0
	0
	0



