Supplementary information

for

Mangrove tree aerial root extract mediated  green synthesis of Ag/Fe3O4/GO nanocomposite and its application as a catalyst for one pot synthesis of 7-phenyl-6H,7H-benzo[4,5]imidazo[2,1-b]chromeno[4,3-d][1,3]thiazin-6-one derivatives

Devendiran Parthiban1, Muniyan Ramasamy Kuppusamy1, Chinnaswamy Vanitha1, Ayyanan Gomathi1, Dhanasekaran Suraksha1*

1Research Department of Chemistry, Rajeshwari Vedachalam Government Arts College, Chengalpattu, Tamilnadu,India-603001.

* Corresponding author mail id: surakshadhanasekaran211@gmail.com

GRAPHICAL ABSTRACT

Synthesis of Graphene Oxide and Fe3O4/GO

Graphite powder was used to prepare Graphene oxide (GO) using improved version of Hummer's method.54 iron oxide/ graphene oxide (Fe3O4/GO) nanocomposite was prepared by the co-precipitation of Fe2+ and Fe3+ in the presence of graphene oxide by dissolving 0.31 g of FeCl2.4H2O and 0.75 g of FeCl3·6H2O (molar ratio of 1:2) in 30 mL of distilled water under sonication for 10 min, then adding 0.2758 g graphene oxide pre-dissolved in 30 ml of distilled water, carefully stirred  for about 25 min at room temperature, then, adding 3 mL of aqueous ammonia to increase pH to alkaline (10–11) condition. The formation of Fe3O4 was confirmed by observing the colour change from light brown to black. The resultant suspension was heated to 80oC for about 15 min, then kept at room temperature for 1 h. The synthesized Fe3O4/GO nanoparticles were removed from reaction vessel with help of external bar magnet. The Fe3O4/GO nanoparticles were washed with water and ethanol in order to remove unreacted reactants. Finally, the precipitate was dried at 80oC in oven for 4 h.

Preparation of Mangrove tree aerial root extract

The mangrove tree aerial root extract was prepared using fresh part of aerial root tip, washed with water, chopped into fine pieces. About 5 g of chopped aerial roots was grained using mortar and pestle. chopped aerial roots was mixed with 100 mL of distilled water. The mixture was stirred for 2 h at 80oC and cooled down to room temperature. The extract was centrifuged with help of Remi R-80C+ centrifuging machine at 4000 rpm for 20 minutes and finally the clear extract was stored in glass container at 5 oC. (Fig 4)

- b)

Figure 4:  a) Mangrove aerial root tip b) Mangrove root extract

Synthesis of Ag/Fe3O4/GO nanocomposite using Mangrove aerial root extract

0.5 g of Fe3O4/GO nanocomposite was dispersed in 50 mL of water and was sonicated for 15 minutes. 20 mL of 0.1 M aqueous solution of AgNO3 was added drop wise into the suspension of Fe3O4/GO nanocomposite and sonication was continued for 1 h. 40 mL of Mangrove aerial root extract was then added drop wise into the above mixture and pH was reached 9.0 by adding aqueous solution of NaOH under the continuous stirring and heated at 80 oC for 3 h. After the completion of reaction, the obtained Ag/Fe3O4/GO nanocomposite was separated by applying external magnetic field, washed with distilled water for several times, dried in oven at 80 oC for 12 h.(Fig 5)

a)      b)

Synthesis of Ag/Fe3O4/GO a) Before addition of Mangrove extract b) After addition of Mangrove extract.

Scheme of synthesis of Ag/Fe3O4/GO nanocomposite using banyan and mangrove root extracts.

General procedure for synthesis of 7-phenyl-6H,7H-benzo[4,5]imidazo[2,1-b]chromeno[4,3-d][1,3]thiazin-6-one derivatives

The mixture of hydroxycoumarin (10 mmol), mercaptobenzimidazole (10 mmol) and different aldehyde (10 mmol), Ag/Fe3O4/rGO (45 mg) and 10 ml of EtOH was taken in 100 ml round bottom flask, refluxed on water bath for appropriate time and the progress of the reaction was monitored by TLC. After completion of the reaction as indicated by TLC, the reaction mixture was cooled to room temperature. The solid formed upon cooling was filtered, dried and purified by recrystallizing in hot ethanol. The synthesised compounds were characterised partially by proton NMR.

Scheme 1 Synthesis of 7-phenyl-6H,7H-benzo[4,5]imidazo[2,1-b]chromeno[4,3-d][1,3]thiazin-6-one derivatives

FT-IR spectra of Mangrove aerial root extract mediated Ag/Fe3O4/rGO nanocomposite

XRD pattern of mangrove tree aerial root extract mediated Ag/Fe3O4/rGO nanocomposite

SEM image of mangrove tree aerial root mediated Ag/Fe3O4/rGO nanocomposite

- Magnification of 10 µm

- Magnification of 500 nm

EDAX spectrum of mangrove tree aerial root mediated Ag/Fe3O4/rGO nanocomposite

VSM spectra of mangrove aerial root extract mediated Ag/Fe3O4/rGO nanocomposite

Spectral data for selected few compounds

Proton NMR spectrum of 7-(p-tolyl)-6H,7H-benzo[4,5]imidazo[2,1-b]chromeno[4,3-d][1,3]thiazin-6-one (4e)

Integration multiplied by 2

Proton NMR spectrum of 7-(4-methoxyphenyl)-6H,7H-benzo[4,5]imidazo[2,1-b]chromeno[4,3-d][1,3]thiazin-6-one (4f)

Integration multiplied by 2

Proton NMR spectrum of 7-(3,4,5-trimethoxyphenyl)-6H,7H-benzo[4,5]imidazo[2,1-b]chromeno[4,3-d][1,3]thiazin-6-one (4g)