Supplementary Information

Making color display cool: An electrochemical self-cooled dynamic structural color device

Shenghao Jin1, Fan Yi1, Dong Yang2, Yujie Peng2, Mengqi Liu1, C.Y. Zhao1, Ming Xiao2,3 *, and B.X. Wang1,4,5,6 *

1 Institute of Engineering Thermophysics, School of Mechanical Engineering, Shanghai Jiao Tong University, Shanghai 200240, China

2 College of Polymer Science and Engineering, Sichuan University, Chengdu, 610065, China

3 State Key Laboratory of Polymer Materials Engineering, Sichuan University, Chengdu 610065, China

4 2020 X-Lab, Shanghai Institute of Microsystem and Information Technology, Chinese Academy of Sciences, Shanghai 200050, China

5 State Key Laboratory of Transducer Technology, Shanghai Institute of Microsystem and Information Technology, Chinese Academy of Sciences, Shanghai 200050, China

6 School of Graduate Study, University of Chinese Academy of Sciences, Beijing 100049, China

Correspondence:

wangboxiang@mail.sim.ac.cn (B.X. Wang) and mingxiao@scu.edu.cn (M. Xiao)

Supplementary Note 1. Generalized optical model of PMEs

The optical spectra and electric field distribution within the PMEs are modeled employing the transfer matrix method (TMM)S1, S2. The device consists of a multilayered structure between the glass substrate and ambient air. The optical transfer matrix 2×2 formalism is applied to calculate the interference of reflected and transmitted light waves at each interface in the stack. Each layer j (j=1, 2, …, m) have a thickness of dj, and complex refractive index of nλ=nλ+ikλ. A plane wave is incident from the glass substrate (layer 0) and traveling to the ambient air (layer m+1) at an incident angle of θ0. Then, the electric field at each point in layer j within the multilayered stacking can be represented by two components: positive superscript Ej+ for the waves traveling in positive x direction (from layer 0 to layer m+1), and negative superscript Ej- for the waves traveling in the opposite direction. Then, an interface matrix can describe each interface in the structure:

Ijk=1tjk1rjkrjk1,#S1

where rjk and tjk are the Fresnel complex reflection and transmission coefficients at interface jk:

rjk, TE=njcosθj-nkcosθknjcosθj+nkcosθk,rjk, TM=nkcosθj-njcosθknkcosθj+njcosθk,#S2a

tjk, TE=2njcosθjnjcosθj+nkcosθk,tjk, TM=2njcosθjnkcosθj+njcosθk,#S2b

The phase matrix describing the propagation through layer j is described by:

Lj=e-ikz,jdj00eikz,jdj,#S3

where dj is the thickness of layer j, and kz,j=2πnjλcosθj is wavevectors of layer j in z direction.

Combining the interface matrix and the layer matrix, the total system transfer matrix S, which relates the electric filed at glass substrate side (layer 0) and ambient air (layer m+1) is described by:

E0+E0-=SEm+1+Em+1-,#S4

where S=S11S12S21S22=v=1mIv-1vLvImm+1 is the product of all interface and layer matrices. Then, the spectral reflectance and transmittance of the total stacked structures can be derived as:

R=S21S112,#S5

TTE=1S112Renm+1cosθm+1Ren0cosθ0, TTM=1S112Renm+1cosθm+1*Ren0cosθ0*, #S6

In the calculation, the reflectance spectra are calculated by averaging the results of TM and TE polarizations. The refractive index of materials used in the PMEs are given in Supplementary Fig.3.

Then, for the electric field at a distance x in the layer j in the multilayered structure can be expressed as:

Ejx=Ej+x+Ej-x,#S7

To express Ejx in term of known quantities, S is split into two partial transfer matrices Sj' and Sj'', by the relation S=Sj'LjSj'' .The above two matrices are defined as:

Sj'=Sj11'Sj12'Sj21'Sj22'=v=1j-1Iv-1vLvIj-1j,#S8a

Sj''=Sj11''Sj12''Sj21''Sj22''=v=j+1mIv-1vLvImm+1.#S8b

Therefore, for the partial system transfer matrices of layer j

E0+E0-=Sj'Ej'+Ej'-,#S9a

Ej''+Ej''-=Sj''Em+1+Em+1-,#S9b

where Ej'+ and Ej'-are refer to the left boundary (j-1)j, Ej''+and Ej''- are refer to the right boundary j(j+1). Eventually, the Ejx can be expressed as:

Ejx=Ej+x+Ej-x=tj+ei2πnjλx+rj''ei2πnjλ2dj-xE0+,#S10

where

tj+=Sj11'+Sj12'rj''e2i2πnjλdj-1,#S11

rj''=Sj21''Sj11''.#S12

Here, since the glass substrate used in this work has a large thickness of ~0.5 mm which is much greater than the coherence length of sunlight, the glass is not included in the transfer matrix calculation. The light intensity in the glass transferred to the glass/stacked structure’s interface was calculated incoherently. Then the total spectral reflectance and transmittance of the PME-glass substrate system can be expressed as:S3

Rtotλ=R*λ+T*λ11-RλR*λRλT*λ,#S13

Ttotλ=1-R*λTλ1-RλR*λ,#S14

where R*λ and T*λ are the spectral reflectance and transmittance of the glass substrate, Rλ and Tλ are the spectral reflectance and transmittance of the stacked structures with SiO2 as the incident medium calculated by TMM. Then, the modulus squared of the electric field E0,gλ2 from the glass to the stacked structure is:

E0,gλ2=1-R*λnglass1-RλR*λE0λ2=BE0λ2#S15where E0λ2 is the modulus squared of the electric field in the free space, nglass is the refractive index of the glass substrates, B=1-R*λnglass1-RλR*λ is the modified factor.

Then, according to the above model, the optical absorption in the layer j of the stacked structure can be calculated by:

Ajz,λ=αjλIjx,λI0=4πkjλnjλBλEjz,λE0λ2,#S16

Supplementary Note 2. The selection of a metallic layer as the bottom reflector and the initial design of PME

For the Fabry–Pérot resonances, according to the temporal coupled mode theory (TCMT)S4, the metal layer is the central component determining the electromagnetic mode damping of the optical resonant mode, which has a significant impact on optical properties of the resonant peak and ultimately determine the solar reflection and coloration capability. Furthermore, the metal required to function as the bottom reflector in our coloration strategy should be RMED-compatible (that is, capable of being deposited or dissolved by electrochemical reactions). Hence, noble metals like silver (Ag) and copper (Cu), which exhibit a comparatively low optical damping rate and are compatible with RMED technology, are highly desired.

Meanwhile, the most straightforward nanostructure to induce FP resonances is the metal-dielectric-metal tri-layered structure. Therefore, the metal-dielectric bilayered structures are desired to develop as the working electrodes for FP resonance excitation via RMED. Here, we first demonstrate a series of excellent conductive Ag/ITO bilayered structures as the working electrodes, which can induce FP resonances in conjunction with the ED-metal (Supplementary Fig. 4). Then, the selection of the electrodeposited metallic layer and corresponding RMED technology is accomplished by comparing the resonance efficiency of Ag/ITO/ED-metal structures.

It is known the depth and bandwidth of the reflection dip in a reflectance spectrum is an important indicator of resonance efficiency. The greater the depth and the narrower the bandwidth of this dip, the better the efficiency of resonance. Meanwhile, an absorption peak with a large depth and narrow bandwidth is more desirable for coloration without introducing excessive solar absorption. Therefore, to select the suitable bottom metallic reflector and corresponding RMED technology, the comparison between the reflection dips of Ag/ITO structures with opaque Ag and Cu bottom reflective layers is provided in Supplementary Fig. 5. It is obvious that the Ag/ITO structures with Ag bottom reflectors have a large dip depth and much narrower bandwidth due to the lower optical damping of Ag in the entire visible spectrum. Therefore, the Ag bottom reflector can achieve a larger average solar reflection than the Cu bottom reflector when exhibiting nearly identical color saturation.

However, as mentioned in the main text, the large lattice mismatch prevents the growth of a high-quality electrodeposited silver (ED-Ag) layer on the dielectric layer. Considering that a Pt seed layer should be adopted for the lattice matching in the actual PMEs, the comparison between the reflection dips of Ag/ITO/10 nm Pt structures with opaque Ag and Cu bottom reflective layers is also provided in Supplementary Fig.7. The depth and bandwidth of the reflection dip are mostly determined by the high-damping Pt layer, as most of the optical absorption occurs in this layer. Nevertheless, due to the blocking of sunlight by the top Ag layer, the choice between silver or copper as the bottom reflective layer will not significantly affect the average reflection compared to the original state. Furthermore, due to the low electromagnetic damping loss of Ag, the FP resonances excited by Ag/ITO/Pt/Ag structures have large dip depth and much narrower bandwidth, leading to higher average solar reflection and color saturation compared to the Ag/ITO/Pt/Cu structures

Therefore, according to the above criteria, Ag-based RMED is selected as the ideal choice for the proposed FP nanocavity-based dynamic colorful radiative cooling (DCMRCs) in this work. Going further, DCRMCs with Cu-based RMED can also be investigated in future works.

Supplementary Note 3. Theoretical model of the radiative cooling performance

To quantify the radiative cooling performance of radiative coolers, theoretical calculations at different temperature Ts are performed. Considering energy balance, the net radiative cooling power can be calculated with:S5

PcoolingTs=PradTs-Psun-PatmTamb-Pnon-rad,#S17

where Tamb is the ambient temperature. In Equation S17, the radiative power emitted by per area of DCMRC (PradTs) is:

PradTs=0∞02π0π2ελ,θIbbTs,λsinθcosθdθdφdλ,#S18

where IbbTs,λ=2hc2λ51ehcλkBTs-1 is the spectral blackbody radiation intensity of DCMRC at temperature of Ts, and ελ,θ is the spectral directional emissivity of the DCMRC. h= 6.626×10-34 J∙Hz-1 is the Planck constant, c=3×108ms is the speed of light in vacuum, kB=1.38×10-23 J∙K-1 is the Boltzmann constant.

The absorbed power of DCMRC due to incident atmospheric thermal radiation (PatmTamb) is:

PatmTamb=0∞02π0π2εatmλ,θελ,θIbbTamb,λsinθcosθdθdφdλ,#S19

where IbbTamb,λ is the spectral blackbody radiation intensity of atmosphere at Tamb=303 K. εatmλ,θ is the spectral directional emissivity of atmosphere calculated as εatmλ,θ=1-tλ,01cosθ.S6 tλ,0 is the atmospheric transmittance in the zenith directionS7.

The absorbed power of DCMRC due to incident solar radiation (Psun) is:

Psun=0∞ελ,θSun∙IAM1.5λdλ,#S20where IAM1.5λ is the solar irradiation intensity with direct normal irradiance power of 900 W/m2, θSun is the angle which DCMRC faces the sun, and ελ,θSun is the spectral emissivity of the DCMRC at the angle of θSun. Here, we assume that DCMRC is facing the sun. As a result, ελ,θSun is represented by the spectral emissivity of the DCMRC under normal incidence ελ,0, where θSun=0°. The spectral emissivity ε is calculated by ελ,0=1-Rλ,0. The average solar reflection is calculated by Rsol=300 nm2500 nmRλIAM1.5λ300 nm2500 nmIAM1.5λ

The non-radiative absorbed power (Pnon-rad) due to convection and conduction is:

Pnon-rad=hcTamb-Ts,#S21

where hc is the non-radiative heat transfer coefficient containing the effect of convection and conduction. For the calculation of non-radiative absorbed power, we assume that hc=6.9Wm2∙K according to Ref. 26.

To quantify the radiative cooling performance of DCMRCs shown above, two parameters can be used. One is the temperature drop ∆T=Tamb-Ts of DCMRC when the net radiative cooling power is zero (Pcooling=0). The other is the net radiative cooling power when the temperature of DCMRC is the same as the ambient temperature (Ts=Tamb).

Supplementary Note 4. Color representation calculation

The CIE 1931 color coordinate system based on the CIEXYZ coordinate space was used to calculate the color of the DCMRCs via the simulated reflection spectrum. The color information of objects can be expressed by the tristimulus values comprising X, Y, and Z which can be calculated by CIE color-matching functions  xλ, yλ, zλ and reflection spectrum of samples Rλ as:S8

X=kRλD65λxλdλ#S22

Y=kRλD65λyλdλ#S23

Z=kRλD65λzλdλ#S24

where D65λ is spectral power distribution of CIE Illuminant D65, k is the normalization parameter and CIE specifies that Y=100, which leads to k=100D65λyλdλ.

Then, the chromaticity of samples can be specified by the two normalized values (x and y) derived from the tristimulus values and located in the 2D CIE 1931 color space as:

x=XX+Y+Z#S25

y=YX+Y+Z#S26

Moreover, every chromaticity point has a brightness (luminance) value which can be represented by the tristimulus value Y of corresponding color. As a result, a certain color can be quantified by three basic parameters as x,y,Y.

In addition, the color difference, ∆E, can be utilized to provide a quantitative value representing the difference between the color representation of different designed structures. For the CIELAB color difference ∆E is based on the CIEL*a*b* coordinate space, a transformation from CIEXYZ coordinate space to CIEL*a*b* coordinate space can be conducted by following equations:S9

L*=116fYYn-16#S27

a*=500fXXn-fYYn#S28

b*=200fYYn-fZZn#S29

where Xn=95.047, Yn=100, Zn=108.883 corresponding to the CIE XYZ tristimulus value of the reference white point under CIE Illuminant D65 and the function of ft is

ft=t13    t>6293t3×6292+429    t≤6293#S30

After getting the three color values L*,  a*, b*, the color saturation can be calculated by:S10

S=a*2+b*2L*.#S31

Finally, the color difference between two colors can be calculated by: S9

∆E=∆L*2+∆a*2+∆b*2#S32

Supplementary Note 5. The composition analysis of PME under two working states

The composition of the deposited metal film was characterized by comparing the X-ray photoelectron spectroscopy (XPS) and X-ray diffraction (XRD) of the identical PME with and without the ED metal layer. The peaks at 368.4 and 374.4 eV in the Ag 3d scan confirm the existence of the metallic Ag(0) on the bottom surface of PME with the ED metal layer. Meanwhile, the shift in Ag 3d peaks’ binding energy scan from PME with and without ED metal layer clearly demonstrates the change from Ag+ ion to metallic Ag after the electrodeposition (Ag(Ⅰ): 367.9 eV/Ag3d5/2 and 373.9 eV/Ag3d3/2; Ag(0): 368.4 eV/Ag3d5/2 and 374.4 eV/Ag3d3/2).S23 The change in the elements on the bottom surface of PME can also be evaluated by the increase in counts of Ag 3d peaks (Supplementary Fig.16a) and the disappearance of Pt 4f peaks after the silver deposition (Supplementary Fig.16b).S24 XRD analyses indicate that the peak at 39.9° which can be assigned to Pt (111) in the 10 nm Pt layer disappears after the metal deposition (Fig.16c).S25 Meanwhile, due to the PME’s thickness of only 125 nm, the signal of the 40 nm top Ag layer within it will unavoidably be detected via GIXRD. Nevertheless, following the process of the electrodeposition, the intensity of the peaks at 38.4°, 44.5°, 64.8°, and 77.6° which can be assigned to Ag crystals (111), (200), (220), and (311) are notably enhanced in comparison to the initial PME. S26

Supplementary Note 6. Construction of the DCMRC devices and multiplexed adaptive display devices

DCMRC devices

As shown in Fig.2a in the main text, the DCMRC devices consist of the PME deposited on quartz wafers as working electrodes, the sandwiched Ag-based gel electrolyte, and the commonly used ITO-coated glass as the counter electrode. For the working electrodes, since the MIR emissivity of the quartz wafers is insufficient for effective cooling, highly transparent 500 μm commercially available poly(dimethylsiloxane) (PDMS) films are coated on the top of quartz wafers. These films can significantly enhance the MIR emission of the DCMRC devices (Supplementary Fig.15). For the sandwiched Ag-based gel electrolyte, 0.5 mm silicon rubber spacers were used for sealing and preventing the working electrode from directly contacting the counter electrodes. For the counter electrodes, the commercially available flat ITO-coated glass (~10 Ω/sq, 5 cm×5 cm×1.1 mm) were purchased from Zhuhai Kaivo Optoelectronics Technology Co., Ltd., China. Conductive copper tapes are attached to the surface of PME and ITO-coated glass for connection to the electrochemical workstation.

Multiplexed adaptive display devices

We developed two types of multiplexed adaptive display devices in this work, as shown in Fig.4 in the main text. To fabricate the first multiplexed adaptive display devices (Fig.4b), nine of PMEs (2 cm×2 cm, coloration area 1cm2) are constructed as three-by-three multiplexed switchable array and then integrated with a 6 cm×6 cm commercially available flat ITO-coated glass (~10 Ω/sq, Zhuhai Kaivo Optoelectronics Technology Co., Ltd., China) and 0.5 mm rubber spacers. Conductive copper tapes are attached to the surface of PMEs and ITO-coated glass for connection to the multichannel electrochemical workstation (CHI1040C). The nine PMEs are electrically isolated from each other, allowing for independent control by applying voltage through the multi-channel electrochemical workstation.

Meanwhile, the second multiplexed adaptive display devices (Supplementary Figs.4c-d in the main text) are fabricated based on a PME (5 cm×5 cm, coloration area 1cm2×9) integrated with nine of ITO-coated glass (2 cm×2 cm, ~10 Ω/sq, Zhuhai Kaivo Optoelectronics Technology Co., Ltd., China) and 0.5 mm rubber spacers. Conductive copper tapes are attached to the surface of PMEs and ITO-coated glass for connection to the multichannel electrochemical workstation (CHI1040C). Similarly, the nine ITO-coated glasses are electrically isolated from each other, allowing for independent control by applying voltage through the multi-channel electrochemical workstation.

The nine independent pixel units are numbered consecutively, as shown in Supplementary Fig. 26. The channel numbers to which voltage is applied to create the multi-colorful letters "S", "J", "T", and "U" on the multiplexed adaptive display devices are as follows: “S”: 3, 4, 7, 8, 9; “J”: 1, 3, 4, 7, 8, 9; “T”: 1, 4, 7, 8, 9; “U”: 1, 2, 3, 4, 5, 6, 7. Note we used channels “1, 3, 4, 8, 9” to input voltage and generate the mirror-symmetric S in the devices shown in Fig.4c-d. To enhance the resemblance to the actual S shape, we employed the mirror symmetry of the photograph in the manuscript. Nevertheless, this modification does not affect the multiplexed dynamic display capabilities we expect the device to demonstrate.

Supplementary Note 7. Energy consumption modeling of cooling requirements due to solar thermal loads for display devices

To evaluate the energy consumption of different display technologies due to the heat dissipation requirements resulting from the solar thermal load, we assume a prefabricated large-scale vertical display screen with an area of 450 m2 (length: 30m, height: 15m, Supplementary Fig. 28) under direct sunlight. The displays are achieved by nine different display technologies shown in Supplementary Table 1. Under the outdoor environment during the daytime, the large-scale vertical display screen is heated by solar irradiance and dissipates heat outward through passive natural convection and MIR radiation emission. When passive cooling cannot reduce the temperature to the suitable operating level, the excessive heat load should be dissipated using active cooling equipment with additional power consumption. According to the energy balance, the total heat load required to be dissipated (Qcool-active) can be calculated as:

Qcool-active=Qsun-QncTs,Tamb-Qrad, netTs,Tamb,#S33

where Qsun is the hourly absorbed solar irradiance by the vertical display screen, Qnc is the hourly heat dissipation of natural convection between the vertical display screen and outside air, Qrad, net is the hourly net radiative energy exchange between the vertical display screen and atmosphere. Tamb is the ambient temperature and Ts is the surface temperature of the vertical display screen. Considering the optimal operating temperature of the display device and inside electrical components, as well as the global weather conditions in hot summer, we assume Ts=308 K in this energy consumption modeling.

The hourly absorbed solar irradiance of the vertical display screen due to incident solar radiation (Qsun) is:

Qsun=As∙Qsol,#S34

where As is the solar absorption of the vertical display screen (taken from Supplementary Table 1). Qsol is the incident solar radiation to the vertical display screen. Here, since the vertical display screen is opaque, the solar absorption As is calculated by As=1-Rs for practicality, in which Rs is the solar reflection of vertical display screen during the colorful state. The incident solar radiation of a vertical object (Qsol) can be derived by:S11

Qsol=QSβ+QDβ+QGβ,#S35

in which QSβ is the hourly direct solar radiation on the surface, QDβ is the hourly diffuse sky radiation on the surface, QGβ is the hourly ground reflected radiation on the surface. β=90° is the surface tilt angle.

The hourly direct solar radiation on the surface can be expressed by:S12

QS=Qsol,dircosθ=Qsol,dirsinθzcosφ-γ,#S36

where Qsol,dir is the hourly direct normal solar radiation, θ is the incidence angle of the direct normal on the surface. θz is solar zenith angle; φ is solar azimuth angle, γ is the azimuth angle of the calculated surface (here we assume that the vertical surface is facing south, γ=180° in the Northern Hemisphere, and facing north, γ=0° in the Southern Hemisphere). The solar zenith angle θz and solar azimuth angle φ can be calculated by: S13

θz=90°-α=90°-sin-1sinϕsinδ+cosϕcosδcosh,#S37

φ=cos-1sinδcosϕ-cosδsinϕcoshcosα  if h≤0360°-cos-1sinδcosϕ-cosδsinϕcoshcosα  if h>0,#S38

where α is the solar elevation angle, δ=-23.44×cos360365dn+10 is solar declination (dn is the number of days since January 1st UTC (00:00: hr)), h=15°×LST-12 is hour angle (LST is the local solar time in hours), ϕ is the geographic latitude in degrees (which is positive in the Northern Hemisphere and negative in the Southern Hemisphere).

For the hourly diffuse sky radiation on the surface QD and hourly ground reflected radiation on the surface QG, we utilize the model assuming isotropy for calculation, which can be expressed as:S11

QD=12Qsol,diff1+cosβ#S39

and

QG=12Qsol,globRG1-cosβ,#S40

where Qsol,diff and Qsol,glob are the hourly diffuse and global horizontal solar radiation, β=90° is the surface tilt angle, RG is the ground albedo, which can be customary to use the average value of 0.2. S14

The hourly heat dissipation of natural convection between the vertical display screen and outside air Qnc (in Wh/m2) can be calculated by the empirical formula for natural convection on vertical walls as: S15

QncTs,Tamb=hcTs-Tamb×36003600=4.995+1.444vTs-Tamb,#S41

where v is the wind speed.

The hourly net radiative energy exchange between the vertical display screen and atmosphere Qrad, net (in Wh/m2) can be derived as:

Qrad, net=PradTs-PatmTamb×36003600,#S42

in which:S16

PradTs=0∞0π0π2ελ,θ2IbbTs,λsinθcosθdθdφdλ,#S43

PatmTamb=0∞0π0π2εatmλ,θελ,θ2IbbTamb,λsinθcosθdθdφdλ,#S44

where ελ,θ2 is the material’s emissivity towards the upper half of the hemispherical angle. Here, we are assuming that all display devices have an isotropic MIR emitter with high emissivity of 0.9, which is higher than commonly-used substrates of typical EC materials (such as quartz) and thus enhances the heat dissipation via MIR thermal emission. Meanwhile, the atmospheric transmittance in the zenith direction is obtained by the MODTRAN model.S17

Then, the hourly heat load Qcool-active can be derived by Eq.(S33). The weather data and environmental parameters including hourly direct normal solar radiation Qsol,dir, hourly diffuse Qsol,diff, global horizontal solar radiation Qsol,glob, ambient temperature Tamb (dry bulb temperature), and wind speed v of different locations and cities can be obtained from online resources provided by the U.S. Department of Energy (EnergyPlus)S18. When Qcool-active<0, it indicates that the display device can achieve the suitable working temperature without additional active cooling power consumption, thus it can be considered that Qcool-active=0.

Finally, the total heat load required to be dissipated can be calculated by summing the hourly heat dissipation requirement over a summer (from May 1st to Aug 31th in the Northern Hemisphere, from Nov 1st to Feb 28th in the Southern Hemisphere) as:

Qcool-active,tot=450×n=1123 or 120Qcool-active, n.#S45

In this calculation, we select 36 metropolises in the world to evaluate the energy consumption and energy saving, including Shanghai, Beijing, Hong Kong, Shenzhen, Guangzhou, Taipei, Tokyo, Inchon, Singapore, Bangkok, Mumbai, Abu Dhabi, New York, Chicago, Los Angeles, Philadelphia, Boston, Vancouver, London, Paris, Berlin, Rome, Geneva, Moscow, Sao Paulo, Buenos Aires, Cape Town, Melbourne, Sydney, Auckland, Riyadh, Karachi, Cairo, Tunis, Casablanca, Johannesburg. The calculation results are summarized in Supplementary Table 2.

Finally, the total heat load Qcool-active,tot is assumed to be dissipated with a standard cooling system with a coefficient of performance (COP) of 2.8.S19 Then, the electricity savings of our cooled display compared to Si-based LED display can be derived (Qs=Qcool-active,totCOP). In this calculation, the optical properties of the Si-based LED display device are simplified to those of the bulk silicon substrate for calculation. Note that the calculation of electrical energy-saving is conducted only considering the dissipation of solar heat load, while the dissipation of heat resulting from the display itself is not taken into account. However, given that the energy consumption of LED displays is an order of magnitude greater than that of RMED and other EC-based displays due to the insufficient energy conversion efficiency of LED lighting, our energy-saving calculation that merely considers solar heat load can provide an approximation for the lower limit of electrical power-saving and quantitatively estimate the effect of manipulating the solar spectra of display technologies.

Supplementary Fig. 1. The ideal spectra for achieving a self-cooled colorful display and the visible reflection spectra of existing EC-based materials and devices in the previous work. (a) The ideal spectra for achieving self-cooled color display. A controllable narrowband absorption peak is highly desirable for realizing color switching, while high MIR emissivity is also required for radiative cooling.(b) WO3-based multilayered structure.14 (c) WO3-based metamaterial.39 (d) Conventional RMED with metallic nanoparticles (NPs).17 (e) RMED-based metamaterial.40 (f) Al-based RMED (Al reflector on electrode).43 (g) W-based RMED (W reflector on electrode).44 (h) Liquid photonic crystal (PCs).41 (i) Soft-solid photonic crystal (PCs).45 (j) Swellable photonic crystal (PCs).46 (k) Cholesteric liquid crystal ink.42

Supplementary Fig. 2. The solar reflection spectra of the existing dynamic radiative coolers based on thermochromic (TC) pigments (a)47, microcapsules (b)48, and dye (c)49. Since the manipulation principle of these TC materials is dependent on increasing solar absorption, even a small volume fraction can result in a significant reduction in solar reflection. (d) The comparison of average solar reflection of different dynamic radiative coolers before and after color-switching. The average solar reflection is calculated by the measured solar reflectance.

Supplementary Fig. 3. The refractive index of materials used in the optical property calculation of PMEs. (a) Ag. The measured refractive index via spectroscopic ellipsometry agrees well with the previous literature S20. (b) TiO2. The measured refractive index via spectroscopic ellipsometry agrees well with the previous literature S21. (c) ITO. The measured refractive index is used in the calculation. (d) Pt. The refractive index based on the Lorentz-Drude model is used in the calculation S22.

Supplementary Fig. 4. Schematic diagrams of Ag/ITO (metal-dielectric) electrode before and after RMED for FP resonance excitation.

Supplementary Fig. 5. The comparison between Ag/ITO structures with opaque Ag and Cu bottom reflective layers. (a) The reflection dips of Ag/ITO/Ag structure. (b) The reflection dips of Ag/ITO/Cu structure. (c) The average solar reflection of Ag/ITO structure before and after the metal deposition. (d) The color saturation of Ag/ITO/Ag and Ag/ITO/Cu structure.

Supplementary Fig. 6. The comparison between the measured and theoretical spectra of different electrodes with ED-Ag. (a) Ag/ITO electrode. Due to the large lattice mismatch between ITO and Ag, high-quality silver layer deposition cannot be achieved. There is also a great difference between the measured and theoretical spectra. Moreover, the quality of the ED-Ag layer deteriorates with the cycles, resulting in a decrease in the Q-factor of the resonant peak (decrease from 8.4 to 3.2 in 8 cycles). (b) Ag/ITO/TiO2/Pt electrode. The measured spectra agree well with the theoretical due to the high-quality silver layer deposited on the Pt seed layer, which is capable of maintaining numerous cycles (The Q factor remains 8.6 throughout 50 cycles).

The Q-factor is calculated by the commonly-used definition as: Q=ω0γ, where ω0 is the resonant frequency, γ is the damping coefficient of the resonance. As the single resonant mode, γ is the full-width at half maximum (FWHM) of the resonance frequency. S29

Supplementary Fig. 7. The comparison between Ag/ITO/Pt structures with opaque Ag and Cu bottom reflective layers. (a) The reflection dips of Ag/ITO/Pt/Ag structure. (b) The reflection dips of Ag/ITO/Pt/Cu structure. (c) The average solar reflection of Ag/ITO/Pt structure before and after the metal deposition. (d) The color saturation of Ag/ITO/Pt/Ag and Ag/ITO/Pt/Cu structure.

Supplementary Fig. 8. The electric field and optical absorption of PME under two working states (a-b) The electric field distribution of PME without and with ED-Ag at the resonant wavelength (555 nm). (c-d) The electric field distribution of PME without and with ED-Ag with respect to wavelength and structure. (e-f) The optical absorption inside PME without and with ED-Ag with respect to wavelength and structure.

Supplementary Fig. 9. The color gamut of all PMEs (top Ag: 15 nm-40 nm, ITO: 20-130 nm, TiO2: 10-50 nm, Pt: 10 nm) without ED-Ag and corresponding self-cooled PMEs at 323 K and 303 K.

Supplementary Fig. 10. The comparison of the optical properties of PMEs with and without the ED-Ag (a) Color swatches of PMEs without the ED-Ag. (b) Color swatches of PME with the ED-Ag. (c) The color saturation of PMEs without the ED-Ag. (d) The color saturation of PMEs with the ED-Ag. (e) The difference between the average solar reflection of PMEs with and without the ED-Ag. (f) The difference between the average visible transmission of PMEs with and without the ED-Ag.

Supplementary Fig. 11. The angle dependence of the structural coloration based on FP resonances in the PME electrodes. (a) PMEs without the ED-Ag. (b) PMEs with the ED-Ag.

Supplementary Fig. 12. The cyclic voltammetry tests of the electrochromic 2-electrode system of the DMSO-Ag electrolyte.

Supplementary Fig. 13 The cyclic voltammetry tests of the electrochromic 3-electrode system of the DMSO-Ag electrolyte.

Supplementary Fig. 14. The measured spectral reflectance (0.3-2.5 μm) and emissivity (2.5-20 μm) of the yellow and cyan DCMRCs with and without ED-Ag.

Supplementary Fig. 15. The measured MIR emissivity of different MIR emitters including 500 μm PDMS, 1.1 mm ITO-Glass (Soda-Lime Glass), and 1 mm quartz. The PDMS coating (ε8-13 μm=0.89) provides a enhancement of 14% in ε8-13 μm compared to the bare quartz (ε8-13 μm=0.75).

The averaged spectral emissivity of these MIR emitters in the atmosphere window can be calculated by: ε8-13 μm=8 μm13μmIbbλ, Tamb∙ελdλ8 μm13μmIbbλ, Tambdλ, where Tamb=303 K.

Supplementary Fig. 16. XPS and XRD analyses of the PME with and without ED-Ag. (a) XPS analysis of Ag element. (b) XPS analysis of Pt element. (c) XRD analysis.

Supplementary Fig. 17. (a) The color difference ∆E of three DCMRCs during the reversible Ag deposition. (b) The comparison between the reflectance spectra of DCMRCs before and after the ED.

Supplementary Fig. 18. The potentiostatic cycling curves of the 200 cyclic test and Real-time reflectance changes of different cycles measured at 555 nm. (a) The potentiostatic cycling curves in the cycles of 1st-200th. (b-c) The potentiostatic cycling curves in the cycles of 1st-10th and 140th-150th. Two of potentiostatic cycling curves are identical to each other. (d) the comparison between the Real-time reflectance changes of different cycles measured at 555 nm.

Supplementary Fig. 19. The potentiostatic cycling curves of the 500 cyclic test. (a) The potentiostatic cycling curves in the cycles of 1st-500th. (b-c) The potentiostatic cycling curves in the cycles of 1st-10th and 490th-500th.

Supplementary Fig. 20. The reflection spectra corresponding to the Ag deposition and stripping state at different cycles during the 500 cyclic test. (a) Spectral reflectance of the DCMRC with ED-Ag at different cycles. (b) Spectral reflectance of the DCMRC without ED-Ag at different cycles. The detailed spectral reflectance of the DCMRC with ED-Ag at (c) 1st-100th, (d) 200th-300th, (e) 300th-400th, (f) 400th-500th are also provided

Supplementary Fig. 21. The potentiostatic cycling curves of the 100 cycles of color switching during the measurement of outdoor cooling performance.

Supplementary Fig. 22. The power density consumption of different display technologies.

Supplementary Fig. 23. The environmental conditions during the outdoor experiments. (a-b) Relative humidity and wind speed during the 100-cycle color switching. (c-d) Relative humidity and wind speed during the continuous 6-hour cooling performance measurement.

Supplementary Fig. 24. The measured temperature of yellow and cyan DCMRCs compared to the ambient air temperature in the test setup during the continuous 6-hour cooling performance measurement. (Insert: images of DCMRCs under sunlight. The color switching of three DCMRCs from whitish to yellow, magenta, and cyan can be observed.)

For the yellow DCMRC, the maximum temperature drop of 8.2 °C appears at nighttime when the relative humidity is at its lowest value of around 52%. Meanwhile, the cyan-DCMRCs, which are regulated by the more sensitive electrochemical workstation (CHI760E), achieve a maximum temperature decrease of 10.6 °C during the daytime, which may probably be attributed to the fast stripping of the ED-Ag film on the PME and subsequent Ag deposition on the bottom counter electrode (ITO-glass). Under this circumstance, the transmitted solar energy from PME and semi-transparent electrolyte can be reflected by the ED-Ag film on the bottom electrode, further reducing the thermal load of the device and bringing better cooling performance (Supplementary Fig. 25).

Supplementary Fig. 25. The possible states of DCMRC when the reverse voltage is continuously applied. (a) Depositing metallic silver on the counter electrode of the device will reflect sunlight transmitted through the PME, enhancing the cooling effect. (b) The spectral transmittance of ITO-Glass and the quartz /DMSO-Ag electrolyte/ITO-Glass structure. The quartz /DMSO-Ag electrolyte/ITO-Glass structure exhibits high visible transmission nearly identical to the ITO-Glass. (c) Relative transmittance of quartz /DMSO-Ag electrolyte/ITO-Glass structure compared to the ITO-Glass. (d) The spectral reflectance of ED-Ag in the solar wavelength.

Supplementary Fig. 26. Two types of multiplexed adaptive display devices. (a) 2cm*2cm DCMRC pixels with 6cm*6cm ITO-Glass. (b) 2cm*2cm ITO-Glass pixels with 5cm*5cm DCMRC.

Supplementary Fig. 27. The reflectance spectra of Ag (40 nm)/ITO (50 nm)/TiO2 (50 nm)/Pt (3 nm) with and without ED-Ag. Compared to the PME (40 nm Ag) with 10 nm Pt, this PME has a much narrower resonant peak and higher Q factor (18.7), resulting in a better color appearance.

Supplementary Fig. 28. The model of a prefabricated large-scale vertical display screen under direct sunlight. (a) Schematic of heat transfer between the vertical display screen and outdoor environment. (b) Illustration of solar zenith angle θz, solar elevation angle α, and solar azimuth angle φ.

Supplementary Fig. 29. The comparison between the measured and simulated spectral reflectance of DCMRCs. (a) Front side, measured by the fiber optic spectrometer with an integrating sphere of 20 mm. (b) Back side, measured by the fiber optic spectrometer with an integrating sphere of 20 mm. (c) Front side, measured by the spectrometer with an integrating sphere of 150 mm. (d) Back side, measured by the spectrometer with an integrating sphere of 150 mm.

Supplementary Fig. 30. The spectra of LDPE film (a) and aluminized mylar (b) used in the measurement system.

Supplementary Table 1. The average visible and solar reflection of different display technologies.

| Color switching for display |  | Rvis | Rsol-mid | Rsol-max | Rsol-min | Ref |
| --- | --- | --- | --- | --- | --- | --- |
| WO3-based multilayered structure | +0.5 V | 0.31 | 0.38 | 0.15 | 0.65 | 14 |
|  | -0.4 V | 0.14 | 0.13 | 0.06 | 0.56 |  |
|  | -0.8 V | 0.09 | 0.09 | 0.04 | 0.53 |  |
| WO3-based metamaterial | 0 mC/cm2 | 0.36 | 0.20 | 0.18 | 0.67 | 39 |
|  | 3 mC/cm2 | 0.24 | 0.14 | 0.11 | 0.61 |  |
|  | 8 mC/cm2 | 0.15 | 0.10 | 0.07 | 0.56 |  |
| Conventional RMED with NPs | -1.5 V (1s) | 0.15 | 0.10 | 0.05 | 0.56 | 17 |
|  | -1.5 V (2s) | 0.16 | 0.12 | 0.08 | 0.57 |  |
|  | -1.5 V (4s) | 0.12 | 0.11 | 0.05 | 0.55 |  |
| RMED-based metamaterial | original (R) | 0.16 | 0.15 | 0.07 | 0.57 | 40 |
|  | -2.7 V (R) | 0.14 | 0.22 | 0.06 | 0.56 |  |
|  | original (G) | 0.10 | 0.11 | 0.04 | 0.54 |  |
|  | -2.7 V (G) | 0.10 | 0.13 | 0.05 | 0.54 |  |
|  | original (B) | 0.08 | 0.08 | 0.03 | 0.53 |  |
|  | -2.7 V (B) | 0.17 | 0.17 | 0.07 | 0.57 |  |
| Liquid PCs | 4.5 V (0s) | 0.03 | 0.02 | 0.007 | 0.50 | 41 |
|  | 4.5 V (1s) | 0.02 | 0.01 | 0.0003 | 0.50 |  |
|  | 4.5 V (3s) | 0.02 | 0.02 | 0.0005 | 0.50 |  |
| Swellable PCs | 0 V | 0.06 | 0.04 | 0.005 | 0.52 | 46 |
|  | 4 V | 0.06 | 0.04 | 0.005 | 0.52 |  |
| Soft-solid PCs | 0 V | 0.20 | 0.13 | 0.10 | 0.59 | 45 |
|  | 3 kV | 0.13 | 0.10 | 0.07 | 0.55 |  |
| Liquid crystal | 0 V | 0.25 | 0.24 | 0.12 | 0.62 | 42 |
|  | 3 V | 0.29 | 0.33 | 0.14 | 0.64 |  |
|  | 6 V | 0.32 | 0.27 | 0.16 | 0.65 |  |
| Al-based RMED | original | 0.68 | 0.65 | 0.32 | 0.84 | 43 |
|  | -2.7 V-1 | 0.4 | 0.40 | 0.18 | 0.69 |  |
|  | -2.7 V-2 | 0.38 | 0.38 | 0.17 | 0.68 |  |
|  | -2.7 V-3 | 0.39 | 0.40 | 0.18 | 0.69 |  |
| W-based RMED | original (R) | 0.22 | 0.22 | 0.10 | 0.60 | 44 |
|  | -2.7 V (R) | 0.40 | 0.48 | 0.20 | 0.69 |  |
|  | original (G) | 0.18 | 0.16 | 0.08 | 0.58 |  |
|  | -2.7 V (G) | 0.50 | 0.52 | 0.25 | 0.74 |  |
|  | original (B) | 0.20 | 0.19 | 0.10 | 0.59 |  |
|  | -2.7 V (B) | 0.45 | 0.51 | 0.22 | 0.72 |  |
| Si-based LED (determined by the optical properties of Si substrate) | - | 0.63 | 0.50 | 0.50 | 0.50 | S27-28 |
| This work | original (C) | 0.92 | 0.92 | 0.92 | 0.92 | - |
|  | -2.7 V (C) | 0.93 | 0.93 | 0.93 | 0.93 |  |
|  | original (M) | 0.91 | 0.91 | 0.91 | 0.91 |  |
|  | -2.7 V (M) | 0.92 | 0.92 | 0.92 | 0.92 |  |
|  | original (Y) | 0.93 | 0.93 | 0.93 | 0.93 |  |
|  | -2.7 V (Y) | 0.92 | 0.92 | 0.92 | 0.92 |  |

Note:

The Rvis is calculated based on the spectral reflectance taken from previous literature (Supplementary Fig. 1) via Rvis=400 nm780 nmRλIAM1.5λdλ400 nm780 nmIAM1.5λdλ. Meanwhile, since the UV and NIR spectra of most EC-based materials and devices are not measured, we here adopt three calculation methods for Rsol. Rsol-mid is calculated based on the assumption that the spectral reflectance in UV and NIR is identical to R400 nm and R780 nm. Rsol-min is calculated based on the assumption that the spectral reflectance in UV and NIR is 100%, while Rsol-max is calculated based on the assumption that the spectral reflectance in UV and NIR is 0.

Supplementary Table 2. The required heat dissipation of different display technologies in the summer of 36 cities and the electrical energy-saving potential of DCMRCs compared to the Si-based LED display.

| City | Qc,tot,LED (kWh/m2) | Qc,tot,EC-mid (kWh/m2) |  | Qc,tot,EC-max (kWh/m2) |  | Qc,tot,EC-min (kWh/m2) |  | Qc,tot,DCMRC (kWh/m2) |  | Qs (compared to LED) (kWh) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Shanghai | 26.2 | 23.5 | 104.2 | 63.5 | 106.8 | 4.7 | 26.8 | 0.3 | 0.5 | 4140 |
| Beijing | 44.5 | 40.1 | 157.6 | 99.7 | 161.3 | 7.1 | 45.4 | 0.1 | 0.2 | 7116 |
| Hong Kong | 19.1 | 16.5 | 93.9 | 55.1 | 96.3 | 0.8 | 19.7 | 0 | 0 | 3069 |
| Shenzhen | 40.5 | 36.3 | 148.9 | 93.9 | 152.3 | 5.2 | 41.3 | 0.1 | 0.1 | 6485 |
| Guangzhou | 33.6 | 30.4 | 115.6 | 73.9 | 118.2 | 6.3 | 41.3 | 0.1 | 0.2 | 5370 |
| Taipei | 44.5 | 40.6 | 142.6 | 93.1 | 145.7 | 9.1 | 45.3 | 0.5 | 0.7 | 7036 |
| Tokyo | 15.6 | 13.5 | 84.9 | 46.5 | 87.4 | 1.3 | 16.0 | 0 | 0 | 2501 |
| Incheon | 8.4 | 7.0 | 66.7 | 33.1 | 68.9 | 0.2 | 8.7 | 0 | 0 | 1352 |
| Singapore | 33.5 | 29.4 | 137.5 | 85.4 | 140.7 | 1.2 | 34.4 | 0 | 0 | 5385 |
| Bangkok | 53.4 | 48.6 | 167.3 | 110.8 | 170.8 | 10.9 | 54.4 | 0.3 | 0.5 | 8489 |
| Mumbai | 32.8 | 28.9 | 136.0 | 83.1 | 139.3 | 2.6 | 33.7 | 0.03 | 0.03 | 5270 |
| Abu Dhabi | 61.8 | 57.7 | 163.4 | 112.3 | 166.5 | 23.4 | 62.6 | 6.2 | 7.3 | 8753 |
| New York | 26.5 | 23.1 | 132.6 | 75.5 | 136.3 | 2.8 | 27.2 | 0.002 | 0.02 | 4253 |
| Chicago | 31.8 | 28.3 | 136.5 | 80.7 | 140.0 | 3.9 | 32.5 | 0.4 | 0.5 | 5031 |
| Los Angeles | 2.5 | 1.8 | 75.3 | 28.0 | 78.6 | 0.0 | 2.7 | 0 | 0 | 403 |
| Philadelphia | 26.9 | 23.8 | 121.4 | 70.4 | 124.7 | 2.8 | 27.5 | 0.06 | 0.09 | 4307 |
| Boston | 17.4 | 14.9 | 113.0 | 59.5 | 116.5 | 1.7 | 17.9 | 0.1 | 0.2 | 2767 |
| Vancouver | 14.2 | 11.4 | 123.9 | 62.7 | 127.9 | 0.04 | 14.9 | 0 | 0 | 2289 |
| London | 15.1 | 12.8 | 97.4 | 51.9 | 100.4 | 0.7 | 15.6 | 0 | 0 | 2431 |
| Paris | 18.5 | 15.9 | 109.3 | 59.2 | 112.7 | 0.9 | 19.1 | 0 | 0 | 2979 |
| Berlin | 23.8 | 20.8 | 113.1 | 64.8 | 116.3 | 2.3 | 24.4 | 0 | 0 | 3818 |
| Rome | 30.3 | 25.9 | 159.5 | 91.6 | 163.7 | 1.5 | 31.2 | 0 | 0 | 4869 |
| Geneva | 29.4 | 25.7 | 139.6 | 80.6 | 143.4 | 1.9 | 30.1 | 0 | 0 | 4717 |
| Moscow | 28.1 | 24.4 | 145.5 | 82.8 | 149.5 | 2.0 | 28.9 | 0 | 0 | 4522 |
| Sao Paulo | 18.6 | 16.1 | 98.2 | 54.6 | 101.0 | 1.3 | 19.1 | 0 | 0 | 2983 |
| Buenos Aires | 27.0 | 23.7 | 131.1 | 75.1 | 134.7 | 3.2 | 27.7 | 0.1 | 0.2 | 4310 |
| Cape Town | 12.0 | 10.1 | 90.1 | 44.1 | 93.2 | 0.9 | 12.4 | 0 | 0 | 1925 |
| Melbourne | 15.8 | 13.9 | 98.7 | 50.2 | 102.1 | 3.0 | 16.3 | 0.4 | 0.5 | 2463 |
| Sydney | 13.1 | 11.1 | 92.9 | 47.3 | 95.9 | 1.4 | 13.5 | 0.3 | 0.3 | 2045 |
| Auckland | 2.4 | 1.7 | 58.1 | 21.9 | 60.7 | 0 | 2.5 | 0 | 0 | 378 |
| Riyadh | 78.2 | 73.6 | 190.9 | 134.7 | 194.4 | 33.9 | 79.2 | 11.9 | 13.6 | 10382 |
| Karachi | 69.1 | 64.0 | 192.5 | 131.3 | 196.2 | 21.6 | 70.2 | 4.6 | 5.5 | 10221 |
| Casablanca | 21.6 | 18.9 | 120.6 | 66.1 | 124.1 | 3.7 | 22.2 | 1.2 | 1.3 | 3263 |
| Tunis | 53.1 | 48.2 | 185.8 | 117.5 | 190.1 | 12.7 | 54.1 | 0.8 | 1.2 | 8341 |
| Cairo | 60.7 | 55.8 | 184.6 | 122.2 | 188.4 | 16.2 | 61.8 | 2.8 | 3.4 | 9209 |
| Johannesburg | 11.6 | 9.6 | 95.5 | 47.4 | 98.7 | 0.1 | 12.1 | 0 | 0 | 1864 |

Supplementary References：

- Pettersson LA, Roman LS, Inganäs O. Modeling photocurrent action spectra of photovoltaic devices based on organic thin films. Journal of Applied Physics 86, 487-496 (1999).

- Byrnes SJ. Multilayer optical calculations. arXiv preprint arXiv:160302720,  (2016).

- Persson N-K, Arwin H, Inganas O. Optical optimization of polyfluorene-fullerene blend photodiodes. Journal of Applied Physics 97, (2005).

- Suh W, Wang Z, Fan S. Temporal coupled-mode theory and the presence of non-orthogonal modes in lossless multimode cavities. IEEE Journal of Quantum Electronics 40, 1511-1518 (2004).

- Zhao B, Hu M, Ao X, Chen N, Pei G. Radiative cooling: A review of fundamentals, materials, applications, and prospects. Applied energy 236, 489-513 (2019).

- Granqvist C, Hjortsberg A. Radiative cooling to low temperatures: General considerations and application to selectively emitting SiO films. Journal of Applied Physics 52, 4205-4220 (1981).

- Lord SD. A new software tool for computing Earth's atmospheric transmission of near-and far-infrared radiation. Ames Research Center (1992).

- Schanda J. Colorimetry: understanding the CIE system. John Wiley & Sons (2007).

- Mokrzycki W, Tatol M. Colour difference∆ E-A survey. Mach Graph Vis 20, 383-411 (2011).

- Xiao M, Stephenson AB, Neophytou A, Hwang V, Chakrabarti D, Manoharan VN. Investigating the trade-off between color saturation and angle-independence in photonic glasses. Optics Express 29, 21212-21224 (2021).

- Maxwell EL, Stoffel TL, Bird RE. Measuring and modeling solar irradiance on vertical surfaces.). Solar Energy Research Inst.(SERI), Golden, CO (United States) (1986).

- Chen Y, Wang S, Yang X, Fan Y, Ge J, Li Y. Temporal variation of wall flow and its influences on energy balance of the building wall. City and Built Environment 1, 3 (2023).

- https://solarsena.com/solar-azimuth-angle-calculator-solar-panels/

- Liu BY, Jordan RC. The long-term average performance of flat-plate solar-energy collectors: with design data for the US, its outlying possessions and Canada. Solar energy 7, 53-74 (1963).

- Jayamaha S, Wijeysundera N, Chou S. Measurement of the heat transfer coefficient for walls. Building and Environment 31, 399-407 (1996).

- Zhou J, et al. Angle-selective thermal emitter for directional radiative cooling and heating. Joule 7, 2830-2844 (2023).

- http://modtran.spectral.com/modtran_home

- https://energyplus.net/weather

- Deru M, et al. US Department of Energy commercial reference building models of the national building stock. (2011).

- Yang HU, D'Archangel J, Sundheimer ML, Tucker E, Boreman GD, Raschke MB. Optical dielectric function of silver. Physical Review B 91, 235137 (2015).

- Kischkat J, et al. Mid-infrared optical properties of thin films of aluminum oxide, titanium dioxide, silicon dioxide, aluminum nitride, and silicon nitride. Applied optics 51, 6789-6798 (2012).

- Rakić AD, Djurišić AB, Elazar JM, Majewski ML. Optical properties of metallic films for vertical-cavity optoelectronic devices. Applied optics 37, 5271-5283 (1998).

- Firet NJ, et al. Operando EXAFS study reveals presence of oxygen in oxide-derived silver catalysts for electrochemical CO 2 reduction. Journal of Materials Chemistry A 7, 2597-2607 (2019).

- Lebedeva M, Ragutkin A, Antropov A, Yashtulov N. The features of bimetallic Pt-Ru nanoparticles formation on the Nafion membrane for electrodes of chemical power sources. In: IOP Conference Series: Materials Science and Engineering). IOP Publishing (2020).

- Zhao X, Li Y, Ai C, Wen D. Resistive switching characteristics of Li-doped ZnO thin films based on magnetron sputtering. Materials 12, 1282 (2019).

- Guo W, et al. MOFs derived Ag/ZnO nanocomposites anode for Zn/Ni batteries. Journal of Solid State Chemistry 272, 27-31 (2019).

- Wu Y, Ma J, Su P, Zhang L, Xia B. Full-color realization of micro-LED displays. Nanomaterials 10, 2482 (2020).

- Tian P, et al. Characteristics and applications of micro-pixelated GaN-based light emitting diodes on Si substrates. Journal of Applied Physics 115, (2014).

- Wang B, et al. High‐Q plasmonic resonances: fundamentals and applications. Advanced Optical Materials 9, 2001520 (2021).