Supporting Information

Cobalt on Tungsten Titanium Carbide MXene: A Electrocatalyst for Industrial-Scale High Current Density Alkaline Hydrogen Evolution Reaction

Xiaopeng Liua,‡, Fan Yanga,‡, Deep M. Patela,‡, Mohammad Albloushia, Shan Jiangb, Christian J. Brecknerb, Connor W. Schroedera, Ruoyu Cuic,d, Tao Mae, Dapeng Jingf, Wenyu Huangc,d, Jeffrey T. Millerb,*, Wenzhen Lia,*, Luke T. Rolinga,*, Yue Wua,*

Correspondence to: yuewu@iastate.edu; roling@iastate.edu; wzli@iastate.edu; and jeffrey-t-miller@purdue.edu

Supplementary Fig. 1. Theoretical XRD of (a) W2TiAlC2 and (b) W2TiC2 simulated by VESTA; Comparison of experimental and calculated XRD from 2θ = 5° to 70° of (c) W2TiAlC2 and (d) W2TiC2; (e) Lattice structure model of W2TiAlC2 and W2TiC2 for the simulation, color code: Al (pink), W (cyan), Ti (dark blue), and C (dark brown).

Supplementary Fig. 2. SEM images of (a) Co/W2TiC2-600 and (b) Co/W2TiC2-700; TEM images of (c) Co/W2TiC2-600 and (d) Co/W2TiC2-700.

Supplementary Fig. 3. TEM image of Co/W2TiC2-500 showing lattice fringes of cobalt on the MXene surface.

Supplementary Fig. 4. XPS survey spectra of W2TiC2 and Co/W2TiC2 annealed at 500, 600, and 700℃.

Supplementary Fig. 5.  Co K-edge XANES from 7.700 to 7.750 keV of (a) Co F oil, CoO, and Co500; k2-Weighted and the magnitude (solid) and imaginary (dash) part of the Fourier transform of the Co K edge EXAFS of (b) Co foil, (c) CoO reference, and (d) Co/W2TiC2-500.

Supplementary Fig. 6. Linear sweep voltammetry (LSV) curves of the synthesized Co/W2TiC2-700 catalyst in (a) 1 M KOH, 1 M PBS, 0.5 M H2SO4 and (b) 0.1-1 M PBS. PBS stands for phosphate buffered saline.

Supplementary Fig. 7. LSV curves and Tafel slopes of Co/W2TiC2 catalysts, Co/WC and W2TiC2 in 0.5 M H2SO4.

Supplementary Fig. 8. (a) LSV curves of Co/W2TiC2-700 in 0.5 M H2SO4 at initial test and after leaving in electrolyte without applying current for 30 min; (b) TEM images of Co/W2TiC2-700 and (c) aggregation of Co after reacting in acidic electrolyte.

Supplementary Fig. 9. SEM images of Co/W2TiC2-700 after reacting in (a) 1 M KOH and (b) 0.5 M H2SO4.

Supplementary Fig. 10. LSV curves of H23 carbon paper, carbon paper with the Vulcan layer, and commercial 20% Pt/C compared with the Co/W2TiC2 catalysts in N2 saturated 1 M KOH;

Supplementary Fig. 11. High current density LSV curves of Co/W2TiC2-700 catalyst compared with commercial 40% Pt/C in N2 saturated 1 M KOH;

Supplementary Fig. 12. Cyclic voltammetry (CV) curves of W2TiC2 and Co/WC at different scan rates in a non-Faradaic region and electrochemical double-layer capacitance calculated from charging current density differences against scan rates plots.

Supplementary Fig. 13. CV curves of (a) Co/W2TiC2-700, (b) Co/W2TiC2-600, and (c) Co/W2TiC2-500 and (d) electrochemical double-layer capacitance of the catalysts.

Supplementary Note 1: Estimation of number of active sites from ECSA and comparison with loading mass derived quantities

The electrochemical active surface area (ECSA) can be obtained from electrochemical double-layer capacitance (Cdl), by dividing Cdl by the specific capacitance for a flat standard with 1 cm2 of real surface area (Cs). The metal plane value of smooth metal plane is generally found to be in the range of 20-60 µF cm−2 1, we conservatively using 60 µF cm−2 to estimate the number of active sites. The geometric area of the sprayed electrodes are 1 × 1 cm2, thus ECSA of the catalysts can be calculated as:

AECSA(Co/W2TiC2-700) = (55.47 mF/cm2) × 1 cm2 / (60 μF/cm2) = 924.5 cm2

AECSA(Co/W2TiC2-600) = (38.61 mF/cm2) × 1 cm2 / (60 μF/cm2) = 643.5 cm2

AECSA(Co/W2TiC2-500) = (11.76 mF/cm2) × 1 cm2 / (60 μF/cm2) = 196.0 cm2

Co NP number in Co/W2TiC2-700 was further calculated by converting the electrochemical surface area to the number of binding sites. On this catalyst, the hydrogen is considered binding to the W atoms close to the Co-W interfaces (most stable H-binding sites marked on the DFT Co nanoparticle/W2TiC2 model, Figure 5a) in the ECSA tests at non-Faradaic region, while under reaction condition, hydrogen is proposed forming at the Co-W interface sites due to the most stable W sites poisoned by strong binding of H. The specific surface area per W atom on the (111) plane of W2TiC2 can be calculated as: Sa(111) = √3/4 × a2 = 3.39 × 10-16 cm2 2. Thus, the number of W surface sites can be obtained as NW = ECSA / Sa(111). Considering the amount of such W sites adjacent to each Co particle, and the number of Co-W interface sites on each Co NP, the number of active sites can be obtained as:

NCo-W(ECSA) = (924.5 cm2 / 3.39 × 10-16 cm2) / 6 × 3 = 1.36 × 1018

The quantity of active sites was checked through calculations based on the actual loading mass of Co. Given that EXAFS analysis revealed in Co/W2TiC2-700 Co existing entirely in the form of nanoparticles, determination of NP amount can be to dividing the total count by the number of Co atoms within a single particle of around 0.9 nm size:

NCo NPs(loading mass) = (0.49 mg/cm2) × 1 cm2 / (28.01 g/mol) × NA / 22 = 4.79 × 1017

NCo-W(loading mass) = NCo NPs × 3 = 1.44 × 1018

In which the NA is Avogadro constant and NCo-W(loading mass) stands for the active sites number directly derived from Co loading amount. The values obtained from two methods were similar (1.36 × 1018 and 1.44 × 1018), this numerical approximations derived from both methods further substantiate the specific structure of Co on W2TiC2.

Supplementary Fig. 14. High current LSV curves of Co/W2TiC2-700 and commercial Pt/C paired with Ni foam in a 2 × 2 cm2 flow cell electrolyzer in 1 M KOH;

Supplementary Fig. 15. Chronopotentiometry curve of Co/W2TiC2-700 in 1 M KOH at a constant current density of 1000 mA/cm2 for 20 h.

Supplementary Fig. 16. Top views and side views of the optimized structure of: (a) clean W2TiC2; (b) Isolated Co@W2TiC2; (c) Co dimer@W2TiC2; (d) Co trimer@W2TiC2; (e) Co tetramer@W2TiC2. Color code: Co (pink), W (blue), C (dark grey), Ti (light grey).

Supplementary Note 2: Effect of Co-Co coordination environment and H* surface coverage on the H* binding strength

To investigate the effect of Co-Co coordination environment on the H* binding strength, DFT calculations were performed for H* coverage varying from 0.11 ML to 0.44 ML on different W2TiC2 surfaces (see methods section in the main text for details). We note that when geometric optimization calculations were performed with an initial guess of single H* placed symmetrically or asymmetrically on top or at the hollow sites involving Co atoms on all the considered Co/W2TiC2 surfaces (i.e., isolated, dimer, trimer, and tetramer of Co), H* always shifted to a different binding site (fcc site for isolated Co/W2TiC2 and Co dimer/W2TiC2; W top site for Co trimer/W2TiC2 and Co tetramer/W2TiC2). Combining these observations with the most stable binding sites of H* on respective materials (Supplementary Figure 18), we note that H* does not prefer to bind with a single Co atom or ensemble of Co atoms, and therefore the expected active site for the HER chemistry at the isolated, dimer, trimer, and tetramer of Co on W2TiC2 might be the Co-W interface (same as Co NP) .

Supplementary Figure 17b summarizes trends in the adsorption free energies of H* (GnH*) for the most stable binding geometries across all the considered Co/W2TiC2 surfaces and at H* coverages ranging from 0.11 ML to 0.44 ML. The snapshots of the most stable binding geometries of H* are provided in Figure S18. The qualitative trend in the adsorption free energies across different surfaces remains same at all the considered H* coverages – H* binds weakest on isolated Co/W2TiC2 and strongest on the clean W2TiC2, with an exception at 0.22 ML H* coverage where stronger H* binding was observed on Co tetramer/W2TiC2 compared to that on clean W2TiC2 with differential adsorption free energies of 0.39 eV. Such coverage sensitive trend in the GnH* across different materials indicates that the trend in the HER activity across different W2TiC2-based materials might be sensitive to the concentration of protons in the solution. This is evident from the significantly different experimental LSV profiles in the presence of 1 M KOH (Figure 4a) and 0.5 M H2SO4 (Figure 4b). Further, comparing the overall trend in the GH* across different Co/W2TiC2 surfaces, H* binding becomes stronger as the Co starts aggregating, i.e., H* binds stronger on Co tetramer/W2TiC2 (GH*: -0.49 eV) compared to that on isolated Co/W2TiC2 (GH*: -0.38 eV). This trend in H* binding is explained by a strong correlation between GH* and the d-band center of the W closest to H* (Figure 5b). This correlation suggests that the addition of Co on W2TiC2 surface alters the electronic structure of the interfacial W atoms, which ultimately impacts the binding strength of H* at the Co-W interface.

Supplementary Fig. 17. (a) Formation energy of Co cluster (ECo, eV) for different configurations of Co on W2TiC2 at respective H* coverages (ML), (b) Cumulative adsorption free energy of nH* (GnH*, eV) on different W2TiC2 surfaces at respective H* coverages (ML). All the data points for a given surface coverage of H* are joined by a solid line for ease of visualization of the overall trend in both the figures. The snapshots of the most stable optimized geometries of respective systems are shown in Figure S18.

Supplementary Fig. 18. Top views of the most stable binding geometries of H* on isolated Co, Co dimer, Co trimer, and Co tetramer at H* coverage of (a)-(d) 0.11 ML, (e)-(h) 0.22 ML, (i)-(l) 0.33 ML, and (m)-(p) 0.44 ML. Atom color code: H (yellow), Co (pink), W (blue), C (dark grey), Ti (light grey).

Supplementary Fig. 19. (a), (b) Top view and side view of Co nanoparticle/W2TiC2 system used for theoretical calculations. Atom color code: H (yellow), Co (pink), W (blue), C (dark grey), Ti (light grey).

Supplementary Fig. 20. High current LSV curves of Co/W2TiC2-700 and commercial Pt/C paired with IrO2 in the flow cell electrolyzer in 1 M KOH at 60℃.

Supplementary Fig. 21. Flow cell electrolyzer tests at high temperature. (a) Chronopotentiometry profiles of Co/W2TiC2-700 (paired with IrO2) at 50-400 mA/cm2 in 1 M KOH at 60℃ compared with Pt/C; (c) Comparison of hydrogen production and hydrogen Faradic efficiency on Co/W2TiC2-700 and Pt/C at 50-400 mA/cm2 at 60℃.

Supplementary Note 3: Energy efficiency analysis of flow cell tests

To further assess the performance of the flow cell electrolyzer using Co/W2TiC2 as the catalyst, the energy efficiency was calculated for the IrO2||Co/W2TiC2-700 at 60℃. The equation for cell energy efficiency is:

ηe (Energy Efficiency) = ηv (Voltage Efficiency) × ηF (Faradaic Efficiency)

While energy efficiency is equal to equilibrium cell potential divided by the cell voltage. For water electrolyzer, the equilibrium cell potential is 1.229 V at room temperature (20℃) and 1.218 V at 60℃. At 400 mA/cm2, the averaged H2 faradaic efficiency in 3 h on Co/W2TiC2-700 is 94.88%, and cell voltage is 2.85 V, thus the energy efficiency can be calculated as:

ηe (400mA/cm2) = (1.218V / 2.85 V) × 94.88% = 40.55%

Conventional alkaline water electrolyzers (AWE) are capable of achieving energy efficiencies ranging of 52%-69% when operating at current densities of 200-400 mA/cm² 3. The primary difference is posited to be the internal resistance attributed to the cation exchange membrane (CEM) that conducts K+ ions as compared to the liquid potassium hydroxide (KOH) utilized in AWEs. Therefore, the internal resistance led voltage drop was subtracted from the total cell voltage and iR-free voltage was calculated. Using EIS measured internal resistance values of 0.977 Ω, 1.02 Ω, and 0.967 Ω, the iR-free cell voltage at 200, 300, and 400 mA/cm2 are 1.85 V, 2.05 V, and 2.46 V, respectively. The corresponding energy efficiencies are:

ηe (400mA/cm2) = (1.218V / 2.46 V) × 94.88% = 46.98%

ηe (300mA/cm2) = (1.218V / 2.07 V) × 94.61% = 56.21%

ηe (200mA/cm2) = (1.218V / 1.85 V) × 99.23% = 65.33%

While the iR-free ηe for IrO2||Pt at the same conditions are 44.63%, 52.08% and 58.31%. Also, the efficiency values of IrO2||Co/W2TiC2-700 after excluding the impact of internal resistance are comparable with state-of-the-art water electrolyzers, indicating the high efficiency of this catalyst in the flow cell system.

Supplementary Table 1. Calculated lattice parameters and atomic coordinates for W2TiAlC2 and W2TiC2 by fitting the experimental XRD

| W2TiAlC2 |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Lattice parameters |  |  |  |  |  |  |  |  |  |  |  |  |
|  | a (Å) |  | b (Å) |  | c (Å) |  | α (°) |  | β (°) |  | γ (°) |  |
|  | 2.98338 |  | 2.98338 |  | 18.73010 |  | 90 |  | 90 |  | 120 |  |
| Atomic coordinates |  |  |  |  |  |  |  |  |  |  |  |  |
|  | W(1) | W(2) | W(3) | W(4) | Ti(1) | Ti(2) | Al(1) | Al(2) | C(1) | C(2) | C(3) | C(4) |
| x | 0.6667 | 0.3333 | 0.3333 | 0.6667 | 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.3333 | 0.6667 | 0.6667 | 0.3333 |
| y | 0.3333 | 0.6667 | 0.6667 | 0.3333 | 0.0000 | 0.0000 | 0.0000 | 0.0000 | 0.6667 | 0.3333 | 0.3333 | 0.6667 |
| z | 0.3648 | 0.6352 | 0.8648 | 0.1352 | 0.5000 | 0.0000 | 0.2500 | 0.7500 | 0.4776 | 0.5224 | 0.9776 | 0.0224 |
| W2TiC2 |  |  |  |  |  |  |  |  |  |  |  |  |
| Lattice parameters |  |  |  |  |  |  |  |  |  |  |  |  |
|  | a (Å) |  | b (Å) |  | c (Å) |  | α (°) |  | β (°) |  | γ (°) |  |
|  | 2.98660 |  | 2.98660 |  | 30.08700 |  | 90 |  | 90 |  | 120 |  |
| Atomic coordinates |  |  |  |  |  |  |  |  |  |  |  |  |
|  | W(1) | W(2) | W(3) | W(4) | Ti(1) | Ti(2) | C(1) | C(2) | C(3) | C(4) |  |  |
| x | 0.6667 | 0.3333 | 0.3333 | 0.6667 | 0.0000 | 0.0000 | 0.3333 | 0.6667 | 0.6667 | 0.3333 |  |  |
| y | 0.3333 | 0.6667 | 0.6667 | 0.3333 | 0.0000 | 0.0000 | 0.6667 | 0.3333 | 0.3333 | 0.6667 |  |  |
| z | 0.4063 | 0.5937 | 0.9063 | 0.0937 | 0.5000 | 0.0000 | 0.4776 | 0.5224 | 0.9776 | 0.0224 |  |  |

Supplementary Table 2. Quantitative information of the XANES data and EXAFS fits

| Samples | Pre-edge Energy, keV | XANES Energy, keV | Scatter | CN | R, Å | δ2 (x103) | E0, eV |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Co Foil (Co0 ref) | - | 7.709 | Co-Co | 12 | 2.49 |  |  |
| CoO (Co2+ ref) | 7.7084 | 7.7166 | Co-O | 6 | 2.13 |  |  |
| Co/W2TiC2-500 | - | 7.7087 | Co-Co | 2.8 | 2.48 | 8.0 | -4.4 |
|  |  |  | Co-O | 2.1 | 1.97 | 6.0 | -2.8 |
| Co/W2TiC2-600 | - | 7.7087 | Co-Co | 3.3 | 2.49 | 8.0 | -4.8 |
|  |  |  | Co-O | 1.1 | 1.96 | 6.0 | 1.1 |
| Co/W2TiC2-700 | - | 7.7087 | Co-Co | 3.8 | 2.47 | 10.0 | -5.0 |
|  |  |  | Co-O | - | - | - | - |

Supplementary Table 3. Summary of distribution of Co on the different catalysts

| Catalyst | Single sites | NPs | NPs true CN | NPs size |
| --- | --- | --- | --- | --- |
| Co/W2TiC2-700 | - | 100% | 3.8 | 0.9 nm |
| Co/W2TiC2-600 | ~25% | ~75% | 4.4 | 1.0 nm |
| Co/W2TiC2-500 | ~50% | ~50% | 5.6 | 1.5 nm |

Supplementary Table 4. ICP-OES elemental analysis of the Co/W2TiC2 samples

| Catalysts | Co Weight% | Averaged Co Weight% |
| --- | --- | --- |
| Co/W2TiC2-700 | 4.27% | 4.3% |
|  | 4.36% |  |
|  | 4.28% |  |
| Co/W2TiC2-600 | 4.04% | 4.0% |
|  | 3.89% |  |
|  | 3.95% |  |
| Co/W2TiC2-500 | 4.10% | 4.1% |
|  | 4.15% |  |
|  | 4.01% |  |

Supplementary Table 5. The Co and total loading mass of different catalysts on the electrodes

| Catalysts | Loading of catalyst | Loading of Co |
| --- | --- | --- |
| Co/W2TiC2-700 | 12.3 mg/cm2 | 0.49 mg/cm2 |
| Co/W2TiC2-600 | 12.9 mg/cm2 | 0.52 mg/cm2 |
| Co/W2TiC2-500 | 12.8 mg/cm2 | 0.51 mg/cm2 |
| Co/WC | 14.7 mg/cm2 | 0.59 mg/cm2 |
| W2TiC2 | 12.5 mg/cm2 | - |

Supplementary Table 6. Summary of HER activity catalyzed by different Co/MXene catalysts

| Catalyst | Overpotential @ 10 mA/cm2 | Tafel slope |
| --- | --- | --- |
| Co/W2TiC2-700 | 62.58 mV | 44.34 mV/dec |
| Co/W2TiC2-600 | 88.78 mV | 50.78 mV/dec |
| Co/W2TiC2-500 | 99.34 mV | 71.00 mV/dec |
| Co/WC | 211.93 mV | 166.30 mV/dec |
| W2TiC2 | 291.11 mV | 268.04 mV/dec |

Supplementary Table 7. Summary of HER activity catalyzed by Co/MXene catalysts and Pt

| Samples | Overpotential @ 10 mA/cm2 | Overpotential @ 100 mA/cm2 |
| --- | --- | --- |
| Co/W2TiC2-700 | 62.58 mV | 191.18 mV |
| Co/W2TiC2-600 | 88.78 mV | 231.90 mV |
| Co/W2TiC2-500 | 99.34 mV | 349.60 mV |
| Co/WC | 211.93 mV | 387.03 mV |
| W2TiC2 | 291.11 mV | 476.21 mV |
| Commercial 40% Pt/C | 51.74 mV | 238.02 mV |

Supplementary Table 8. Summary of high current density HER activity catalyzed by Co/W2TiC2-700 and Pt

| Overpotential | Commercial 40% Pt/C | Co/W2TiC2-700 |
| --- | --- | --- |
| η @ 10 mA/cm2 | 51.74 mV | 62.58 mV |
| η @ 100 mA/cm2 | 238.02 mV | 191.18 mV |
| η @ 200 mA/cm2 | 312.41 mV | 245.79 mV |
| η @ 300 mA/cm2 | 362.49 mV | 286.33 mV |
| η @ 400 mA/cm2 | 398.65 mV | 309.47 mV |
| η @ 500 mA/cm2 | 423.90 mV | 330.43 mV |
| η @ 1000 mA/cm2 | 499.19 mV | 407.72 mV |

Supplementary Table 9. Comparison of alkaline HER performance reported for cobalt and transition metal carbide based non-noble metal catalysts

| Catalysts | η @ 10 mA/cm2 (mV) | Tafel slope (mV/dec) | η @ 100 mA/cm2 (mV) | η @ 500 mA/cm2 (mV) | η @ 1000 mA/cm2 (mV) | Stability | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Co/W2TiC2Tx-700 | 62.58 | 44.34 | 191.18 | 330.43 | 407.72 | 500h @10 mA/cm2 100h @1000 mA/cm2 | This work |
| NiFe-LDH/Ti3C2Tx/NF | 132 | 70 | - | 205 | - | 280h @10 mA/cm2 200h @1000 mA/cm2 | [4] |
| MoS2@Mo2CTx | 176 | 207 | - | - | - | 8h @0.400 V | [5] |
| Ni0.9Co0.1@Nb-doped Ti3C2Tx | 43.4 | 116 | - | - | - | 50h @10 mA/cm2 | [6] |
| Nb4C3T | 398 | 122 | - | - | - | 50h @0.398 V (~10 mA/cm2) | [7] |
| WP–W2C | 43 | 42.11 | 139 | - | 560 | 40h @350 mA/cm2 60h @570 mA/cm2 60h @1000 mA/cm2 | [8] |
| Mo2C@C | 47 | 71 | - | - | - | - | [9] |
| MoS2–Mo2C | 56 | 64.2 | 171 | - | 446 | - | [10] |
| HC-MoS2/Mo2C | - | - | - |  | 441 | 24h @500 mA/cm2 | [11] |
| MoS2–Mo2C | - | 43 | - | 191 | 220 | 24h @200 mA/cm2 | [12] |
| Mo2C/MoC/carbon nanotube | 82 | 42 | - | 201 | 233 | 336h @1000 mA/cm2 | [13] |
| MoC–Mo2C-790 | 98.2 | 59 | - | 292 | - | 100h @100 mA/cm2 50h @300 mA/cm2 50h @500 mA/cm2 2400h @1000 mA/cm2 | [14] |
| Co2P/N@Ti3C2Tx@NF | 15 | 30 | - | - | - | 4h @10-80 mA/cm2 | [15] |
| CoP/Ti3C2Tx | 113 | 57 | - | - | - | 24h @50 mA/cm2 | [16] |
| Co7Se8/Ti3C2Tx | 270 | 128.5 | - | - | - | 24h @50 mA/cm2 | [16] |
| Co-CeO2 | - | - | 132 | 215 | - | 14h @150 mV (~40 mA/cm2) 14h @200 mV (~70 mA/cm2) | [17] |
| Co3Mo/Cu | 12 | 40 | 96 @ 400 mA/cm2 |  |  | 1000h @60 mA/cm2 500h @210 mA/cm2 | [18] |
| Co-Mo5N6 | 19 | 29 | - | - | 280 | 10h @5000 mA/cm2 | [19] |
| CoP/MoP@NC/CC | 94 | 40 | - | - | 475 | - | [20] |
| CoP | - | 78 | 141 | 243 | 290 | 300h @1000 mA/cm2 | [21] |
| N−Co2P/CC | 34 | 51 | - | - | - | - | [22] |
| Co-B-P/NF | 42 | 42.1 | - | - | 165 | 20h @1000 mA/cm2 | [23] |
| A-NiCo LDH | 36 | 57 | 151 | 286 | 381 | 72h @1000 mA/cm2 72h @1000 mA/cm2 | [24] |
| NiCo/NiCo-OH | 19 | 42 | 104 | 184 | - | 24h @500 mA/cm2 | [25] |

Supplementary References

1.	McCrory, C. C. L., Jung, S., Peters, J. C., Jaramillo, T. F., Benchmarking heterogeneous electrocatalysts for the oxygen evolution reaction. J. Am. Chem. Soc. 135, 16977-16987 (2013).

2.	Bergeret, G., Gallezot, P., Handbook of Heretogeneous Catalysis. vol. 2, pp. 738-765 (Wiley-VCH, 2008).

3.	Carmo, M., Fritz, D. L., Mergel, J., Stolten, D., A comprehensive review on PEM water electrolysis. Int. J. Hydrogen Energy 38, 4901-4934 (2013).

4.	Yu, M. et al., A hierarchically porous and hydrophilic 3D nickel–iron/MXene electrode for accelerating oxygen and hydrogen evolution at high current densities. Nano Energy 63, 103880 (2019).

5.	Ren, J. et al., 2D organ-like molybdenum carbide (MXene) coupled with MoS2 nanoflowers enhances the catalytic activity in the hydrogen evolution reaction. CrystEngComm 22, 1395-1403 (2020).

6.	Du, C.-F. et al., Synergy of Nb doping and surface alloy enhanced on water–alkali electrocatalytic hydrogen generation performance in Ti-based MXene. Adv. Sci. 6, 1900116 (2019).

7.	Tan, Y. et al., Nb4C3Tx (MXene) as a new stable catalyst for the hydrogen evolution reaction. Int. J. Hydrogen Energy 46, 1955-1966 (2021).

8.	Huang, J., Jian, C., Cai, Q., Hong, W., Liu, W., A large scale self-supported WP–W2C nanoporous network for efficient hydrogen evolution reaction in alkaline media. J. Mater. Chem. A 10, 10990-10997 (2022).

9.	Chen, Y.-Y. et al., Pomegranate-like N,P-doped Mo2C@C nanospheres as highly active electrocatalysts for alkaline hydrogen evolution. ACS Nano 10, 8851-8860 (2016).

10.	Jian, C., Cai, Q., Liu, W. J. C. C., A three-dimensional macroporous framework molybdenum disulfide–carbide heterojunction for highly efficient electrocatalytic hydrogen evolution at high current densities. Chem. Commun. 57, 11819-11822 (2021).

11.	Zhang, C. et al., High-throughput production of cheap mineral-based two-dimensional electrocatalysts for high-current-density hydrogen evolution. Nat. Commun. 11, 3724 (2020).

12.	Luo, Y. et al., Morphology and surface chemistry engineering toward pH-universal catalysts for hydrogen evolution at high current density. Nat. Commun. 10, 269 (2019).

13.	Li, C. et al., Ultrafast self-heating synthesis of robust heterogeneous nanocarbides for high current density hydrogen evolution reaction. Nat. Commun. 13, 3338 (2022).

14.	Liu, W. et al., A durable and pH-universal self-standing MoC–Mo2C heterojunction electrode for efficient hydrogen evolution reaction. Nat. Commun. 12, 6776 (2021).

15.	Lv, Z. et al., Co‐constructing interfaces of multiheterostructure on MXene (Ti3C2Tx)‐modified 3D self‐supporting electrode for ultraefficient electrocatalytic HER in alkaline media. Adv. Funct. Mater. 31, 2102576 (2021).

16.	Selvam, N. C. S. et al., MXene supported CoxAy(A=OH, P, Se) electrocatalysts for overall water splitting: unveiling the role of anions in intrinsic activity and stability. J. Mater. Chem. A 7, 27383-27393 (2019).

17.	Jiang, S. et al., Promoting formation of oxygen vacancies in two-dimensional cobalt-doped ceria nanosheets for efficient hydrogen evolution. J. Am. Chem. Soc. 142, 6461-6466 (2020).

18.	Shi, H. et al., Spontaneously separated intermetallic Co3Mo from nanoporous copper as versatile electrocatalysts for highly efficient water splitting. Nat. Commun. 11, 2940 (2020).

19.	Lin, F. et al., Electrocatalytic hydrogen evolution of ultrathin Co‐Mo5N6 heterojunction with interfacial electron redistribution. Adv. Energy Mater. 10, 2002176 (2020).

20.	Tang, Y.-J. et al., Solid-phase hot-pressing of POMs-ZIFs precursor and derived phosphide for overall water splitting. Appl. Catal., B 245, 528-535 (2019).

21.	Li, Y. et al., Bifunctional porous cobalt phosphide foam for high-current-density alkaline water electrolysis with 4000-h long stability. ACS Sustainable Chem. Eng. 8, 10193-10200 (2020).

22.	Men, Y. et al., Tailoring the electronic structure of Co2P by N doping for boosting hydrogen evolution reaction at all pH values. ACS Catal. 9, 3744-3752 (2019).

23.	Sun, H. et al., Superhydrophilic amorphous Co–B–P nanosheet electrocatalysts with Pt-like activity and durability for the hydrogen evolution reaction. J. Mater. Chem. A 6, 22062-22069 (2018).

24.	Yang, H., Chen, Z., Guo, P., Fei, B., Wu, R., B-doping-induced amorphization of LDH for large-current-density hydrogen evolution reaction. Appl. Catal., B 261, 118240 (2020).

25.	Zhu, W. et al., NiCo/NiCo–OH and NiFe/NiFe–OH core shell nanostructures for water splitting electrocatalysis at large currents. Appl. Catal., B 278, 119326 (2020).