Supplementary Information

Ethanol selectively inducing the separation of single-chirality carbon nanotubes from polymer-dispersed mixture

Dehua Yang,1,2,6,* Xuan Chang,1,2,6 Xiaoyang Yuan,1,2 Xiaofei Yang,1,2 Linhai Li,3,4  Wei Xi,3,4 Huaping Liu,3,4,5,* and Jianhui Chen1,2*

1Advanced Passivation Technology Lab, College of Physics Science and Technology, Hebei University, Baoding 071002, China.

2Province-Ministry Co-Construction Collaborative Innovation Center of Hebei Photovoltaic Technology, College of Physics Science and Technology, Hebei University, Baoding 071002, China.

3Beijing National Laboratory for Condensed Matter Physics, Institute of Physics, Chinese Academy of Sciences, Beijing 100190, China.

4Center of Materials Science and Optoelectronics Engineering, and School of Physical Sciences, University of Chinese Academy of Sciences, Beijing 100049, China.

5Songshan Lake Materials Laboratory, Dongguan, Guangdong, 523808, China.

6These authors contributed equally: Dehua Yang, Xuan Chang.

e-mail: yangdehua@hbu.edu.cn; liuhuaping@iphy.ac.cn; chenjianhui@hbu.edu.cn.

a

b

Supplementary Figure 1. Chiral enhancement induced by ethanol. a) Optical absorption spectra of remained SWCNTs in dispersions after removing the reaggregated SWCNTs at different toluene/ethanol ratios. b) Photograph of SWCNT dispersions after standing for 3 hours with and without ethanol. Flocculent agglomerates emerge in the sample with ethanol/toluene ratio of 0.08:1. “Tol.” and “eth.” are abbreviation for “toluene” and “ethanol”, respectively.

a

b

Supplementary Figure 2. Comparison of separation purity enhancement with/without adding ethanol over time. a) Optical absorption spectra of remained SWCNTs in dispersions after allowing to stand for a duration with/without addition of ethanol. After separation using traditional selective dispersion method, ethanol was added (0.02:1). The SWCNT dispersion with ethanol was allowed to stand for 48 h, followed by centrifugation for 5 min at 8500 g to remove the reaggregated SWCNTs. As for the control group, SWCNTs separated by the traditional method were allowed to stand for 48 h without ethanol, and then centrifuged for 5 min at 8500 g. The SWCNT concentration of the sample with ethanol is relatively lower than that of the control group. It indicates that the addition of even a trace of ethanol enhances the reaggregation. b) Normalized absorbance of corresponding SWCNT dispersions in a). The relative contents of each semiconducting (n, m) species are nearly unchanged. But the M11 peaks decrease after standing for a duration, suggesting enhancement in semiconducting purity. Moreover, the decrease in M11 peaks is more distinct in the sample treated with ethanol. It demonstrates that the selective reaggregation is primarily induced by ethanol rather than standing.

a

b

c

Supplementary Figure 3. Variation of SWCNTs remaining in the solutions after standing for different times at ethanol/toluene ratio of 0.08:1. a) Optical absorption spectra of SWCNTs after standing for 0-96 hours followed by centrifugation to remove the reaggregated nanotubes. b) Relative contents of different (n, m) species with standing time. c) Decrease in SWCNT concentration over time at 0.08:1 eth./tol. The percentage decrease in SWCNT concentration is calculated by dividing the sum of the absorption peak areas in the range of 950-1400 nm by the sum of the initial S11 peak areas: 1 - Area (t)/Area (t = 0), where the Area (t) represent the sum of S11 peak areas of SWCNT dispersions achieved by standing for t hours with ethanol. The decrease rate is the slope of concentration decrease.

Supplementary Figure 4. Comparison of the separated results with/without the initially formed flocculent agglomerates. HiPco was dispersed with PFO followed by centrifugation to remove the undispersed SWCNTs. Then, ethanol was added (0.08:1, ethanol/toluene). The SWCNT dispersions were divided into two parts. After standing for 3 h, flocculent agglomerates that are visible to naked eyes were formed. We eliminated the agglomerates in one of the dispersions, while leaving the agglomerates intact in the other dispersion. Then, the two dispersions were allowed to stand for another 45 h, followed by centrifugation to remove the reaggregated SWCNTs. Clearly, without the initially formed agglomerates, the selectivity and efficiency of reaggregation decreased, suggesting that the agglomerates contribute to selectivity reaggregation.

Supplementary Figure 5. Optical absorption spectra of remained SWCNTs in dispersions after mixing with undispersed SWCNTs for different durations.

a

b

Supplementary Figure 6. The relationship between reaggregation rate and amount of undispersed SWCNTs. a) Optical absorption spectra of the SWCNTs remaining in solutions after standing for 48 h with different amount of undispersed SWCNTs. The undispersed SWCNTs were collected from the components that were not dispersed during selective dispersion of raw HiPco with PFO. They were added into the dispersions at various concentrations followed by bath sonication and stirring. b) Proportion of decrease in SWCNT concentration as a function of undispersed SWCNT concentration after standing for 48 h. The decrease in SWCNT concentration is calculated according to the peak area in S11 region (950-1400 nm): 1 - Area (c)/Area (c = 0), where Area (c) represents the sum of peak area of SWCNTs remaining in solutions after standing for 48 h at a specific undispersed SWCNT concentration. The amount of undispersed SWCNT affect the rate of reaggregation. As the concentration of undispersed SWCNT increases, the concentration of SWCNTs remaining in the solution decreases faster, confirming the accelerated reaggregation process. Compared with the initial SWCNT concentration of 0.3 mg/ml, a small amount of undispersed SWCNT induced significant selective reaggregation after standing for 48 h. When all the undispersed SWCNTs generated during the selective dispersion are employed, the rate of reaggregation reached a plateau.

a

b

Supplementary Figure 7. Selective reaggregation through combining ethanol and undispersed SWCNTs. a) Optical absorption spectra of SWCNTs remaining in dispersion after standing with undispersed SWCNTs in 0.08:1 eth./tol. solutions for different durations. b) Optical absorption spectra of separated SWCNTs by simultaneously employing ethanol and undispersed SWCNTs to dispersions and allowing them to stand for 48 h.

Supplementary Figure 8. Structure illustrations of the commercially available polymers used in this work.

Supplementary Figure 9. Chiral separation results of CoMoCAT(6, 5) and CoMoCAT(7, 6) in PFO and PFDD systems.

Supplementary Figure 10. Schematic diagram of the separation process of (7, 6) and (9, 7) SWCNTs using PFO. (7, 6) and (9, 7) were separated from CoMoCAT (7, 6) and Plasma-SWCNTs, respectively. Their separation procedures are the same. For instance, CoMoCAT(7, 6) and AP-SWCNTs were dispersed with PFO in toluene, respectively. The AP-SWCNT dispersion was centrifuged at 8500 g for 30 min. The undispersed AP-SWCNT pellet were collected. After centrifugation for 2 h at 26000 g, the supernatant of CoMoCAT(7, 6) was collected as the CoMoCAT(7, 6) dispersion. Note that this centrifugation is relatively intensive to ensure that no small bundles remain in the supernatant, because these small bundles may preferentially reaggregate during the subsequent separation processes and decrease the separation purity. Then, the undispersed AP-SWCNTs were added to the supernatant of CoMoCAT(7, 6) dispersion. After standing for 3-6 h, the target (n, m) species reaggregated onto the AP-SWCNT pellet. Then, the pellet were redispersed with 0.1-mg/ml PFO, followed by a centrifugation for 2 h at 26000 g. PFO selectively disperse the target (n, m) species attaching on AP-SWCNTs. Eventually, the supernatant of the redispersed SWCNTs was collected. The corresponding optical absorption of this procedure is shown in Supplementary Fig. 11. Notably, when separating (7, 6) in the PFDD system, the above procedure is not needed, because the PFDD has a better chiral selectivity for (7, 6) than PFO. Single-chirality (7, 6) can be obtained using the simple procedure in Fig. 2a through applying ethanol and undispersed SWCNTs to PFDD-dispersed CoMoCAT(7, 6). The results are shown in Supplementary Fig. 9.

Supplementary Figure 11. Optical absorption spectra of the pellet and supernatant obtained by mixing undispersed AP-SWCNTs with CoMoCAT(7, 6) dispersion. The pellet and supernatant correspond to the sample indicated by the red and blue boxes exhibited in Supplementary Fig. 10. CoMoCAT(7, 6) was dispersed with PFO and centrifuged, with the supernatant collected as the CoMoCAT(7, 6) dispersion. The as-prepared CoMoCAT(7, 6) dispersion is plotted in black curve. PFO selectively dispersed semiconducting SWCNTs in CoMoCAT(7, 6), with the content of (7, 6) being highest in the supernatant. In contrast, PFO cannot effectively disperse AP-SWCNTs, leading to most of the AP-SWCNTs remaining in the undispersed fraction. Then, the undispersed AP-SWCNT pellets and ethanol were added into the CoMoCAT(7, 6) dispersion. After standing for 3 h, the mixture was centrifuged. The resulting pellet (blue curve) and supernatant (red curve) were exhibited. After mixing with undispersed AP-SWCNTs, (7, 6) SWCNTs remaining in the CoMoCAT(7, 6) dispersion distinctly decreased. A large number of (7, 6) reaggregated onto undispersed AP-SWCNTs. These reaggregated (7, 6) and AP-SWCNTs were dispersed with PFDD for optical absorption characterization (blue curve). Distinct S11 peak of (7, 6) along with the S22 peaks of large-diameter SWCNTs were observed in the pellet (blue curve). Finally, these pellet containing (7, 6) and large-diameter SWCNTs were redispersed with PFO. PFO selectively dispersed (7, 6) SWCNTs as shown in Fig. 3c. Given that there are no (7, 6) SWCNTs in raw AP-SWCNTs, the redispersed (7, 6) from the pellet must arise from the selective reaggregation.

Supplementary Figure 12. Separation procedure of (8, 6) and (10, 6) SWCNTs. a) The rinse procedure to remove polymer. (10, 6)/(8, 6)-enriched sample was obtained through the procedure shown in Fig. 2a in a PFO-BPy system. Ethanol was added (0.2:1, eth./tol.) to induce the precipitation of (10, 6)/(8, 6). After a centrifugation for 5 min at 8500 g, the supernatant containing PFO-BPy was removed. Then, net toluene at 80 ºC was added to dissolve the residual polymer, followed by removal of this toluene solution. Subsequently, net toluene was again added to the SWCNT pellet followed by a bath sonication for 10 min to redisperse the SWCNTs in the pellet. Then, ethanol was added and the rinse step was repeated for 10 times. the PFO-BPy was removed as much as possible. b) The iterative separation procedure of (8, 6) and (10, 6) SWCNTs. The (10, 6)/(8, 6) pellet was used as the starting materials. 0.05-mg/ml PFO was applied to redisperse the pellet. PFO exhibits high chiral selectivity for (7, 5), (7, 6), (8, 6) and (8, 7), as shown in Fig. 1. So, (8, 6) was selectively dispersed in the PFO solution via tip-sonication for 40 min at 30% amplitude followed by centrifugation for 1 h at 26000 g. Then, the pellet was rinsed with net toluene to remove the residual PFO. Eventually, the undispersed SWCNTs in pellet was redispersed with PFO-BPy (0.3 mg/ml) for 30 min at 30% amplitude by tip homogenizer, followed by centrifugation for 30 min at 8500 g, to obtain (10, 6) SWCNTs.

Supplementary Figure 13. Evaluation of purities of separated single-chirality (n, m) species. The purities were calculated as the ratio of the S11 peak area of target (n, m) species to the sum of peaks according to the formula: Purity (n, m) = Area (n, m)/∑Area (n, m).

b

a

Supplementary Figure 14. Separation results of large-diameter SWCNTs at different ethanol concentrations. a) Optical absorption spectra of remained SWCNTs in dispersions after removing the reaggregated SWCNTs at different toluene/ethanol ratios. The mass ratio of initial raw SWCNT and polymer is 0.3/0.5. b) Photograph of SWCNT dispersions after standing for 3 h with and without ethanol. Flocculent agglomerates emerge in the sample with ethanol/toluene ratio of 0.08:1.

a

b

c

d

e

f

Supplementary Figure 15. Semiconducting SWCNTs separated at different SWCNT/polymer ratios. a)-c) Normalized optical absorption spectra of large-diameter SWCNTs separated at different SWCNT/polymer ratios. e)-f) Optical absorption spectra of corresponding samples. We prepared three groups of dispersions with different initial SWCNT concentrations of 0.3 mg/ml, 0.4 mg/ml and 0.5 mg/ml, while maintaining a fixed polymer concentration of 0.5 mg/ml. After centrifugation removing the undispersed SWCNTs, ethanol was added to each of the supernatant at the ethanol/toluene ratio of 0.08:1 and the dispersions were left to stand for 0-36 h. Then, the reaggregated SWCNTs were eliminated by centrifuge at 8500 g for 5 min. Each sample was diluted to the same volume and characterized by optical absorption for comparison.

Supplementary Figure 16. Relationship between standing time after adding ethanol and ACNT of separated SWCNTs at different SWCNT/polymer ratios corresponding to Supplementary Fig. 15.

a

b

c

d

Supplementary Figure 17. Raman spectra of large-diameter SWCNTs achieved by traditional method and the SWCNTs separated by introducing ethanol at ethanol/toluene ratio of 0.08:1 and allowing to stand for 36 h. The spectra were excited at the wavelength of 633 nm a) and 532 nm b). G- and D-band excited at 633 nm and 532 nm are exhibited in c) and d), respectively. Given that the metallic SWCNTs content is extremely low, and the diameters of semiconducting SWCNTs that exhibit S33 peaks at 633 nm are close to 2 nm, it is reasonable that the intensity of Raman spectra excited at 633 nm is dramatically lower than the Raman intensity excited at 532 nm.

Supplementary Figure 18. Optical absorption spectra of large-diameter SWCNTs separated by combining ethanol and undispersed SWCNTs. Raw AP-SWCNTs was dispersed with PFO-BPy at the SWCNT/polymer mass ratio of 0.5/0.5 and allowed to stand with ethanol (0.08:1) and undispersed SWCNTs for 48 h, followed by a centrifugation to eliminate undispersed SWCNTs and reaggregated ones.

500 nm

a

b

c

d

500 nm

Supplementary Figure 19. Length distribution of SWCNTs prepared by the traditional method and the selective reaggregation method. a) SEM image of SWCNTs separated by the traditional method. SWCNTs were dispersed with PCz and centrifuged. The supernatant was collected and its length distribution is exhibited in c). b) SEM image of SWCNTs separated by introducing ethanol and undispersed SWCNTs. SWCNTs that dispersed with PCz were mixed with ethanol and the undispersed SWCNTs for 6h, followed by centrifugation. The length distribution of the supernatant is exhibited in d).

Table S1. Separation parameters of various (n, m) species through selective reaggregation.

| Chirality | SWCNT | Polymer | Ethanol/toluene | Standing time |
| --- | --- | --- | --- | --- |
| (6, 5) | 0.3 mg/ml CoMoCAT(6, 5) | 1 mg/ml PFO-BPy | 0.08:1 | 3 h |
| (7, 5) | 0.3 mg/ml CoMoCAT(6, 5) | 1 mg/ml PFO | 0.04:1 | 48 h |
| (7, 5) | 0.3 mg/ml CoMoCAT(6, 5) | 0.3 mg/ml PCz | 0.04:1 | 48 h |
| (7, 5) | 0.3 mg/ml HiPco | 1 mg/ml PFO | 0.08:1 | 48 h |
| (8, 7) | 0.3 mg/ml HiPco | 1.3 mg/ml PFO | 0.02:1 | 48 h |
| (7, 6)* | 0.3 mg/ml CoMoCAT(7, 6) | 0.5 mg/ml PFO | 0.02:1 (mixing with undispersed AP-SWCNT ) | 6 h (mixing with undispersed AP-SWCNTs) |
| (7, 6) | 0.3 mg/ml CoMoCAT(7, 6) | 0.3 mg/ml PFDD | 0.04:1 | 12 h |
| (9, 7)* | 0.3 mg/ml Plasma | 0.3 mg/ml PFO | 0.02:1 (mixing with undispersed AP-SWCNTs) | 3 h (mixing with undispersed AP-SWCNTs) |
| (10, 5) | 0.3 mg/ml HiPco | 0.3 mg/ml F8BT | 0.04:1 | 12 h |
| (11, 6)/(8, 6) | 0.3 mg/ml HiPco | 1 mg/ml PFO-BPy | 0.04:1 | 24 h |

* The separation procedures are shown in Supplementary Fig. 10. An additional step to redisperse the pellet is necessary for enhancing the chiral purity of (7, 6) and (9, 7) in PFO system.