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The raw data of variables such as stability index, peri-implant bone loss, supporting bone volume, and bone to implant contact ratio.
	Surgical condition
	Stability index
	　
	Peri-implant bone loss (mm)
	Supporting bone volume (mm3)
	Bone to implant contact ratio (%)

	Sample
	Position
	Type
	PITV(N·cm)
	A4
	O4
	A8
	O8
	A12
	　
	B
	L
	M
	D
	mean
	MAX
	　
	MIN
	　
	BV
	TV
	BV/TV
	B
	L
	mean

	1
	1L
	1
	I
	20
	70.7
	69.0
	67.0
	68.0
	65.3
	　
	4.29
	3.32
	3.23
	3.99
	3.71
	4.29
	B
	3.23
	M
	17.20
	46.31
	37.14
	31.1
	34.1
	32.7

	2
	1L
	2
	I
	10
	66.0
	59.0
	66.3
	57.7
	66.3
	　
	4.85
	4.10
	3.67
	4.52
	4.28
	4.85
	B
	3.67
	M
	18.08
	72.06
	25.09
	14.9
	44.3
	30.2

	3
	1L
	3
	I
	10
	70.7
	73.0
	72.7
	72.0
	70.3
	　
	2.90
	1.46
	2.81
	2.99
	2.54
	2.99
	D
	1.46
	L
	23.72
	48.77
	48.63
	51.3
	67.3
	59.2

	4
	1L
	4
	I
	20
	64.0
	63.0
	68.0
	69.3
	65.7
	　
	4.15
	1.84
	5.95
	2.64
	3.64
	5.95
	M
	1.84
	L
	20.67
	80.82
	25.58
	41.4
	37.5
	39.5

	5
	1R
	1
	I
	30
	44.3
	52.7
	65.3
	56.3
	44.7
	　
	5.49
	5.05
	5.32
	5.62
	5.37
	5.62·
	D
	5.05
	L
	18.54
	66.69
	27.80
	17.9
	30.4
	23.7

	6
	1R
	2
	I
	25
	74.7
	74.0
	73.3
	73.0
	71
	　
	3.04
	1.19
	3.09
	2.82
	2.53
	3.09
	M
	1.19
	L
	24.76
	94.37
	26.23
	14.7
	49.5
	32.3

	7
	1R
	3
	I
	15
	72.0
	68.0
	74.7
	72.3
	72
	　
	1.78
	2.38
	3.55
	2.05
	2.44
	3.55
	M
	1.78
	B
	22.97
	45.94
	50.00
	49.5
	49.9
	49.7

	8
	1R
	4
	I
	25
	67.3
	65.0
	68.7
	70.3
	68.3
	　
	2.68
	2.87
	2.61
	3.28
	2.86
	3.28
	D
	2.61
	M
	23.06
	43.15
	53.45
	59.4
	37.7
	48.5

	9
	2L
	1
	E
	40
	76.0
	80.0
	76.3
	67.0
	75.3
	　
	1.68
	0.63
	1.30
	1.11
	1.18
	1.68
	B
	0.63
	L
	18.79
	55.87
	33.63
	61.2
	62.6
	61.9

	10
	2L
	2
	E
	40
	44.7
	83.0
	80.7
	82.0
	72
	　
	1.52
	0.83
	1.70
	1.12
	1.29
	1.70
	M
	0.83
	L
	22.99
	56.34
	40.81
	66.2
	62.1
	64.1

	11
	2L
	3
	I
	20
	65.0
	59.0
	67.0
	60.0
	fail
	　
	N/A
	N/A
	N/A

	12
	2L
	4
	I
	20
	63.0
	61.0
	67.3
	64.0
	61.3
	　
	4.78
	4.16
	5.02
	4.20
	4.54
	5.02
	M
	4.16
	L
	21.63
	38.30
	56.48
	34.7
	38
	36.4

	13
	2R
	1
	I
	15
	73.7
	71.0
	73.0
	74.3
	68.3
	　
	2.66
	2.65
	2.28
	3.87
	2.86
	3.87
	D
	2.28
	M
	18.47
	47.65
	38.76
	37.3
	48.7
	43

	14
	2R
	2
	I
	15
	81.0
	67.0
	79.0
	83.0
	77
	　
	1.52
	0.64
	1.02
	0.51
	0.92
	1.52
	B
	0.51
	D
	23.43
	60.18
	38.94
	69.1
	75.3
	72.2

	15
	2R
	3
	E
	20
	74.7
	67.0
	76.7
	79.0
	77
	　
	1.84
	0.98
	1.74
	1.00
	1.39
	1.84
	B
	0.98
	L
	23.32
	57.24
	40.74
	55.5
	71.5
	63.1

	16
	2R
	4
	E
	20
	68.7
	66.7
	70.0
	72.3
	72.3
	　
	4.27
	2.45
	3.15
	3.98
	3.46
	4.27
	B
	2.45
	L
	20.75
	43.90
	47.27
	42.6
	51
	46.6

	17
	3L
	1
	I
	40
	74.7
	80.0
	75.3
	84.0
	77
	　
	0.91
	0.25
	0.50
	0.41
	0.52
	0.91
	B
	0.25
	L
	23.07
	52.36
	44.07
	73.9
	74.1
	74

	18
	3L
	2
	I
	40
	67.7
	70.0
	73.0
	72.0
	77.7
	　
	1.84
	1.12
	2.12
	1.60
	1.67
	2.12
	M
	1.12
	L
	24.50
	51.46
	47.61
	21.1
	64.4
	42.1

	19
	3L
	3
	E
	25
	67.0
	65.3
	71.3
	72.0
	79.7
	　
	2.29
	1.07
	2.13
	1.99
	1.87
	2.29
	B
	1.07
	L
	25.21
	52.27
	48.22
	61.9
	72.3
	67.1

	20
	3L
	4
	E
	20
	65.0
	62.0
	67.7
	70.0
	71.3
	　
	4.61
	2.53
	4.66
	3.45
	3.81
	4.66
	M
	2.53
	L
	23.75
	45.99
	51.65
	32.6
	58.9
	46.3

	21
	3R
	1
	E
	40
	72.3
	67.0
	74.3
	71.0
	72.7
	　
	3.53
	3.50
	3.20
	3.91
	3.53
	3.91
	D
	3.20
	M
	21.62
	40.36
	53.57
	42.9
	53..6
	48.4

	22
	3R
	2
	E
	40
	69.0
	66.0
	65.7
	62.0
	65.3
	　
	5.32
	5.91
	3.92
	6.67
	5.45
	6.67
	D
	3.92
	M
	17.78
	37.50
	47.42
	38
	25.5
	31.6

	23
	3R
	3
	I
	30
	63.3
	58.0
	fail
	fail
	fail
	　
	N/A
	N/A
	　
	N/A
	　

	24
	3R
	4
	I
	20
	70.0
	67.7
	69.7
	74.0
	71
	　
	2.44
	1.35
	1.61
	1.64
	1.76
	2.44
	B
	1.35
	L
	22.75
	49.02
	46.42
	59.8
	50.5
	55.1

	25
	4L
	1
	E
	40
	44.0
	48.0
	45.0
	53.0
	44
	　
	4.51
	6.96
	6.92
	6.52
	6.23
	6.96
	L
	4.51
	B
	15.44
	34.57
	44.66
	32.4
	11.6
	22.1

	26
	4L
	2
	E
	35
	69.3
	65.0
	68.3
	68.0
	71.7
	　
	4.03
	2.45
	3.97
	3.63
	3.52
	4.03
	B
	2.45
	L
	24.18
	44.89
	53.86
	38.6
	51.1
	44.6

	27
	4L
	3
	E
	30
	70.0
	67.0
	71.3
	70.0
	72.3
	　
	5.23
	1.48
	5.08
	5.05
	4.21
	5.23
	B
	1.48
	L
	24.19
	51.77
	46.73
	30.8
	59.1
	44.4

	28
	4L
	4
	E
	30
	65.0
	62.7
	71.0
	70.0
	70.3
	　
	3.57
	3.09
	3.71
	4.51
	3.72
	4.51
	D
	3.09
	L
	21.75
	41.95
	51.85
	42.9
	52.4
	47.6

	29
	4R
	1
	E
	40
	76.0
	75.0
	74.0
	80.0
	74.7
	　
	2.37
	1.12
	1.80
	2.58
	1.97
	2.58
	D
	1.12
	L
	20.12
	52.57
	38.28
	48.4
	50.2
	49.4

	30
	4R
	2
	E
	40
	44.0
	55.0
	65.3
	64.0
	72.3
	　
	2.44
	6.34
	2.12
	5.48
	4.10
	6.34
	L
	2.12
	M
	23.61
	49.14
	48.06
	63.2
	21.5
	42.8

	31
	4R
	3
	E
	15
	39.7
	30.0
	64.7
	60.0
	70.3
	　
	4.73
	3.53
	4.55
	4.71
	4.38
	4.73
	B
	3.53
	L
	24.29
	46.08
	52.71
	17.2
	32.3
	24.9

	32
	4R
	4
	E
	20
	73.0
	73.3
	75.0
	80.0
	77.3
	　
	1.27
	2.13
	1.88
	2.40
	1.92
	2.40
	D
	1.27
	B
	27.93
	57.05
	48.96
	69.4
	60.2
	64.7

	Mean
	65.82
	65.32
	70.25
	70.02
	69.81
	　
	3.22
	2.58
	3.15
	3.27
	3.06
	3.78
	　
	2.19
	　
	21.95
	52.15
	43.82
	44.00
	49.79
	46.94

	Standard deviation
	10.70
	10.03
	6.32
	7.83
	8.13
	　
	1.38
	1.76
	1.55
	1.71
	1.44
	1.64
	　
	1.28
	　
	2.83
	12.75
	8.96
	17.43
	16.46
	14.28


L: left; R: right; I: internal connection; E: external connection; PITV: peak insertion torque value; A4,A8,A12: Anycheck® value at 4, 8, 12 weeks; O4,O8: Osstell® value at 4, 8 weeks;
B: buccal; L: lingual; M: mesial; D: distal; MAX: maximum value; MIN: minimum value; N/A: not applicable; BV: bone volume; TV: total volume; BV/TV: bone volume-to-total volume ratio.
