Supplementary Table S1.

The raw data of variables such as stability index, peri-implant bone loss, supporting bone volume, and bone to implant contact ratio.

| Surgical condition |  |  |  |  | Stability index |  |  |  |  |  | Peri-implant bone loss (mm) |  |  |  |  |  |  |  |  | Supporting bone volume (mm3) |  |  | Bone to implant contact ratio (%) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample | Position |  | Type | PITV(N·cm) | A4 | O4 | A8 | O8 | A12 |  | B | L | M | D | mean | MAX |  | MIN |  | BV | TV | BV/TV | B | L | mean |
| 1 | 1L | 1 | I | 20 | 70.7 | 69.0 | 67.0 | 68.0 | 65.3 |  | 4.29 | 3.32 | 3.23 | 3.99 | 3.71 | 4.29 | B | 3.23 | M | 17.20 | 46.31 | 37.14 | 31.1 | 34.1 | 32.7 |
| 2 | 1L | 2 | I | 10 | 66.0 | 59.0 | 66.3 | 57.7 | 66.3 |  | 4.85 | 4.10 | 3.67 | 4.52 | 4.28 | 4.85 | B | 3.67 | M | 18.08 | 72.06 | 25.09 | 14.9 | 44.3 | 30.2 |
| 3 | 1L | 3 | I | 10 | 70.7 | 73.0 | 72.7 | 72.0 | 70.3 |  | 2.90 | 1.46 | 2.81 | 2.99 | 2.54 | 2.99 | D | 1.46 | L | 23.72 | 48.77 | 48.63 | 51.3 | 67.3 | 59.2 |
| 4 | 1L | 4 | I | 20 | 64.0 | 63.0 | 68.0 | 69.3 | 65.7 |  | 4.15 | 1.84 | 5.95 | 2.64 | 3.64 | 5.95 | M | 1.84 | L | 20.67 | 80.82 | 25.58 | 41.4 | 37.5 | 39.5 |
| 5 | 1R | 1 | I | 30 | 44.3 | 52.7 | 65.3 | 56.3 | 44.7 |  | 5.49 | 5.05 | 5.32 | 5.62 | 5.37 | 5.62· | D | 5.05 | L | 18.54 | 66.69 | 27.80 | 17.9 | 30.4 | 23.7 |
| 6 | 1R | 2 | I | 25 | 74.7 | 74.0 | 73.3 | 73.0 | 71 |  | 3.04 | 1.19 | 3.09 | 2.82 | 2.53 | 3.09 | M | 1.19 | L | 24.76 | 94.37 | 26.23 | 14.7 | 49.5 | 32.3 |
| 7 | 1R | 3 | I | 15 | 72.0 | 68.0 | 74.7 | 72.3 | 72 |  | 1.78 | 2.38 | 3.55 | 2.05 | 2.44 | 3.55 | M | 1.78 | B | 22.97 | 45.94 | 50.00 | 49.5 | 49.9 | 49.7 |
| 8 | 1R | 4 | I | 25 | 67.3 | 65.0 | 68.7 | 70.3 | 68.3 |  | 2.68 | 2.87 | 2.61 | 3.28 | 2.86 | 3.28 | D | 2.61 | M | 23.06 | 43.15 | 53.45 | 59.4 | 37.7 | 48.5 |
| 9 | 2L | 1 | E | 40 | 76.0 | 80.0 | 76.3 | 67.0 | 75.3 |  | 1.68 | 0.63 | 1.30 | 1.11 | 1.18 | 1.68 | B | 0.63 | L | 18.79 | 55.87 | 33.63 | 61.2 | 62.6 | 61.9 |
| 10 | 2L | 2 | E | 40 | 44.7 | 83.0 | 80.7 | 82.0 | 72 |  | 1.52 | 0.83 | 1.70 | 1.12 | 1.29 | 1.70 | M | 0.83 | L | 22.99 | 56.34 | 40.81 | 66.2 | 62.1 | 64.1 |
| 11 | 2L | 3 | I | 20 | 65.0 | 59.0 | 67.0 | 60.0 | fail |  | N/A |  |  |  |  |  |  |  |  | N/A |  |  | N/A |  |  |
| 12 | 2L | 4 | I | 20 | 63.0 | 61.0 | 67.3 | 64.0 | 61.3 |  | 4.78 | 4.16 | 5.02 | 4.20 | 4.54 | 5.02 | M | 4.16 | L | 21.63 | 38.30 | 56.48 | 34.7 | 38 | 36.4 |
| 13 | 2R | 1 | I | 15 | 73.7 | 71.0 | 73.0 | 74.3 | 68.3 |  | 2.66 | 2.65 | 2.28 | 3.87 | 2.86 | 3.87 | D | 2.28 | M | 18.47 | 47.65 | 38.76 | 37.3 | 48.7 | 43 |
| 14 | 2R | 2 | I | 15 | 81.0 | 67.0 | 79.0 | 83.0 | 77 |  | 1.52 | 0.64 | 1.02 | 0.51 | 0.92 | 1.52 | B | 0.51 | D | 23.43 | 60.18 | 38.94 | 69.1 | 75.3 | 72.2 |
| 15 | 2R | 3 | E | 20 | 74.7 | 67.0 | 76.7 | 79.0 | 77 |  | 1.84 | 0.98 | 1.74 | 1.00 | 1.39 | 1.84 | B | 0.98 | L | 23.32 | 57.24 | 40.74 | 55.5 | 71.5 | 63.1 |
| 16 | 2R | 4 | E | 20 | 68.7 | 66.7 | 70.0 | 72.3 | 72.3 |  | 4.27 | 2.45 | 3.15 | 3.98 | 3.46 | 4.27 | B | 2.45 | L | 20.75 | 43.90 | 47.27 | 42.6 | 51 | 46.6 |
| 17 | 3L | 1 | I | 40 | 74.7 | 80.0 | 75.3 | 84.0 | 77 |  | 0.91 | 0.25 | 0.50 | 0.41 | 0.52 | 0.91 | B | 0.25 | L | 23.07 | 52.36 | 44.07 | 73.9 | 74.1 | 74 |
| 18 | 3L | 2 | I | 40 | 67.7 | 70.0 | 73.0 | 72.0 | 77.7 |  | 1.84 | 1.12 | 2.12 | 1.60 | 1.67 | 2.12 | M | 1.12 | L | 24.50 | 51.46 | 47.61 | 21.1 | 64.4 | 42.1 |
| 19 | 3L | 3 | E | 25 | 67.0 | 65.3 | 71.3 | 72.0 | 79.7 |  | 2.29 | 1.07 | 2.13 | 1.99 | 1.87 | 2.29 | B | 1.07 | L | 25.21 | 52.27 | 48.22 | 61.9 | 72.3 | 67.1 |
| 20 | 3L | 4 | E | 20 | 65.0 | 62.0 | 67.7 | 70.0 | 71.3 |  | 4.61 | 2.53 | 4.66 | 3.45 | 3.81 | 4.66 | M | 2.53 | L | 23.75 | 45.99 | 51.65 | 32.6 | 58.9 | 46.3 |
| 21 | 3R | 1 | E | 40 | 72.3 | 67.0 | 74.3 | 71.0 | 72.7 |  | 3.53 | 3.50 | 3.20 | 3.91 | 3.53 | 3.91 | D | 3.20 | M | 21.62 | 40.36 | 53.57 | 42.9 | 53..6 | 48.4 |
| 22 | 3R | 2 | E | 40 | 69.0 | 66.0 | 65.7 | 62.0 | 65.3 |  | 5.32 | 5.91 | 3.92 | 6.67 | 5.45 | 6.67 | D | 3.92 | M | 17.78 | 37.50 | 47.42 | 38 | 25.5 | 31.6 |
| 23 | 3R | 3 | I | 30 | 63.3 | 58.0 | fail | fail | fail |  | N/A |  |  |  |  |  |  |  |  | N/A |  |  |  | N/A |  |
| 24 | 3R | 4 | I | 20 | 70.0 | 67.7 | 69.7 | 74.0 | 71 |  | 2.44 | 1.35 | 1.61 | 1.64 | 1.76 | 2.44 | B | 1.35 | L | 22.75 | 49.02 | 46.42 | 59.8 | 50.5 | 55.1 |
| 25 | 4L | 1 | E | 40 | 44.0 | 48.0 | 45.0 | 53.0 | 44 |  | 4.51 | 6.96 | 6.92 | 6.52 | 6.23 | 6.96 | L | 4.51 | B | 15.44 | 34.57 | 44.66 | 32.4 | 11.6 | 22.1 |
| 26 | 4L | 2 | E | 35 | 69.3 | 65.0 | 68.3 | 68.0 | 71.7 |  | 4.03 | 2.45 | 3.97 | 3.63 | 3.52 | 4.03 | B | 2.45 | L | 24.18 | 44.89 | 53.86 | 38.6 | 51.1 | 44.6 |
| 27 | 4L | 3 | E | 30 | 70.0 | 67.0 | 71.3 | 70.0 | 72.3 |  | 5.23 | 1.48 | 5.08 | 5.05 | 4.21 | 5.23 | B | 1.48 | L | 24.19 | 51.77 | 46.73 | 30.8 | 59.1 | 44.4 |
| 28 | 4L | 4 | E | 30 | 65.0 | 62.7 | 71.0 | 70.0 | 70.3 |  | 3.57 | 3.09 | 3.71 | 4.51 | 3.72 | 4.51 | D | 3.09 | L | 21.75 | 41.95 | 51.85 | 42.9 | 52.4 | 47.6 |
| 29 | 4R | 1 | E | 40 | 76.0 | 75.0 | 74.0 | 80.0 | 74.7 |  | 2.37 | 1.12 | 1.80 | 2.58 | 1.97 | 2.58 | D | 1.12 | L | 20.12 | 52.57 | 38.28 | 48.4 | 50.2 | 49.4 |
| 30 | 4R | 2 | E | 40 | 44.0 | 55.0 | 65.3 | 64.0 | 72.3 |  | 2.44 | 6.34 | 2.12 | 5.48 | 4.10 | 6.34 | L | 2.12 | M | 23.61 | 49.14 | 48.06 | 63.2 | 21.5 | 42.8 |
| 31 | 4R | 3 | E | 15 | 39.7 | 30.0 | 64.7 | 60.0 | 70.3 |  | 4.73 | 3.53 | 4.55 | 4.71 | 4.38 | 4.73 | B | 3.53 | L | 24.29 | 46.08 | 52.71 | 17.2 | 32.3 | 24.9 |
| 32 | 4R | 4 | E | 20 | 73.0 | 73.3 | 75.0 | 80.0 | 77.3 |  | 1.27 | 2.13 | 1.88 | 2.40 | 1.92 | 2.40 | D | 1.27 | B | 27.93 | 57.05 | 48.96 | 69.4 | 60.2 | 64.7 |
| Mean |  |  |  |  | 65.82 | 65.32 | 70.25 | 70.02 | 69.81 |  | 3.22 | 2.58 | 3.15 | 3.27 | 3.06 | 3.78 |  | 2.19 |  | 21.95 | 52.15 | 43.82 | 44.00 | 49.79 | 46.94 |
| Standard deviation |  |  |  |  | 10.70 | 10.03 | 6.32 | 7.83 | 8.13 |  | 1.38 | 1.76 | 1.55 | 1.71 | 1.44 | 1.64 |  | 1.28 |  | 2.83 | 12.75 | 8.96 | 17.43 | 16.46 | 14.28 |

L: left; R: right; I: internal connection; E: external connection; PITV: peak insertion torque value; A4,A8,A12: Anycheck® value at 4, 8, 12 weeks; O4,O8: Osstell® value at 4, 8 weeks;
B: buccal; L: lingual; M: mesial; D: distal; MAX: maximum value; MIN: minimum value; N/A: not applicable; BV: bone volume; TV: total volume; BV/TV: bone volume-to-total volume ratio.