Table 1: Test beam designations.

| BeamNO. | Nomination | Elevated Temp.(oC) | CFRP Configurations | Loading type |
| --- | --- | --- | --- | --- |
| 1 | C-4PL | 23 | NA | 4-point symmetric |
| 2 | HD450-4PL | 450 | NA | 4-point symmetric |
| 3 | C-SSP-4PL | 23 | Straight SNSM-CFRP ropes | 4-point symmetric |
| 4 | C-SPP-4PL | 23 | Parabolic SNSM-CFRP ropes | 4-point symmetric |
| 5 | HD450-RSP-4PL | 450 | Straight SNSM-CFRP ropes | 4-point symmetric |
| 6 | HD450-RPP-4PL | 450 | Parabolic SNSM-CFRP ropes | 4-point symmetric |
| 7 | C-6PL | 23 | NA | 6-point symmetric |
| 8 | HD450-6PL | 450 | NA | 6-point symmetric |
| 9 | C-SSP-6PL | 23 | Straight SNSM-CFRP ropes | 6-point symmetric |
| 10 | C-SPP-6PL | 23 | Parabolic SNSM-CFRP ropes | 6-point symmetric |
| 11 | HD450-RSP-6PL | 450 | Straight SNSM-CFRP ropes | 6-point symmetric |
| 12 | HD450-RPP-6PL | 450 | Parabolic SNSM-CFRP ropes | 6-point symmetric |
| 13 | C-Asy | 23 | NA | 6-point Asymmetric |
| 14 | HD450-Asy | 450 | NA | 6-point Asymmetric |
| 15 | C-SSP-Asy | 23 | Straight SNSM-CFRP ropes | 6-point Asymmetric |
| 16 | C-SPP-Asy | 23 | Parabolic SNSM-CFRP ropes | 6-point Asymmetric |
| 17 | HD450-RSP-Asy | 450 | Straight SNSM-CFRP ropes | 6-point Asymmetric |
| 18 | HD450-RPP-Asy | 450 | Parabolic SNSM-CFRP ropes | 6-point Asymmetric |

SNSM, Side Near Surface Mounted; C, Control; HD, Heat Damaged; SSP, Strengthened Straight Profile; SPP, Strengthened Parabolic Profile; RSP, Repaired Straight Profile; RPP, Repaired Parabolic Profile.

Table 2: Mechanical characteristics of all concrete beams.

| Name | Pu (kN) | R % | St (MN/M) | R % | T (J) | R % | DD (mm/mm) | R % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C-4PL | 112 | 100 | 14.42 | 100 | 1759 | 100 | 3.6 | 100 |
| HD450-4PL | 97 | 86 | 14.42 | 100 | 1454 | 83 | 3.44 | 96 |
| C-SSP-4PL | 177 | 158 | 16.5 | 114 | 1773 | 101 | 2.41 | 67 |
| C-SPP-4PL | 197 | 176 | 18.3 | 127 | 2522 | 143 | 3.11 | 86 |
| HD450-RSP-4PL | 160.1 | 143 | 19 | 132 | 1715 | 98 | 3.07 | 85 |
| HD450-RPP-4PL | 160.4 | 143 | 18 | 125 | 1834 | 104 | 3.20 | 89 |
| C-6PL | 190.7 | 100 | 24.6 | 100 | 2246 | 100 | 2.96 | 100 |
| HD450-6PL | 173 | 90 | 24.6 | 100 | 2170 | 97 | 2.92 | 99 |
| C-SSP-6PL | 299 | 157 | 27.7 | 113 | 3198 | 142 | 2.45 | 83 |
| C-SPP-6PL | 305 | 160 | 29.6 | 120 | 3265 | 145 | 2.78 | 94 |
| HD450-RSP-6PL | 282 | 148 | 28.8 | 117 | 3289 | 146 | 2.74 | 93 |
| HD450-RPP-6PL | 292 | 153 | 33 | 134 | 2730 | 122 | 2.31 | 78 |
| C-ASY | 174 | 100 | 23.2 | 100 | 1437 | 100 | 2.32 | 100 |
| HD450-ASY | 150 | 86 | 23.2 | 100 | 1016 | 71 | 1.95 | 84 |
| C-SSP-ASY | 300 | 173 | 30.9 | 133 | 2722 | 190 | 2.25 | 97 |
| C-SPP-ASY | 289 | 166 | 31.2 | 135 | 2362 | 164 | 2.20 | 95 |
| HD450-RSP-ASY | 270 | 155 | 31 | 134 | 2895 | 200 | 3.03 | 131 |
| HD450-RPP-ASY | 247 | 142 | 31.7 | 137 | 2224 | 154 | 2.69 | 116 |

N., Name of specimens; Pu, Ultimate load capacity; St, Stiffness values; T, Toughness values; DD, Displacement Ductility; %, residual mechanical characteristics; R, residual

Table 3: Performance factor for strengthened /repaired concrete beams.

| Specimen Name | Pu (kN) | P0.001 (kN) | SF | ∆u (mm) | ∆0.001 (mm) | DF | PF |
| --- | --- | --- | --- | --- | --- | --- | --- |
| C-SSP-4PL | 177 | 103 | 1.72 | 14.57 | 4.6 | 3.17 | 5.44 |
| C-SPP-4PL | 197 | 103 | 1.91 | 18.32 | 4.45 | 4.12 | 7.87 |
| C-SSP-6PL | 299 | 162 | 1.84 | 16 | 4.84 | 3.31 | 6.10 |
| C-SPP-6PL | 305 | 162 | 1.88 | 15.77 | 4.32 | 3.65 | 6.87 |
| C-SSP-ASY | 300 | 144 | 2.08 | 13.87 | 3.88 | 3.57 | 7.45 |
| C-SPP-ASY | 289 | 144 | 2.01 | 12.48 | 3.7 | 3.37 | 6.77 |
| HD450-RSP-4PL | 160.12 | 71 | 2.26 | 15.34 | 3.18 | 4.82 | 10.88 |
| HD450-RPP-4PL | 160.44 | 71 | 2.26 | 16.08 | 3.1 | 5.19 | 11.72 |
| HD450-RSP-6PL | 282 | 111 | 2.54 | 17.14 | 3.28 | 5.23 | 13.28 |
| HD450-RPP-6PL | 292 | 111 | 2.63 | 14.34 | 3.1 | 4.63 | 12.17 |
| HD450-RSP-ASY | 270 | 98 | 2.76 | 15.56 | 2.63 | 5.92 | 16.30 |
| HD450-RPP-ASY | 247 | 98 | 2.52 | 13.12 | 2.47 | 5.31 | 13.39 |

P0.001, load at service stress; Pu, Ultimate load capacity; SF, strength factor, DF, deformability; PF, performance factor; ∆u, deflection at ultimate; ∆0.001, deflection at service stress.

Table 4: Strain-induced (in SNSM CFRP ropes) and failure mode for different strengthened/repaired concrete beams.

| Name | εf | Strain Estimated | Residual strain | Mode of failure |
| --- | --- | --- | --- | --- |
| C-SSP-4PL | 0.013 | analytically | 82 | RR then SCC |
| C-SPP-4PL | 0.0158 | analytically | 99 | RR then SCC |
| C-SSP-6PL | 0.0148 | analytically | 93 | RR then SCC |
| C-SPP-6PL | 0.0154 | analytically | 97 | RR then SCC |
| C-SSP-ASY | 0.016 | experimentally | 100 | RR then SCC |
| C-SPP-ASY | 0.014 | experimentally | 88 | RR then SCC |
| HD450-RSP-4PL | 0.01129 | analytically | 71 | RR then SCC |
| HD450-RPP-4PL | 0.01133 | analytically | 71 | RR then SCC |
| HD450-RSP-6PL | 0.0141 | analytically | 89 | RR then SCC |
| HD450-RPP-6PL | 0.0151 | analytically | 95 | RR then SCC |
| HD450-RSP-ASY | 0.0083 | experimentally | 52 | CCD |
| HD450-RPP-ASY | 0.0131 | experimentally | 82 | RR then SCC |

εf, strain in CFRP rope at failure; RR: rope rupture, SCC: separation of concrete cover, CCD: concrete cover delamination.