A colorimetric smartphone-based sensor for on-site AA detection

based on MCTs nanocomposite materials

Food Analytical Methods

Huanhuan She1 a · Chaoling Wu1 a · Ruotong He1 · Weihong Xie1 · Yi Zhang1 *

1 School of Life and Health Sciences, Hubei University of Technology, Wuhan 430068, China

* Corresponding author (Yi Zhang)

E-mail addresses: zhangyi@hbut.edu.cn

a These authors contributed equally to this work.

Fig. S1 The particle size distribution diagram of Fe3O4 and MCTs.

Fig. S2 (A) UV-vis absorbance values at 400~800 nm for various systems. (B) Effect of pH on the peroxidase activity of MCTs. (C) Effect of temperature on the peroxidase activity of MCTs. (D) Effect of material dosage on the peroxidase activity of MCTs.

Fig. S3 The influence of MCTs and MCTT on absorbance at different concentrations (50 M/100 M/150 M)

Table S1 The kinetic parameters of MCTs and some other peroxidase mimetics with TMB and H2O2 as substrates.

| catalys | substrate | Km (mM) | Vmax (10-8 M·s-1) | Reference |
| --- | --- | --- | --- | --- |
| HRP | TMB | 0.43 | 10.0 | (Gao et al. 2007) |
|  | H2O2 | 3.70 | 8.7 |  |
| Pd-Ir cubes | TMB | 0.13 | 6.50 | (Xia et al. 2015) |
|  | H2O2 | 340 | 5.10 |  |
| PBMNPs3 | TMB | 0.307 | 1.06 | (Zhang et al. 2010) |
|  | H2O2 | 323.6 | 1.17 |  |
| CNPs | TMB | 26.06 | 4.27 | (Yadav et al. 2019) |
|  | H2O2 | 0.05 | 6.06 |  |
| Citrate-CuNPs | TMB | 1.63 | 4.90 | (Chen et al. 2021) |
|  | H2O2 | 83.69 | 2.50 |  |
| MCTs | TMB H2O2 | 0.87 185 | 1.65 1.27 | This work |

Fig. S4 Ascorbic acid content in 6 commercial beverages, a for Master Kong Daily C Sunshine Sweet Orange, b for Master Kong Daily C Sunshine Grape Juice, c for Farmer's Orchard (50% mixed fruit and vegetables), d for Farmer's Orchard (30% mixed fruit and vegetables), e for Water Soluble C100 (grapefruit flavour) and f for Water Soluble C100 (lemon flavour).

Reference

Gao LZ, Zhuang J, Nie L et al (2007) Intrinsic peroxidase-like activity of ferromagnetic nanoparticles. Nat Nanotechnol 2(9):577-583.

https://doi.org/10.1038/nnano.2007.260

Xia XH, Zhang JT, Lu N et al (2015) Pd-Ir Core-Shell Nanocubes: A Type of Highly Efficient and Versatile Peroxidase Mimic. ACS Nano 9(10):9994-10004. https://doi.org/10.1021/acsnano.5b03525

Zhang XQ, Gong SWY, Zhang Y et al (2010) Prussian blue modified iron oxide magnetic nanoparticles and their high peroxidase-like activity. J Mater Chem 20(24):5110-5116. https://doi.org/10.1039/c0jm00174k

Yadav PK, Singh VK, Chandra S et al (2019) Green Synthesis of Fluorescent Carbon Quantum Dots from Azadirachta indica Leaves and Their Peroxidase-Mimetic Activity for the Detection of H2O2 and Ascorbic Acid in Common Fresh Fruits. ACS Biomater Sci Eng 5(2):623-632. https://doi.org/10.1021/acsbiomaterials.8b01528

Chen SH, Li Z, Huang ZZ et al (2021) Investigation of efficient synergistic and protective effects of chitosan on copper nanoclusters: Construction of highly active and stable nanozyme for colorimetric and fluorometric dual-signal biosensing. Sens Actuators B 332:129522.

https://doi.org/10.1016/j.snb.2021.129522