Green Synthesis of Nickel-Oxide Nano particles from Lawasonia inermis leaf extract for promising Methyl red Uptake and

Efficient Iodine Adsorption

Rimsha Khalid1, Saqlain Raza, Isham Areej1*, Faiza Ashraf1, Amin Abid1*

Department of Chemistry, University of Sahiwal, Sahiwal-57000, Pakistan

Corresponding author ishamareej123@gmail.com, mabid@uosahiwal.edu.pk

Table S1: Effect of pH on adsorption

| Initial Concentration (mg/L) | Solution Volume (L) | Adsorbent Dose (g) | Solution pH | Ce (mg/g) | qe (mg/g) | Removal Efficiency (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 30 | 0.05 | 1 | 1 | 6.9 | 1.155 | 77 |
| 30 | 0.05 | 1 | 2 | 6.3 | 1.185 | 79 |
| 30 | 0.05 | 1 | 3 | 5.55 | 1.2225 | 81.5 |
| 30 | 0.05 | 1 | 4 | 4.8 | 1.26 | 84 |
| 30 | 0.05 | 1 | 5 | 3.3 | 1.335 | 89 |
| 30 | 0.05 | 1 | 6 | 5.1 | 1.245 | 83 |
| 30 | 0.05 | 1 | 7 | 8.25 | 1.0875 | 72.5 |
| 30 | 0.05 | 1 | 8 | 9.3 | 1.035 | 69 |
| 30 | 0.05 | 1 | 9 | 13.2 | 0.84 | 56 |
| 30 | 0.05 | 1 | 10 | 16.62 | 0.669 | 44.6 |
| 30 | 0.05 | 1 | 11 | 19.35 | 0.5325 | 35.5 |
| 30 | 0.05 | 1 | 12 | 22.05 | 0.3975 | 26.5 |

Table S2: Effect of Contact Time on adsorption

| Initial Concentration (mg/L) | Solution Volume (L) | Adsorbent Dose (g) | Contact Time (min-1) | Ct (mg/g) | qt (mg/g) | Removal Efficiency (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 30 | 0.05 | 1 | 10 | 16.59 | 0.6705 | 44.7 |
| 30 | 0.05 | 1 | 20 | 14.87 | 0.7565 | 50.43 |
| 30 | 0.05 | 1 | 30 | 12.76 | 0.862 | 57.47 |
| 30 | 0.05 | 1 | 40 | 10.94 | 0.953 | 63.53 |
| 30 | 0.05 | 1 | 50 | 8.57 | 1.0715 | 71.43 |
| 30 | 0.05 | 1 | 60 | 7.98 | 1.101 | 73.4 |
| 30 | 0.05 | 1 | 70 | 6.13 | 1.1935 | 79.57 |
| 30 | 0.05 | 1 | 80 | 5.93 | 1.2035 | 80.23 |
| 30 | 0.05 | 1 | 90 | 4.87 | 1.2565 | 83.77 |
| 30 | 0.05 | 1 | 100 | 4.32 | 1.284 | 85.6 |
| 30 | 0.05 | 1 | 110 | 3.79 | 1.3105 | 87.37 |
| 30 | 0.05 | 1 | 120 | 3.56 | 1.322 | 89 |

Table S3: Effect of Adsorbent dose on adsorption

| Initial Concentration (mg/L) | Solution Volume (L) | Adsorbent Dose (g) | Ce (mg/g) | qe (mg/g) | Removal Efficiency (%) |
| --- | --- | --- | --- | --- | --- |
| 30 | 0.05 | 0.1 | 22.2 | 0.39 | 26 |
| 30 | 0.05 | 0.2 | 16.8 | 0.66 | 44 |
| 30 | 0.05 | 0.4 | 11.4 | 0.93 | 62 |
| 30 | 0.05 | 0.6 | 7.5 | 1.125 | 75 |
| 30 | 0.05 | 0.8 | 5.4 | 1.23 | 82 |
| 30 | 0.05 | 1 | 3.3 | 1.335 | 89 |
| 30 | 0.05 | 1.2 | 3.3 | 1.335 | 89 |
| 30 | 0.05 | 1.4 | 3.3 | 1.335 | 89 |
| 30 | 0.05 | 1.6 | 3.15 | 1.3425 | 89.5 |

Table S4: Effect of MR dye Initial Concentration on Adsorption

| Initial Concentration (mg/L) | Solution Volume (L) | Adsorbent Dose (g) | Ce (mg/g) | qe (mg/g) | Removal Efficiency (%) |
| --- | --- | --- | --- | --- | --- |
| 5 | 0.05 | 1 | 1.905 | 0.15475 | 61.9 |
| 10 | 0.05 | 1 | 2.83 | 0.3585 | 71.7 |
| 20 | 0.05 | 1 | 4.02 | 0.799 | 79.9 |
| 30 | 0.05 | 1 | 4.14 | 1.293 | 88.5 |
| 50 | 0.05 | 1 | 8.15 | 2.0925 | 83.7 |
| 70 | 0.05 | 1 | 15.09 | 2.7455 | 78.44 |
| 90 | 0.05 | 1 | 27.09 | 3.1455 | 69.9 |
| 110 | 0.05 | 1 | 39.82 | 3.509 | 63.8 |
| 130 | 0.05 | 1 | 52.13 | 3.8935 | 59.9 |
| 150 | 0.05 | 1 | 67.98 | 4.101 | 54.68 |

Table S5: Effect of temperature on adsorption

| Initial Concentration (mg/L) | Solution Volume (L) | Adsorbent Dose (g) | Temperature (˚C) | Ce (mg/g) | qe (mg/g) | Removal Efficiency (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 30 | 0.05 | 1 | 10 | 3.3 | 1.335 | 89 |
| 30 | 0.05 | 1 | 20 | 5.7 | 1.215 | 81 |
| 30 | 0.05 | 1 | 30 | 7.11 | 1.1445 | 76.3 |
| 30 | 0.05 | 1 | 40 | 8.49 | 1.0755 | 71.7 |
| 30 | 0.05 | 1 | 50 | 10.83 | 0.9585 | 63.9 |
| 30 | 0.05 | 1 | 60 | 14.37 | 0.7815 | 52.1 |
| 30 | 0.05 | 1 | 70 | 16.02 | 0.699 | 46.6 |
| 30 | 0.05 | 1 | 80 | 18.06 | 0.597 | 39.8 |

Table S6: Effect of Agitation Speed on adsorption

| Initial Concentration (mg/L) | Solution Volume (L) | Adsorbent Dose (g) | Agitation Speed (rpm) | Ce (mg/g) | qe (mg/g) | Removal Efficiency (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 30 | 0.05 | 1 | 0 | 12.6 | 0.87 | 58 |
| 30 | 0.05 | 1 | 50 | 10.65 | 0.9675 | 64.5 |
| 30 | 0.05 | 1 | 100 | 9.9 | 1.005 | 67 |
| 30 | 0.05 | 1 | 150 | 9.3 | 1.035 | 69 |
| 30 | 0.05 | 1 | 200 | 7.65 | 1.1175 | 74.5 |
| 30 | 0.05 | 1 | 250 | 6.15 | 1.1925 | 79.5 |
| 30 | 0.05 | 1 | 300 | 3.45 | 1.3275 | 88.5 |
| 30 | 0.05 | 1 | 350 | 3.3 | 1.335 | 89 |
| 30 | 0.05 | 1 | 400 | 3.3 | 1.335 | 89 |

Table S7: Effect of Reusability on adsorption

| Initial Concentration (mg/L) | Solution Volume (L) | Adsorbent Dose (g) | Cycles | Ce (mg/g) | qe (mg/g) | Removal Efficiency (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 30 | 0.05 | 1 | 1 | 3.3 | 1.335 | 89 |
| 30 | 0.05 | 1 | 2 | 3.9 | 1.305 | 87 |
| 30 | 0.05 | 1 | 3 | 4.8 | 1.26 | 84 |
| 30 | 0.05 | 1 | 4 | 6 | 1.2 | 80 |
| 30 | 0.05 | 1 | 5 | 6.9 | 1.155 | 77 |
| 30 | 0.05 | 1 | 6 | 7.8 | 1.11 | 74 |
| 30 | 0.05 | 1 | 7 | 9.3 | 1.035 | 69 |
| 30 | 0.05 | 1 | 8 | 10.5 | 0.975 | 65 |
| 30 | 0.05 | 1 | 9 | 11.1 | 0.945 | 63 |
| 30 | 0.05 | 1 | 10 | 12 | 0.9 | 60 |

Table S8: Experimental data of Langmuir adsorption isotherm model

| Co (mg/L) | volume (L) | Adsorbent dose (g) | Ce (mg/g) | 1/Ce (mg/g) | qe (mg/g) | 1/qe (mg/g) | Removal % |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 5 | 0.05 | 1 | 1.905 | 0.52493 | 0.15475 | 6.46204 | 61.9 |
| 10 | 0.05 | 1 | 2.83 | 0.35336 | 0.3585 | 2.78940 | 71.7 |
| 20 | 0.05 | 1 | 4.02 | 0.24876 | 0.799 | 1.25156 | 79.9 |
| 30 | 0.05 | 1 | 4.14 | 0.24155 | 1.293 | 0.77339 | 86.2 |
| 50 | 0.05 | 1 | 8.15 | 0.12269 | 2.0925 | 0.47789 | 83.7 |
| 70 | 0.05 | 1 | 15.09 | 0.06627 | 2.7455 | 0.36423 | 78.44 |
| 90 | 0.05 | 1 | 27.09 | 0.03691 | 3.1455 | 0.31791 | 69.9 |
| 110 | 0.05 | 1 | 39.82 | 0.02511 | 3.509 | 0.28498 | 63.8 |
| 130 | 0.05 | 1 | 52.13 | 0.01918 | 3.8935 | 0.25684 | 59.9 |
| 150 | 0.05 | 1 | 67.98 | 0.01471 | 4.101 | 0.24384 | 54.68 |

Table S9: Experimental data of Freundlich adsorption isotherm model

| Co (mg/L) | Volume (L) | Adsorbent dose (g) | Ce (mg/g) | ln Ce (mg/g) | qe (mg/g) | ln qe (mg/g) | Removal % |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 5 | 0.05 | 1 | 1.905 | 0.27989 | 0.15475 | -0.81037 | 61.9 |
| 10 | 0.05 | 1 | 2.83 | 0.45179 | 0.3585 | -0.44551 | 71.7 |
| 20 | 0.05 | 1 | 4.02 | 0.60423 | 0.799 | -0.09745 | 79.9 |
| 30 | 0.05 | 1 | 4.14 | 0.61700 | 1.293 | 0.111599 | 86.2 |
| 50 | 0.05 | 1 | 8.15 | 0.91116 | 2.0925 | 0.320665 | 83.7 |
| 70 | 0.05 | 1 | 15.09 | 1.17869 | 2.7455 | 0.438621 | 78.44 |
| 90 | 0.05 | 1 | 27.09 | 1.43281 | 3.1455 | 0.49769 | 69.9 |
| 110 | 0.05 | 1 | 39.82 | 1.60010 | 3.509 | 0.545183 | 63.8 |
| 130 | 0.05 | 1 | 52.13 | 1.71709 | 3.8935 | 0.59034 | 59.9 |
| 150 | 0.05 | 1 | 67.98 | 1.83238116 | 4.101 | 0.61289 | 54.68 |

Table S10: Experimental data of Temkin adsorption isotherm model

| Co (mg/L) | Volume (L) | Adsorbent dose (g) | Ce (mg/g) | ln Ce (mg/g) | qe (mg/g) | Removal % |
| --- | --- | --- | --- | --- | --- | --- |
| 5 | 0.05 | 1 | 1.905 | 0.27989 | 0.15475 | 61.9 |
| 10 | 0.05 | 1 | 2.83 | 0.45179 | 0.3585 | 71.7 |
| 20 | 0.05 | 1 | 4.02 | 0.60423 | 0.799 | 79.9 |
| 30 | 0.05 | 1 | 4.14 | 0.61700 | 1.293 | 86.2 |
| 50 | 0.05 | 1 | 8.15 | 0.91116 | 2.0925 | 83.7 |
| 70 | 0.05 | 1 | 15.09 | 1.17869 | 2.7455 | 78.44 |
| 90 | 0.05 | 1 | 27.09 | 1.43281 | 3.1455 | 69.9 |
| 110 | 0.05 | 1 | 39.82 | 1.60010 | 3.509 | 63.8 |
| 130 | 0.05 | 1 | 52.13 | 1.71709 | 3.8935 | 59.9 |
| 150 | 0.05 | 1 | 67.98 | 1.83238 | 4.101 | 54.68 |

Table S11: Experimental data of D-R adsorption isotherm model

| Co | Ce | Co (mol/L) | Ce (mol/L) | qe (mol/L) | ln qe | E=RTlN(1+1/Ce) | E2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 5 | 1.905 | 1.85667E-05 | 7.0739E-06 | 5.74638E-07 | -14.3695 | 29100.79 | 846855948.6 |
| 10 | 2.83 | 3.71333E-05 | 1.0509E-05 | 1.33123E-06 | -13.5294 | 28129.57 | 791272503.3 |
| 20 | 4.02 | 7.42666E-05 | 1.4928E-05 | 2.96695E-06 | -12.728 | 27268.25 | 743557654.3 |
| 30 | 4.14 | 0.0001114 | 1.5373E-05 | 4.80134E-06 | -12.2466 | 27196.08 | 739626584.2 |
| 50 | 8.15 | 0.000185667 | 3.0264E-05 | 7.77014E-06 | -11.7652 | 25534.05 | 651987601.3 |
| 70 | 15.09 | 0.000259933 | 5.6034E-05 | 1.01949E-05 | -11.4936 | 24022.49 | 577079911.6 |
| 90 | 27.09 | 0.0003342 | 0.00010059 | 1.16803E-05 | -11.3576 | 22586.75 | 510161456.4 |
| 110 | 39.82 | 0.000408466 | 0.00014786 | 1.30301E-05 | -11.2483 | 21641.63 | 468359938.4 |
| 130 | 52.13 | 0.000482733 | 0.00019358 | 1.44579E-05 | -11.1443 | 20980.73 | 440191166.4 |
| 150 | 67.98 | 0.000557 | 0.00025243 | 1.52284E-05 | -11.0924 | 20329.44 | 413286115.7 |

Table S12: Experimental data of Pseudo 1st order kinetic model

| Time (˚C) | Co (mg/L) | Volume (L) | Adsorbent Dose (g) | Ct (mg/g) | Qt (mg/g) | Qe (mg/g) | qe-qt (mg/g) | ln (qe-qt) (mg/g) | Removal % |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 10 | 30 | 0.05 | 1 | 16.59 | 0.6705 | 1.293 | 0.6225 | -0.47401 | 44.7 |
| 20 | 30 | 0.05 | 1 | 14.87 | 0.7565 | 1.293 | 0.5365 | -0.62269 | 50.43 |
| 30 | 30 | 0.05 | 1 | 12.76 | 0.862 | 1.293 | 0.431 | -0.84165 | 57.47 |
| 40 | 30 | 0.05 | 1 | 10.94 | 0.953 | 1.293 | 0.34 | -1.07881 | 63.53 |
| 50 | 30 | 0.05 | 1 | 8.57 | 1.0715 | 1.293 | 0.2215 | -1.50733 | 71.43 |
| 60 | 30 | 0.05 | 1 | 7.98 | 1.101 | 1.293 | 0.192 | -1.65026 | 73.4 |
| 70 | 30 | 0.05 | 1 | 6.13 | 1.1935 | 1.293 | 0.0995 | -2.3076 | 79.57 |
| 80 | 30 | 0.05 | 1 | 5.93 | 1.2035 | 1.293 | 0.0895 | -2.41352 | 80.23 |
| 90 | 30 | 0.05 | 1 | 4.87 | 1.2565 | 1.293 | 0.0365 | -3.31044 | 83.77 |
| 100 | 30 | 0.05 | 1 | 4.32 | 1.284 | 1.293 | 0.009 | -4.71053 | 85.6 |

Table S13: Experimental data of Pseudo 2nd order kinetic model

| Time (˚C) | Co (mg/L) | Volume (L) | m (g) | Ct (mg/g) | Qt (mg/g) | t/qt (mg/g) | Removal % |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 10 | 30 | 0.05 | 1 | 16.59 | 0.6705 | 14.91424 | 44.7 |
| 20 | 30 | 0.05 | 1 | 14.87 | 0.7565 | 26.43754 | 50.43 |
| 30 | 30 | 0.05 | 1 | 12.76 | 0.862 | 34.80278 | 57.47 |
| 40 | 30 | 0.05 | 1 | 10.94 | 0.953 | 41.97272 | 63.53 |
| 50 | 30 | 0.05 | 1 | 8.57 | 1.0715 | 46.66356 | 71.43 |
| 60 | 30 | 0.05 | 1 | 7.98 | 1.101 | 54.49591 | 73.4 |
| 70 | 30 | 0.05 | 1 | 6.13 | 1.1935 | 58.65103 | 79.57 |
| 80 | 30 | 0.05 | 1 | 5.93 | 1.2035 | 66.47279 | 80.23 |
| 90 | 30 | 0.05 | 1 | 4.87 | 1.2565 | 71.62754 | 83.77 |
| 100 | 30 | 0.05 | 1 | 4.32 | 1.284 | 77.88162 | 85.6 |
| 110 | 30 | 0.05 | 1 | 3.79 | 1.3105 | 83.93743 | 87.37 |
| 120 | 30 | 0.05 | 1 | 3.56 | 1.322 | 90.77156 | 88.13 |

Table S14: Experimental data of Intra-particles diffusion kinetic model

| Time (˚C) | Co (mg/L) | V (L) | m (g) | Ct (mg/g) | qt (mg/g) | t 0.5 | Removal % |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 10 | 30 | 0.05 | 1 | 16.59 | 0.6705 | 3.162278 | 44.7 |
| 20 | 30 | 0.05 | 1 | 14.87 | 0.7565 | 4.472136 | 50.43 |
| 30 | 30 | 0.05 | 1 | 12.76 | 0.862 | 5.477226 | 57.47 |
| 40 | 30 | 0.05 | 1 | 10.94 | 0.953 | 6.324555 | 63.53 |
| 50 | 30 | 0.05 | 1 | 8.57 | 1.0715 | 7.071068 | 71.43 |
| 60 | 30 | 0.05 | 1 | 7.98 | 1.101 | 7.745967 | 73.4 |
| 70 | 30 | 0.05 | 1 | 6.13 | 1.1935 | 8.3666 | 79.57 |
| 80 | 30 | 0.05 | 1 | 5.93 | 1.2035 | 8.944272 | 80.23 |
| 90 | 30 | 0.05 | 1 | 4.87 | 1.2565 | 9.486833 | 83.77 |
| 100 | 30 | 0.05 | 1 | 4.32 | 1.284 | 10 | 85.6 |
| 110 | 30 | 0.05 | 1 | 3.79 | 1.3105 | 10.48809 | 87.37 |
| 120 | 30 | 0.05 | 1 | 3.56 | 1.322 | 10.95445 | 88.13 |

Table S15: Experimental data of adsorption Iodine

| Time | Removal (%) |
| --- | --- |
| 0 | 0 |
| 1 | 40 |
| 2 | 65 |
| 3 | 100 |
| 5 | 165 |
| 10 | 200 |
| 20 | 220 |
| 30 | 223 |
| 40 | 225 |
| 50 | 225 |
| 60 | 225 |
| 65 | 225 |
| 70 | 225 |