# Supplementary Information

# Characterizing the photoluminescence of fluorescein-labeled cellulose

# in aqueous and alcohol solutions: influence of the cellulose backbone

Chi-Yang Yen1, Shailesh Rana2, Kamlesh Awasthi2, Nobuhiro Ohta2,*, Masahito Oh-e1,*

1 Institute of Photonics Technologies, Department of Electrical Engineering,

National Tsing Hua University, 101 Sec. 2 Kuang-Fu Road, Hsinchu 300044, Taiwan

2 Department of Applied Chemistry and Institute of Molecular Science, and Center for Emergent Functional Matter Science, National Yang Ming Chiao Tung University, 1001 Ta-Hsueh Road, Hsinchu 300093, Taiwan

* Corresponding authors

This Supplementary Information includes the complementary photoluminescence (PL) properties of fluorescein-labeled cellulose (FLC) in water, methanol, and ethanol.

Using the fast τ1 and slow τ2 components enabled deducing their respective quantum yields as well as the rate constants of radiative and nonradiative decay for each component, as summarized in Tables S1 and S2. Notably, the rate constants krfast and krslow of radiative decay, which were obtained from the τ1 and τ2 components of FLC, are still about one order of magnitude lower and even lower than those of the single decay component in the fluorescein isothiocyanate (FITC) counterpart solutions. This suggests that the lifetime of the PL component that exhibits static quenching is still much shorter (and hence undetectable) than that of the fast-decaying component observed in the PL decay profiles. The data from the decomposition are consistent with the conclusion obtained by comparing the radiative decay rate constants determined using the total fluorescence quantum yield ϕPL and the average lifetime τavg in the main text.

Supplementary Table S1. Quantum yields ϕPLfast and ϕPLslow of the fast τ1 and slow τ2 components.

| Solute | Solvent | ϕPL | A1τ1A1τ1+A2τ2 | A2τ2A1τ1+A2τ2 | ϕPLfast (τ1, ns) | ϕPLslow (τ2, ns) |
| --- | --- | --- | --- | --- | --- | --- |
| FLC | Water | 0.014 | 0.097 | 0.903 | 0.0014 (0.087) | 0.0126 (2.79) |
|  | Methanol | 0.014 | 0.169 | 0.831 | 0.0024 (0.115) | 0.0113 (2.69) |
|  | Ethanol | 0.018 | 0.245 | 0.755 | 0.0044 (0.127) | 0.0136 (2.45) |

Note: The fluorescence was monitored at λ = 520 nm. A1τ1(A1τ1+A2τ2) and A2τ2(A1τ1+A2τ2) are the intensity ratios of the rapidly and slowly decaying components, respectively. As the PL of the FITC solutions exhibits a mono-exponential decay profile, decomposing ϕPL is not required.

Supplementary Table S2. Rate constants of radiative (krfast and krslow) and nonradiative (knrfast and knrslow) decay of the fast τ1 and slow τ2 components.

| Solute | Solvent | ϕPLfast (ϕPLslow) | krfast (krslow) ×108 / s-1 | knrfast (knrslow) ×109 / s-1 | krS.B. ×108 / s-1 |
| --- | --- | --- | --- | --- | --- |
| FLC | Water | 0.0014 (0.0126) | 0.157 (0.045) | 11.48 (0.354) | 1.40‒2.53* |
|  | Methanol | 0.0024 (0.0116) | 0.206 (0.045) | 8.68 (0.367) | 1.36‒2.45* |
|  | Ethanol | 0.0044 (0.0136) | 0.347 (0.055) | 7.84 (0.402) | 1.41‒2.54* |

Note: krfast (krslow) and knrfast (knrslow) were determined from ϕPLfastτ1 ϕPLslowτ2 and 1τ1-krfast (1τ2-krslow), respectively. krS.B. is the rate constant of radiative decay calculated using the Strickler‒Berg formula. * See the section “Quantifying the fluorescein moieties per chain” in the main text for the estimation of these values.