Supplementary Information

Micro-engineered Nanowire Electron Source for Atomic Resolution Imaging

Han Zhang1*, Yu Jimbo2, Akira Niwata2, Akihiro Ikeda2, Akira Yasuhara2, Cretu Ovidiu1, Koji Kimoto1, Takeshi Kasaya3, Hideki T. Miyazaki3, Naohito Tsujii4, Hongxin Wang1, Yasushi Yamauchi1, Daisuke Fujita1, Shin-ichi Kitamura2, Hironobu Manabe2

- Research center for advanced material characterization, National Institute for Materials Science, Tsukuba, Ibaraki, Japan;

- JEOL ltd., Akishima, Tokyo, Japan;

- Research center for functional materials, National Institute for Materials Science, Tsukuba, Ibaraki, Japan;

- International center for materials nanoarchitectonics, National Institute for Materials Science, Tsukuba, Ibaraki, Japan;

* to whom correspondence should be sent: ZHANG.han@nims.go.jp

- HRTEM image taken at 800kx magnification

Sfigure1. The 800kx HRTEM image taken by using the LaB6 NW emitter. Red rectangle marked the region where the FFT diffractogram of figure 2e is created from.

- Probe size determination

Sfigure2. (a) 2D electron probe profile simulated using QSTEM based on diffraction and lens aberration conditions of the experiment. Image width: 200pm; (b) A gaussian-shaped beam profile simulating additional probe broadening effect through instrument instability and source size. Image width: 200pm; (c) Theoretical probe profile simulated by convoluting (a) with (b). Image width: 200pm; (d) Line profiles of (a), (b), (c), showing the 87.6pm FWHM of the convoluted probe.

- Lowest un-monochromated EELS ZLP

Sfigure3. Un-monochromated EELS ZLP comparison among LaB6 nanowire emitter, W (310) emitter and Schottky emitter, used in aberration corrected TEMs. 0.2eV and 0.27 eV are the lowest possible FWHM energy spreads measured for LaB6 nanowire emitter and W (310) emitter in the same NeoArm200F TEM.