Supporting Information

Modulation of the oxygen sensing properties of iridium (III) complexes by changing their substitution groups

Merve Zeyrek Ongun1, Murat Sahin2, Sibel Oguzlar3, Tuğçe Akbal Aytan2, Devrim Atilla2,*, Sevinc Zehra Topal2,*

1 Dokuz Eylul University, Izmir Vocational High School, Chemistry Technology Program, Izmir, Turkey

2 Gebze Technical University, Faculty of Science, Department of Chemistry, Kocaeli, Turkey

3 Dokuz Eylul University, Center for Fabrication and Application of Electronic Materials, Izmir, Turkey

Corresponding authors

E-mail addresses: datilla@gtu.edu.tr, sztopal@gtu.edu.tr

Scheme S1. Synthetic pathway of  Cl2dppz.

Fig.S1. 1H NMR spectrum of 1,10-phenantroline-5,6-dion.

Fig.S2. 1H NMR spectrum of Cl2dppz.

Scheme S2. Synthetic pathway of  Ir-dimer.

Fig.S3. 1H NMR spectrum of 2-(3-trifloromethyl-phenyl)-4-methoxypyridin.

Fig.S4. 1H NMR spectrum of Ir-Dimmer.

Fig.S5. The mass spectrum of L1.

Fig.S6. 1H NMR spectrum of L1 in CDCl3.

Fig.S7. The mass spectrum of L2.

Fig.S8. 1H NMR spectrum of L2 in CDCl3.

Fig.S9. The mass spectrum of L3.

Fig.S10. 1H NMR spectrum of L3 in CDCl3.

Fig.S11. The mass spectrum of L4.

Fig.S12. 1H NMR spectrum of L4 in CDCl3.

Fig.S13. The mass spectrum of Ir-1.

Fig.S14. 1H NMR spectrum of Ir-1 in CDCl3.

Fig.S15. The mass spectrum of Ir-2.

Fig.S16. 1H NMR spectrum of Ir-2 in CDCl3.

Fig.S17. The mass spectrum of Ir-3.

Fig.S18. 1H NMR spectrum of Ir-3 in CDCl3.

Fig. S19. The mass spectrum of Ir-4.

Fig.S20. 1H NMR spectrum of Ir-4 in CDCl3.

Fig.S21. Oxygen induced phosphorescence emission spectra of Ir-1 in EC thin film under various oxygen partial pressure conditions, inset: Stern-Volmer plot for oxygen.

Fig.S22. Oxygen induced phosphorescence emission spectra of Ir-2 in EC thin film under various oxygen partial pressure conditions, inset: Stern-Volmer plot for oxygen.

Fig.S23. Oxygen induced phosphorescence emission spectra of Ir-3 in EC thin film under various oxygen partial pressure conditions, inset: Stern-Volmer plot for oxygen.

Fig.S24. Time-based kinetic response of Ir-1 in thin film in an alternating atmosphere of 100.0% N2 and 100.0% O2.

Fig.S25. Time-based kinetic response of Ir-2 in thin film in an alternating atmosphere of 100.0% N2 and 100.0% O2.

Fig.S26. Time-based kinetic response of Ir-3 in thin film in an alternating atmosphere of 100.0% N2 and 100.0% O2.

Table S1. Decay-times of Ir-1-4 complexes in THF and EC-based thin films in the absence and presence of the oxygen.

| Dye |  | EC |  |  |  |  |  | THF |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | N2 |  |  | O2 |  |  | N2 |  |  | O2 |  |  |
|  |  | Decay Time (µs) | Std.Dev. (µs) | Rel. (%) | Decay Time (µs) | Std.Dev. (µs) | Rel. (%) | Decay Time (µs) | Std.Dev. (µs) | Rel. (%) | Decay Time (µs) | Std.Dev. (µs) | Rel. (%) |
| Ir-1 | τ1 | 52.24 | 0.48 | 20.54 | 2.95 | 0.18 | 17.53 | 11.33 | 0.07 | 70.41 | 3.28 | 0.23 | 41.67 |
|  | τ2 | 210.62 | 1.46 | 48.66 | 15.95 | 0.17 | 64.31 | 67.75 | 0.72 | 29.59 | 11.59 | 0.31 | 58.33 |
|  | τ3 | 875.32 | 4.52 | 30.81 | 98.03 | 1.65 | 18.16 | - | - | - | - | - | - |
|  | τavr | 382.82 |  |  | 28.57 |  |  | 28.02 |  |  | 8.13 |  |  |
| Ir-2 | τ1 | 37.38 | 0.39 | 16.66 | 20.09 | 0.29 | 59.58 | 4.59 | 0.06 | 53.91 | 2.70 | 0.27 | 37.74 |
|  | τ2 | 201.87 | 1.87 | 42.59 | 111.28 | 2.33 | 40.42 | 16.38 | 0.12 | 46.09 | 11.42 | 0.27 | 62.26 |
|  | τ3 | 813.23 | 5.02 | 40.75 | - | - | - | - | - | - | - | - | - |
|  | τavr | 423.59 |  |  | 56.95 |  |  | 10.02 |  |  | 8.13 |  |  |
| Ir-3 | τ1 | 73.81 | 0.50 | 19.66 | 13.47 | 0.14 | 56.15 | 29.81 | 0.0274 | 99.22 | 2.89 | 0.26 | 40.22 |
|  | τ2 | 292.40 | 1.76 | 47.47 | 55.59 | 1.33 | 33.34 | 171.97 | 6.5271 | 0.78 | 11.84 | 0.32 | 59.78 |
|  | τ3 | 986.88 | 4.00 | 32.86 | 206.94 | 6.44 | 10.52 | - | - | - | - | - | - |
|  | τavr | 477.61 |  |  | 47.86 |  |  | 30.92 |  |  | 8.24 |  |  |
| Ir-4 | τ1 | 95.74 | 0.7982 | 24.83 | 3.74 | 0.08 | 40.13 | 10.67 | 0.0157 | 90.83 | 10.54 | 0.04 | 100.00 |
|  | τ2 | 310.07 | 2.4124 | 51.73 | 17.53 | 0.25 | 48.49 | 77.22 | 0.4326 | 9.17 | - | - | - |
|  | τ3 | 995.81 | 6.4305 | 23.45 | 101.90 | 2.05 | 11.37 | - | - | - | - | - | - |
|  | τavr | 417.68 |  |  | 21.59 |  |  | 16.77 |  |  | 10.54 |  |  |