Supporting Information

Ultra-Sensitive Hydrogen Sulfide Detection via Hybrid Small-Molecule Nano-arrays

Xing Xing1, 2, Luyan Wu3, Yuchen Zhang1, Jiahao Pan1, Yusuke Ishigaki4, Takanori Suzuki4, Deju Ye3, Weihua Zhang1, Zhenda Lu1, 2, 3 *

1College of Engineering and Applied Sciences, Jiangsu Key Laboratory of Artificial Functional Materials, Nanjing University, Nanjing 210023, China

2School of the Environment, Research Center for Environmental Nanotechnology (ReCENT), Nanjing University, Nanjing 210023, China

3State Key Laboratory of Analytical Chemistry for Life Science, School of Chemistry and Chemical Engineering, Nanjing University, Nanjing 210023, China

4Department of Chemistry, Faculty of Science, Hokkaido University, N10 W8, North-ward, Sapporo 060-0810, Japan

*E-mail: luzhenda@nju.edu.cn

Figure S1. (a) 4×4 enlarged AFM height profile of the nanoarray. (b) The height distribution on the blue line in Figure S1a which indicates the spot size in a single spot is around 100 nm.

Figure S2. (a) The absorption spectra of RB, CD, F12+, and F12+@RB6@CD on a cover glass. (b) The absorption spectra of F12+@RB6@CD on a cover glass before (red) and after (inset black curve) reaction with NaHS. After the reaction with NaHS, there is a significant decrease in absorption for F1 molecular.

Figure S3. Schematic illustration and its corresponding photoluminescence (PL) image obtained by assembly (a) RB, (b) RB/cyclodextrin, and (c) RB/cyclodextrin/F12+ molecules. Scale bar, 5 μm. (d, e) The statistics of the fluorescence intensity of spots in the 5×5 array in Figures b and c, showing the average fluorescence intensity decreased to 9% of the RB/CD spots after adding F12+ molecules.

Figure S4. PL images of serial NaHS concentration in 0.1 fM, 1 fM, 10 fM, 100 fM, 1 pM, and 10 pM in the assay of 5×5 molecules nano-array. Scale bar, 5 μm.

Figure S5. The data processing process of a typical fluorescence image in 5×5 nano-array, including (a) original fluorescence image, (b) effective fluorescence images after subtracting background, and (c) divided into the separated spots.

Figure S6. The fluorescence intensity results of all spots in Figure S4 with NaHS concentration from 0.1 fM to 1 μM.

Figure S7. The data processing process of a typical fluorescence image in 20×20 array experiment, including (a) original fluorescence image, (b) effective fluorescence images after subtracting background, and (c) divided into 400 spots.

Table S1 The fitting parameters of all the 4-parameters logistic regression fitting. All the threshold value was obtained by A1+(A2-A1)×0.05.

| Figure | y = A2 + (A1-A2)/(1 + (x/x0)^p) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | R2 | A1 | A2 | X0 | p |
| Figure 3b | 0.9963 | 12684 | 441090 | 2535.7 | 0.36555 |
| Figure 4b (red) | 0.9903 | 65.211 | 425.55 | 2.9678 | 0.54671 |
| Figure 4b (black) | 0.9999 | 416750 | 1.3818×107 | 165.42 | 0.47203 |