Supplementary Material

Mingyu Huang1a, Xierong Luo2a, Yu Shi1, Chang’e Liu1, Jinquan Chen1,2*

1Yunnan Key Laboratory for Plateau Mountain Ecology and Restoration of Degraded Environments, School of Ecology and Environmental Science, Yunnan University, Kunming, 650091, China

2Yunnan International Cooperative Center of Plateau Lake Ecological Restoration and Watershed Management & Yunnan Think Tank of Ecological Civilization, Kunming, Yunnan, 650091, China

a Co-first author

* Co-corresponding Author: E-mail: chengjinquan@ynu.edu.cn (J. Cheng).

Figures：

Fig. S1. FTIR of biochar at 300℃.

Fig. S2. Linear regression fitting of urease and ammonium nitrogen.

Fig. S3. Co-networks of bacterial in soil. (a)CK, (b)AN-B15, (c)BC(5%), (d)15BC(5%).

Fig. S4. Correlation analysis of soil chemical properties and soil enzyme activities with species（**p < 0.01、*p < 0.05）.

Tables :

Table S1 Physicochemical properties of straw biochar used in this study.

Table S2 The fitting peak of XPS.

Table S3 Soil biodiversity index.

Table S4 Adonis test based on Bary distance(15BC(5%) VS (CK+BC(5%)+AN-B15).

Table S5 The features of Co-networks.

Table S6 Relative abundance of OTU000087 and Pseudomonas in four treatments

Figures：

Fig. S1. FTIR of biochar at 300℃.

Fig. S2. Linear regression fitting of Urease and ammonium nitrogen.

Fig. S3. Co-networks of bacterial in soil: (a)CK, (b)AN-B15, (c)BC(5%), (d)15BC(5%).

Fig. S4. Correlation analysis of soil chemical properties and soil enzyme activities with species（**p < 0.01、*p < 0.05）.

Tables :

Table S1 Physicochemical properties of straw biochar used in this study.

| Parameter |  | Value |
| --- | --- | --- |
| pH |  | 7.1 |
| BET (m²/g) |  | 245.12 |
| t-Plot (cm³/g) |  | 0.0071 |
| Elemental composition | P(%) | 20.62 |
|  | S(%) | 16.37 |
|  | Cl(%) | 9.99 |
|  | Si(%) | 3.68 |
| Metal content | K(%) | 8.68 |
|  | Mg(%) | 2.95 |
|  | Fe(%) | 7.91 |
|  | Al(%) | 0.75 |
|  | Mn(%) | 0.46 |

Table S2 The fitting peak of XPS.

| Sample | Assignment | Peak BE（ev） | Area | Atomic% |
| --- | --- | --- | --- | --- |
| BC | Cr(Ⅲ)2p1 | 585.53 | 1037.98 | 68.28 |
|  | Cr(Ⅲ)2p3 | 576 | 2005.55 |  |
|  | Cr(Ⅵ)2p1 | 588.35 | 480.93 | 31.72 |
|  | Cr(Ⅵ)2p3 | 579.1 | 929.43 |  |
| BC+AN-B15 | Cr(Ⅲ)2p1 | 585.59 | 887.91 | 71.45 |
|  | Cr(Ⅲ)2p3 | 576.18 | 1715.58 |  |
|  | Cr(Ⅵ)2p1 | 588.36 | 353.85 | 28.55 |
|  | Cr(Ⅵ)2p3 | 579.2 | 684.73 |  |

Table S3 Soil biodiversity index.

| Treatment groups | ACE | Chao1 | Shannon |
| --- | --- | --- | --- |
| Cr | 1974.7 ± 461.7a | 1800.5 ± 444.2a | 5.6 ± 0.3b |
| AN-B15 | 1832.9 ± 290.6a | 1679.0 ± 365.6a | 5.6 ± 0.1b |
| BC | 1924.8 ± 120.8a | 1750.7 ± 110.8a | 5.7 ± 0.1b |
| AN-B15BC | 1673.7 ± 332.6a | 1542.6 ± 305.5a | 6.6 ± 0.2a |

The different letters suggested that the differences in each treatment are significantly (p < 0.05) using Duncan’s test. The values are presented as the mean ± one standard deviation (n = 3).

Table S4 Adonis test based on Bary distance(15BC(5%) VS (CK+BC(5%)+AN-B15).

| Diffs | Sums of Sqs | Mean Sqs | F value | R2 | P value | Significant |
| --- | --- | --- | --- | --- | --- | --- |
| 15BC(5%) VS (CK+BC(5%)+AN-B15) | 0.1392 | 0.1392 | 4.8891 | 0.3294 | 0.007 | ** |

Table S5 The features of Co-networks.

| Treatment group | Edge | Node | Weighted average | The density of figure |
| --- | --- | --- | --- | --- |
| Cr | 40 | 38 | 2.1 | 0.06 |
| AN-B15 | 50 | 44 | 2.3 | 0.07 |
| BC | 50 | 38 | 2.6 | 0.05 |
| AN-B15BC | 50 | 35 | 2.9 | 0.08 |

Table S6 Relative abundance of OTU000087 and Pseudomonas in four treatments.

|  | CK | AN-B15 | BC | AN-B15BC |
| --- | --- | --- | --- | --- |
| OTU000087 | 0.0092 ± 0.0061 | 0.0400 ± 0.0192 | 0.0362 ±0.0168 | 0.3841 ± 0.3803 |
| Pseudomonas | 0.0296 ± 0.0241 | 0.0476 ± 0.0356 | 0.0843 ± 0.0351 | 0.4548 ± 0.4151 |

The values are presented as the mean ± one standard deviation (n = 3).